## Slide 1: Modelization of Radiation-Induced Damage in FLUKA and Material damage estimates for CERN injectors and future facilities
Jose A. Briz
    EN-STI-FDA, CERN
    V. Vlachoudis and F. Cerutti EN-STI-FDA (CERN)
1st Workshop of ARIES WP17 PowerMat – 27-28/11/2017

## Slide 2: FLUKA
FLUKA is a Monte Carlo code for calculations of particle transport and interactions with matter.
Wide range of applications:
      Proton and electron accelerator shielding, target design, calorimetry, activation, dosimetry, detector design, Accelerator Driven Systems, cosmic rays, neutrino physics, Radiotherapy, etc.
Extensively used at CERN for:
  Beam-machine interactions
  Radio-Protection calculations
  Facility design of future projects
Courtesy: E. Skordis
FLUKA geometry of the LHC warm section of IR7

## Slide 3
Interaction and Transport Monte Carlo Code
Info: http://www.fluka.org
Hadron-nucleus interactions
Nucleus-Nucleus interactions
Electron interactions
Photon interactions
Muon interactions (inc. photonuclear)
Neutrino interactions
Decay
Low energy neutrons
Ionization
Multiple scattering
Combinatorial geometry
Voxel geometry
Magnetic field
Analogue or biased
On-line buildup and evolution of induced radioactivity and dose
User-friendly GUI thanks to Flair

## Slide 4
Different kinds of damage
Precious materials (healthy/tragic damage) energy (dose) deposition, radioisotope production and decay & positron annihilation and photon pair detection
Oxidation by generation of chemically active radicals (e.g. PVC
de-hydrochlorination by X and g-rays, radiolysis,…)
Accidents energy (power) deposition
Degradation energy (dose) deposition, particle fluence, DPA
Gas production residual nuclei production
Electronics high energy hadron fluence, neutron fluence, energy (dose) deposition
Activation residual activity and dose rate
from Radiation-Matter interaction
F.Cerutti

## Slide 5: DPA as Radiation Damage Estimator
The dpa quantity is a measure of the amount of radiation damage in irradiated materials. It means the average number of displacements that every atom in the crystal structure has suffered.
A is the mass number
NA is the Avogadro number
𝜌 is the density
NF is the number of defects or Frenkel pairs.
Experimentally: no direct determination. Indirect through study of macroscopic effects (electric and thermal conductivities, radiation hardening, swelling…)
Amount of dpa Macroscopic effects

## Slide 6: Frenkel pairs
vacancy
interstitial
Frenkel pair NF (defect or disorder), is a compound crystallographic defect formed when an atom or ion leaves its place in the lattice (leaving a vacancy), and lodges nearby in the crystal (becoming an interstitial)
NNRT Defects by Norgert, Robinson and Torrens κ=0.8 is the displacement efficiency T kinetic energy of the primary knock-on atom (PKA) x(T) partition function (LSS theory) x(T) T directly related to the NIEL(non ionizing energy loss) Eth damage threshold energy

## Slide 7: Damage Threshold
Damage threshold depends on the direction of the recoil in the crystal lattice.
Also depends on the compound combination:
FLUKA use the “average” threshold over all crystallographic directions (user defined)
Sensitivity studies using different Eth values can provide upper and lower limits on dpa
From: NEA/NSC/DOC(2015)9
Typical values used
in NJOY99 code
e.g. NaCl: Eth(Na-Na), Eth(Na-Cl), Eth(Cl-Na), Eth(Cl-Cl)

## Slide 8
Displacement efficiency
κ Stoller vs Nordlund
27-28/11/2017
1st Workshop of ARIES WP17 Power Mat - Politecnico de Torino
8
FLUKA (Stoller Fit)
Recombination
from overlap of
collision cascades,
“athermal recombination-corrected” dpa:
Arc-dpa
Thermal recombination
of defects not considered
becomes relevant
for high temperatures
Overestimation of dpa’s
Nordlund
Stoller results
Comes from
Molecular Dynamics
simulations

## Slide 9: Lindhard partition function x
BAD Strong discrepancies for high energies
Fraction of
stopping power
S(T) going
into NIEL
(non-ionizing
energy loss)

## Slide 10: Nuclear Stopping Power
The total (S), nuclear (Sn) and electronic (Se) stopping power. The partition function Sn/(Sn+Se) is also plotted. The abscissa is the ion total kinetic energy
O on Si
Ag on Au
F.Cerutti
Partition function decreases with energy
And increases with charge
NIEL/DPA are dominated by
Low energy (heavy) recoils

## Slide 11: Restricted Nuclear Stopping Power
Lindhard approximation uses the unrestricted NIEL. Including all the energy losses also those below the threshold Eth  Overestimation of DPAs
FLUKA is using a more accurate way by employing the restricted nuclear losses where: S(E,Eth) is the restricted energy loss N atomic density T energy transfer during ion-solid interaction ds/dT differential scattering cross section maximum fraction of energy transfer during collision

## Slide 12: Comparison with other simulation codes
76Ge ion pencil beam of 130 MeV/A uniform in W target a disc of R=0.3568 mm, 1.2 mm thickness
×2.5 with a k=0.8 fixed efficiency
Non-restricted
provides higher
values if we consider fixed
Displ. Effic.
Overestimation of DPA

## Slide 13: FLUKA Implementation
Charged particles and heavy ions
During transport
  Calculate the restricted non ionizing energy loss
Below threshold
  Calculate the integrated nuclear stopping power with the Lindhard partition function
At (elastic and inelastic) interactions
  Calculate the recoil, to be transported or treated as below threshold
Neutrons:
High energy En>20 MeV
  Calculate the recoils after interaction Treat recoil as a “normal” charged particle/ion
Low energy En≤20 MeV (group-wise)
  Calculate the NIEL from NJOY
Low energy En≤20 MeV (point-wise)
  Calculate the recoil if possible Treat recoil as a “normal” charged particle/ion
Implementation in FLUKA: A. Fasso et al. Prog. In Nucl. Science and Technology, Vol. 2, p769-775 (2011)

## Slide 14
Example of fission/evaporation
1 A GeV 208Pb + p reactions Nucl. Phys. A 686 (2001) 481-524
Quasi-elastic
Spallation
Deep
spallation
Fission
Fragmentation
A<18 nuclei
~ 50000 combinations
up to 6 ejectiles
Evaporation
600 possible emitted
particles/states (A<25)
Data
after cascade
after pre-equilibrium

## Slide 15
Isotope production for natFe(p,x):
Data: Michel et al. 1996 and 2002

## Slide 16: Estimates for CERN injectors and future facilities
Beam Dump Facility
BLIP capsule
PS Internal Beam Dumps

## Slide 17: Beam Dump Facility (BDF)
Beam:
Protons: 400 GeV/c
Sweep pattern:
  radius 3 cm
  1s 0.6 cm
Geometry:
1.4 m long cylinder discs of
TZM enclosed in Ta
W enclosed in Ta
1.5 mm Ta cladding and
5 mm water gaps
Materials:
Tungsten Ed=90 eV
SS 316N Ed=40 eV
Tantalum Ed=53 eV
TZM (Mo,Zr,Ti…) Ed=60 eV
TZM
W
Ta cladding
Water cooling
Courtesy: J. Canhoto-Espadanal
Notes: https://indico.cern.ch/event/679079/contributions/2781694/attachments/1560677/2456781/Students_coffee_BDF.pdf

## Slide 18: BDF Results: H/He[appm] vs DPA
Water
Ta
TZM
W
Courtesy: J. Canhoto-Espadanal
Notes: Suggestion that only H1 and He4 should be included but we do see as H2 and H3 are not negligible…

## Slide 19: BLIP capsule
Beam
  Proton E=181 MeV
  sx,y = 5.1 mm
Geometry: Layers of
  Window SS304L 0.3mm
  TZM 0.5mm
  CuCrZr 0.5mm
  Ir 0.5mm
  Graphite(0.85g/cm3) 0.1mm
Courtesy: J. Canhoto-Espadanal

## Slide 20: DPA High-Z BLIP [FLUKA vs MARS]
Chart: 
| TZM | CuCrZr | Ir | Graphite 0.85
FLUKA | 0.15244 | 0.19055 | 0.3502 | 0.03193
FLUKA-NRES | 0.43054 | 0.48564 | 0.9922 | 0.06695
MARS | 0.41 | 0.46 | 1.1 | 0.013
DPA / 1.03 1012p+
Note: NRT model of MARS
Courtesy: J. Canhoto-Espadanal

## Slide 21: H appm/DPA High-Z BLIP
Chart: 
| TZM | CuCrZr | Ir | Graphite 0.85
FLUKA | 987.0286 | 658.8887 | 390.8867 | 1906.0272
FLUKA-NRES | 349.4743 | 258.5247 | 137.9648 | 909.0284
MARS | 231 | 177 | 84.8 | 2150
CuCrZr
TZM
Ir
C85
Courtesy: J. Canhoto-Espadanal

## Slide 22: He appm/DPA High-Z BLIP
Chart: 
| TZM | CuCrZr | Ir | Graphite 0.85
FLUKA | 226.8491 | 195.1413 | 84.8896 | 1458.7167
FLUKA-NRES | 80.3198 | 76.5666 | 29.9621 | 695.6957
MARS | 20.3 | 21.6 | 3.67 | 928
Probably due to “Old” MARS
event generator used
CuCrZr
TZM
Ir
C85
Warning:
Log-scale
Courtesy: J. Canhoto-Espadanal

## Slide 23: PS Internal Beam Dumps
23 cm
BEAM
4 cm
Challenging Energy density
Superficial energy deposition
40 µm
BEAM

## Slide 24
PS Internal Beam Dumps: Damage
Damage threshold energies considered:
Eth(Graphite) = 30 eV - typical value 30-35 eV
Eth(CuCrZr and SS304L) = 40 eV
Graphite
CuCrZr
0.5 DPA/year
0.02 DPA/year
0.002 DPA/year
in CuCrZr
0.03 DPA/year in Graphite
Beam properties:
26 GeV/c proton beam
2.4e17 POT per year
𝞼h=1.74 mm 𝞼v=0.87 mm
Beam is shaved in a thin top most layer
Graphite:
Experience at CERN with CNGS air cooled graphite target (SPS beam). About 1200°C reached for each pulse. At the end of operation: 1.5 DPA
    No problem observed on graphite
23 cm
  CuCrZr:
  Literature on neutron irratiation indicated for similar dpa damage some possible radiation hardening and thermal conductivity degradation but not dramatic effects
BEAM
4 cm

## Slide 25
Summary
FLUKA dpa model uses a restricted NIEL computed during initialization and run time.
Not based on Lindhard but reworked all formulas
The only free parameter for the user is the damage threshold. It depends on the direction of the recoil. Simple averaging is not correct
Uniform treatment from the transport threshold up to the highest energies
Use of Stoller displacement efficiency instead of a fixed 0.8 as NRT suggests
Not considered thermal recombination of defects  overestimation of dpa. Improving the estimate would require Molecular Dynamics simulations

## Slide 26: Summary
FLUKA is employed to evaluate radiation-induced damage on new dumps facilities (BDF, BLIP) and elements of the CERN injector chain (PS internal dumps)
Simulations provided a way of quantifying the damage through estimation of dpa and gas production (H, He)
Comparison of estimations of dpa (simulations) and modifications of macroscopic quantities (experimental: thermal, electric, etc…, properties) helps to extract conclusions on radiation-induced damage
Possible Future improvements:
  Implementation of the Nordlund arc-dpa
  More accurate recoil momentum cross section for pair production and Bremsstrahlung
  Point wise treatment of low energy neutrons will provide correct recoil information
  Multiple damage thresholds for compounds

## Slide 27: Thank you for your attention! Any question?

## Slide 28: Extra slides

## Slide 29: Outline
Introduction to FLUKA
Radiation damage estimation: dpa
dpa estimation in FLUKA:
  Damage threshold
  Displacement efficiency
  Lindhard partition function and Restricted Nuclear Stopping Power
Damage estimates for CERN Injectors and Future Facilities
Summary

## Slide 30: Eth Damage Threshold Energy
Eth is the value of the threshold displacement energy averaged over all crystallographic directions or a minimum energy to produce a defect Typical values used in NJOY99 code
The only variable requested for FLUKA MAT-PROP WHAT(1) = Eth (eV) WHAT(4,5,6) = Material range SDUM = DPA-ENER

## Slide 31: Damage Threshold in Compounds
NJOY (MT=444) sums up the cross section multiplied by the damage energies, which is the damage production cross section representing the effective kinetic energy of recoiled atom for reaction types i at neutron energy En
Problematic:
Damage threshold depends on the lattice structure
Damage threshold can be quite different for each combination for the specific compound e.g. NaCl: Eth(Na-Na), Eth(Na-Cl), Eth(Cl-Na), Eth(Cl-Cl)
Simple weighting with the atom/mass fraction doesn’t work
FLUKA’s approximation is using a unique average damage threshold Eth for the compounds as well  A sensitivity study can be performed
Only free parameter for the FLUKA user is Eth

## Slide 32: κ displacement efficiency
k=0.8 value deviates from the hard sphere model (K&P), and compensates for the forward scattering in the displacement cascade
The displacement efficiency κ can be considered as independent of T only in the range of T≤1−2 keV. At higher energies, the development of collision cascades results in defect migration and recombination of Frenkel pairs due to overlapping of different branches of a cascade which translates into decay of κ(T).
From molecular dynamics (MD*) simulations of the primary cascade the number of surviving displacements, NMD, normalized to the number of those from NRT model, NNRT, decreases down to the values about 0.2–0.3 at T≈20−100 keV. The efficiency in question only slightly depends on atomic number Z and the temperature. NMD/NNRT = 0.3–1.3
where X ≡ 20 T (in keV).
Roger E. Stoller, J. Nucl. Mat., 276 (2000) 22
D.J. Bacon, F. Gao and Yu.N. Osetsky, J. Comp.-Aided Mat. Design, 6 (1999) 225.

## Slide 33: Factor of 2 (Kinchin & Pease)
The cascade is created by a sequence of two-body elastic collisions between atoms
In the collision process, the energy transferred to the lattice is zero
For all energies T < Ec electronic stopping is ignored and only atomic collisions take place. No additional displacement occur above the cut-off energy Ec
The energy transfer cross section is given by the hard-sphere model. ν(T)=0 for 0<T< Eth (phonons) ν(T)=1 for Eth<T<2Eth ν(T)=T/2Eth for 2Eth<T<Ec ν(T)=Ec/2Eth for T > Ec
Schematic relation between the number of displaced atoms in the cascade and the kinetic energy T of the primary knock-on atom
Energy is equally shared between two atoms after the first collision
Compensates for the energy lost to sub threshold reactions

## Slide 34: Lindhard partition function x [1/2]
The partition function gives the fraction of stopping power S that goes to NIEL
Approximations used: Electrons do not produce recoil nuclei with appreciable energy, lattice binding energy is neglected, etc... where
approximated to
Nice feature: It can handle any projectile Z1,A1 whichever charged particle
Z,A charge and mass
1 projectile
2 medium
T recoil energy (eV)

## Slide 35: Nuclear Stopping power
Nuclear stopping power (unrestricted)
Energy transferred to recoil atom
Deflection angle, by integrating over all impact parameters b
Universal potential
where: Fs(x) = S ai exp(-ci x) screening function rs=0.88534 rB / (Z10.23 + Z20.23) screening length rs=0.88534 rB Z1-1/3 in case of particle
ICRU-49

## Slide 36: Ziegler approximation
Reduced kinetic energy e (T in keV)
Reduced stopping power if if Important features of Reduced Stopping Power
  Independent from the projectile and target combination
  Accurate within 1% for e<1 and to within 5% or better for e>3
Stopping power (MeV/g/cm2)
ICRU-49

## Slide 37: Restricted Stopping Power
The restricted nuclear stopping power is calculated the same way only integrating from 0 impact parameter up to a maximum bmax which corresponds to a transfer of energy equal to the Eth= Wmin(qmin,T)
To find bmax we have to approximately solve the previous q integral using an iterative approach for This can be done either by integrating numerically for q or using the magic scattering formula from Biersack-Haggmark that gives a fitting to sin2(q/2)

## Slide 38: Implementation: Charged Particles
During the transport of all charged particles and heavy ions the dpa estimation is based on the restricted nuclear stopping power while for NIEL on the unrestricted one.
For every charged particle above the transport threshold and for every Monte Carlo step, the number of defects is calculated based on a modified multiple integral
Taking into account also the second level of sub-cascades initiated by the projectile
Below the transport threshold (1 keV) it employs the Lindhard approximation
restricted
partition function
Lindhard
partition function

## Slide 39: Group Wise Neutron Artifacts
Due to the group treatment of low-energy neutrons, there is no direct way to calculate properly the recoils.
Therefore the evaluation is based on the KERMA factors calculated by NJOY, which in turn is based on the Unrestricted Nuclear losses from using the NRT model.
>20MeV using models with more accurate treatment
<20MeV using NRT from NJOY

## Slide 40: Implementation: others
For Bremsstrahlung and pair production the recoil is sampled randomly from an approximation of the recoil momentum cross section
Bremsstrahlung
Pair production
both can be written in the same approximate way as
where the recoil momentum is sampled randomly by rejection from a similar function

## Slide 41: Coalescence:
d, t, 3He, and alpha’s generated during the (G)INC and preequilibrium stage
All possible combinations of (unbound) nucleons and/or light fragments checked at each stage of system evolution
FOM evaluation based on phase space “closeness” used to decide whether a light fragment is formed rather than not
  FOM evaluated in the CMS of the candidate fragment at the time of minimum distance
  Naively a momentum or position FOM should be used, but not both due to quantum non commutation
  … however the best results are obtained with a Wigner transform FOM (assuming gaussian wave packets) which should be the correct way of considering together positions and momenta
Binding energy redistributed between the emitted fragment and residual excitation (exact conservation of 4-momenta)

## Slide 42: Coalescence
High energy light fragments are emitted through the coalescence mechanism: “put together” emitted nucleons that are near in phase space.
Example : double differential t production from 542 MeV neutrons on Copper
Warning: coalescence is OFF by default
Can be important, ex for . residual nuclei.
To activate it:
PHYSICS 1. COALESCE
If coalescence is on, switch on Heavy ion transport and interactions (see later)

## Slide 43: Particle production in C(p,x) reaction
Data: JNST36 313 1999, PRC7 2179 1973

## Slide 44
Energy Density Distribution from FLUKA
BEAM
HL-LHC beam
p=26 GeV/c
2.4e13 ppp
σxxσy=1.74 mm x 0.87 mm
εx=1.8 mm mrad
εy=1.8 mm mrad
Values shown are accumulated per pulse
Graphite
CuCrZr
CuCrZr
HL-LHC

## Slide 45: Structural Damage on Dump Core
Lower general damage than current dump
(~1 order of magnitude)
Lower peak DPA on copper region than
current dump
(~2 orders of magnitude)
Graphite protects the copper block from structural damage
POT=2.4e17 (assumed same POT for current and future dumps)
Graphite
CuCrZr
0.5 DPA/year
0.02 DPA/year
0.002 DPA/year
in CuCrZr
0.03 DPA/year in Graphite
Damage threshold energies considered:
Eth(Graphite) = 30 eV - typical value 30-35 eV
Eth(CuCrZr and SS304L) = 40 eV

## Slide 46: Irradiation on Graphite
0.03 DPA/year estimated in Graphite block of PS dump
Experience at CERN: CNGS air cooled graphite target (SPS beam)
About 1200°C reached for each pulse
At the end of operation: 1.5 DPA
No problem observed on graphite
3.5 x 1013 protons per pulse,
10.5 µs pulse length < 1 mm spot size
2 extractions per cycle separated by 50 ms, occurring every 6 s
 2 000 000 extractions achieved by end of 2009
 4.5 x 1019 protons at 400 GeV/c on CNGS target per year
[Ref]: Spallation materials R&D for CERN’s fixed target program, M. Calviani et al. IWSMT, Oct. 2014, Austria
Graphite rods 2020PT (Mersen)
PS dump graphite irradiation shall not be a concern

## Slide 47: Irradiation on CuCrZr
[1] C. Bobeldijk (ed.). (1994). Atomic and Plasma-Material Interaction Data for Fusion. Vol. 5. Supplement to the Journal Nuclear Fusion
[2] S.A. Fabritsiev & S.J. Zinkle & B.N. Singh. (1996). Evaluation of copper alloys for fusion reactor divertor and first wall components. Journal of Nuclear Materials. Vol. 233-237. pp. 127-137.
[3] M. Li & M.A. Sokolov & S.J. Zinkle. (2009). Tensile and fracture toughness properties of neutron-irradiated CuCrZr. Journal of Nuclear Materials. Vol. 393. pp. 36-46.
Peak value obtained of 0.002 DPA per year (0.04 DPA in 20 years) in CuCrZr block of PS Dump
Localized peak DPA
Information for neutron irradiation found in literature
CuCrZr shows radiation hardening until saturation values around 0.1 – 0.5 DPA [1][3]  Some hardening may occur
CuCrZr is void swelling resistant [1][2] (below 2% density change for up to 150 DPA [1])
Some thermal conductivity degradation may occur (5 – 10 % reduction for doses > 0.1 DPA at < 150 °C [2])
[1]
[2]
[3]
Elastic
region
Plastic
region