## Slide 1: ARIES WP14 – Task 14.4: Industrial production of materials for extreme thermal management
F. Carra1
1CERN – European Organization for Nuclear Research
1st Workshop of ARIES
WP17 PowerMat
Politecnico di Torino, Turin (IT)
27-28 November 2017

## Slide 2: WP task 14.4
WP14: Promoting Innovation (PI) – WP leader M. Losasso (CERN). Close relation to industry, final aim to provide society with identified commercial applications of the supported research potential.
Task 14.4: Industrial production of materials for extreme thermal management
  Contribute to material development in collaboration with WP17 (PowerMat)
  Produce at least 10 samples of MgB2 by Additive Manufacturing on Copper substrate for characterization of the R&D  applications in critical accelerator environments (beam pipes, RF cavities) and other technical domains
  Demonstrate feasibility of production for industrialisation (with large dimensions, small tolerances)
Production objectives:
  30 samples of MgB2 on metal substrate
  30-50 samples of CuCD
  40 samples of metal-diamond composite for luminescence studies
  50 samples of carbide-graphite or metal-graphite composites
  1 large size block of carbide-graphite or metal-graphite composite with tight mechanical tolerance to proof industrialisation
RHP
CERN with industrial partner (BrevettiBizz)

## Slide 3: Deliverable
D14.3 : Production of material samples of carbon-based composites and metal-diamond composites
Production of: 50 samples of carbon-based composites with different production cycles and 30 samples of metal-diamond composites, 20 for high energy impact studies and 10 for luminescence studies
Deliverable Number | Deliverable Title | Lead beneficiary | Type | Dissemination level | Due Date (in months)
D14.3 | Production of material samples of carbon-based composites and metal-diamond composites | CERN | Demonstrator | Public | 24
Our goal: complete it by month 12, to provide inputs for WP17

## Slide 4: Deliverable Status
Brevetti Bizz: 50 samples of ceramic carbide – graphite
  December 2017: 25 threaded samples of MG6403Fc (or equivalent), for dynamic characterization at PoliTo
  Mid 2018: 25 threaded samples of another material, composition to be decided
  2020?: Industrialization (not in the scope of the deliverable), can we go to 45 mm thick (and longer/larger) blocks?

## Slide 5: Deliverable Status
RHP: 20 samples of copper-diamond for high-energy impact studies, 10 samples for luminescence
  July 2017: 10 rods 247x10x10 mm produced for tests in Multimat ✔
  End 2017, 2018: can we identify a suitable geometry for dynamic testing at PoliTo and produce samples?
  Luminescence: several samples produced, 6 delivered to GSI (important to document the production for the deliverable).
  MgB2 (not in the scope of the deliverable): production plan drafted, to be discussed with M. Losasso at the WP14 kickoff meeting (8th December 2017)

## Slide 6
Next: WP14 KoM
CERN, 8th December 2017

## Slide 7: Budget
Beneficiary short name* | Person - months | Monthly personnel costs | Personnel direct costs | Travel direct costs | Equipment and consumables | Other direct costs | Sub-contracting costs | Material direct costs | Total direct costs | Total indirect costs** | Total costs (direct + indirect) | EC requested funding
CERN | 3.00 | 8'000.00 | 24'000.00 | 3'000.00 | 0.00 |  |  | 3'000.00 | 27'000.00 | 6'750.00 | 33'750.00 | 9'312.50
Bizz Brevetti | 6.00 | 3'500.00 | 21'000.00 | 5'000.00 | 50'000.00 | 10'000.00 |  | 65'000.00 | 86'000.00 | 21'500.00 | 107'500.00 | 60'000.00
RHP | 6.00 | 3'500.00 | 21'000.00 | 5'000.00 | 110'000.00 | 10'000.00 |  | 125'000.00 | 146'000.00 | 36'500.00 | 182'500.00 | 91'250.00
Total | 15.00 | 59'365.00 | 66'000.00 | 13'000.00 | 160'000.00 | 20'000.00 | 0.00 | 193'000.00 | 259'000.00 | 64'750.00 | 323'750.00 | 160'562.50