## Slide 1: Oxidation behavior of graphite in air at high temperature
A. Perillo-Marcone, M. Calviani (EN-STI-TCD)
In collaboration with EN/MME
153rd MPP meeting

## Slide 2
Oxidation of graphite at high temperature over milliseconds
Performed at CERN by EN/MME

## Slide 3: Methodology
Impacting samples with laser beam in air
Temperature reached ~900-1300 °C
Exposition time ~10 ms
Materials
      Sigrafine (high density graphite in TDE)
      Sigraflex (low density graphite in TDE)
Examine changes in:
      Microstructure
      Chemical composition
      Phase

## Slide 4: Results

## Slide 5: Laser Impact – Conclusions
No clear indication of oxidation
Observed damage generated by thermo-mechanical stresses (not representative of stresses from proton beams)
Highly pessimistic conditions in comparison to TDE:
    Exposition times ~10ms (instead of us for TDE)
    Atmosphere 100% air

## Slide 6
Oxidation in air furnace
Performed at CERN by EN/MME

## Slide 7: Scope
Remove thermomechanical stresses
Overly conservative exposition time
Exposition to 100% air atmosphere

## Slide 8: Methodology
Preheating air furnace to >1100 °C
Insertion of samples in furnace (temperature drop to ~850 °C)
Samples maintained in furnace during 100s
Microscopy and chemical analysis of samples

## Slide 9: Results
No apparent change in microstructure
Amount of O and Si keep constant before and after the study
Material does not seem to be affected by oxidation
Further test in oven at 1100°C under way

## Slide 10
Oxidation at 2500 °C – 10s
Performed by SGL

## Slide 11: Methodology
Five samples of Sigrafine and Sigrafoil tested separately
Heating up in argon to 2500 °C
Injection of air in furnace
Exposition time ~10s

## Slide 12: Tested samples
Sigraflex
Sigrafine

## Slide 13: Results
After exposition to air at 2500 °C in air during 10s, there is a mass loss of:
    0.66% in Sigrafine
    0.99% in Sigraflex
Sigrafine
Sigraflex

## Slide 14: Conclusions
Attack limited to surface
  Thermal energy too high for O2 to penetrate/diffuse in the bulk
Findings in line with previous studies found in literature, limited to 1500 °C
Low temperature oxidation not located on surface  voids would appear in the bulk (longer times required for this)

## Slide 15
Oxidation at 1200 °C – 100s, 1000s
Performed by SGL

## Slide 16: Methodology
Only samples of Sigrafine investigated so far
Furnace heated up to 1200 °C, in argon atmosphere
Switch to air during 100/1000 s
Switch back to argon
Cool-down in argon
Micro scale to measure weight
Physical and mechanical properties measured before/after test

## Slide 17: Results
Strong reaction observed after the air meets the graphite surface
In all three cases, a pattern of the air flow around the sample observed
After 1000s, holes observed on the surface
Mass loss remains limited: ~1% for 100s, ~4% for 1000s
No changes in density, electrical resistivity or dynamic modulus
Air flow indicated by the arrows

## Slide 18: General conclusions
As well known, graphite is sensitive to oxidation at high temperature
Oxidation highly dependent on temperature and exposition time
At significantly high T (>1500°C) oxidation limited to surface, for exposition times of 10s
Greater mass loss observed for longer exposition times, but still attack limited to surface
All tests several times more pessimistic that actual conditions in TDE
These studies allow to exclude the possibility of graphite igniting at high temperature in the presence of air in the TDE scenarios
Comprehensive report including all these studies being written. Expected to be released by end of 2017/beginning 2018

## Slide 19
Back-up slides

## Slide 20: Laser heating – CERN/EN-MME

## Slide 21: Samples
L20010
Anisotropic
Ø 10 mm x 2 mm
L25012
Anisotropic
Ø 10 mm x 2.5 mm
R7300 P500
Isotropic
10 mm x 10 mm x 12 mm
Material supplied by SGL
  Sigraflex I (SI)
  Sigraflex II (SII)
  Sigrafine

## Slide 22: Laser Parameters
3.5 mm
Laser ≠ Proton Beam
Focused beam
Laser source
Sample
400 µm
Best parameters after several trials…
Energy | Frequency | Power | Wavelength | Height
1 J | 1 Hz | 1 W | 1064 mm | Defocused beam Z – 3.5mm
Energy | Frequency | Power | Wavelength | Height
4 J | 1 Hz | 4 W | 1064 mm | Defocused beam Z – 3.5mm
Sigraflex
Sigrafine
Less Energy density in order to minimize the thermomechanical stress on the sample

## Slide 23: Inspection procedure
  Chemical Analysis  chemical composition
Digital microscope KEYENCE VHX 1000
OM “ZEISS Axio Imager” with “ZenCore” software
SEM, field emission gun FEG Sigma (ZEISS)
50 mm2 X Max Energy dispersive X-ray spectroscopy EDS detector (Oxford), INCA software
  Phase Analysis  change in the crystalline phases after the laser impact
X-ray diffraction (XRD), θ/2θ or grazing angle
*OM: Optical Microscope
*SEM: Scanning Electron Microscope
  On sample as received and after impact
  Microscopy observation (OM* and SEM*)  surface aspect

## Slide 24: OM and SEM – Sigraflex
LVD*
MVD*
LVD = Least Visual damage
MVD = Most Visual damage
1.266 °C
9 ms (2 ms/div)
1.393 °C
10 ms (2 ms/div)
1.105 °C
9 ms (2 ms/div)
1.354 °C
10 ms (2 ms/div)

## Slide 25: OM and SEM – Sigraflex
LVD*
MVD*
Discontinuities
1 mm2
0.8 mm2
0.4 mm2
0.65 mm2
Decohesion
Flake like morphology
Swelling
Embossed Surface

## Slide 26: EDS – Sigraflex as received
Peak of C, O, Si
Similar Chemical Analysis
Ʃ peak | E (keV) | El.
C + C | 0.54 | O
C x 3 | 0.81 | -
C + Si | 2.02 | P
Presence and quatification of O cannot be 100% ensured
Examples:
One chosen as reference

## Slide 27: EDS – Sigraflex after impact
Reference
Reference
Higher amount of O and Si
Common features in all Sigraflex samples

## Slide 28: OM – Sigrafine after impact
1.013 °C
10 ms (2 ms/div)
953 °C
9 ms (2 ms/div)
No laser impact visible with OM

## Slide 29: SEM – Sigrafine after impact
Presence of a macro-voids
No changes of Microstructure

## Slide 30: Furnace heating – CERN/EN-MME

## Slide 31: SEM – Sigraflex
No apparent change in Microstructure
Discontinuities
Decohesion
Flake like morphology

## Slide 32: EDS – Sigraflex
Reference
Reference
Pollution: Al, Si, P
No changes in Si and O content

## Slide 33: SEM – Sigrafine
No apparent change in Microstructure
Production marks
Roughness
Irregular

## Slide 34: EDS – Sigrafine
Reference
Same amount of O

## Slide 35: Summary of observations
Laser Impact
Oven Studies
Microstructure:
Embossed surface and Expansion of graphite  Swelling
Degradation of material  Evaporation of material
Microstrucure:
No apparent change in microstructure
Chemical Analysis:
Amount of O and Si keeps constant before and after the study
Chemical Analysis:
Higher amount of O and Si
Presence of pollution  probably due to manipulation
Phase Analysis: no apparent change
The graphite does not seem to be affected thermally
Further study on-going in oven at 1100°C