## Slide 1: Radiation-induced effects on data integrity and -link stability of RD53A Pixel 2018, Taipei
M. Vogt* on behalf of the rd53 collaboration
*Physikalisches Institut, Universität Bonn

## Slide 2: Introduction - RD53A
The RD53 collaboration is a common effort, shared between ATLAS and CMS
Goal: Development of designs and methods for a hybrid pixel detector readout chip in a 65 nm technology
RD53A is the first large (=half) scale demonstrator, produced in 2017, available for testing since 12.2017
Features of RD53A
  Three different analog frontend designs and two memory architectures for comparison
  Fast data link to the readout system
    Aurora protocol
    Several configurable data rate options: 1x 640 Mb/s … 4x 1.28 Gb/s
  Designed to withstand at least 500 Mrad

## Slide 3: introduction
Motivation
  Radiation effects in 65 nm CMOS have been modeled and studied for prototypes
    Transistor level simulation model, using worst case bias conditions
    DRAD test chip to study radiation effects on digital standard cells in 65 nm, agrees with models
  In RD53, most of the previous irradiation campaigns focused on the analog front end performance  The digital performance of the prototype chip RD53A has to be studied, as RD53B is being designed
Main focus of this campaign
  Data link stability and signal integrity, as a function of , and TID
600 Mrad in multiple steps
  Dose rate: 4.5 Mrad/h for the first 20 Mrad, then 6 Mrad/h
  During irradiation: The chip is cooled and operated with a monitor script (digital scan, threshold scan, temperature, power consumption)
  At each TID step: Time consuming and detailed measurements like full shmoo scan and eye diagrams

## Slide 4: Introduction - CDR bypass mode
Default operation mode: CDR/PLL block generates
  Command clock: Recovered from the command data stream
  Serializer: Multiplied (1,2,4,8) command clock
In order to observe only the digital logic behavior, the chip was operated in CDR-bypass mode
  Clocks have to be provided externally
  Generated by the FPGA PLL of the readout system
    CMD_CLK  160 ± 20 MHz
    SER_CLK  640* ± 80 MHz *(the chip was operated in 640 Mbit/s mode)
Analog chip bottom
Digital chip bottom
CDR/ PLL
Cable driver
Serializer
Aurora encoder
CMD decoder
CMD
Pixel matrix
DATA
CMD data
CMD clock
SER clock
CMD CLK
SER CLK
config registers
Hit data
Fixed factor (1, 2, 4*, 8)

## Slide 5
Setup

## Slide 6: X-Ray setup
X-ray cabinet
  Tungsten target X-ray tube: 60 kV, 58 mA max
  Up to ~6 Mrad/h at a beam spot diameter, suitable for RD53A (3 cm)
X-ray cabinet

## Slide 7: X-Ray setup
The chip was operated in direct powering mode: Fixed , variable
Data lane 0: DAQ, monitoring of the serial data link status (errors, sync losses)
Data lane 1: Various data link parameters (amplitude, eye opening, jitter) were measured
X-Ray cabinet
CMD
CLK_CMD CLK_SER
Data lane 0
Data lane 1
Nitrogen or dry air
Chiller
Power supply (with sensing)
BDAQ with FMC adapter card
Oscilloscope

## Slide 8: Temperature control
Temperature of the cooling plate set to
Monitored close to the chip: Fluctuation of during the campaign
Measurements were performed at these
temperatures

## Slide 9
Results: Power and

## Slide 10: Current consumption
Starting from 200 Mrad*, we enabled the clock to the complete pixel matrix  Increased digital power, slope barely affected  Slope for analog power changed
*
Preliminary
Chip didn’t lock during a few scans
Preliminary

## Slide 11: Reference current
Preliminary
RD53A uses a bandgap voltage reference and an internal voltage divider to generate its main reference current
  Nominal value of was trimmed before the irradiation
During the campaign, decreased by ~7.5%
  Caused by the temperature-stable, but radiation sensitive divider (poly silicon + diffusion resistor)
  For RD53B, external resistors will be used instead

## Slide 12
Results: Digital

## Slide 13: Digital scans – SHMOO plots
Question: How large are the margins in terms of digital supply voltage and reference frequency?
Method: Digital scans within a parameter space with 100 injections into every pixel  Expectation: 7.68e6 hits
No link
No hits
Partial FE response
Preliminary
How to read the shmoo plots?
Grey: No link  scan failed
Red: No hits  Link established, but no FE response
Yellow: Only partial FE response
Green: Expected FE response
Nominal operation

## Slide 14: Digital scans – SHMOO plots
1 Mrad
No link
No hits
200 Mrad
600 Mrad
Preliminary
Preliminary
Preliminary
Partial FE response
Outlier
With increasing dose
  fewer combinations of operating condition are working
  the margin decreases

## Slide 15: Digital scans – SHMOO plots
The digital logic is supposed to work at 0.9 V after 200 Mrad (according to simlations)
1 Mrad
No link
No hits
200 Mrad
600 Mrad
Probably a POR issue
Preliminary
Preliminary
Preliminary
Preliminary
Lower digital current indicates incomplete POR/configuration
Partial FE response
Preliminary
Preliminary

## Slide 16: Digital scans – SHMOO plots
200 Mrad POR@1.2V
600 Mrad POR@1.2V
Preliminary
1 Mrad
No link
No hits
Partial FE response
200 Mrad
600 Mrad
Probably a POR issue
Preliminary
Preliminary
Preliminary
Additional scan introduced with different reset conditions
POR is more reliable, when the chip is first powered (and reset) at 1.2 V, before lowering
Preliminary

## Slide 17: Power-on reset
The POR circuit was designed using the analog corner ()
With , the reset signal is only a short pulse, which is insufficient to reset the logic reliably
POR simulation
1.2 V 
1.2 V 
1.2 V 
1.1 V 
0.75 V 
60 mV 
 2.5 mV

## Slide 18: Command/data phase shift
In CDR bypass mode, the phase between command clock and data is critical
Measurement with a controllable external two channel clock generator after the campaign: Ch1: FPGA (CMD data), Ch2: CMD clock to the chip. Phase between channels was varied
The setup- and hold timing changes with temperature and dose
  Hold time (distance between data transition and clock edge) increases by
  The critical phase region increases from ~20° at 10 Mrad to ~45° at 600 Mrad
Only in these small regions, the link failed
Absolute phase value depends on cables etc.

## Slide 19: PLL: VCO tuning range
In the default operation mode of the chip, a CDR/PLL block locks to the CMD clock and provides several clocks, derived from the internal VCO
Measurement of the VCO gain curve
  is scanned from 25 mV to 1.2 V, while the frequency is measured
  Compared to a non-irradiated chip, the VCO gain decreased and the frequency range shifted slightly
Preliminary
Nominal VCO operating frequency: 1.28 GHz

## Slide 20: EYE diagrams
Most interesting values from the eye diagrams
  Time Interval Error: RMS of the total jitter (1)
  Eye width(2), height (3): Define the eye opening, bit amplitude(4)
Cross-coupling of SER_CLK can be seen on the data line: (4) in bypass mode – no issue for the data link
(2)
(2)
(1)
(3)
Cross talk in bypass mode (4)
PLL mode
Bypassmode
Preliminary
Preliminary
(4)

## Slide 21
Results: Analog Front Ends

## Slide 22: Threshold
0 Mrad SYNC
0 Mrad LIN
0 Mrad DIFF
600 Mrad SYNC
600 Mrad LIN
600 Mrad DIFF
SYNC
LIN
DIFF
Preliminary
Preliminary
Preliminary
Preliminary
Preliminary
Preliminary

## Slide 23: noise
0 Mrad SYNC
0 Mrad LIN
0 Mrad DIFF
600 Mrad SYNC
600 Mrad LIN
600 Mrad DIFF
SYNC
LIN
DIFF
Preliminary
Preliminary
Preliminary
Preliminary
Preliminary
Preliminary

## Slide 24: conclusion
RD53A 0x0C5B has been irradiated to 600 Mrad
Observations:
  No significant degradation of the cable driver and the VCO tuning range
  POR is not reliable at after 200 Mrad. Confirmed by simulation, to be improved in the next version.
  decreases by ~7,5%  Mitigation by usage of external precision resistors for RD53B
  Operational temperature critical after irradiation (need to stay below ~-10 °C for stable operation)
Future plans
  Irradiation of a few samples to different TID
  Non-uniform irradiation
  SEU/SET studies

## Slide 25
THANK YOU

## Slide 26
Backup

## Slide 27: BACKUP - readout system
Two readout systems for testing have been developed within the RD53 collaboration
  YARR: Comprehensive PCIe-based readout system with software framework written in C
  BDAQ53: Easy to use characterization and verification environment based on Python
Main purpose: Evaluation of the RD53A prototype chips:
  Electrical characterization (single chip)
  test beam performance measurements
  multi-chip (module) tests
  wafer-level tests with a probe station
BDAQ53 was used for this campaign: Ease of use
  Single board, no additional adapters
  Ethernet interface
  No specific PC needed, even works with a Laptop
  Python based software: Fast debugging
  Alternative HW platforms supported: Xilinx KC705, USBPix3
BDAQ53 setup with RD53A Single Chip Card

## Slide 28: BACKUP - Bdaq53 Firmware
Several firmware modules are instantiated from the Basil firmware library (FIFO, GPIO, I²C etc.)
“Basil Bus”
  Simple 32-bit wide bus for internal control signals
  Firmware modules are addressed
  Bus master: Interface to the SiTCP Ethernet IP core (1Gbit/s)
AXI4-Stream
  Aurora IP core from Xilinx (GTX transceivers)
  Wrapper translates to the generic FIFO-style interface of SiTCP
Command encoder
  Programmable sequencer
  Arbitration of triggers and idle/sync patterns
Future plans
  10 Gbit/s Ethernet for SFP+
  DDR3 memory FIFO
Computer
Basil bus
RD53A
Programmable reference clock
Ethernet PHY
Xilinx Kintex 7 FPGA
DAQ system board
CMD encoder
Aurora receiver
PLL
I²C
Basil bus master
SiTCP IP core
BRAM FIFO
TLU controller
TLU
GTX
SelectIO