## Slide 1: TISD activities in 2017/18
Sebastian ROTHE
EN-STI-RBS

## Slide 2: The Target and ion Source Development (TISD) team
Providing a large choice of intense and pure radioactive beams
Constant development is required to keep ISOLDE at the forefront of RIB facilities
J. Ballof
Y.Martinez
T. Stora
F. Boix Pamies
S.Rothe
J.P.Ramos
D. Leimbach

## Slide 3: RILIS Team

## Slide 4: ISBM working group
R&D for
Ion Source &
Beam
Manipulation
(ISBM)
Scheme
development
Laser
development
RILIS
operation
Laser
spectroscopy
Target
development
Target
construction
Target operation
Technical
coordination
of ISOLDE
EN/STI
LP
EN/STI
RBS
Negative ion beams
LIST
Fast beam gating
Ion beam multiplexing
ISCOOL upgrades
FEBIAD optimization
VADLIS
ToFLIS
HRS upgrade
Ongoing development projects
Ion source selectivity
Optical pumping in ISCOOL
Development of refractory metal beams

## Slide 5: Target and ion Source Development (TISD) mandate
Providing a large choice of intense and pure radioactive beams
Constant development is required to keep ISOLDE at the forefront of RIB facilities
target and ion source units
target materials
beam interactions (p2n converter)
ion source design / mode of operation shared with ISBM group
yield & release study
ion source efficiency measurements
prototype tests
Sharing same resources as the ISOLDE physics program
WORKSHOP: target unit production
OFFLINE: target quality control
ISOLDE: beamtime

## Slide 6: Expected TISD @ ISOLDE (presented to GUI February 2017)
Sc: Ti foils (CF4, RILIS)
Te: yields with RILIS
M(CO)x formation @ MEDICIS irradiation point
ThO felt + Negative ion source
LIEBE @ GPS-online
STAGISO beam test
Si from UCx
TiC-CNT (pending safety clearance)

## Slide 7: Expected TISD @ ISOLDE (presented February 2017)
DONE
DONE
ongoing
ongoing
DONE
ongoing
pending
ongoing
Sc: Ti foils (CF4, RILIS)
Te: yields with RILIS
M(CO)x formation @ MEDICIS irradiation point
ThO felt + Negative ion source
LIEBE @ GPS-online
STAGISO beam test
Si from UCx
TiC-CNT (pending safety clearance)

## Slide 8: Scandium beams
 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50 | 51
FC |  |  |  | 1.5E+07 | 1.2E+07 | 8.1E+06 | 7.3E+05 |  | 
betas |  |  |  |  |  |  | 7.6E+05 | 1.8E+04 | 
MR-TOF |  |  |  | 2.3E+06 | 1.6E+06 | 1.2E+06 | 7.4E+05 | 1.3E+04 | 
Extrap. | 3.6E+05 | 1.2E+06 |  |  |  |  |  |  | 1E+02
Target: #565 Ta Ta
Mass scan (FC.558)
ISOLTRAP
MT-ToF spectrum

## Slide 9: 5 RILIS elements in one week: new record!
Titanium
Scandium
Selenium
Dysprosium
Scandium
Dysprosium
Nickel
B.Marsh
Samarium
Convenient
efficient
one-laser
2-step scheme
Selenium
Tested
on-line
But further beam development
needed

## Slide 10: The LIEBE target – Assembled
LIEBE fully assembled and coupled to offline 1
LIEBE loop before enclosement.
F. Boix Pamies

## Slide 11: Dedicated test stand for ion source development
Main features:
ion beam extraction and detection
residual gas analyzer (RGA)
automated control and data recording (LabVIEW)
First application:
negative ion source development
investigation of source poisoning and regeneration
Future plans:
long-term performance studies
thermal stress tests
destructive tests
  operational limits
  failure mode analysis
ISOLDE calibration stand
integration
D.Leimbach

## Slide 12: Low work function materials for negative ion production
Improvement of ionization efficiency:
Elements with low affinities are not efficiently ionized by LaB6
New compounds needed:
  SrVO3 with expected work function <2eV
First steps:
Production of suitable candidates
Electron emission tests with LaB6 as benchmark
Performance studies
Next steps:
Compare geometries offline
D.Leimbach
MK4 – Pellet source
Tubular low workfunction cavity

## Slide 13: LIST
HFS studies of polonium / supression of francium (IS456, September 2012)
Proton
beam
On-line implementation and first operation of the Laser Ion Source and Trap at ISOLDE/CERN, D. Fink et al., NIMB 344, 83-95 (2015)
In-Source Laser Spectroscopy with the Laser Ion Source and Trap: First Direct Study of the Ground-State Properties 217,219Po, D. Fink et al., PRX 5, 011018 (2015)
90 mm
Isobaric suppression > 1000, efficiency loss ≈ 50
R.Heinke

## Slide 14: LIST 2018
Obtained technical drawings from Larissa Group Mainz
LIST 2.0 assembly will be provided from Mainz
To be verified: status of RF cable at GPS
LIST control system: replicate 2012 setup
https://edms.cern.ch/document/1400724/1
R.Heinke

## Slide 15: LIST Development (LS2)
Full integration to ISOLDE infrastructure
Fast line heating inversion
Connection to quartz transfer line
Connection to ToFLIS project

## Slide 16
Ionization
Motivation
Production
J.Ballof

## Slide 17
Up next
Irradiations at MEDICIS
carbonyl formation and
Stability at ISOLDE
J.Ballof

## Slide 18: Neutron deficient SeCO beams
Target #605 and #612
Zirconia fibers, stabilized with ca. 10% Yttria
Principle:
Se + CO  SeCO
Beam available since many years.
but….
SeCO gone after a few days
Atomic Se still released after days
Shifting the mass to get pure beams
Why does SeCO disappear,
even if we inject CO2?
Injecting 13CO2….
…extracting Se12CO
Injected CO2 gas does not
promote SeCO formation!
Carbon from the ion source?
-> Placed graphite grid, but still depleting
Carbon from the target material?
-> EDS (preliminary) shows no carbon in ZrO fibers
What’s the source of carbon?
Indications, that CF4 gas might serve as carbon source. Work in progress.
Chart: 
| Day 0 | Day 3
71Se | 560000 | 88000
71SeCO | 360000 | 1
71Se
71SeCO
CF4
injection
J.Ballof

## Slide 19: Boron fluoride beams
First production unit #606
Despite high injection,
low fluorination, and presence of oxygen. H2O or air leak?
Not clear, if the unit
would produce BFx beams.
Principle:
B + 3 F  BF3
Volatilization of refractory boron by injection of SF6 gas
First prototype #499
Small gas leak (3.7e-5 mbar L / s)
Absence of TaFx and SFx in mass spectra
Unit did not produce BFx beams
no fluorine saturation
Second prototype #513
Increased leak (1.84e-4 mbar L/s)
Strong TaFx and SFx peaks
No TaO peaks
Stable and intense 8BFx beams
TaOxFy deposits in target
Gas line rupture

## Slide 20: Clean 206Hg beams with VADLIS
3rd on-line application of VADLIS ion source for an experiment
  (full Hg chain for in source laser spectroscopy; Mg + Ne for ISOLTRAP, 206Hg for Miniball)
RILIS–mode achieves similar efficiency to VADIS-mode
Note: RILIS-mode efficiency is expected to improve by at least 2 x if the adjustable-extractor VADIS is used.
B.Marsh

## Slide 21: VADIS / VADLIS developments
Standard VADIS
VADIS Dev. [1]
Y.Martinez
Extraction plates 0 V
Extraction plates -100 V
[1] Y. Martinez et al. In preparation

## Slide 22
ISOLDE neutron converter design
Main challenges: Large oven to heat up and electrical insulate tungsten from oven current
Proton fluences
Neutron Fluences
 | New | Old
n-ind fissions (/s) | 2.79E11 | 4.55E10
p-ind fission ratio | 10.8% | 16.1%
Deposited Power | 690 W | 553 W
UCx Volume | 60 cc | 30 cc
Done:
Systematic FLUKA simulations for geometry optimizations
At the moment:
Thermomechanical simulations of the larger oven
Procurement of materials
mechanical design of prototype
J.P.Ramos

## Slide 23: FEM model p2n Target: container temperature (1000 A)
M. Ballan, INFN
Container outer diameter: 51 mm
Container thickness: 0.25 mm
SGL® SIGRATHERM thermal screen: 10 mm
  https://edms.cern.ch/document/1128002/1
Mo thermal screen: 0.2 mm
To be used for MEDICIS target and potentially for p2n target at TRIUMF
S. Marzari

## Slide 24: Ucx production: Previous process
2UO (s) + 3 C (s)-> 2 UC (s) + CO2 (g)
Setting ramp
Monitor pressure via webcam
Write down values manually
Detect end of carburization
by pressure drop
May result in inconsistent carburization.
Time consuming (~10 days).

## Slide 25: Automatic UCx Production
Setting a ramp
Set thresholds
Start carburization
Heating is regulated automatically
Successfully used for UC611 and UC618
Finished in 4 days without human intervention

## Slide 26: ISOLDE Yield Database YYDB(https://isoyields2.web.cern.ch)
Features
CERN SSO
New Database design
In target production (ABRABLA)
Release curves available
More target details visible
Issue tracking
Philosophy
All measurements (TISD, USERS) get entered into YYDB
Manually change attribute (measured -> validated -> published)
Attribute determines visibility (after login, no login required)
Future
Web based interface allows entering of yields to registered users
Add FLUKA results for in-target production
Add yield prediction
Establish link to CRIBE database
J.Ballof

## Slide 27: Potential TISD @ ISOLDE, 2018
LIEBE @ GPS-online (2017)
LIST 2.0
M(CO)x formation @ MEDICIS irradiation point
P2n converter prototype test
Negative ion source
Si beam development
VADLIS prototype online

## Slide 28
Thanks to the TISD and RILIS teams

## Slide 29: MWCNT Target production for #606
CERN has forbidden any handling of nanomaterial
Nanomaterials are requested at ISOLDE for physics (in this case MWCNT)
Powder technology laboratory in EPFL, has a class “nano 2”
Accordingly to EPFL specifications “nano 3” is needed to handle MWCNT (need to have the nanomaterial sealed in glovebox)
Glove’s bag was bought from Sigma Aldrich and used instead of Glove’s box.
Possible solution to lift the prohibition of handling nanomaterials
Successful press of full batch of MWCNT for ISOLDE target #606
J.P. Ramos, B. Crepieux, T. Stora, et al.

## Slide 30: Nanolab
Option 1
Option 2
Funding secured
Construction to be finished 2018
Connection of ventilation foreseen in 2019

## Slide 31: p2n-converter development (as Presented in previous GUI)
50 kW , 500 MeV beam
Converter
UCx
Beam
Project Started in December
Weekly meetings with CERN/TRIUMF/SCK
Within CERN-TRIUMF MoU
+ SCK-CEN
Concept
Design + Offline Tests
Prototype ready
TRIUMF tests
Apr-2017
Sep-2017
Jan->May-2018
Aug->Dec-2018
ISOLDE test
?-2018
Preliminary time line:
ANSYS
FLUKA
J.P.Ramos

## Slide 32: Dedicated oven for CaO production
Current issues:
Thermocouple positioning difficult (can’t trust readout)
  Use pyrometer but readout is difficult in the 700 – 800 °C range
Thermal gradient in the container makes process much longer than should
CaO production unit difficult to handle in gloves box
Target unit building
Material production
Glove’s box for material transfer into unit (very sensitive to CO2 and H2O)
Calibration Target + Ion Source
Offline tests
ISOLDE
CaCO3 → CaO + CO2
About a week to produce material in pump stand
Precise control of temperature
Temperature uniformity
Higher quality CaO
Quartz tube easy to handle in glovesbox
Production will be reduced to half-day.
J.P. Ramos, et al.

## Slide 33: STAGISO vs NORMISO Study
J.P. Ramos
Chart: 142 on Converter
| 6 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 120 | 140 | 160 | 200 | 300 | 400 | 500 | 650
NORM | 0.001726 | 0.001778 | 0.0017947 | 0.0018459 | 0.0018814 | 0.0019912 | 0.0020288 | 0.0020922 | 0.0021325 | 0.0022039 | 0.0021632 | 0.0021732 | 0.0021952 | 0.0021139 | 0.0021587 | 0.0020376 | 0.0021805 | 0.0019865 | 0.0019415 | 0.0015557 | 0.0013106 | 0.0011822 | 0.00088959
STAG | 0.0018433 | 0.0018255 | 0.0018113 | 0.0017702 | 0.001799 | 0.0018986 | 0.0019882 | 0.0019724 | 0.0019799 | 0.0020855 | 0.0021006 | 0.001947 | 0.0021486 | 0.0020204 | 0.0018901 | 0.0019772 | 0.002032 | 0.0018593 | 0.0016824 | 0.0017523 | 0.0014041 | 0.0011888 | 0.0010119
Chart: 142 on Target
| 6 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 120 | 140 | 160 | 200 | 300 | 400 | 500 | 650
NORM | 0.019272 | 0.01922 | 0.020548 | 0.021659 | 0.021721 | 0.021784 | 0.02253 | 0.023491 | 0.023945 | 0.024592 | 0.027252 | 0.027252 | 0.029368 | 0.028507 | 0.028535 | 0.028724 | 0.025906 | 0.025021 | 0.019449 | 0.0181 | 0.015126 | 0.012555
STAG | 0.018427 | 0.018903 | 0.018931 | 0.020105 | 0.020119 | 0.022022 | 0.0221 | 0.023498 | 0.024848 | 0.025968 | 0.027377 | 0.027098 | 0.025769 | 0.027372 | 0.028184 | 0.027264 | 0.027108 | 0.023317 | 0.019955 | 0.017958 | 0.016836 | 0.012957
2.3 μs in NORM
16 μs in STAG
230 ns in NORM
Booster pulse pictures from PhD Thesis, R. Wilfinger
Release measured on:
GPS and HRS
Target and Converter
26Na and 142Cs
Results to be published soon.
No difference between STAGISO vs NORM

## Slide 34: Tellurium beams
A (Te) | t1/2 | Te Yield | Cs yield | t1/2 | A (Cs)
132 | 76.3 | 5.40E+08 |  | 6.47 d | 132
133 | 12.5 m | 7.50E+07 |  | stable | 133
133m | 55.4 m | 1.50E+08 |  | stable | 133
134 | 41.8 m | 1.90E+08 | 1.10E+09 | 2.90 h | 134m
135 | 18.6 s | 5.40E+06 | 5.50E+08 | 53 m | 135m
136 | 17.5 s | 5.40E+06 | 5.30E+08 | 19 s | 136m
137 | 2.5 s | 1.20E+05 |  | 30.17 y | 137
Chart: Te mass
| 132 | 133 | 133 | 134 | 135 | 136 | 137
Measured Yield | 540000000 | 75000000 | 150000000 | 190000000 | 5400000 | 5400000 | 120000
In-target production (ABRABLA) | 905000000 | 596000000 | 596000000 | 605000000 | 153000000 | 79600000 | 10100000
Chart: t1/2 (s)
| 274680 | 750 | 3324 | 2508 | 18.600000000000001 | 17.5 | 2.5
 | 0.59669 | 0.12584 | 0.25168 | 0.31405 | 0.035294 | 0.067839 | 0.011881
J.P. Ramos, S. Rothe, et al.
Total efficiency = Ionization efficiency x release efficiency
Target #601 UC n

## Slide 35: The LIEBE target – Offline tests
Offline tests:
  Leak tests
  Vibration tests
  Heat exchanger calibration
  Ion source test
Chart: Temperature of LBE [°C]
| 200 | 300 | 400 | 500 | 600
1 | 467.959 | 760.4548 | 1082.764 | 1419.076 | 1773.911
2 | 576.407 | 926.507 | 1288.058 | 1661.427 | 2042.951
3 | 633.8471 | 1040.662 | 1467.323 | 1921.356 | 2399.828
4 | 1183.309 | 1971.556 | 2778.174 | 3559.626
5 | 2409.721 | 3955.254
Ansys CFX simulations of heat exchanged for every water channel.
1
2
3
5
4
Offline tests 6th-10th November
Operational review 3rd week of November
Target to be installed at GPS end of November
3D model of the heat exchanger, 5 water channels to cope with 5 different temperatures.
F. Boix Pamies