## Slide 1
WP 13.2.1 Establishing new resistive materials for high rate RPCs
P. Fonte

## Slide 2: WP 13.2.1
DESCRIPTION
A list of low resistivity materials like HPL, Glass, Ceramics and new plastics is established;
Their resistivity (bulk, surface) and homogeneity are studied;
Their ageing properties due to large integrated doses are also determined;
The materials are qualified by determining the rate response and ageing properties of RPCs (single and multi-gap) by exposing these materials to intense sources/beams
DELIVERABLES
“Validation of new resistive materials for high rate RPCs through the study of the rate and ageing properties of small RPC prototypes (single and multi-gap-detectors) exposed to intense sources/beams.” [M36]

## Slide 3: Global schedule
 | Year 1 | Year 2 | Year 3 | Year 4
Definition of standards/procedures |  |  |  | 
Inventory and procurement of materials |  |  |  | 
Exploratory tests electrical/RPC |  |  |  | 
Electronics development |  |  |  | 
Detailed tests in lab of chambers made out of the best candidate materials |  |  |  | 
Address ageing |  |  |  | 
Beam test of small but realistic systems |  |  |  | 
Conclusion and reporting |  |  |  | 
We are here

## Slide 4: Materials considered
4
Beam-tested
low  PVdF+C (plate 400x300x2 mm3 produced by injection by the Lyon group)
KREFINE (large plate bought, cut and distributed to the participants)
Phosphate glass (kindly provided by Tsinghua University)
Thin (0.4mm) soda-lime glass for reference
Not tested because of too small size
Pestov glass (obtained from GSI stock)
Ceramics (developed by HZDR - Helmholtz-Zentrum Dresden-Rossendorf)
Procedures
Besides traditional beam-testing, all chambers were tested at several stages by argon-discharge, allowing to measure the resistance of the electrode in-chamber and infer the resistivity, while monitoring the stability of the material and the presence of strong surface anomalies (examples ahead).

## Slide 5: PVdF + carbon nanoparticles
PVdF is a thermoplastic material and has similar chemical and mechanical characteristics as PEEK, but could be melt at a lower temperature (180 °C for PVdF and around 400 °C in the PEEK case) which facilitates its production.
Several loadings (6 to 8%) were tested. Plates of 30 cm  40 cm of 2 and 3 mm were produced by injection process at the IPC company in France.
Plates with the black-carbon 6% loading were found to have a bulk resistivity of 1012 cm. Several RPC detectors were produced and successfully tested. Efficiency reaching 96% were measured.
The plates with higher loading (8%) reach lower resistivity values (a few 1010 cm).

## Slide 6: PVdF + carbon nanoparticles
Example of argon test of a PVdF-C chamber
The resistive electrode was composed by two 2.5mm thick plates glued together

## Slide 7: Phosphate glass
Phosphate glass is produced by Tsinghua University for high-rate RPC applications
[Jingbo Wang et al., 2010]
[Yi Wang et al., 2012]

## Slide 8: Phosphate glass
Argon tests of the phosphate glass chambers
pre-beam post-beam
No significative changes
The resistive electrode was composed by a single 0.7 mm thick plate

## Slide 9: Phosphate glass
Long term argon test to evaluate resistivity stability
The material shows an essentially stable conductivity over time, suggesting a minor ionic contribution to its conductivity.

## Slide 10: KREFINE
An interesting range of resistivies
Quite expensive (~3k€/m2)

## Slide 11: KREFINE
Argon tests of the KREFINE chambers
pre-beam post-beam
The resistive electrode was composed by two 3 mm thick plates
No significative changes

## Slide 12: KREFINE
Long term argon test to evaluate resistivity stability
The material shows a conductivity that decreases at a progressively lower rate over time, suggesting a mixed ionic and electronic conductivity.
Nevertheless, the electronic part seems to assure a usable long-term conductivity within a factor 2 of its short-term value.

## Slide 13: Beam test - hardware
Fig. 7 – Left hand: in the spacerless construction the gap between the electrodes is defined by a glue pillar outside the active area. Right hand: RPC inside its shielding box.
Resistive anode
(PVdF in this case)
Stainless steel cathode (100 cm2)
All chambers of identical construction: 1 mm gas gap
1 stainless steel cathode
1 resistive anode
Painted HV layer
No internal spacers
Spacerless construction
Shielding box
9 readout pads

## Slide 14: Beam test - hardware
Inner view
Outer view w/out shielding
Beam line view
Both charge and time could be read on each pad (not at same time)

## Slide 15: Beam test – relative rate capability
As expected,
phosphate glass and KREFINE allow at least two orders of magnitude larger rate capability than thin soda-lime glass

## Slide 16: Beam test – relative rate capability
soda-lime
Single spill @ intense beam
phosphate
PVdF
KREFINE

## Slide 17: Aging – resistivity
Long term argon-discharge test to evaluate resistivity stability
Small or tolerable effects

## Slide 18: Aging – soda-lime
Post-beam examination
No alterations

## Slide 19: Aging – PVdF
Post-beam examination
No alterations

## Slide 20: Aging – Phosphate
Post-beam examination
Alterations visible on the glass, but not on the SS. Both chambers worked normally.
Clean regions! Maybe by the argon discharge.
This deposit could be wiped clean with alcool.
Clear cathodes

## Slide 21: Aging – KREFINE
Post-beam examination
Stains on the plastic, some transferred to the SS. Both chambers worked normally.
Some stains. Looks like erosion.
Little hole + transfer of material to the cathode

## Slide 22: Conclusion
Three different new resistive materials for high rate RPCs were identified or developed and extensively tested.
Eight RPCs were made, two of each kind of new material, plus two made out of standard soda-lime glass, for reference. In these chambers the cathodes were made out of stainless-steel plates and there were no internal spacers, to isolate as possible the materials’ behavior from the constructive details.
The resistivity of the materials was measured in the chambers themselves by the argon-discharge method, both before and after irradiation.
A beam test was performed on the set of eight chambers, confirming their different rate capability.
After-beam observations revealed that the resistivity of the materials was not changed, but that some signs of surface alterations were visible on some of the materials. Despite such alterations the chambers continued to operate normally.
Future work should include similar tests with the resistive electrodes also performing as cathodes and longer irradiations.