## Slide 1
Davide Tommasini
Task Force 11T Meeting
Friday 10 November 2017
Proposed insulation scheme for the 11 T

## Slide 2
Introductory remarks
the insulation thickness unfortunately has to be < 100 µm, imposed by design
the 11T are in series with the main dipoles
Nb3Sn performance is very sensitive to stress
stress distribution depends on insulation scheme (Susana)
evidence that performance of models is limited by conductor degradation
From available data we can suspect that degradation is caused by:
excessive peak stress on the conductor
excessive longitudinal strain
Case 1 may be cured by using a different insulation scheme and by better collaring procedure
Case 2 by thicker end plates in short magnets, probably not necessary in long magnets
Considering the enormous effect of the insulation, very likely most of present problems are linked to the insulation scheme and to collaring, but it is not excluded that at higher fields the longitudinal effect may become important.
To identify the exact causes of degradation is essential first to perform training at 4.2K !

## Slide 3
Proposed insulation
Considering the introductory remarks, the proposed insulation system consists of the same layout considered for the FCC, with a reduced thickness to fit in the 100 µm limit, as the scheme shown by Susana:
mica/glass sheet 31 mm (gap 0.9 mm nominal) followed by glass fibre
The mica side of the sheet shall be towards the conductor, the glass side on the outside.
This should be implemented, from now, on all next coils, but only after having performed at least one impregnation test to validate the 31 mm (if poor impregnation use 30 mm).
We also remark that, to precisely identify the causes of a possible performance limitation, on next model magnets is essential first to perform a training at 4.2K !

## Slide 4
Thank you for your attention