## Slide 1: Copper Measurements with High Frequency Ultrasound Microscope
Antti Meriläinen1,2, Ivan Kassamakov1,2, Markus Aicheler2, Kenneth Österberg1,2 and Edward Hæggström1
1) Department of Physics, University of Helsinki
2) Helsinki Institute of Physics

## Slide 2: Why Acoustic Microscope
Optical methods do not measure elasticity
Tapping mode AFM is not easy to calibrate for elasticity
µCT Does not see elasticity close to the surface
Ultrasound transducer
Goniometer tilt stage
XY Stage
Sample
1 cm
Goniometer tilt stage

## Slide 3: Pulse Echo Measurements
Time-of-Flight
Single Pixel
Echo Amplitude
Time-of-Flight: Surface Topography
Amplitude: Mechanics

## Slide 4: Math of Acoustic Reflection
Time-of-Flight
Echo Amplitude Calibration
UV Fused
Silica
Silicon
Sapphire
Copper

## Slide 5: Math of Acoustic Reflection
Echo Amplitude: Mechanics from acoustic impedance
is Poisson's ratio of copper
is the density of copper

## Slide 6: Scanning Acoustic Microcopy
10 mm
Frequency range: 130 – 370 MHz
Pixel-by-Pixel Imaging
Areas 1 mm * 1 mm
  Stepping 1-3 µm
Focus size: less than 3.5 µm
Imaging time: ~1-5 min/mm2
10 mm

## Slide 7: Copper Sample #1 Field Emission Sample

## Slide 8: Field Emission Areas 250 MHz Transducer
Optical
Ultrasound
HR-SEM

## Slide 9: Large Area US Images 400MHz Transducer
Resolution 2.5 μm
Transducer is uncalibrated
  Normalized color scale

## Slide 10: Large Area US Images 400MHz Transducer
Resolution 2.5 μm
Transducer is uncalibrated
  Normalized color scale

## Slide 11: Beneath the surface
Challenges:
Over 90% of sound reflects from Cu surface
Focused transducer are designed for water
  Limited working distance
  Total reflection
  Wave bend in water-copper interface
Echoes are weak
  Low noise system needed
  Background rejection
Synthetic Aperture Focusing Technique (SAFT)
  Good phase control
  CPU, GPU and memory needed
  Only qualitative contrast

## Slide 12: Synthetic Aperture Focusing Technique (SAFT)
∑(…) =
Delay Filter
Rx Signals

## Slide 13: SAFT Results 250 MHz Transducer
-70 μm Focus
Original
-70 μm Focus
-30 μm Focus
Original Focus
-30 μm Focus

## Slide 14: Future Work
Surface elasticity (GPa)
  Scattering from non-flat surface
Surface wave-velocity
  Another acoustic parameter
  V(z) -technique
  More accurate stiffness
Look under the surface / SAFT
  Need more research

## Slide 15: Questions and Comments
Thank you for your attention!
Acknowledgements to:
Dr. Marek Jacewicz
Mr. Jere Hyvönen

## Slide 16: Z-Focus vs Amplitude

## Slide 17: Pulse Compression Cross Correlation
dt descript depth resolution
dt depends on bandwidth
dt

## Slide 18: Coded Signal and SNR
SNR =0.1
SNR =1