## Slide 1: Compression test on annealed copper samples – HT Nb3Sn EDMS 1871901
Christian Löffler – CERN Dr.-Ing. David von Mirbach – MPA Stuttgart Dr.rer.nat. Joachim Kinder – MPA Stuttgart CA6931507
LMF_FEA-meeting 24-11-17

## Slide 2: scope
Three batches of copper samples, heat treated at three different temperature for 48 h.
  210 °C, 400 °C and 640 °C
  CU-OFE-ASTM C10100 D 12,7 mm
  One batch = four samples
  50 K/h
WHY?
  No material data available for fully annealed copper in compression

## Slide 3: experiment
Compression test at room temperature after the heat treatment
  DIN 50106:2016-11
  1 mm/min
  Contact sample to die was lubricated
  One extensometer on the die and one on the sample
  Rdp0.2 after DIN 50106
  Per batch:
    2 samples were cycled to 50, 100, 150 MPa
    2 samples directly to 30 % compression

## Slide 4: experiment
sample – 12.6 x 15 mm
setup

## Slide 5: Results
HT to 210 °C reduces the RPdp0.2 from 309 to 248 MPa
HT to 400 and 640 °C changes the material to show basically no elastic behavior
  400 °C - RPdp0.2 35 MPa
  640 °C - RPdp0.2 19 MPa
Chart: Stress-Strain curve, copper after heat treatment

## Slide 6: Results – no HT
No heat treatment
No plastification at 100 MPa
First irreversible deformation at 120 MPa
Chart: Stress-Strain curve, copper no HT

## Slide 7: Results – HT 210 °C
Heat treatment to 210 °C
Elastic behavior until 50 MPa
First plasticity occurs at 65 MPa
Elliptic stress-strain curve
Chart: Stress-Strain curve copper after heat-treatment 210°C 48 h

## Slide 8: Results – HT 400 °C
Heat treatment to 400 °C
Elastic behavior until 8 MPa
No elepticity
Chart: Stress-Strain curve copper after heat-treatment 400°C 48 h

## Slide 9: Results – HT 400 °C
Plot zoomed in
Heat treatment to 400 °C
Elastic behavior until 8 MPa
Chart: Stress-Strain curve copper after heat-treatment 400°C 48 h

## Slide 10: Results – HT 640 °C
Heat treatment to 640 °C
Elastic behavior until 5 MPa
Chart: Stress-Strain curve copper after heat-treatment 640°C 48 h

## Slide 11: Results – HT 640 °C
Plot zoomed in
Heat treatment to 640 °C
Elastic behavior until 5 MPa
Chart: Stress-Strain curve copper after heat-treatment 640°C 48 h

## Slide 12: conclusion
After a heat treatment to 640 °C the copper is fully annealed with a yielding point of 5 MPa
  The behavior is nearly perfectly bi-linear
  Tangent modulus 1.5 – 2.5 GPa
  Modulus after plastification 85 – 95 GPa
Very similar values were used in the past for the strain dependency analysis Nb3Sn by:
  G. Vallone, C. Löffler, N. Mitchell etc.