## Slide 1: Overview of parameters used in structural FEM simulations for the 16T magnets
J. Munilla, F. Toral - CIEMAT

## Slide 2
Materials and Conditions as agreed
MATERIAL | σVM (MPa) |  | σ1 (MPa), 4K | E (GPa) |  | Poisson | CTE
 | 293 K | 4,2 K |  | 293 K | 4,2 K |  | Integ (293 K to 4,2 K)
Coil | 150 | 200 | - | Ex = 52 | Ex = 52 | 0,3 | X = 3,1E-3
 |  |  |  | Ey = 44 | Ey = 44 |  | Y = 3,4E-3
 |  |  |  | Gxy = 21 | Gxy = 21 |  | 
316LN St. Steel | 350 | 1050 | - | 193 | 210 | 0,28 | 2,80E-03
Al7075 | 480 | 690 | - | 70 | 79 | 0,3 | 4,20E-03
Iron (Ferromag) | 180 | 720 | 380 | 213 | 224 | 0,28 | 2,00E-03
Ti6Al4V | 800 | 1650 | - | 115 | 126 | 0,3 | 1,70E-03
Supporting structure and same conditions checked up to 105% of magnetic loads
Frictional coefficient for FEM analysis: 0,2
Limit stress values in the table are considered maximum for first design, and linear+elastic behavior up to it
Plane Stress conditions for 2D first designs
Coil properties in the table are considered perfectly homogeneous in the whole block for this first stage

## Slide 3
Materials and Conditions as agreed
MATERIAL | σVM (MPa) |  | σY (MPa) | σ1 (MPa), 4K | E (GPa) |  | Poisson | CTE
 | 293 K | 4,2 K | 4,2 K |  | 293 K | 4,2 K |  | Integ (293 K to 4,2 K)
Coil | 150 | 200 |  | - | Ex = 52 | Ex = 52 | 0,3 | X = 3,1E-3
 |  |  |  |  | Ey = 44 | Ey = 44 |  | Y = 3,4E-3
 |  |  |  |  | Gxy = 21 | Gxy = 21 |  | 
316LN St. Steel | 350 | 1050 | 600 | - | 193 | 210 | 0,28 | 2,80E-03
Al7075 | 480 | 690 | 400 | - | 70 | 79 | 0,3 | 4,20E-03
Iron (Ferromag) | 180 | 720 | 700 | 380 | 213 | 224 | 0,28 | 2,00E-03
Ti6Al4V | 800 | 1650 |  | - | 115 | 126 | 0,3 | 1,70E-03
Remark on the stress limits
These are typical values for yield stress
So, in some materials plastic strains can be reached

## Slide 4
Added materials, updates,…
New information available point out the need of a deep investigation on coil properties
MATERIAL | σVM (MPa) |  | σ1 (MPa), 4K | E (GPa) |  | Poisson | CTE
 | 293 K | 4,2 K |  | 293 K | 4,2 K |  | Integ (293 K to 4,2 K)
Coil | 150 | 200 | - | Ex = 52 | Ex = 52 | 0,3 | X = 3,1E-3
 |  |  |  | Ey = 44 | Ey = 44 |  | Y = 3,4E-3
 |  |  |  | Gxy = 21 | Gxy = 21 |  | 
316LN St. Steel | 350 | 1050 | - | 193 | 210 | 0,28 | 2,80E-03
Al7075 | 480 | 690 | - | 70 | 79 | 0,3 | 4,20E-03
Iron (Ferromag) | 180 | 720 | 380 | 213 | 224 | 0,28 | 2,00E-03
Ti6Al4V | 800 | 1650 | - | 115 | 126 | 0,3 | 1,70E-03
These numbers could be risky because degradation…
maybe a value around 175 MPa should be used at cold.
This should to be perfectly defined and then the table updated.

## Slide 5
Added materials, updates,…
These are some typical values for the lately added materials involved in the designs, but at this moment no official agreement was set on their properties
This could be a proposal, but it is open to fix the same numbers for everyone
MATERIAL | σVM (MPa) |  | σ1 (MPa) | E (GPa) |  | Poisson | CTE
 | 293 K | 4,2 K |  | 293 K | 4,2 K |  | Integ (293 K to 4,2 K)
Invar | 670 | 1400 | - | 193 | 210 | 0,28 | 4,00E-04
Copper | 170 | 450 | - | 130 | 130 | 0,3 | 3,20E-03
G10 | 400 | 750 | - | Ex = 28 | Ex = 35 | 0,15 | 7,00E-03
 |  |  |  | Ey = 22 | Ey = 26 |  | 
 |  |  |  | Gxy = 10 | Gxy = 12 |  | 

## Slide 6
Conclusion
Material properties and main FEM parameters related to structural simulations in the scope of this project have been summarized.
Data being used which is not included in the official table have been reported. Agreement on the values is needed