## Slide 1: Superconducting RF Cavities R&D Towards Future High Energy Accelerators
Mattia Checchin

## Slide 2: Outline
Introduction
High Q-factor
High accelerating gradient
New directions
Conclusions

## Slide 3: State-of-the-art treatments
High-Q0
(e.g. LCLS-II)
High-Q0
High-Eacc
(e.g. ILC)
High-Eacc
(e.g. ILC)

## Slide 4: What are we seeking for HE colliders?
3 – 4 MV/m
Multipacting
5 MV/m
Thermal Breakdown
10 – 15 MV/m
Field Emission
20 - 25 MV/m
Q-SLOPE
35 – 40 MV/m
Q > 5e10
At medium field !!
Q > 2e10
At high field
?
Eacc > 100 MV/m
Q > 5e10
Enabling future efficient and affordable High Energy Machines

## Slide 5: Why high Q?
courtesy of A. Grassellino
8 GeV CW SRF Linac

## Slide 6: Why high gradient?
For example, the ILC:
From the ILC TDR: “[the cost] is dominated by the SRF components and related systems, together with the conventional facilities. These two elements account for 73% of the total. The main linac itself corresponds to 67% of the total project.”
Increasing the gradient, the number of CMs to reach the design center-of-mass energy is lower cost reduction!
Main linac cost breakdown from ILC TDR
Mattia Checchin | ICHEP 2018, Seoul, South Korea

## Slide 7: ILC cost reduction – cost model and R&D pathways
A cost model has been developed based on the ILC TDR and new progress in the SRF technology on cavity achievable efficiency (Q) and acceleration (Eacc)
Achievable cavity Q and acceleration are among the main cost drivers
Improving simultaneously Q and gradient can give substantial cost cut >10% of the total linac cost
~ 10%
~ 15%
Mattia Checchin | ICHEP 2018, Seoul, South Korea

## Slide 8
High Q-factor:
Doping and efficient management of trapped flux

## Slide 9: Nitrogen doping of Nb cavities (N-doping)
Q-factor improvement after N-doping – up to 4 times higher Q than standard Nb cavities
Typical Q vs Eacc curve obtained with 120C bake (standard ILC treatment)
Average Q at 16MV/m:
Standard ILC treatment:
N-doping:
Anti-Q-slope
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013) – Rapid Communications

## Slide 10: Trapped flux surface resistance
⇒ temperature-dependent part of the surface resistance
⇒ intrinsic residual resistance
If pinned, vortices may survive in the Meissner state introducing dissipation
—flux trapping efficiency
—trapped flux sensitivity
—external magnetic field
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Pinning points
Trapped vortices

## Slide 11: Example: no field trapped
Courtesy of M. Martinello

## Slide 12: Example: 10 mG fully trapped
Btrap=10.7 mG
Courtesy of M. Martinello
Btrap=10.8 mG
S=1.5 nW/mG

## Slide 13: Flux trapping efficiency
Large thermal gradients
  efficient flux expulsion
Small thermal gradients
  poor flux expulsion
Large variability depending on the material batch
  better flux expulsion in high T annealed materials
Preliminary correlation between low and high local misorientation areas
M. Martinello, TTC Workshop, RIKEN, Japan (2018)
S. Posen, TTC Workshop, Milan, Italy (2018)
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014)
A. Romanenko et al., J. Appl. Phys. 115, 184903 (2014)
Good expulsion
Bad expulsion

## Slide 14: Trapped flux sensitivity
Pinning
regime
Flux-flow
regime
Small – pinning regime :
  increases with and
Large – flux-flow regime :
  decreases with , independent on
Pinning
  M. Checchin et al., Appl. Phys. Lett. 112, 072601 (2018)
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
Pinning
regime
Flux-flow
regime

## Slide 15
High accelerating gradient:
Engineering of the first ~ 100 nm of RF surface

## Slide 16: 120 C baking
LIMITED TO

## Slide 17: LE-SR data on 120 C baked cavities cut-outs
120 C baked cavities show a high layer at the surface
A. Romanenko et al., Appl. Phys. Lett. 104, 072601 (2014)

## Slide 18: 120 C N-infusion
times higher gradient
times higher Q-factor
LIMITED TO
A. Grassellino et al., Supercond. Sci. Technol. 30, 094004 (2017)

## Slide 19: Impurity profiles in cavity cutouts by TOF-SIMS
Nitrogen diffuses within ~ 20 nm
Comparing EP cavity cutout with EP + 120 C 48h N-infused cavity cutout
Oxide
A. Romanenko et al., IPAC 2018, Vancouver, Canada
M. Checchin et al., IPAC 2018, Vancouver, Canada
N-infused cavities are an example of layered superconductors
N-enriched layer in the first ~ 20 nm

## Slide 20: Summary
Material analysis suggest that cavities baked at 120 C (N-infused and not) show a high layer at the surface
120 C baked
120 C N-infused
EP/BCP
N-doped
High layer
Low bulk
Constant bulk

## Slide 21: Summary
Material analysis suggest that cavities baked at 120 C (N-infused and not) show a high layer at the surface
120 C baked
120 C N-infused
EP/BCP
N-doped
High layer
Low bulk
Constant bulk
What do we expect in terms of vortex penetration and maximum field limit for high-𝜅 layered materials?

## Slide 22: Energy barrier to vortex nucleation
Normal-conducting
Meissner
RF vortex penetration is believed to be the ultimate gradient limitation of SRF cavities
If the superconductor surface is flawless vortex penetration is a kinetic process (nucleation) not thermodynamic
The energy barrier to vortex nucleation keeps the material in a meta-stable Meissner state up to
Field rise
C. P. Bean and J. D. Livingston, Phys. Rev. Lett. 12, 14 (1964)
Field rise
Meta-stable
Meissner
Mixed

## Slide 23: What does happen if another interface is added?
T. Kubo, in proceedings of LINAC14, Geneva, Switzerland (2014)
G. S. Mkrtchyan et al., Zh. Eksp. Theor. Fiz. 63, 667 (1972)
The vortex is pushed by the S-S boundary to the direction of the material with a larger .
A second BL-like barrier is acting at the S-S interface
The force acting on the vortex as a function of depth can be calculated in the London and GL framework
Vacuum-S
interface
S-S
interface

## Slide 24: Layer thickness dependence
M. Checchin et al., in proceedings of LINAC16, MSU, East Lansing, USA (2016)
T. Kubo, LINAC 2014, Geneva, Switzerland (2014)
Courtesy of T. Kubo
BL
S-S
Wide layer two peaks in the force
Thin layer forces summation (one peak)

## Slide 25: Modeling of the maximum gradient
QPs energy, momentum and occupation
Adapted from: V. Ngampruetikorn, TTC Workshop, RIKEN, Japan (2018)

## Slide 26: Current density distribution in the superconductor
V. Ngampruetikorn, TTC Workshop, RIKEN, Japan (2018)

## Slide 27: Enhancement of the accelerating gradient
V. Ngampruetikorn, TTC Workshop, RIKEN, Japan (2018)

## Slide 28
New directions:
Nb3Sn and layered superconductors

## Slide 29: Why Nb3Sn?
Adapted from: S. Posen, FCC week, Berlin, Germany (2017)
Higher operational temperature
Higher superheating field
For and :
For Nb3Sn,

## Slide 30: Why layered superconductors?
Thin films ) of high- SC materials on top of clean and oxide-free niobium
Possible candidates:
  Nb3Sn
  Nb3Ge
  NbN
  …
Expected gradients higher than Nb3Sn
Nb3Sn/Nb and Nb(high )/Nb predictions based on:
T. Kubo, Supercond. Sci. Technol. 30, 023001 (2017)

## Slide 31
Conclusions

## Slide 32: Conclusions
High Q-factors enable affordable CW accelerators
  N-doping decreases T-dependent surface resistance
  Trapped flux surface resistance is tunable by acting on sensitivity and expulsion
High gradients enable affordable HE accelerators
  120 C baked and N-infused cavities show high gradients and dirty layer at the surface
  Engineering of the first ~ 50 nm of material seems beneficial in terms of gradient enhancement

## Slide 33: New exciting results!
times higher gradient
UP TO in ILC-type single-cell cavities
A. Grassellino et al., to be published

## Slide 34
Acknowledgments:
M. Martinello, A. Grassellino, A. Romanenko, S. Posen, A. Melnychuck, D. A. Sergatskov, S. Aderhold, D. Bice, S. Chandrasekaran, Z.-H. Sung, S. Belomestnykh (Fermi National Accelerator Laboratory),
V. Ngampruetikorn, J. Sauls (Northwestern University)
Thank you for your attention

## Slide 35: Qualitative description of the anti-Q-slope
M. Martinello et al., arXiv:1707.07582v1
A. Grassellino et al., Supercond. Sci. Technol. 26 102001 (2013)
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)
Anti-Q-slope emerges from decreasing with RF field
Equilibrium distribution of QPs
Non-equilibrium distribution of QPs
Smaller with non-equilibrium QPs distribution
QPs driven out-of-equilibrium by microwave absorption (if QP relaxation slower than RF)
  decreases

## Slide 36: Latest Nb3Sn results at Fermilab
Substantial improvement in our second year of coating
Still some Q-slope, not yet flat Q0 like Cornell
Very high Q0 at 2.0 K, similar to Wuppertal
S. Posen, TTC Workshop, RIKEN, Japan (2018)
Mattia Checchin | ICHEP 2018, Seoul, South Korea