## Slide 1
CEA Nb3Sn quadrupole magnet : test results and future

## Slide 2: Content
Magnet design and components
Test results and first interpretations
  Magnet cool down
  Quench start inside the coil at 4.2K
  Quench start in splice region
  Standard current cycles
Future actions

## Slide 3: Magnet design
Cable insulation relying on S2-glass fiber tape
Angular and End wedges realized in Al-80%wt Cu
End wedges insulation and inter-turn insulation made up of 0.1-mm-thick mica foils
Model design based on the design of LHC arc quadrupole magnets
Rutherford-type cable developed by ALSTOM MSA relying on available Nb3Sn wires
Strand Ø : 0.825 mm
Jc (4.2K, 7T ) : 1850 A/mm2
Effective filament Ø : 19 µm

## Slide 4: Magnet Instrumentation
13 voltage taps per coil : 9 in the end parts, 4 in splice region
4 Quench antenna and 16 capacitive gauges (coil polar planes)
3
10
0
1
2
4
5
6
7
8
9

## Slide 5: Magnet cool down
The magnet has been cooled down in 6 days, with a plateau at 100K for 3 days.
Measured RRR value for the Nb3Sn part is of about 200.
Coil to ground insulation before and after cool down > 200Mohm at 500V

## Slide 6: Quench at 4.2K
8/9 quenches started on Pole I, between 4860 and 4920 A
[ Ramps to 5 kA, by steps of 1kA up to 4kA, then 500 A – ramp rate : 10A/s ]

## Slide 7
Quench # 3 at 4.2K Iq = 4900A

## Slide 8: Quench localization
Inner layer
Lead end

## Slide 9
Quench propagation from coil to Nb3Sn/ NbTi splice
Quench # 3 at 4.2K Iq = 4900A

## Slide 10
Quench propagation from the lead end to the center of the magnet
v = 0.95 m/s
Quench antenna 5
Quench antenna 4
Quench # 3 at 4.2K Iq = 4900A

## Slide 11: Transverse quench propagation ?

## Slide 12
Temperature rise about 25 min before the quench
DT = 0.2 K
Temperature gauges uncovering
Quench # 3 at 4.2K Iq = 4900A

## Slide 13: Thermal effects
Heat source is far from temperature gauges but it has an impact on helium bath

## Slide 14: Quench in splice region
Quench started on Pôle III Splice 1, during current plateau at 4500 A
Pôle III Splice #1 (inner layer), then Pole III/Pole II internal connection, then Pôle II Splice 2 (outer layer)

## Slide 15: Standard current cycles at 4.2K

## Slide 16
Standard current cycles at 4.2K

## Slide 17
R independent from I for I > 2 kA
R = 200-250 nohm, RRR = 200  Defect length = 3 cm
Standard current cycles at 4.2K

## Slide 18: Future actions
  Results analysis has to be completed  october
  Discussion with CERN  october
  New test campaign ?
  Mechanical tests on spare coil ?
  Reacted Nb3Sn cable micrographies?
  Cable Ic measurements under stress ?
  Cold mass dessassembling ?