## Slide 1: Production of phosphorus-vacancy centers in diamond for optical and spin characterization
B. L. Green,1 M. E. Newton,1 and K. Johnston2
1Department of Physics, University of Warwick, Coventry CV4 7AL, United Kingdom
2CERN, CH-1211 Geneva, Switzerland
58th Meeting of the INTC

## Slide 2: Single emitters in diamond
Adapted from I. Aharonovich et al., Adv. Opt. Mater. 2, 911 (2014)
Diamond is an ideal host matrix for functional point defects with optically-accessible quantum properties:
  high Debye temperature
  low spin-density
  large band gap  broadband optical transparency (220 – 2400 nm)

## Slide 3
NV—
Fast optical spin initialization
High fidelity optical spin readout at room temperature
Long coherence times
Broadband emission
Sensitive to strain
1.8 K
293 K
S. Yang et al., Nat. Photonics 10, 507 (2016)
S. Zaiser et al., Nat. Commun. 7, 12279 (2016)
B. Hensen et al., Nature 526, 682 (2015)
W. B. Gao et al., Nat. Photonics 9, 363 (2015)
Y.-C. Chen et al., Nat. Photonics 11, 77 (2017)
W. Pfaff et al., Science 345, (2014)
H. Bernien et al., Nature 497, 86 (2013)
A. Jarmola et al., Phys. Rev. Lett. 108, 197601 (2012)

## Slide 4: NV—
Now a well-understood system
Applications include:
Widefield biological magnetometry
10.1038/nature12072
Nanoscale metrology
10.1038/nnano.2012.50
Fundamental quantum mechanics
10.1038/nature15759

## Slide 5
SiV—
Slow spin initialization
Slow spin readout (and only at 4 K or lower)
Short coherence at >100 mK
Narrowband emission
Tuneable ZPL
293 K
4.2 K
B. Pingault et al., Nat. Commun. 8, 15579 (2017)
D. D. Sukachev et al., Phys. Rev. Lett. 119, 223602 (2017)
A. Sipahigil et al., Phys. Rev. Lett. 113, 113602 (2014)
A. Sipahigil et al., Science 354, 847 (2016)
Y.-I. Sohn et al., arXiv:1706.03881 (2017)

## Slide 6
SiV—
Slow spin initialization
Slow spin readout (and only at 4 K or lower)
Short coherence at >100 mK
Narrowband emission
Tuneable ZPL
Applications primarily photonic
Integrated photonic networks
10.1126/science.aah6875
Arrays of SiV— for QKD
10.7567/APEX.7.115201

## Slide 7
NV—
Fast optical spin initialization
High fidelity optical spin readout at room temperature
Long coherence times
Broadband emission
Sensitive to strain
SiV—
Slow spin initialization
Slow spin readout (and only at 4 K or lower)
Short coherence at >100 mK
Narrowband emission
Tuneable ZPL

## Slide 8: Single emitters in diamond
Significant similarities between different “vacancy-cage” optical emitters
S=0
S=½
S=1
NV0
NV—
SiV—
SiV0
GeV—
SnV—
SiV2—
GeV2—
SnV2—
PV—
PV0
PV+
Optically
inert
[1]
[1] T. Iwasaki et al., arXiv:1708.03576 (2017)
Optically
initializable
spin
?

## Slide 9: Production at ISOLDE
31Al
30Si
644 ms
98.4%
1.6%
31P
157 min
31Si
Implant at ~50 keV
Anneal to form 31SiV
Monitor decay of SiV
Look for PV spectrum
>800°C to mobilize vacancies

## Slide 10: Production at ISOLDE
157 min
Time | No. 31Si t1/2 | Stage | Notes
00:00 | 0 | Implantation of 31Al | Decays to Si with t1/2<1 s
02:30 | 1.0 | Insertion into furnace | Furnace at 850°C
04:30 | 1.7 | Removal from furnace | 
05:00 | 1.9 | Insertion into cryostat | Cryostat pre-cooled to 100 K
05:30 | 2.1 | PL measurements begin | 
31P
31Si
Implant
Anneal
Measure

## Slide 11: Measurement at ISOLDE
Close proximity of implantation beam and measurement enables rapid turnaround
  Measurements start at ~2 t1/2
  Matrix of doses (single to ensemble)
Modular PL system
  Simple to add additional excitation
Wide detection window
  High efficiency detection 350-1700 nm
Conditions at ISOLDE are unique for maximising the probability of detecting PVx

## Slide 12: Charge state control
a1g
a2u
eu
eg
SiV0
Problem:
  substitutional phosphorus in diamond is a donor (~0.6 eV)
  PV is predicted to be a deep acceptor [1]
  Hard to stabilize neutral and positive charge states of PV:
    P0 + PV0  P+ + PV—
Solution:
  charge state control through doping and surface termination
  Light (~1017 cm-3) B-doping  p-type
  Ultrapure (<1013 cm-3 impurities) material  intrinsic
  Samples to be supplied at zero cost by the Quantum Technologies group at Element Six Ltd.

## Slide 13: Conclusion
Identification and optical / spin characterization of PVx in diamond
Use rapid turnaround, high-efficiency measurements at ISOLDE to maximise the chance of detecting transient decay of
Use offline time between first and second requested runs to:
  feedback from original measurements and optimize second run
  perform additional experiments at Warwick e.g. confocal microscopy, optically detected magnetic resonance
Primary goal:
Approach:
31SiV  31PV