## Slide 1: EUROPEAN ORGANIZATION FOR NUCLEAR RESEARCH Proposal to the ISOLDE and Neutron Time-of-Flight Committee
Hyperfine interactions in hydrogenated TiO2 thin films
and powders for photocatalytic reactions
Dmitry Zyabkin 1
Juliana Schell2,3, Doru C. Lupascu3, Haraldur Pall Gunnlaugson4, Hilary Masenda5, Roberto Mantovan6, Krish-Baruth-Ram7,8, Sveinn Ólafsson9, Hafliði P. Gíslason9, BingCui Qi9, Petko Krastev10, Joao Guilherme Martins Correia2,11, Ulrich Vetter1, Peter Schaaf1
1. Department of Materials for Electronics, Institute of Materials Science and Engineering, TU Ilmenau, Ilmenau, Germany
2. EP Department, ISOLDE-CERN, CH-1211 Geneva 23, Switzerland
3. Institute for Materials Science and Centre for Nanointegration, Duisburg-Essen (CENIDE),
4. Science Institute, University of Iceland, Dunhaga
5. School of Physics, University of the Witwatersrand, Johannesburg, 2050, South Africa
6. Laboratorio MDM, IMM-CNR, Via Olivetti 2, 20864, Agrate Brianza (MB), Italy
7. Durban University of Technology, Durban, 4000, South Africa.
8. School of Chemistry and Physics, University of KwaZulu-Natal, Durban, 4000, South Africa
9. Science Institute University of Iceland
10. Institute for Nuclear Research and Nuclear Energy, Bulgarian Academy of Sciences, 72, 1784, Bulgaria
11. Centro de Ciências e Tecnologias Nucleares (C2TN), Instituto Superior Técnico, Universidade de Lisboa, Portugal
Notes: Resolve questions upon PhD
Study defects they’re main reason for improved photocat activity

## Slide 2
Why study TiO2:H?
TiO2+ H2 Plasma
Black TiO2
Lots of defects (VO, VH, Ti )
Absorption improved
More electron-hole pairs
Better performance?
Absorption
3 hours of H treatment
Notes: 1)Plasma treatment which does…., but is there truly better perfomance?
2)

## Slide 3
MILD PLASMA
doesn’t alter structure
photocatalytic performance rates better
defects (Ti2+,Ti3+ Vo, VH)
Generation rates for methane and CO in the photocatalytic reduction of CO2 with H2O through H-TiO2: H2
Light absorption
TiO2
Rate
Why study TiO2:H?
H:TiO2
TiO2
H2 30 sec
H2 1 min
Notes: 1)Better perfomance? At least not in every reported paper
2) Thats why there is another mild plasma where less defects but they are still
3

## Slide 4
Investigation of
local defects induced with plasma in the nanostructured TiO2 materials by PAC and eMS having a significant impact on the electron-hole recombination;
dopants and H2 interactions i.e. possibly leading to a “new” black TiO2 ;
charge transfer?
defects evolution under various atmospheres and conditions.
OBJECTIVES
Sample production& characterisation
(PVD,CVD, XPS, UV/Vis, TEMS, CEMS)
TDPAC& eMS
measurements
TU Ilmenau
ISOLDE
Notes: 1. Доппинг имеет серьезное влияние на дефекты, абсорбция это еще не все

## Slide 5
PAC SPECTROSCOPY at ISOLDE
How?
As a function of
sample stoichiometry with different amount of defects H2 annealing and measuring temperature from 450-700 K
111mCd is used in doping of TiO2 and only at ISOLDE
Experience and sufficient amount of setups
Interactions of Cd with VH, Vo and Ti defects
        + no after-effect
Implantation depth at 30 keV is ~ 10-12 nm (111mCd in TiO2)
Notes: Just to understand how the material interact with diff atmost either healing out, water nucleation;
111m no after effect

## Slide 6
Emission MÖSSBAUER SPECTROSCOPY at ISOLDE
Complement of the PAC study:
Probe-host or probe-defect interaction
Valence(/spin) state of probe atom (Xn+)
In earlier work (2014)* Ti and Vo defects were probed
HOW?
As a function of
Sample stoichiometry
Annealing and measuring temperature
*Gunnlaugsson et al J. Phys. D: Appl.Phys.47 (2014)
Implantation depth at 30 keV is ~ 11-16 nm (57Mn in TiO2)

## Slide 7: The eMS setups
The old setup:
Limitations (such as temperatures, additional vibrations, long-sample-changing option)
Complexity of extension for chemical experiments
The new setup:
UV irradiation (laser 365 nm, 3B class)
Better vibration isolation
Less pumping time
Compact & easy to assemble for a run
Precise T-control
Compatible with old cryo, magnetic lids

## Slide 8
FEASIBILITY OF CURRENT PROPOSAL
eMS spectra of TiO2 :H-RT
TU Ilmenau/ISOLDE 2017
Fe 2+ S=0 or S=2 ?
Fe 3+ ?
Does H act as an electronic donor?
Leading to a charge transfer?
Fe3+ + Ti3+ <-> Fe2+ + Ti4+?
Mn
Ti
O
H?
Gunnlaugsson et al J. Phys. D: Appl.Phys.47 (2014)
Notes: Preliminary measurements and differ from 2014
Fe2/Fe3+ related to a charge transfer during lifetime of 57Mn (Ti3+ XPS)
TiO2 Mn/Fe doped + H2 ?
New black co-doped Titania?
The SL component observed above 600 K is presumably due
to the collapsing of the sextet belonging to the Sz = ± 1/2
Kramers doublet state

## Slide 9
Schell et al, JAP 121, 145302 (2017)
TU-Ilmenau/ISOLDE 2017
111mCd(111Cd) in TiO:H2
111In(111Cd) in TiO2
Cd
TiO2 pristine films (TDPAC)
Rutile structure
ω0 ~100 Mrad/s
and η ~0.1
Rutile structure
ω0 ~100 Mrad/s
and η ~0.2
Notes: In prostine samples there are the same frequency and asymmetry parameter like in Schell et al
Then with hydrogen treatment

## Slide 10
TU-Ilmenau/ISOLDE 2017
Two local enviroments with static nuclear quadrupole interactions:
Site 1: well-defined frequency for Cd at the Ti-site with distortion caused by the presence of H atoms (η ~0.5).
Site 2: major fraction at 150oC and 200oC
Hydrogenation treatment with high frequency distribution. Higher EFG asymmetry in respect to site 1 (η ~1).
TiO2 hydrogenated films (TDPAC)
Notes: We couldclearly say there are
Two local environments with pure static QPI
2 different plasma induced defects
Second site has large width of freq-cies distributions, assigned to local defects from ion implantation
Fraction 1 dominates till H200, then 2 starts

## Slide 11
Mössbauer spectroscopy under light irradiation
A. H. Mkrtchyan, R. P. Vardapetyan, E. M. Harutyunyan, A. V Khachatryan, V. V Nalbandyan, and H. R. Muradyan, “Modification of Mössbauer Reflection Spectra of Group AIIBVI Single Crystals with Fe 57 Nuclei under Influence of Infrared Radiation,” J. Contemp. Phys., vol. 44, no. 4, pp. 194–196, 2009.
Sample: CdS:57Fe(0.2%)

## Slide 12
BEAM TIME REQUEST
Perturbed Angular Correlations Studies |  |  |  |  |  |  | 
Required isotope | Implanted beam | Probe element | Type of experiment | Intensity [at/μC] | Target / Ion source | Atoms per sample | № of shifts
111mCd (48 min) | 111mCd | 111Cd | γ-γ PAC | 108 | Molten Sn; plasma | 2x1010 | 3
Mössbauer studies |  |  |  |  |  |  | 
57Mn (1.5 min) + TESTING of eMS | 57Mn | 57Fe | eMS | 2 x 108 | UCx, RILIS (Mn) | 1x1012 | 2 + 2
Notes: Whats why we need just these amont of shifts to measure the main points and after that the picture is clear

## Slide 13: FUNDING INVOLVED
BMBF
Bundesministerium für Bildung und Forschung
Erforschung kondensierter Materie mit Großgeräten
Ausbau und Unterhalt der Einrichtungen an ISOLDE/CERN
Germany, contract: 5K16SI1

## Slide 14
Thank you for your attention!

## Slide 15
Similar frequency value (257 Mrad/s) in respect to the well-defined frequencies obtained with H:TiO2 (300 Mrad/s), but since it had no H and the sample was a single crystal, it presents lower EFG asymmetry:
111mCd:TiO2 Syngle Crystal
ω0 ~257 Mrad/s
and η ~0
Schell et al, Hyp. Int. (2017) 238:2.
Additional information TDPAC

## Slide 16
m(5/2+)= -0.766(3)mN
Q(5/2+)= +0.74(8)b
A22 (111mCd) = 0.1786
A22 (111In) = -0.1782
111mCd(111Cd)
Additional information TDPAC

## Slide 17
57Mn/57Fe
Additional information eMS