## Slide 1
HGTD schedule (done for 4 layers/side)
Install HGTD: June 2025 (A side)
September 2025 (C side)
  2018-2020: R&D
  2021-2024: Construction
  2025-2027: Integration/Installation/commissioning
More Robust schedule for optimised “2L+1” layout (~ ½ modules than in IDR)
2018 2019 2020 2021 2022 2023 2024 2025
6
Technical Proposal

## Slide 2
HGTD Sensor Test Overview

## Slide 3: HGTD Sensor Wishlist
Wafer active thickness: 50 µm (baseline) and 35 µm (option)
Pad size always 1.3x1.3 mm²
Structures (LGAD if not noted otherwise)
  LGAD single pad, PIN single pad
  Arrays of 2x2 and 3x3 pads
    Inter-pad gap variations: 30, 50, 70 µm? (CNM standard 64 µm physical)
    Slim edge variations: 100, 200, 300 µm? -> optimized edge design (GR etc.) for each
    Large passivation openings for wire-bonding/probe needles
  Arrays of 5x5 pads
    Compatible to next version of HGTD readout chip (ALTIROC1, mid 2018)
    Standard inter-pad gap (50-100 µm) and standard edge (300-500 µm) (conservative values)
    2 different passivation openings or alternatively biasing structures to allow both UBM/bump-bonding and probing/wirebonding
  Large arrays of 15x15 pads (single-chips) and 30x15 pads (double-chips)
    Compatible to final HGTD readout chip (~2019)
    Designed as single-chip sensors, but arranged to allow yield-evaluation and dicing as pseudo-doubles and quads for module proto-typing
    Standard inter-pad gap (50-100 µm) and standard edge (300-500 µm) (conservative values)
    2 different passivation openings or alternatively biasing structures to allow both UBM/bump-bonding and probing/wirebonding
15 pads
1.3 mm

## Slide 4: Bump-Bonding
Need to bump-bond sensor to readout chip
Need Under-Bump-Metalisation (UBM)
  Provided by vendor?
  Which process? Is a mask used to protect other metal not foreseen for UBM?
    Do structures for UBM need to be on one part of the wafer?
HGTD bump-bonding tests so far
  On CNM HGTD run (2x2 arrays for first version of readout chip: ALTIROC0)
  Passivation opening of 90 µm diameters
  Electro-less UBM in house by CNM
  Bump-deposition of 80 µm diameter bumps and flip-chipping
  Good results: hybrid works and delivers signal; good mechanical stability
How do we assure probing (IV) and sensor selection on wafer?
  Several options possible
    Implement 2 passivation openings on same pad: both small opening for UBM and large opening for probing/wire-bonding -> allows to probe IV of large sensors with probe card
    Temporary metal to shorten all pads
    Biasing structures like for pixels (e.g. punch-through or poly-Si)
a) UBM opening
for bumps
b) Large opening for wire-bond+probe
c) Also biasing structure?

## Slide 5
ATLAS
CMS
5x5 arrays with UBM
~2*17=
34 devices
2x2 arrays
No UBM
Possibly gap variations
~22+24+26=
72 devices
15x15 arrays
with UBM
~8 devices
Single pads
No UBM
One line in centre to study wafer uniformity
~16+22+28+30+62=
158 devices
3x3 arrays
No UBM
~22 devices
6 inch LGAD wafer layout proposal (sketch)
Shared between ATLAS/CMS (half-half)
ATLAS pad: 1.3x1.3 mm² active area
Some PINs for each structure
Here not completely closely packed/well aligned (just a sketch) and each sensor has conservative 500 µm inactive width at each edge (incl. GR, margin, cut line) -> slightly higher density possible
Typically arrays have safe standard inter-pad gap of ~50-100 µm (tbd)
2x2 arrays can have variations
  Gap of e.g. 30, 50, 70 µm to optimise fill factor
  Slim edge (100, 200, 300 µm)
Large sensors (5x5, 15x15)
  UBM (90 µm passivation hole in centre)
  Additional structures for probing (larger openings for needles/wire bonds, maybe biasing structure)
  8 15x15 single-chip sensors
    Designed as single-chip sensors, but arranged to allow yield-evaluation and dicing as pseudo-doubles and quads for module proto-typing
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P=PIN
Fast feedback by CNM
Generally no showstopper
Very hard to dice (e.g. central single-pad line “impossible”)
Need space for test structures/alignment marks
Need ALTIROC top-layer for UBM
P
P
P
P
P
P
P