## Slide 1: MQXFS1d Welding Status
Antonios Vouris
Cold Mass Status Meeting
25 January 2018

## Slide 2: Coil pre-stress changes with SS skin pre-tensions
Impact of the SS skin has been performed in our 3D model by applying different interferences between S.S. vessel and the magnet structure.
The plot on the right presents the coil (pole) azimuthal stress along the magnet length with deferent SS skin pre-tensions induced by welding shrinkage.

## Slide 3: Δ σCoil compared with Giorgio’s results
The coil stress increases by ~3.2 MPa / 0.1mm weld shrinkage (half shell). This denotes about 48 MPa coil stress increasing is expected for a 50 mil (1.5 mm) weld shrinkage (half shell).
This value is close to the results Giorgio presented in the his slides “MQXF – Vessel Welding” (05/12/2017) .
Both 2D and 3D results shows the current weld shrinkage is relatively high for the coil pre-stress.

## Slide 4
Criteria to achieve correct tightness after welding: CSTEELAFTOT = CALTOT - .020 in.
CBW = Circumference of inside of steel shell half before welding
CALTOT =Total Circumference of Outside surface of Aluminum shell
G = Gap size before welding per side = .094 in.
CSTEELAFTOT = Total Circumference of Inner surface of Steel shell after welding
CSTEELBEFTOT = CBW +CBW +G+G
Total shrinkage during welding = .090 in. (over entire azimuth) = .045 in. per side.
CSTEELBEFTOT = CSTEELAFTOT + Total Shrinkage during welding
Aluminum magnet shell
Stainless shell
CALTOT
CSTEELAFTOTAL
CALTOT = 24.199 in. x ∏ = 76.023 in.
Therefore, CSTEELBEFTOT = 76.023 in. -.020 in. + .090 in. = 76.093 in.
G
G
CSTEELBEFTOTT
CBW
CBW
Stainless shell
Aluminum magnet shell
Therefore, CBW = (CSTEELBEFTOT - 2G)/2
Therefore, CBW = (76.093 in.– .188 in.)/2 = 37.952 in.
Measured dia. of Aluminum Shell O.D. = 614.657 mm = 24.199 in.
Calculation of Shell Weld Preparation
And the inside diameter of the steel before welding is 76.093/ ∏ =24.221 in.

## Slide 5
Criteria to achieve correct tightness after welding: CSTEELAFTOT = CALTOT - .020 in.
COBW = Circumference of outside of steel shell half before welding
CALTOT =Total Circumference of Outside surface of Aluminum shell
G = Gap size before welding per side = .094 in.
CSTEELAFTOT = Total Circumference of Inner surface of Steel shell after welding
COUTSTEELBEFTOT = COBW +COBW +G+G
Total shrinkage during welding = .090 in. (over entire azimuth) = .045 in. per side.
COUTSTEELBEFTOT = COUTSTEELAFTOT + Total Shrinkage during welding
Aluminum magnet shell
Stainless shell
CALTOT
CSTEELAFTOTAL
Outside circumference of steel after welding = COUTSTEELLAFTOT = 24.859 in. x ∏ = 78.096 in.
Therefore, COUTSTEELBEFTOT = 78.096 in. -.020 in. + .090 in. = 78.166 in.
G
G
COBW
Stainless shell
Aluminum magnet shell
COBW
COUTSTEELBEFTOTT
Therefore, COBW = (COUTSTEELBEFTOT - 2G)/2
Therefore, COBW = (78.166 in.– .188 in.)/2 = 38.989 in.
Measured dia. of Aluminum Shell O.D. = 614.657 mm = 24.199 in.
Calculation of Shell Weld Preparation
(Using Outside Diameter)
Outside dia. Stainless Shell after welding = 24.199 in. + (.330)(2) = 24.859 in.
COUTSTEELAFTOT
And the outside diameter of the steel before welding is 78.166/ ∏ =24.881 in.

## Slide 6
CBW
½ G
½ G
½ CSTEELBEFTOTT
Inside Radius of steel shell
½ G = .094 in./2 = .047 in.
½ CSTEELBEFTOTT = 76.093 in/2 = 38.046 in.
CBW = 37.952 in.
Wall thickness of shell = .330 inches.
Shell wall thickness
COUTBEF
Inside dia of shell = 24.221 inches.
Outside dia of shell = 24.221 inches + (.330)(2) = 24.881 in.
Therefore COUTBEF = outside circumference of shell half – (½ G)(2) = (78.166/2) – (.047)(2) = 38.989 in.
Shell Half before Welding
Outside circumference of shell = 24.881 x ∏ = 78.166 in.
(Using Outside Diameter calculated geometrically)

## Slide 7: Fuji film plan

## Slide 8
Measurements of center section of MQXFS1C shell.

## Slide 9: Status
Next steps:
Wire up the strain gauges
Scribe the centerline both sides
Insert the Fuji films
Fit up the shells
Welding
  Final shell leveling wrt. equipment
  Monitor temperatures
  Measure strain gauges after each passes