## Slide 1
FCC Conductor Development Workshop
A. Ballarino
CERN, 5-6 March 2018

## Slide 2: The CERN FCC Conductor Development Program
Present baseline of the 100 TeV, 100 km FCC machine: 16 T dipoles relying on Nb3Sn technology
Scope of the conductor development program:
  Provide feedback on possibility of achieving beyond state-of-the-art HL-LHC Nb3Sn high-field performance (Jc @ 16 T) to enable design of compact and cost effective 16 T magnets;
  Foster Nb3Sn conductor development in industry and support the industrial development with academic activities (material studies and characterization) in laboratories and institutes world-wide;
  Procure (and cable) Nb3Sn conductor to feed the on-going magnet model-coils activity (procurement started in 2017);
  Investigate potentials of other superconductors (performance in high fields and cost)
A. Ballarino, CERN

## Slide 3: Nb3Sn: Requirements and challenges
Performance increase
Jc at 16 T required to be up to  30% -50 % higher than what achieved on the HL-LHC Nb3Sn series production
Cost reduction is required to make 16 T magnets commercially affordable. Present cost of high-performance (HL-LHC) Nb3Sn is > 20 Euro/kA m (4.2 K, 16 T). FCC target is 5 Euro/kA m (4.2 K, 16 T). Required: increase of Jc, production of large billets, optimization of raw materials – with no performance penalty, optimization of processing cost, savings in labor cost. Cost studies are part of the on-going conductor development program.
Feasibility of large ( 7000-9000 tons for FCC h-h,  2500 tons for HE-LHC) Nb3Sn series production
  ITER:  500 tons total, 100 tons/year, 8 companies
  HL-LHC:  20 tons total (initially 2 companies, now 1 company)
  FCC h-h: 7000-9000 tons total (  1000 tons/year (7 years production) with 7-8 companies)
A. Ballarino, CERN

## Slide 4
Development targets – Nb3Sn
Wire diameter | mm |  1
Non-Cu Jc (16 T, 4.2 K)* | A/mm2 |  1500
M(1 T, 4.2 K) | mT |  150
Deff | m |  20
RRR | - |  150
Unit length | km |  5
Cost | Euro/kA m** |  5
*Je  600 A/mm2
*Cu:non Cu  1
** 16 T, 4.2 K
 50
 0.1
(starting with a 4 years program)
Process shall enable scalability and have potentially low cost for large production
Focus TODAY is on Jc
A. Ballarino, CERN

## Slide 5: On-going agreements
Most of the presented activities started at the earliest in early 2017:
Bochvar Institute (conductor produced at TVEL), Russia
KEK (Jastec and Furukawa), Japan
KAT, Korea
Columbus (being signed), Italy
University of Geneva, Switzerland
Technical University of Vienna, Austria
SPIN, Italy
University of Freiberg (to be signed), Germany
  In addition, being discussed/finalized agreements with:
  Bruker (Germany)
  Luvata Pori (Finland)
A. Ballarino, CERN

## Slide 6: Organization of the Workshop
  Monday the 5th of March
  Plenary sessions until 15:00 (30-7-018 - Kjell Johnsen Auditorium, CERN)
  10:30, during the coffee break: group photo
  Lunch from 12:00 to 13:00 (30-7-018 - Kjell Johnsen Auditorium, CERN)
  Closed sessions from 15:30 until 17:30
  For those who are not involved in the closed sessions: visit of the superconductor and magnets MSC facilities. Group 1
  Dinner starting at 18:30 in the Glass box- Restaurant 1, CERN
  For those who have not yet registered: please contact Carnita Hervet (or myself or S. Hopkins) today before lunch time
A. Ballarino, CERN

## Slide 7: Organization of the Workshop
  Tuesday the 6th of March
  Closed sessions from 9:00 until 11:00 (30-7-018 - Kjell Johnsen Auditorium, CERN)
  For those who are not involved in the closed sessions: visit of the conductor and magnets MSC facilities. Group 2 (from 09:30 until 11:30)
  Free lunch
  Close out (report from reviewers) at 16:00 (30-7-018 - Kjell Johnsen Auditorium)
  Many thanks to all participants
  Many thanks to: L. Bottura, A. Devred, R. Flukiger, L. Rossi and H. Ten Kate for accepting to review the progress on the FCC conductor activity
A. Ballarino, CERN

## Slide 8
For any organizational issues, please contact:
Carnita Hervet
Simon Hopkins
Bernardo Bordini
Amalia Ballarino
Enjoy the Workshop !