## Slide 1
Fe-based superconductors for
very high field applications
Valeria Braccini
CNR-SPIN Genova, Italy
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 2
The scope of this collaboration is to advance the performance of three superconducting materials (Bi-2212, MgB2, IBS), using industrially scalable production methods, to make them suitable for high-field magnet applications.
Acknowledgments:
Collaboration between
CNR – SPIN (M Putti, V Braccini, A Malagoli, M Vignolo)
and CERN (A Ballarino, S Hopkins)
within the Addendum FCC-GOV-CC-0086 of the
Memorandum of Understading FCC-GOV-CC-0004 for the FCC study
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 3
Phase diagram of technical conductors
IBS
MgB2
HTS
FCC should reach a collision energy of 100 TeV thanks to a four times larger radius and double the magnetic field of the LHC. The latter requirement necessitates the development of superconducting materials with increased operating field.
Whilst most efforts are focused on Nb3Sn wires, this is an opportunity to assess the potential for high field application of newer superconductors.
C. Tarantini et al., PRB 84, 184522 (2011)
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 4
Project in China
From Xin SHI,
Institute of High Energy Physics, Beijing
18th Lomonosov Conference on Elementary Particle Physics, Aug 2017
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 5
Objectives of our collaboration with CERN
IBS: develop prototype IBS conductors that meets the Jc requirements through reliable, simpler and scalable techniques that could enable industrialization
V Braccini, G Sylva, A Malagoli, E Bellingeri, C Ferdeghini, M Putti, A Provino, P Manfrinetti
Bi-2212: to reproduce the performance today obtained by high pressure heat treatment with a mechanical deformation process
A Malagoli, A Leveratto, L Leoncino, C Ferdeghini
MgB2: increase the operating field by adopting an original doping method
M Vignolo, G Bovone, M Capra, C Bernini, F Loria, A S Siri
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 6
Iron-based superconductors
Y. Kamihara, T. Watanabe, M. Hirano, H. Hosono: J. American Chemical Society, 130, 2008, S. 3296-3297
Tc ~38 K
Tc ~18 K
Tc ~8 K
Tc ~55 K
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 7
Hc2 and Jc of IBS single crystals and thin films
Thin films
Putti et al., SUST 23, 034003 (2010)
Single crystals
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 8
Jc of technical conductors: comparison
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 9
A Malagoli et al 2015 SuST 28 095015
(Ba,K)Fe2As2 ex situ PIT tapes
Collaboration with E Wiesenmayer, S Marchner, D Johrendt (LMU München, Germany) within
Ba0.6K0.4Fe2As2 powders from LMU
free from impurity phases
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 10
Production of home-made pure (Ba,K)Fe2As2 powders
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018
Powders more than 90 wt.% pure in the 1:2:2 phase, with 8 wt.% of FeAs as extra phase.
Amount of polycrystalline sample prepared is up to 4.0 g.

## Slide 11
In HTS Jc decreases exponentially with GB angle.
In IBS, GBs are weak link but critical misorientation angle is >10°, higher than the 4° of YBCO.
IBS has Advantageous GBs over HTS
S. Kawale et al., IEEE TAS 25, 7300305 (2015)
Si et al, Appl. Phys. Lett. 106, 032602 (2015)
11 bicrystals
122 bicrystals
11 bicrystals
Dependence of Jc on the misorientation angle
Lee et al., Appl. Phys. Lett. 95, 212505 (2009)
Katase et al., Nat. Commun. 2, 409 (2011)
Sagakami et al.,Physica C 494, 181 (2013)
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 12
Given that in IBS the misorientation angle is about 10° and therefore the weak link behaviour is much less critical than in YBCO, it is possible to deposit on biaxially textured metallic substrate with a simpler structure than commercial ones.
Furthermore, oxidation of the metallic template is not an issue for IBS.
It is possible to reduce or even remove buffer layers
Reduce complexity and costs of production
Obtain a larger Je
Idea
Ni alloys + oxide buffers
(CeO2, LaZrO2, CZO)
Iron alloys (Fe/Ni)
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018
Collaboration with
A Augieri, G Celentano, A Mancini, A Vannozzi
ENEA Frascati, Italy

## Slide 13
NiW biaxially textured + CeO2 buffer layer deposited via PLD
NiW5%
CeO2
NiW5% + CeO2
Prepared @ENEA Frascati, I
(11) thin films grow biaxially textured on NiW + CeO2
Rocking Rolling Direction:
Out-of-plane orientation
scan:
in-plane orientation
q – 2q: epitaxial FST film
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 14
Hc2 and Jc up to 18 T
Tc ≈ 18 K
DTc0 ≈ 3 K in 18 T
Hc2 has a very low anisotropy
@ ENEA Frascati
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 15
INVAR36 (36Ni/64Fe)
Commercial alloy 64% Fe , 36% Ni
Low cost
FCC structure, compatible with Fe(Se,Te)
From rods Ø 2 – 10 mm => drawn / flat rolled =>
=> 50 / 70 mm + HT @ 1000 °C / 2h in Ar/H2 atmosphere
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018
20 mm

## Slide 16
INVAR36 (36Ni/64Fe)
Commercial alloy 64% Fe , 36% Ni, FCC
Biaxial texture
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 17
EBSD analysis on INVAR tape
INVAR 500x Map Data 1 - BC+IPF_Z0
INVAR 500x Map Data 1 - Scattered Data
EBSD OXford NORDLYS NANO
on FEG-SEM LEO1525
@ ENEA Frascati
INVAR 500x Map Data 1 - TC
INVAR 500x Map Data 1 - Scattered Data
Presence of
twinned grains
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 18
Growth of epitaxial thin films on INVAR has been demonstrated
First attempts of growth of Fe(Se,Te) on textured INVAR
11 thin films deposited on INVAR through PLD with Nd:YAG laser
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 19
Lowering deposition temperature
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018

## Slide 20
Conclusions and perspectives
NiW + oxide buffer:
We have demonstrated the possibility of growing epitaxial superconducting Fe(Se,Te) thin films on simple RABiTS (NiW + CeO2) with high Tc and good Jc performances
Simpler buffers:
We are working on simpler buffers, i.e. oxides deposited via chemical methods, NbN, not superconducting FeSeTe, …..
INVAR (36Ni/64Fe):
We have demonstrated the possibility of texturing FeNi (INVAR) commercial alloy and depositing expitaxial Fe(Se,Te) thin films without any buffer
We are working to obtain good superconducting thin films
V Braccini FCC Conductor Development Workshop CERN, March 5th, 2018