## Slide 1: AC losses quantification in Nb3Sn magnets
2nd International Workshop on Superconducting Magnet Tests Stands
H. Bajas

## Slide 2: Outline
Origin of the AC loss
Measurement technique
Experimental result
Simulation result

## Slide 3: References

## Slide 4: Origin of AC losses
There are 3 main sources of loss when a transport current is ramped in a superconducting magnet.
  Hysteretic magnetization loss (i.e. flux flow combined with flux pinning, results in a net energy loss when subjected to a field cycle)
    Proportional to the superconductor Jc and filament size (Deff)
  Inter-strand coupling loss (ISCC) and Inter-filament coupling losses (IFCC)
    Combination of individual superconducting filaments and a separating normal-metal matrix results in a coupling Joule loss
    Low thanks to the use of cored cable
    Low at the typical ramp-rate of an accelerator as LHC/FCC (10 A/s)
  Eddy currents in normal-metal
    Iron yoke and saturation effect
Notes: When a filament is in a varying Bext,
its inner part is shielded by currents
distribution in the filament periphery
They do not decay when Bex is held
constant -> persistent currents

## Slide 5: Origin of AC loss

## Slide 6: Origin of AC loss

## Slide 7: AC losses measurement
Measurement issues in superconducting magnet
  The AC losses are delicate measurements as one has to detect Joules (resistive) over hundreds of kJ (inductive voltage).
  It requires High Resolution/precision Digital MultiMeters (DMM 1 uV ± 0.01%).
  Measurement requires to perform a great number of cycles at different ramp rate and level of current. Those are time-consuming measurements that are not systematically done.
  Need a performant framework for automatic analysis over 10th of file, 100th of cycle, 10th of voltages.

## Slide 8
Digital multimeter
Digital analog output
Digital to analog converter
W – energy loss
I – current,
U – voltage,
t - time
Measurement of the voltage across the coil using the voltage taps signals acquired with high precision high resolution DMM Measurement of the the transport current using DCCT signals
Numerical integration of the power over current ramp cycle.
Measurement Procedure (hardware)

## Slide 9: Measurement Procedure (example on SMC11T)

## Slide 10: Measurement Procedure (example on SMC11T)
Current cycle between two level of current
@ different ramp rates

## Slide 11
Current cycle between two level of current
@ different ramp rates
Importance of the cycle and offset definition!!
Measurement Procedure (example on SMC11T)

## Slide 12: Measurement Procedure (example on SMC11T)
E=
Loss/cycle=

## Slide 13: Measurement final result (example on SMC11T - RRP)
AC loss as function of the ramp rate (linear fit)
AC loss as function of the current (quadratic fit)

## Slide 14: Measurement Procedure (example on SMC11T)
Algorithm to automatically process large number of:
magnets / files / cycles / signals

## Slide 15: Measurement final result (example on SMC11T4 - PIT)

## Slide 16: Another example of RMC…
Result for RMC_QXF

## Slide 17: Example of analysis on MQXFS5
Current/voltage (0-50 % Inom & 50 -100 % I nom)
Power over cycle (1 coil)
Loss per cycle function of ramp rate (4 coils)

## Slide 18
Simulation with Roxie (11T dipole)
Our assumption: ISCC and IFCC are negligible, only strand magnetization losses are considered
Courtesy of S.I. Bermudez and G. Willering
Margin on the loadline
Chart: Measured losses on 11 T short model MBHSP012
| 10 | 20 | 50 | 100 | 150 | 200
Meas. Low field | 3896.8789 | 3858.723 | 3869.728 | 3974.209 | 4013.2577 | 4017.5927
Meas. Hig Field | 2282.1203 | 2232.3719 | 2282.1185 | 2335.2496 | 2418.7591 | 2501.7372
  dBp/dI (11T) ~ 1 T/kA
Low field: from 0.1 to 6 kA
High field: From 6 kA to 11.85 kA
11 T (2 apertures) loss per cycle (up+down) ≈ 7 kJ/m
Strand magnetization, which depends on
  Sub-element diameter ()
  Critical current density (non-Cu) ()
  Cu/non-Cu ratio )

## Slide 19
Superconductor current density as specified for HiLumi
  Tc0 = 16 K
  Bc20 =29.38 T
  α = 0.96
  C0 = 188870 A/mm2 T
  3 % cabling degradation
Reference: Deff = 50 µm, no reduction due to flux jumps
Sensitivity analysis to:
  Effective filament size Deff = 20 µm, Deff = 50 µm
  Reduction of strand magnetization at low field due to flux jumps χ= 0.5-1
Courtesy of P. Ferracin
Roxie Model Input

## Slide 20: Roxie Model Input
Temperature margin at nominal current
Iron mesh and vector potential
Margin on the loadline
Courtesy of S.I. Bermudez
and F. Murgia

## Slide 21: Modelling SC magnetization
Courtesy of S.I. Bermudez
Semi-analytical hysteresis model for the superconductor, developed in [1], and implemented in ROXIE [1].
Limited accuracy at low field, partially due the reduction on magnetization observed in Nb3Sn due to flux jumps [2], which can be overcome by introducing a reduction on the strand magnetization below a given field level.
Model has been validated in 11 T [2] and MQXF [3] magnets
[1] C. Vollinger, Superconductor magnetization modelling for the numerical calculation of field errors in accelerator magnets. PhD thesis, 202
[2] S. Izquierdo Bermudez, et.al, Persistent Current Magnetization effects in High-Field Superconducting Accelerator magnets, IEEE 2016
[3] S. Izquierdo Bermudez, et.al, Magnetic Analysis of the Nb3Sn low-beta Quadrupole for the High Luminosity LHC, IEEE 2017

## Slide 22: ROXIE vs AC loss measurement: 11T
11 T - Magnetization loss per aperture (Deff = 0.046 mm, RRP 108/127) | ROXIE | 
 | J/m | J/m3
Pre-Cycle (0- 11.85 kA-0.1 kA) | 4133 | 8.139E+05
Ramp up (0.1 kA -11.85 kA) | 1853 | 3.650E+05
Ramp down (11.85 kA - 0.1 kA) | 2207 | 4.346E+05
Ramp down + Ramp up (11.85 kA-0.1 kA-11.85 kA) | 4060 | 7.996E+05
Chart: Measured losses on 11 T short model MBHSP012
| 10 | 20 | 50 | 100 | 150 | 200
Meas. Low field | 3896.8789 | 3858.723 | 3869.728 | 3974.209 | 4013.2577 | 4017.5927
Meas. Hig Field | 2282.1203 | 2232.3719 | 2282.1185 | 2335.2496 | 2418.7591 | 2501.7372
Measured ramp up + ramp down around 6 kJ, 6/1.7= 3.6 kJ/m for a single aperture (ROXIE gives 4 kJ/m, a bit conservative, but good enough for a first approximation).

## Slide 23: ROXIE vs AC loss measurement: MQXFS
MQXF - Magnetization loss (Deff = 0.039 mm, PIT bundle) | ROXIE | 
 | J/m | J/m3
Pre-Cycle (0-16.47 kA-0.1 kA) | 8474 | 5.994E+05
Ramp up (0.1 kA -16.47 kA) | 3782 | 2.675E+05
Ramp down (16.47 kA -0.1 kA) | 4503 | 3.186E+05
Ramp down + Ramp up (16.47 kA-0.1 kA-16.47 kA) | 8286 | 5.861E+05
Measurements: 7.5 kJ/m, so reasonably close to the 8.3 kJ/m predicted by ROXIE (actually Jc is 5 % lower than the spec in MQXFS5, so the difference is explained with that)

## Slide 24: Conclusion
If the theory behind AC loss is well understood, the literature about Nb3Sn magnet is rather limited and mainly referring to ITER magnet (central solenoid pulse mode).
Experimental results on recent Nb3Sn magnet shows values one order of magnitude higher than NbTi (0.5 kJ/m vs. 8 kJ/m)
A large amount of experimental data is now available from (SMC, RMC, 11T, MQXF) with a defined procedure for AC loss quantification.
A new framework of analysis has been developed following literature procedure to process a large number of files (including old file with different format) can now be treated massively.
So far only electrical method has been used. Next would be to perform calorimetric method.
Simulation work is just recently started at CERN…
Subsidiary goal… can we simulate quench current versus ramp rate using AC loss measurement?