## Slide 1
Luis Gonzalez1, 2
Test of FCC-hh Beam Screen at the KARA Beamline.
Luis Gonzalez
LNF-INFN/CERN TE-VSC
CERN February 20th 2018
Test of FCC-hh Beam Screen at the ANKA Beamline.
Task4.6: Measurements on cryogenic
beam vacuum system prototype
1
2
3
4
5

## Slide 2: Outline
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Motivation of the Experiment
Description of the Experiment
Samples
Geometry
Experimental Configurations
Results and Comparison with Simulations
1

## Slide 3: Motivation of Experiment
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Validation of Simulation Techniques
used for the real machine
PSD
Reflectivity
Heat Load
Photoelectron Generation
CERN February 20th 2018
 | LHC - 0.58A 7TeV | FCC-hh - 0.5A 50TeV
SR power [W/m] | 0,2 | 35,2
Flux* ph/m/s | 4,2·1016 | 1,5·1017
Critical Energy | 44,2eV | 4,3 KeV
R.Kersevan; Beam Dynamics meets Vacuum, Collimations, and Surfaces Workshop. KIT, Karlsruhe. March 2017
*Photon energy above 4eV
2

## Slide 4: Samples: FCC-hh Beam Screen Prototypes
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Prototype #1 July- Oct ‘17
Prototype #2 Jan- May ‘18
Prototype #3 June-Aug‘18
#1: Validation of temperature profile and validity of photon reflector
#2: #1 + Electrode for photoelectron current measurements
#3: Surface treatments as for baseline. Updated internal screen and pumping slots. Substitution Reflector for Sawtooth
CERN February 20th 2018
3

## Slide 5: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
KARA
(KArlsruhe Research Accelerator)
Simulations performed with Synrad; M. Ady, R. Kersevan, M.Grabski, IPAC15. http://test-molflow.web.cern.ch/node/107
Ec FCC-hh = 4.2 KeV
Ec KARA = 6.2KeV
KARA reasonably resembles FCC-hh’s spectrum and linear power, and even at nominal beam energy (2.5 GeV) ANKA’s spectrum is a close match of that of FCC-hh.
CERN February 20th 2018
4

## Slide 6: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
KARA e-Beam
CERN February 20th 2018
5

## Slide 7: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
2m FCC-hh Protoype
KARA e-Beam
CERN February 20th 2018
5

## Slide 8: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
2m FCC-hh Protoype
KARA e-Beam
2m FCC-hh Protoype
CERN February 20th 2018
D-horizontal
5

## Slide 9: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Irradiated length 1.8m
KARA e-Beam
θ
2m FCC-hh Protoype
CERN February 20th 2018
D-horizontal
5

## Slide 10: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Irradiated length 1.8m
2m
KARA e-Beam
θ
2m FCC-hh Protoype
CERN February 20th 2018
D-horizontal
5

## Slide 11: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Irradiated length 1.8m
2m
KARA e-Beam
D-horizontal
D-vertical
2m FCC-hh Protoype
θ
CERN February 20th 2018
5

## Slide 12: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
After collimation :
83% of Photon Flux Cropped
69% of Photon Power Cropped
 | KARA | FCC-hh
SR Flux | 8.7E+16ph/s | 1.5E+17ph/s
SR Power | 32W/m | 32W/m
Angle of Incidence | 18mrad | <2 mrad
Ec | 6.2KeV | 4.2KeV
CERN February 20th 2018
Beam Direction
6
1.8m

## Slide 13: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
The Setup
Beam
BEam Screen Testbench Experiment
BESTEX
CERN February 20th 2018
See Miguel’s presentation
8

## Slide 14: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Experimental Configurations
Ph Flux = 8.73E+16 Ph/s
Ph Flux = 1.44E+17 Ph/s
Geometry #1
Geometry #2
Geometry #4
Geometry #3
Ph Flux = 8.73E+16 Ph/s
Ph Flux = 1.44E+17 Ph/s
Injection @ FCC-hh
Normal operation of FCC-hh
Injection @ FCC-hh
Missalignment @ FCC-hh
CERN February 20th 2018
Power
Flux
7
Power
Flux
Power
Flux
Power
Flux

## Slide 15: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
PSD Studies
Chimney Connection
Middle
BAG + RGA
Back End BAG
Front End BAG
Beam
CERN February 20th 2018
9

## Slide 16: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
CERN February 20th 2018
PSD Studies
Experimental Results Prototype #1
Energy
Flux
Conditioning of the Sample takes place as photon dose increase
10

## Slide 17: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
CERN February 20th 2018
At Geometry #2 a pressure increase takes place.
PSD Studies
Experimental Results Prototype #1
10
Power
Flux

## Slide 18: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
CERN February 20th 2018
At Geometry #2 a pressure increase takes place.
At Geometry #3 The pressure follows the trend of Geometry #2
Large amount of internally reflected photons
PSD Studies
Experimental Results Prototype #1
10
Power
Flux

## Slide 19: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
Levenberg-Marquardt Algorithm
X=-0.54 ± 0.01
X=-0.41 ± 0.01
X=-0.55 ± 0.01
CERN February 20th 2018
Back at Geometry #1 conditioning is rate recovered.
Pressure ~x2 larger than the foreseen after extrapolation.
PSD Studies
Experimental Results Prototype #1
10
Power
Flux

## Slide 20: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
 | 2.5GeV/130mA |  |  |  |  |  |  |  |  | 
 | 3Ah |  |  |  |  | 9.5Ah |  |  |  | 
 | Experiment | Calculations |  | Rel Discrepancy % |  | Experiment | Calculations |  | Rel Discrepancy % | 
 |  | 1st | 2nd | 1st | 2nd |  | 1st | 2nd | 1st | 2nd
Middle (mbar) | 5.7E-09 ± 15% | 2.3E-08 | 6.3E-9 | 74% | 9% | 3.0E-09 ± 15% | 1.2E-08 | 3.3E-9 | 76% | 13.2%
Front (mbar) | 2.9E-09 ± 15% | 4.7E-09 | 2.9E-9 | 33% | 1% | 2.0E-09 ± 15% | 2.8E-09 | 1.6E-9 | 31% | 15%
Back (mbar) | 2.0E-09 ± 15% | 3.8E-09 | 2.8E-9 | 46% | 29% | 1.0E-09 ± 15% | 2.0E-09 | 1.4E-9 | 45% | 25%
PSD Studies
Experimental Results – Comparison with Calculations
1st Calculations
Leak tight Chimney
Perfectly pointy reflector
2nd Calculations (more realistic)
Not leak tight Chimney
Rounded reflector
11

## Slide 21: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Beam
CERN February 20th 2018
Reflectivity Studies
Experimental Equipment
R=
12

## Slide 22: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Reflectivity Studies
Experimental Results Protoype #1
R=
#1
#2
#3
#4
2.4%
0.5%
Photoelectron current measurements at the photon cup show a very low amount of reflected photons for Geometry 4.
13

## Slide 23: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Beam
CERN February 20th 2018
Heat Load Studies
Experimental Equipment
PT100
PT100
15

## Slide 24: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
I
B
J
A
C
CERN February 20th 2018
Heat Load Studies
Experimental Results Prototype #2
Extrapolation
Extrapolation @ 0 mA converge in 20ºC
Reliable experimental data
16

## Slide 25: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Calculation
C
CERN February 20th 2018
Heat Load Studies
Experimental Results Prototype #2
A
B
J
17

## Slide 26: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Photoelectron Generation Studies
Experimental Equipment
A
+
-
SR
e-
Cold Sprayed Isolated Electrode
18

## Slide 27: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Photoelectrons
23.7% Increase
Photon Flux
75.4% Increase
CERN February 20th 2018
Photoelectron Generation Studies
Experimental Results – Prototype #2
A
+
-
SR
e-
#1
#2
19

## Slide 28: Summary and Conclusions
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
After installation of BESTEX at KARA first experimental data have been obtained.
Experiments have been carried out in different irradiation configurations, in order to mimic the different scenarios at FCC-hh
Experimental PSD results in prototype #1 indicate a large amount of reflected photons inside the BS when irradiating outside the reflector region.
PSD calculations were carried out, compared to experimental results and tuned by using more realistic models.
Experimental PSD results and calculations show a discrepancy which remains below 30% in al cases.
Experimental reflectivity measurements show an unforeseen decrease of the amount of reflected photons for the misalignment case. Comparison with simulations is ongoing. Further analysis is needed.
Calculations on the temperature distribution are in good agreement with calculations.
Measurements on Photoelctron generation inside the BS have been peformed for two different configurations so far.
Further data acquisition and data interpretation is needed.
20

## Slide 29: Acknowlegments
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Miguel Gil Costa – Management, Setup development, Installation, mechanical design…
Ignasi Bellafont – Synrad + Molflow Calculations
Javier Fernandez Topham – Comsol Calculations
Antoine Benoit
Abel Gutierrez
Jesus Fernandez
Marton Ady
Alexis Vidal
Bernard Henrist
Berthold Jenninger
Ivo Wevers
Sophie Meunier
Christian Duclos
Herve Rambeau
David Saez
Erhard Huttel
Andreas Graü
CERN February 20th 2018
Paolo Chiggiato -CERN
Roberto Cimino -INFN
Vincent Baglin -CERN
Francis Perez -ALBA
Cedric Garion -CERN
Sara Casalbuoni -KIT-IBPT
Roberto Kersevan -CERN
21
CERN
KIT-IBPT

## Slide 30: Acknowlegments
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
Thank You

## Slide 31
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018

## Slide 32
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018

## Slide 33
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
ANKA Parameters |  | 
Energy | 2.5 | GeV
Emittance | 50 | nm
Circumference | 110.4 | m
Current | 200 | mA
Optics | 4x2 | DBA
DP-Field | 1.5 | T
DP SR Power | 18 | W/mrad
DP SR Photon Flux | 6 1019 | Ph/(s mrad)
Ecritic | 6.2 | KeV
FCC Parameters |  | 
DP SR Power | 32 | W/m*
DP SR Photon Flux | 1x1017 | Ph/(s m*)
BESTEX Parameters (at ANKA after collimation) |  | 
DP SR Power | 32 | W/m*
DP SR Photon Flux | 5 1016 | Ph/(s m*)
Incident angle | 18 | mrad
*m: irradiated length |  | 

## Slide 34
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018

## Slide 35
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018

## Slide 36
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018

## Slide 37
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018

## Slide 38: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Middle
Front
Back
Levenberg-Marquardt Algorithm
X=-0.16 ± 0.01
X=-0.02 ± 0.01
X=-0.23 ± 0.01
CERN February 20th 2018
PSD Studies
Experimental Results
Power
Flux

## Slide 39: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
CERN February 20th 2018
PSD Studies
Experimental Results
Lower starting point lower conditioning rate.
Indicates pre-conditioning of the Geometry #4 region due to scattered photons
Middle
Front
Back
Levenberg-Marquardt Algorithm
X=-0.16 ± 0.01
X=-0.02 ± 0.01
X=-0.23 ± 0.01

## Slide 40: Experiment at KARA
Luis Gonzalez
LNF-INFN/CERN TE-VSC
Test of FCC-hh Beam Screen at the ANKA Beamline.
Geometry #1
Geometry #2
Geometry #3
2.4%
0.5%
1.3%
1.2%
0.3%
Geometry #4
CERN February 20th 2018
Reflectivity Studies
Experimental Results
Photoelectron Currents Ratio
Straight Irradiation
Irradiation after Reflection
Straight Irradiation
Irradiation after Reflection
Straight Irradiation
Irradiation after Reflection
Geometry
#1
Geometry
#2 & #3
Geometry
#4
.
.
2.4%

## Slide 41
Acknowlegments