## Slide 1: A15 Sputtered thin films for SRF applications
G. Rosaz, S. Calatroni, W. Vollenberg, J. B. Descarrega, A. Lunt, A. Gerardin, F. Leaux, A. Sublet,
M. Taborelli, W. Venturini-Delsolaro
KATSIARYNA ILYINA-BRUNNER

## Slide 2: Outline
Motivation
Sample preparation & analysis
Critical temperature
Substrate choice
Achievements and future actions

## Slide 3: Accelerating Superconducting RF cavities
Copper
Niobium
Thin film approach used un CERN : Nb on copper
“-” | “+”
Q-slope not fully understood/explained | “Cheap” bulk material (Cu) High thermal conductivity Well known technique used since LEP generation at CERN

## Slide 4: Accelerating Superconducting RF cavities
Copper
Niobium
Nb
Nb3Sn
Thin film approach used un CERN : Nb on copper
“-” | “+”
Q-slope not fully understood/explained | “Cheap” bulk material (Cu) High thermal conductivity Well known technique used since LEP generation at CERN

## Slide 5: Accelerating Superconducting RF cavities
Copper
Niobium
Nb
Tc | Nb3Sn ~ 18.3 K
 | Nb ~ 9.3 K
RBCS @ 4.2K and 500MHz | Nb3Sn ~ 0.4 nΩ
 | Nb ~ 45 nΩ
Nb3Sn
Thin film approach used un CERN : Nb on copper
“-” | “+”
Q-slope not fully understood/explained | “Cheap” bulk material (Cu) High thermal conductivity Well known technique used since LEP generation at CERN

## Slide 6: Sample preparation by magnetron sputtering

## Slide 7: Sample preparation by magnetron sputtering
Post-coating Annealing
Annealing temperatures | 600 - 800oC
Annealing time | 24 h… 72 h
Reacted After Coating

## Slide 8: Sample preparation by magnetron sputtering
Post-coating Annealing
Annealing temperatures | 600 - 800oC
Annealing time | 24 h… 72 h
Coating temperatures | 600 - 735oC
Alternative Additional Annealing | 24 h… 72 h
Alternative Annealing
Reacted During Coating
Reacted After Coating

## Slide 9: Sample preparation by magnetron sputtering
Post-coating Annealing
Annealing temperatures | 600 - 800oC
Annealing time | 24 h… 72 h
Coating temperatures | 600 - 735oC
Alternative Additional Annealing | 24 h… 72 h
Alternative Annealing
Reacted During Coating
Reacted After Coating
Coating parameters:
Coating gas: Ar or Kr
Coating pressures:
7·10-4 mbar … 5·10-2 mbar
Composition:
Sn 18 At% to 27 At%,

## Slide 10
ACHIEVED RESULTS

## Slide 11: Films Reacted After coating
A15 phase formation. XRD analysis & Morphology

## Slide 12: Films Reacted After coating
A15 phase formation. XRD analysis & Morphology
100 nm
As-deposited

## Slide 13: Films Reacted After coating
A15 phase formation. XRD analysis & Morphology
100 nm
100 nm
As-deposited
Annealed in vacuum furnace - 24h - 800oC
A15 phase confirmed by the presence of Nb3Sn characteristic peaks of (200), (210), (211) … (332)
Absence of non-desired phases NbSn2, Nb6Sn5

## Slide 14: Films reacted during coatings
Characteristics peaks after the coating of (200), (210), (211) … (332) – Confirmation of the superconducting A15 phase
Absence of non-desired phases NbSn2, Nb6Sn5
Dense morphology
200 nm
Cu
Nb3Sn
Pt
100 nm
FIB
SEM

## Slide 15: Critical temperature
[1] A. Godeke. Supercond. Sci. Technol., 19 (2006) R68-R80
Composition
Substrate choice
Additional Annealing
How to increase Tc?

## Slide 16: impact of the substrate choice on Tc transition
Increase of the Tc on 2-4K for the films grown on ceramic substrates
Sharper transition for Nb3Sn synthesised on ceramics
Best Tc
on copper ~ 16 K
on ceramic (Al2O3)~ 17 K

## Slide 17: Copper substrate challenge
Nb and Sn distribution are homogenous
High temperature treatment causes copper interdiffusion
Cu
Nb
Sn
Cu
Nb3Sn
Pt
1 µm
1 µm
1 µm
1 µm
Reacted After Coating (24h - High Temperature Treatment)

## Slide 18: Cracking of the films after annealing
T annealing = 700oC | T annealing = 750oC | T annealing = 700oC
Without solving “cracking” problem not RF compatible
100 µm
10 µm
20 µm

## Slide 19: Proposal: Intermediate layer
Works as “buffer” layer to reduce residual stresses in the films (to solve cracking problem for the films reacted AFTER the coating)
Decrease lattice mismatch, i.e. improving crystalline lattice order (to avoid Tc depression) [2]
Diffusion barrier layer (to prevent copper interdiffusion into Nb3Sn layer)
Possible candidates – Nb, Ta, Al2O3…
[2] Hein. The A15 story. The Science and Technology of Superconductivity pp 333-372

## Slide 20: Intermediate layer: preliminary results
[1] A. Godeke. Supercond. Sci. Technol., 19 (2006) R68-R80
How to increase Tc?

## Slide 21: Summary
We are able to produce high quality films (good composition, crack-free surface, on copper ~ 16 K, ceramic – 17K, on copper with intermediate layer 17.4 K)
Impact of the copper substrate, i.e. increasing in disorder degree and copper interdiffusion after annealing, can be minimised by using intermediate layer. First results showing effectivity of the approach.
First QPR sample in order to test RF properties of the film has been coated and measured. Modest RF performances due to coating technical issue. Next QPR coating expected before July 2018.

## Slide 22
Thank you for your attention!