## Slide 1: Advanced Simulations of Manufacturing Methods for SRF Cavities
Alexandre Amorim Carvalho On behalf of the EN/MME Design Office and Workshop

## Slide 2: Summary
Fabrication Processes
  Metal Forming
  Crab Cavities Challenge
Niobium Sheets under Forming Processes
  Simulating What?
  Material Behavior and Material Models
Simulations Capabilities
  Present and Future

## Slide 3: Sheet Metal Forming
Bending, stretching, compressing, twisting, extruding of metal sheets

## Slide 4: The Crab Cavities Challenge
Manufacturing Challenges!
Material: pure Niobium 4mm thick sheets
Shaping:
  large deformation processes (deep drawing, extrusion..)
  multiple shaping steps on same subcomponent
  highly precise tolerances (±0.3mm)
FE analyses to
Steer manufacturing choices
Speed up tool design and reduce tooling costs
Shaping + Electron Beam welding of 3x main subcomponents
0.5m
0.4m
0.65m
Bowl
Elliptical Cap
Main
Body
DQW

## Slide 5: Sheet Metal Forming Simulations: Why?
Take the initial trials out of the workshop into simulations.
Compare different manufacturing strategies;
Identify forming defects e.g. wrinkles;
Identify highly stressed regions;
Awareness on the final thickness distribution;
Optimize the initial sheet for forming;
Identify tooling's design improvements
Steel 1.2343
Bronze
Explicit Integration

## Slide 6: Sheet Metal Forming Simulations: Why?
Exercise extensively done in the automotive industry and all industries of mass production
Take the initial trials out of the workshop into simulations.
Compare different manufacturing strategies;
Identify forming defects e.g. wrinkles;
Identify highly stressed regions;
Optimize the initial sheet for forming;
Awareness on the final thickness distribution;
Explicit Integration
Identify tooling's design improvements

## Slide 7: Niobium Sheets under Forming Processes
Niobium has Body Centred Cubic (BCC) structure:
Strain Rate Sensitivity (SRS) in the Yield stress.
Strain Rate
Anisotropy
Preferred orientation typically affects sheet metal forming processes.
Anisotropy
Strain Rate
Cyclic Plasticity
Tensile Tests
Compression + Tension
Cyclic plasticity
Testing campaign @ Politecnico di Torino
See EDMS. 1907223

## Slide 8: Niobium Sheets under Forming Processes
Cyclic Plasticity: non-linear Springback is not relevant
Strain rate: workshop processes are barely affected, impact can be estimated
Anisotropy: First indications show it’s not present, further testing is required
Cyclic Plasticity specific material model
springback

## Slide 9: Niobium Sheets under Forming Processes
Typically in BCC …
Cyclic Plasticity: non-linear Springback is not relevant
Strain rate: workshop processes are barely affected, impact can be estimated
Anisotropy: First indications show it’s not present, further testing is required
0.1 1/s
0.001 1/s
0.01 1/s
Strain rate specific material model
In niobium sheets

## Slide 10: Niobium Sheets under Forming Processes
Cyclic Plasticity: non-linear Springback is not relevant
Strain rate: workshop processes are barely affected, impact can be estimated
Anisotropy: First indications show it’s not present, further testing is required
Testing campaign not successful
New tests being prepared
Deep drawing processes done in the workshop tend to confirm that niobium sheets are isotropic.

## Slide 11: Benchmarking of the FE model
Achievements
Thickness accuracy – max. error of 0.1mm;
Dimensional accuracy – max. error of 0.42mm;
Punch Load vs. Punch Stoke – consistent
Displacement & pressure sensors
DAQ
Metrology &
Evaluation of thicknesses via Matlab® code
See EDMS. 1740011

## Slide 12: Simulation capabilities
Tailored material models available
Predict formed shapes (≈ 0.4mm error)
Predict thickness distributions (≈ 0.1mm error)
Estimate springback and sequential processes
Optimize tools and material usage
Introduce the real thickness distribution of the sheet before forming
Export deformed geometry

## Slide 13: Ongoing activities
Exploitation of thickness knowledge for advanced tooling design
Thickening
Thinning

## Slide 14: Ongoing activities
Exploitation of thickness knowledge for advanced tooling design
After forming
Distance mould to punch

## Slide 15: Ongoing activities
Friction coefficient mapping according to tool speeds and surface pressure

## Slide 17: Initial sheet thickness
1.
2.
3.

## Slide 18: Benchmarking – How?
Hydraulic Pressure Machine
SKAG – Type JP-SVF
Max. Load 100tons
Pressure sensor
Displacement sensors
Supply
Graphtec
Δz vs. Fz
Uncertainty for small loads due to variation in hydraulic pressure
Data acquisition:
3 optical displacement sensors;
Pressure sensor in the hydraulic system;
+
Calibration of pressure sensor with load cell
Matlab program maps the points and calculates thickness on a given cross section
EDMS: 1572428
EDMS: 1709479
Post forming metrology
Process data acquisition

## Slide 19: Model vs. Experimental: Thickness
Max. error: 0.08mm
Average error: 0.025mm
Thickness at Minor axis
A
B
C
Chart: Thickness error [mm]
| 39 | 38 | 37 | 36 | 35 | 34 | 33 | 32 | 31 | 30 | 29 | 28 | 27 | 26 | 25 | 24 | 23 | 22 | 21 | 20 | 19 | 18 | 17 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
 | -0.03361 | 0.0034215 | 0.037227 | 0.072311 | 0.06928 | 0.074274 | 0.062295 | 0.048074 | 0.02858 | 0.022008 | 0.022774 | 0.016128 | 0.004707 | 0.0085527 | 0.0065641 | -0.0036465 | 0.0077741 | 0.017451 | 0.029465 | 0.05215 | 0.057297 | 0.053689 | 0.030638 | 0.01441 | 0.0057203 | -0.013913 | -0.028271 | -0.057613 | -0.034258 | -0.012246 | -0.0030525 | 0.0074032 | 0.0022466 | -0.0088052 | -0.0094533 | 0.005885 | -0.0078198 | -0.0086498 | 0.012223
A
C
Thickness at Major axis
Chart: Thickness Error [mm]
| 50 | 49 | 48 | 47 | 46 | 45 | 44 | 43 | 42 | 41 | 40 | 39 | 38 | 37 | 36 | 35 | 34 | 33 | 32 | 31 | 30 | 29 | 28 | 27 | 26 | 25 | 24 | 23 | 22 | 21 | 20 | 19 | 18 | 17 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
 | -0.033637 | 0.053103 | 0.048441 | 0.044004 | 0.044912 | 0.04257 | 0.01868 | -0.0032225 | -0.0088459 | -0.01771 | -0.023278 | -0.036927 | -0.034202 | -0.027066 | -0.038153 | -0.030795 | -0.034058 | -0.017098 | -0.0058773 | 0.01226 | 0.041919 | 0.03171 | -0.029567 | -0.053494 | -0.068116 | -0.074497 | -0.095966 | -0.083116 | -0.074705 | 0.0097692 | -0.0032097 | -0.0074712 | -0.023427 | -0.020869 | -0.0067949 | -0.010482 | 0.0015263 | 0.037415 | 0.010874 | 0.040834 | 0.034742 | 0.043 | -0.043567 | -0.0039996 | -0.008979 | 0.0014037 | -0.0083858 | -0.013943 | -0.006042 | -0.015492
Max. error: 0.1mm
Average error: 0.03mm
C
B
A
A
B
C
2.6%
1.5%
1.4%
1.7%
1.1%
1.2%
Supplier1 sheets
Beyond
Context
Bowl
Diabolo

## Slide 20: Model vs. Experimental: Dimension
Chart: Angle [deg]
RF surface
a
Radius
Bowl before trimming step at the trimming height
Process dispersion
Simulation Vs. Reality
Average: 0.15mm
Maximum: 0.42mm
Considering dimensional deviations of the tools
Beyond
Context
Bowl
Diabolo

## Slide 21: Ongoing activities
Exploitation of thickness knowledge for advanced tooling design
Thickening
Thinning