## Slide 1: Study for luminescence of fine-grained emulsion by charged particles
2018/05/30
T. Shiraishi @ NEWSdm meeting (Anacapri)

## Slide 2: Energy deposition in nuclear emulsion
Ag core Development
Phonons
Light
M. Kimura et al., NIMA (VCI2016) 2016
Energy Deposit
Developed Ag can be seen as a track by microscope
Talk about this!
20 nm crystal
200 nm
40 nm
Luminescence after exposure with the fluorescent lamp
Sensitivity recovered by contribution of NSP?

## Slide 3: Luminescence of AgBr Crystal
Verification of emulsion luminescence excited by light
* Observed at Lq. N2 temperature to decrease heat inactivation
OPERA (200nm)
NIT (40nm)
Luminescence after exposure with the fluorescent lamp
Peak at 577nm
Wavelength (nm)
Relative intensity (a.u.)
NIT (40nm crystal) luminescence spectrum
Conduction Band
Valence Band
E
electron
hole
Hole trap (I-)2
Recombination
Frenkel defects
NIT
40nm crystal
OPERA
200nm crystal
500nm
AgBr crystal
SEM image
* Reported only photoexcitation

## Slide 4: Luminescence of emulsions
NIT (40nm)
OPERA (200nm)
UNIT (20nm)
Exposed white light
Light off
Luminescence
* In liquid N2
** Camera sensitivity is automatically adjusted
Observable luminescence time with the naked eye
OPERA : ~1s
NIT : ~7s

## Slide 5: Motivation 1 Combined analysis with track detection
Locate the recorded track position in emulsion with mm accuracy
Dust and fog don’t luminescent
Identify particle property from luminescence information (intensity, life time, spectrum, …)

## Slide 6: Motivation 2 Elucidation of detection mechanism for charged particles
*1 e-h pair/ 5.8 eV (K. A. Yamakawa, Phys. Rev. 82, 4（1951）)
Charged particle create a huge number of e-h pairs locally at the same time (High illuminance condition)
Agn-1+Ag++e-→Agn
developable at n4
Conduction Band
Valence Band
E
Frenkel defects
electron
hole
energy
deposition
Silver ion
Can we get more information about Ag core creation mechanism from luminescence?
Ag core creation mechanism
 | dE/dx in AgBr crystal | Number of e-h pairs created in 40nm AgBr*
5.48 MeV a-ray | 300 (keV/mm) | 2000 (/fs)
60 keV g-ray | 15 (keV/mm) | 100 (/fs)
1kW pulse laser |  | 0.001 (/fs)
Recombination is probably dominant
 Ag core creation probability decrease
Latent image
*Knowledge on photoexcitation

## Slide 7: Cryostat DAQ
USB → UART
Amplifier
x20
Power Supply
for MPPC
C11204-01
±5V
Power Supply
Cryostat
Hamamatsu C12332-01 module
BNC
feedthrough
MPPC
Sample
Coaxial cable
Ga. He2
Lq. N2
He2 Gas
125Msps,
12bit, 8ch
ADC
Cosmo-Z
ZYNQ
(Xilinx FPGA)
500ksps,
12bit, 8ch
ADC
Cyclone V
(Altera FPGA)
Atlas-SoC
TCP/IP
TCP/IP
Fill He gas inside of chamber to keep no condensation
Adjust amount of Liquid N2 for temperature control
Photon detector : MPPC
MPPC data taking : Cosmo-Z
Pt resistor
Thermal sensor : Pt resistor
Pt resistor data taking : Atlas-SoC
PC

## Slide 8: Cryostat DAQ (Photograph)
MPPC bias voltage cable
MPPC signal cable
Pt resistor cables
± 5V Power supply
Cosmo-Z
(125Msps, 12bit, 8ch ADC and ZYNQ board)
Power supply & Amprifier for MPPC
Atlas-SoC
(500ksps, 12bit, 8ch ADC and Cyclone V soc board)
Send data to PC via LAN cables

## Slide 9: Setup of a-ray and g-ray exposure
241Am RI
a-ray : 5.48MeV
g-ray : 10～60keV
Rate to forward : 33 Hz
Black：241Am g-ray spectrum
Blue：NIT absorbed spectrum
Photon detector
VUV-MPPC (S13370-3050CN)
Light
pixels
Fiducial Area : 9 mm2 Number of pixel : 3600
Aperture : 60%
PDE(@577nm)：32%
Sample (NIT or Gelatin)
12.0mm
MPPC
Stage
a-ray shield
(Al 110μm or no shield)
241Am
3.0mm
1.0mm
Light guide
(PMMA)
59.5keV
17.8
13.9
Notes: Concerning g-ray, main component from am source is around 60keV, but almost of them are through NIT, because the absorption rate is very small. So main component of g-ray absorbed by NIT are 10-20 keV.

## Slide 10: MPPC waveform
10000 events overlay plot
@88K
pre-trigger 288ns
(for pedestal correction)
post-trigger 320ns
Integral ADC (Charge)  Index of number of photon
a-ray exposure
trigger by 1p.e. level
g-ray exposure
10000 events overlay plot
@88K

## Slide 11: Integral ADC (Charge)
1 p.e.
2 p.e.
15 ~ 60 p.e.
This rate is same as number of exposed a-ray
Long waveform data (time window 8ms)
Fluorescence (15~60p.e.)
Phosphorescence
Fluorescence
Phosphorescence

## Slide 12: Detected number of photon
1p.e. peak decision accuracy ~ 1%
Exposed a-ray and g-ray number ~ 2.2%
MPPC noise (cross talk and after pulse rate) ~ 10%
Measurement repeatability ~ 6.8%
a-ray exposure
g-ray exposure
Considered errors

## Slide 13: Detected number of photon (Background subtracted)
Number of emitted photons by a-ray and g-ray are measured
Quenching factor (Nphoton/Ne-h pairs) of AgBr crystal can be calculated
Notes: If we know energy deposition in AgBr crystal, we can estimate quenching factor

## Slide 14: Estimation of energy deposition in AgBr crystal
NIT internal structure
Face centered cubic lattice
Whole density : 3.44 g/cm3
Fill rate of AgBr(I) : 41.5%
Lattice constant : 75.5nm
Integrate energy deposition in crystal by every charged particles
2ry generator condition is more than 5nm
e.g. g-ray simulation
Geant4 simulation Geometry

## Slide 15: Quenching Factor Calculation
Solid angle
～0.14
MPPC photon
detection efficiency
～0.32
AgBr energy gap
～5.8eV
241Am a-ray exposure
Edeptotal = 90000 keV/s
241Am g-ray exposure
Edeptotal = 70 keV/s
Energy deposition in NIT’s AgBr crystal
T=82.3*exp(-0.0165*x)
Number of detected photons
NIT Transmittance of 577nm light
Z (mm)
Z (mm)

## Slide 16: Quenching Factor
dE/dx dependency @ 88K
Temperature dependency
Preliminary
Temperature （K）
Quenching factor (%)
MIP
dE/dx (keV/mm)
Quenching factor (%)
Quenching factor is ~30% for MIP???

## Slide 17: Comparison with typical scintillators
 | Ce : GAGG | Tl : NaI | Scintillating Fiber (BCF-60) | NIT @ 88K (*Gelatin contained)
Density (g/cm3) | 6.63 | 3.67 | 1.2 | 3.44
Life time (ns) | 88 | 230 | 7 | ~100 + ~10000
Deliquescent | no | yes | no | no
Number of photon (photon/MeV) | 60000 (MIP) | 40000 (MIP) | 7100 (MIP) | ~4000 (α 5.48MeV) ~18000 (γ 60keV) ~30000??? (MIP)
Energy resolution (% @ 137Cs-662keV) | 6.3 | 5.6 | ??? | ???
Wavelength (nm) | 520 | 415 | 530 | 570?
Not yet optimized!
We can change amount of Iodine dope, size of AgBr crystal, …
Preliminary

## Slide 18: Luminescence spectrum analysis (On going)
Trigger luminescence by MPPC inside of chamber
Optical fiber guide the luminescence to outside of chamber
Monochromator selects the wavelength (~10nm width)
PMT detects monochro-photon
Optical fiber
Inside of chamber
Optical fiber feedthrough
Monochromator (6/12~ available)
PMT

## Slide 19: Luminescence spectrum analysis (On going)
1 p.e. peak
NIT luminescence + Thermal noise
→ 5.0 cps
Thermal noise  0.02 cps
6/12~ monochromator will be available
NIT luminescence spectrum by charged particles will be able to be observed
PMT signal
(No monochromator measurement)
It is succeed to guide NIT luminescence to outside of chamber with high S/N

## Slide 20: Summary
This is the first observation of luminescence of emulsion by charged particles
Measured the rate of contribution to luminescence of NIT excited by a-ray and g-ray
  Luminescence efficiency is very high at low temperature (may be comparable to plastic scintillator)
Application for detector
  Measure for nuclear recoil event and M.I.P.
  Multi-channel readout
Elucidation of detection mechanism for charged particles
  Spectrum analysis
  Change crystal property
Plan

## Slide 21: Backup

## Slide 22: Cryostat DAQ (for spectrum analysis)
MPPC bias voltage cable
MPPC signal cable
Pt resistor cables
PMT amplifier
High voltage power supply for PMT
Monochromator
PMT
Optical fiber
PMT signal cable
PMT HV cable

## Slide 23: To increase detection efficiency
Use GaAs PMT
  High quantum efficiency
Use wide optical fiber (600mm1mm)
Increase RI rate
  Do anyone have high rate RI (> 100Bq) which can be used at low temperature (77K) ?
Light collection
  It seems difficult to collect light to optical fiber (600μm, NA=0.22)

## Slide 24: GaAs PMT
R943-02（GaAs PMT）
From Hamamatsu data sheet
R1463 (multi-alkali PMT)
Quantum efficiency
30000cps @20℃
20cps @-20℃
100cps @20℃
15% @570nm
7% @570nm
Thermal noise rate

## Slide 25: GaAs PMT を-20℃ぐらいに冷やしたい
密封容器
HV
Signal
GaAs PMT
N2 Gass
光ファイバー
モノクロメータ
入射
出射
どうやって冷やす？
・氷水系は使いたくない
・保冷剤・ドライアイスだと溶ける、温度コントロールできない
霜が付かないように窒素ガス置換

## Slide 26: スターリング冷凍機 SC-UD08
・(10cm)3の体積のアルミニウム（2.7kg）の場合
-20℃から1℃下げるのに38s
-40℃から 48s
-60℃から 66s
冷却性能

## Slide 27
30万円→
12万円→
↑10万円
↑5500円
アダプタ
※100W級の24V電源が必要（Amazonで3000円ぐらい）

## Slide 28: 治具は各自で作れば良い
Φ37.7mm
冷却ステージ
断熱材
？？？
アダプタ
アダプタ
M4ねじ穴
冷凍機
アダプタ
冷凍機
Φ50mm
PMT冷却用
断熱材

## Slide 29: アダプタ

## Slide 30: Data connection
・・・
・・・
PH96
・・・
Data file
Data file
Data file
Data file
50μs
α線による最初の発光（蛍光）
通常の測定
・トリガー閾値：2103
・タイムウィンドウ：600ns
（デッドタイム～800ns）
燐光

## Slide 31: Averaged waveform
赤：トリガー閾値2191、8μsの測定（8μs まではデッドタイムなし）
青：通常の測定（閾値2103、600ns）でデータをつなげたもの
Dead time
Time (ns)
Time (ns)
Pulse Height
log scale

## Slide 32: Long data (time window 8μs)
Average of α-ray long data @ 93K
Average of γ-ray long data @ 93K

## Slide 35: a-ray simulation

## Slide 36: a-ray simulation

## Slide 37: g-ray simulation

## Slide 38: g-ray simulation

## Slide 39: Thermoluminescence of NIT by charged particles
a
Room temperature
Lq.N2 -> Room Temperature
Lq.N2 -> Room Temperature
Room temperature
b
* ISO6400, shutter speed = 4 s (a), shutter speed = 8 s (b)
241Am
90Sr

## Slide 40
日本写真学会誌2016 年79 巻3 号：2–6 高田俊二、久下謙一

## Slide 41: Triboluminescence
日本写真学会誌2016 年79 巻3 号：2–6 高田俊二、久下謙一

## Slide 42: Temperature rise due to phonon effect
 | Total phonon energy in 40 nm [eV] | δT for 40 nm AgBr [K] | δT for 20 nm AgBr [K]
Ag (150 keV) | 18600 | 58 | 234
Br (150 KeV) | 13800 | 43 | 173
C (50 keV) | 734 | 2.3 | 9.2
He (1000 keV) | 15.9 | 0.050 | 0.20
H (1000 keV) | 0.54 | 0.0017 | 0.067
Cv ~ 3.5 x 1020 eV/mol/K @ 93 K (51.8 J/mol/K)
* K. Kamran et al., J. Phys. D : Appl. Phys. 40(2007)869-873
Sensitivity recovery from Ag and Br tracks are promising.
Stopping powers in NIT (SRIM simulation)
Presented at JPS meeting
Autumn 2015
*ESP: Electron stopping power
NSP: Nuclear stopping power

## Slide 43: Temperature rise due to phonon effect
Average phonon energy in 40 nm AgBr layer
by various particles (simulated by SRIM)
Cv ~ 3.5 x 1020 eV/mol/K @ 93 K (51.8 J/mol/K)
* K. Kamran et al., J. Phys. D : Appl. Phys. 40(2007)869-873
Sensitivity recovery from Ag and Br tracks are promising.
Chart: Depth [nm]
 | Total phonon energy in 40 nm [eV] | δT for 40 nm AgBr [K]
Ag (150 keV) | 18600 | 58
Br (150 KeV) | 13800 | 43
C (50 keV) | 734 | 2.3
He (1000 keV) | 15.9 | 0.050
H (1000 keV) | 0.54 | 0.0017

## Slide 44: Calibration of MPPC break down voltage
-189℃
M =
y=V0+p1*x+p2*x2
で補間
y=a(x-b)
縦軸の誤差：
4点測定する間の温度上昇
1光子ピークの決定精度
横軸の誤差：
設定できる最小単位
横軸の誤差：
温度計の測定誤差
Notes: ゲインは1ピクセルの出力電荷を素電荷で割ったもの
(0.24*10^-3)/50*8*10^-9/20/(1.6*10^-19)＝8.6*10^5
0.056 pF
0.1 Vでゲイン2.8変わる
0.2 Vで波高値１変わるかどうかくらい

## Slide 46: Transmittance in NIT

## Slide 47: Transmittance in NIT
T=71.3*exp(-0.0166*x)
577nm light transmittance in NIT
Thickness
NIT
2 times reflection in transmittance measurement
2 times reflection  71.3%
(1-R)2=0.713 ⇒ R=0.155
NIT transmittance is
T=84.5*exp(-0.0166*x)

## Slide 48: Solid angle evaluation
MPPC fiducial area ： 3mm*3mm
NIT
15.0mm
MPPC
Stage
241Am
3.0mm
1.0mm
NIT
15.0mm
MPPC
Stage
241Am
3.0mm
1.0mm
Light guide
(PMMA)
Number of photon
x 39.9
θ

## Slide 49: Solid angle evaluation
MPPC fiducial area ： 3mm*3mm
NIT
4.0mm
MPPC
Stage
241Am
3.0mm
1.0mm
NIT
15.0mm
MPPC
Stage
241Am
3.0mm
1.0mm
Light guide
(PMMA)
Number of photon
x 4.10
θ

## Slide 50: Combined analysis with track detection
NIT
Track
Photon Detector
(e.g. MPPC)
Trigger track position from luminescence
NIT
Wavelength Shifting Fiber
Y axis
X axis
NIT
track
X axis
Y axis
Direct detection by Photon detector
Use WLSF (Wavelength Shifting Fiber) to reduce readout channels

## Slide 51: Cosmo-Z (ADC and ZYNQ board)
ADC : 125MHz, 12bit, 8ch
FPGA : ZYNQ (Xilinx FPGA)

## Slide 52
LPF
LPF
LPF
LPF
125MHz
12bit
ADC
LPF
LPF
LPF
LPF
125MHz
12bit
ADC
LVDS x32
Extension board
memory
DDR3 1GB
ZYNQ
CPU
FPGA
8ch analog input
SD card
Ethernet (1Gbps)
SeriaATA (SSD or HDD)
PCI Express 2.0 (5Gbps)
USB3.0 (4Gbps)
GTX (6Gbps x2ch = 12Gbps)
USB-UART (FPGA writing)
not used
Linux Web server

## Slide 53: Thermal conductivity
 | density (g/cm3) | Specific heat (J/kg・K) | Thermal conductivity (W/m・K)
Air @ 0℃ | 0.001251 | 1005 | 0.0241
Air @ -100℃ | 0.001984 | 1009 | 0.0157
He gas @ 0℃ | 0.000179 | 5192 | 0.1442
Stainless @ 0℃ | ~8 | ~0.5 | ~0.2
Aluminum @ 0℃ | 2.70 | 0.88 | 1.95