## Slide 1
Measurements and Simulations of Surface Radiation Damage Effects on IFX and HPK Test Structures
F. Moscatellia,b, A. Morozzib,c, D. Passerib,c,
S. Mattiazzod, G.-F. Dalla Bettae,f, V. Hingerg and G. M. Bileib
a CNR-IOM of Perugia, via Pascoli 1, 06123, Perugia, Italy
b INFN of Perugia, via Pascoli 1, 06123, Perugia, Italy
c Department of Engineering – University of Perugia, via G. Duranti 93, 06125, Perugia, Italy
d Dipartimento di Fisica e Astronomia e INFN di Padova, via Marzolo 8, 35131 Padova, Italy
e DII University of Trento, via Sommarive 9, 38123, Trento, Italy
f TIFPA INFN, via Sommarive 14, 38123 Trento, Italy
g HEPHY, Austrian Academy of Sciences, 1050 Wien, Austria

## Slide 2: Outline
Motivations
Experimental measurements (X-rays irradiations)
  Different test-structures (MOS capacitors, Gated Diodes, Interstrip resistance test structures)
  Different providers (HPK, IFX) and processes
  TCAD Simulation Results
  Model validation: comparison between simulation findings and experimental data
    Conclusions and future developments

## Slide 3: Motivations and goals
Study the effects of surface damage on silicon devices at high doses (HL-LHC operation greater than 50 Mrad for Outer Tracker and 1 Grad for Inner Tracker).
Surface damage can strongly influence the breakdown, the inter-electrode isolation, the dark current and the charge collection efficiency of the sensor.
Extension of the predictive capability of the past “University of Perugia” numerical TCAD model to these very high doses:
    Physically-grounded parametrization,
    Keep low the number of traps (e.g. avoiding fitting),
    No over-specific modelling (e. g. device and technology independent)
    Deep understanding of physical device behavior.
Extraction from simple test structures of relevant parameters to be included within the model
Validation of the new modeling scheme through comparison with measurements of different test structures manufactured by different vendors with different processes before and after irradiation.

## Slide 4: Test structures IFX and HPK
MOS capacitors
1 gated diode (called GCD)
Strip structures for Rint measurements
IFX
Gated-diode
MOS
capacitor
Cap-TS
for Rint
HPK
MOS
capacitor
Gated-diode
Measurement Campaign: X-ray irradiation
  carried out in Padova (IT). Dose rate 0.8 Mrad/hour
  doses range: 0.05 ÷ 100 Mrad(SiO2)
  Measurements after irradiation / annealing 80°C 10 min.

## Slide 5: IFX devices
1st campaign 0.05-20 Mrad
IFX 8-inch 2S run
MOS
GCD
Rint
2nd campaign
IFX 8-inch 2S run
MOS
2nd campaign
IFX 6-inch PS-S run
MOS
FET

## Slide 6: MOS Capacitors: measurements
p-type substrate.
HF measurements at 100 kHz with a small signal amplitude of 25 mV.
The QS characteristics were measured with delay times of 0.5 s using a voltage step of 100 mV.
Effective oxide charge density NEFF obtained from VFB measurements.
Unbiased devices during the irradiation steps. Dry N flux during measurements.
IFX PS-S
IFX 2S

## Slide 7: IFX 2S MOS CV Measurements after X-ray
VFB  -10 V at 50 krad
VFB  -17 V at 100 krad (not shown in this figure)
VFB  -30 V at 500 krad
VFB-42 V at 1 Mrad
VFB-50 V at
10-20 Mrad

## Slide 8: IFX 2S MOS CV after X-ray 2nd campaign
VFB  -5 V at 50 krad
VFB  -7 V at 100 krad
VFB  -18 V at 500 krad
VFB-23 V at 1 Mrad
VFB-35 V at
10 Mrad
VFB-65 V at
100 Mrad

## Slide 9: IFX PS-S CV after X-rays
VFB  -4 V at 50 krad
VFB  -5 V at 100 krad
VFB  -11 V at 500 krad
VFB-15 V at 1 Mrad
VFB-40 V at
10 Mrad
VFB-55 V at
100 Mrad

## Slide 10: HPK CV after X-rays
P-spray
Process p-stop (no implant under the oxide)

## Slide 11: IFX - MOSFETs
+
Vth = -0.1 (unirradiated)
Unbiased devices during the irradiation steps
Radiation  interface traps (NIT) + trapped-oxide (NOX)  Vth shift (ΔVth).
ΔVth is separated into a contribution due to NIT and due to NOX, from IDS-VGS of MOSFET (method proposed in McWorther Applied Physics Letters 48, 133 (1986))

## Slide 12: IFX p-type Summary of measurements
For NEFF :
  Differences among the three processes at low doses.
  At high doses similar results.
PS-S has higher interface traps

## Slide 13: HPK p-type Summary of measurements
As expected very similar values for HPK devices

## Slide 14: IFX and HPK p-type GCD after X-ray irradiation
Annealing 80°C 10 min
Surface velocity s0 evaluated as a function of the dose
Area 11.71 mm2 Area 6.14 mm2
IFX
HPK

## Slide 15: Interstrip resistance after X-ray irradiation
P-stop 1st campaign
P-stop 2nd campaign
Interstrip resistance values are similar between the two campaigns

## Slide 16: New “University of Perugia” model
TEST STRUCTURE MEASUREMENTS
DETECTOR OPTIMIZATION
MODEL
PARAMETERS EXTRAPOLATION
MODEL VALIDATION

## Slide 17: Surface Damage Model: Gaussian
EC - 0.40
EC
EV
EC - 0.60
EV + 0.70
Interface trap state energy modelling
Type | Peak Energy (eV) | Density (cm-2) |  (eV)
Acceptor | EC - 0.40 | 40% of acceptor NIT [1] (NIT=M·NOX) | 0.07
Acceptor | EC - 0.60 | 60% of acceptor NIT [1] (NIT=M·NOX) | 0.07
Donor | EV + 0.70 | 100% of donor NIT (NIT=M·NOX) | 0.07
F. Moscatelli et al., Effects of Interface Donor Trap States on Isolation Properties of Detectors Operating at High-Luminosity LHC, IEEE Transactions on Nuclear Science, 2017, Vol. 64, Issue: 8, 2259 - 2267

## Slide 18: Surface Damage Model: Uniform Bands
EC
EV
EV + 0.6 eV
EC - 0.56 eV
Interface trap state energy modelling
Acceptor Band
Donor Band
EV + 0.3 eV
Conduction Band
Valence Band
Type | Energy (eV) | Band width (eV) | Concentration (cm-2)
Acceptor | EC ≤ET≤EC-0.56 | 0.56 | Dit = Dit(Φ)
Donor | EV+0.3 ≤ET≤EV+0.6 | 0.30 | Dit = Dit(Φ)
F. Moscatelli et al: “Analysis of surface radiation damage effects at HL-LHC fluences: Comparison of different technology options”, NIMA https://doi.org/10.1016/j.nima.2018.07.081

## Slide 19: IFX 2S MOS capacitors: simulations
Irradiated structures IFX 2S 1st campaign.
C-V measurements compared to simulations at different doses.
  Good agreement for IFX devices!

## Slide 20: IFX 2S 2nd campaign MOS capacitors
Irradiated structures IFX 2S 2nd campaign.
C-V measurements compared to simulations at different doses with measured NIT and NOX of 2S wafer.

## Slide 21: IFX PS-S MOS capacitors
Irradiated structures IFX PS-S 2nd campaign.
Low NOX at low doses
Higher NIT

## Slide 22: HPK p-type MOS capacitors: simulations
Irradiated structures HPK p-type without p-spray.
C-V measurements compared to simulations at different doses.
  Using the same model with measured NOX and NIT good agreement between simulation and experimental data

## Slide 23: HPK MOS capacitors with p-spray: simulations
Irradiated structures HPK p-type with p-spray.

## Slide 24: Gated diodes
p-type substrate
Irradiated structures IFX p-type.

## Slide 25: Interstrip resistance HPK
Good agreement using the same model used to simulate MOS capacitors

## Slide 26: Conclusions
  Extensive measurements campaign on 5 different IFX and HPK n-on-p test structures before and after irradiation with X-rays.
  Surface radiation damage effects have been deeply investigated aiming at the extraction of the most relevant parameters:
    cross-check of NOX, NIT, DIT evaluated by different methodologies from different test structures, for different vendors (HPK and IFX) and different processes.
  Development of the radiation damage modelling scheme, suitable for commercial TCAD tools (e.g. Synopsys Sentaurus), with a good agreement between measurements and simulations
  Application to the analysis and optimization of different classes of silicon detectors to be used in the future HEP experiments.

## Slide 27: Future developments
  Bias the IFX and HPK devices during X-rays irradiation
  Irradiate new HPK batches FZ290 and thFZ240
  Irradiate test structures first with X-rays and then with neutrons to combine surface and bulk damage

## Slide 28: Backup slides

## Slide 29: FBK - MOSFETs
x
x
x
+
Vth = -0.8 ÷ 0.1 V (unirradiated)
Unbiased devices during the irradiation steps
Radiation  interface traps (NIT) + trapped-oxide (NOX)  Vth shift (ΔVth).
ΔVth is separated into a contribution due to NIT and due to NOX, from IDS-VGS of MOSFET (method proposed in McWorther Applied Physics Letters 48, 133 (1986))
pMOSFET
nMOSFET

## Slide 30: FBK Summary of measurements – p-type
Integrated interface trap density (NIT)
Describe the Donor trap state characterisics
Effective oxide charge density (NEFF)
as INPUT PARAMETERS to the TCAD tool

## Slide 31: FBK Summary of measurements – n-type
Integrated interface trap density (NIT)
Describe the Acceptor trap state characterisics
as INPUT PARAMETERS to the TCAD tool
Effective oxide charge density (NEFF)

## Slide 32: Two different irradiation conditions: without/with biasing the devices.