## Slide 1: Displacement cross section measurements in J-PARC and potential for HiRadMat
RaDIATE Collaboration Meeting at CERN Dec 20 2018
(JAEA/J-PARC) Shin-ichiro. Meigo,
H. Matsuda, Y. Iwamoto,
S. Hasegawa, F. Maekawa,
H. Iwamoto
(KEK/J-PARC) M. Yoshida, T. Nakamoto, T. Ishida,
and S. Makimura
Present study includes the results of “Measurement of displacement cross section at J-PARC for structural material utilized at ADS” entrusted to JAEA by MEXT

## Slide 2: Contents
Introduction
  Present and future plan of J-PARC
Experiment for measurement displacement (DPA) cross section at J-PARC
  Experiment Ep 0.4 to 3 GeV at 3NBT
  Comparison with calculation model
Summary

## Slide 3
Neutron beam lines (23)
Bird’s eye photo
Transmutation
Facility (TEF)
(Phase II）
Hadron Experiment Facility
Neutrino Exp. Facility
(294km to Super KAMIOKANDE)
Materials & Life Science Facility (MLF)
3GeV Synchrotron
RCS (25Hz,1MW)
Linac
400MeV(50mA)
JRR-3M
800m to MLF
30GeV Synchrotron
MR (0.75MW)
J-PARC = Japan Proton Accelerator Research Complex
JFY2007 Beam
JFY2008 Beam
JFY2009 Beam

## Slide 4: Targets in Material Life Experimental Facility (MLF)
Muon production target
  Carbon graphite
  Highest μ- intensity
Neutron production target
  Mercury (Hg)
Thick. 2cm
Diam. Φ33cm
L 2m
W 34cm
SS container
Ptron
Hg
Light water
Safety hull
Double wall: Helium layer observed radiation
Highest pulse intensity in the world
8% beam loss

## Slide 5
Target for high-intensity hadron accelerator and superconductor in high radiation area
Proton beam window in J-PARC spallation neutron source: Aluminum alloy (f 0.6 m)
T2K beam window
Titanium alloy (Ti-6Al-4V)
Superconducting magnet system in COMET (J-PARC)
For damage estimation of target material, DPA is utilized based on displacement cross section.
High accuracy of the displacement cross-section is required.
Proton
3 GeV
Proton 30 GeV
Superconductor resistivity change due to radiation is crucial for superconducting magnet.

## Slide 6: ADS proposed by JAEA
~ 30 MW
Beam window
Beam window: 20 dpa/year. Accuracy of dpa is required for damage estimation.
Belgium ADS program MYRRHA at SCK・CEN (Mol) approved 558 M€

## Slide 7: Transmutation Experimental Facility (TEF)
For R&D of ADS, 0.4 GeV beam by LINAC will be delivered to TEF.
Soviet submarine (LBE)

## Slide 8: Beam transport from RCS to MLF
3NBT
3-50BT
3-GeV RCS
50-GeV MR
Neutrino line
Material and Life Science Experimental Facility (MLF)
Neutron target
Muon target
road to coast
Length of 3NBT: 314m
Partial beam goes to MR
FX: 2.48 s, SX: 5.5 s
Ep: 3GeV
Power: 1MW
Already demonstrated
Rep.: 25Hz
JSNS
MUSE
FWHM ~150ns
600ns
600ns
Dump

## Slide 9: Second target station plan
1st target ST (TS-1): 24 Hz: 1MW
2nd target ST (TS-2) 1Hz : 42kW (Designed to accept 1 MW)
TS-1
TS-2
m
n
Ep3GeV

## Slide 10: Proton Beam Window at MLF (A5083)
Lifetime estimation based on Post Irradiation Examination (PIE) for safety shroud (AlMg3) at SINQ in PSI
Considering difference of proton energy, to predict lifetime of the PBW with high accuracy for validation of calculation
Result at SINQ/PSI for 0.6GeV
Y. Dai, et al, J. Nucl Mat. 343 184 (2005)
Height: 3.8m
Weight：10t
Lifetime of PBW: Determined by He gas production (1200 appm) 2 years*
By recent PIE result of the SINQ (2400 apmm), lifetime may be applicable to 3 years.
* S. Meigo, et al, J. Nucl Mat. 450 141 (2012)

## Slide 11: Inspection spent PBW
PBW #1 (obs. 2013 Oct) 1916 MWh (1.4x1022 POT)
PBW #2 (obs. 2017 Aug) 2510 MWh (1.9x1022 POT)
Vacuum side(~1x10-4 Pa)
Helium side (~1bar)

## Slide 12: Beam peak density reduction with octupole magnet
Normal optics (i.e. linear ) → Gaussian
  Nonlinear optics with OCT shaping flat beam to reduce the peak
With OCT
Linear
Phase space
Spatial distribution
Position
Divergence
Position
Position
Position
Intensity
Principal: Folding edge to center
Hori.
Hori.
Vert.
Vert.
Reduction ~40% (10→6 mA/cm2 at 1MW)
OCT 0A
OCT 698A

## Slide 13: Beam operation at MLF
Present 500 kW
Availability ~95%
Major interruption : Earthquake, Hadron facility accident, Water leak Hg target (x2)
Kicker magnet (KM) failed. But keep operation w/o failed KM ( 2 of KM failed out of 8)
Helium bubbler flow choking. Mirror for LDV came off due to welding issue.

## Slide 14: Demonstration of 1 MW for 1h
On July 2018 4th, 1 MW beam test for 1h
Once chance per year before outage
Vacuum worse found at RCS
W/O failed one quadrupole magnet operated

## Slide 15: Vacuum at BT during 1 MW
Overall vacuum pressure was low.
Drastically increase pressure of mass number 3 (probably T) as increase of beam power. (1 MW: ~12 times of 500 kW)
Gas treatment system for exhaust of pump was implemented on summer 2018.
Tritium production in cooling water for magnets and beam scraper is an another issue.
Mass 44 (CO2)
Mass 3
Mass 16 (O2)
C+O2->CO2
Mass 3
1 MW

## Slide 16: PKA and DPA
DPA (Displacement per Atom) is estimated by calculation based on PKA.

## Slide 17: DPA and displacement cross section
Although DPA is widely utilized for estimation of damage, displacement cross section has not been enough validated.
    DPA = flux x Displacement cross section
  Displacement cross section has been measured only Cu and W for a few energies of protons
  Among calculation showing large discrepancies among models.
N. Mokhov HPTW2016

## Slide 18: Measurement of DPA cross section at Kyoto univ
Irradiation on metal at cryogenic temperature with GM cryocooler
By observing increase of electrical resistance, the cross section can be observed.
Measurement for Cu already performed at Kyoto university for 125 MeV proton
Experiment at J-PARC
Samples and GM placed at exit of 3-GeV synchrotron for various energy of proton 0.4 to 3 GeV
Other experiment performed at other sites for energy < 400 MeV

## Slide 19: Experimental condition
Temp rising ~20 K will be acceptable.
If time permits, lowest beam is preferable.
However, it makes worse accuracy of beam
charge. (Vary 1x1010 – 2x1013 protons/shot)
1 nA x 12h = 3x1014 protons
Several shots of beam at MLF
Y. Iwamoto et al.

## Slide 20: Radiation safety for J-PARC exp.
Residual dose: Confirmed enough small for handling
Confirmed to fit criteria of beam loss (1 W/m) for maximum beam to dump (8 kW)
Incident energy | Cooling 4h (mSv/h) | Cooling 7d (mSv/h)
3 GeV | 19 | 0.01
30 GeV | 29 | 0.02
Residual dose at 0.3 m of sample
Particles flux during irradiation
Calc. geom. model
20
Protons： 5x1014
f 30mm

## Slide 21
Beam dump
From RCS
To MLF
Measurement of cross section for 0.4～3 GeV proton
Experiment at RCS with change of radiation license
With changing extraction timing of RCS, kinetic energy of proton can vary from 0.4 to 3 GeV.
Cold head and sample
Vertical view
Vacuum chamber with 4-K GM cooler
1 m
Beam
Under cryotemperature (~ 20 K), displacement cross section(s) was obtained by increase of resistivity (Δρcu) due to proton irradiation with average flux (f(E))
Cu wire (f 0.25 mm) with purity 99.999%
annealed 1,350 K
ρFP: Resistivity change by a Frankel pair (2.2x10-6 Ωm)
40 mm

## Slide 22
Experimental result
Resistance and temperature during irradiation
Experiment was carried out for protons with 0.8, 1.3, 2.2 and 3.0 GeV
To obtain resistance with high accuracy, 4 wire with delta mode with averaging was applied.
Beam width on the sample was obtained with the beam profile monitor.
Error is dominated with resistivity change by creation of the Frankel pair (23%).
50 shots
50 shots
50 shots
150 shots x 3.3x1012 = 5x1014protons
0.4μΩ
Ep (GeV) | Resistivity change (ΔΩm3X10-31) | σdpa (b)
0.8 | 2.35±0.31 | 1070±284
1.3 | 2.32±0.26 | 1053±270
2.2 | 2.49±0.21 | 1133±277
3.0 | 2.49±0.16 | 1010±244
Vertical beam profile

## Slide 23: Cascade sample holder
Experiment at 3NBT in J-PARC
RCNP (Osaka univ.) experiment by Iwamoto
To obtain Cu and Al data, cascade scheme applied.
Achieved ~5 K
Cascade target of 4 pieces (Al, Fe, Cu, W) applied
Temp ~19 K
In future improved to achieve ~5K

## Slide 24: Calculation with PHITS code
Displacement cross section with PHITS implemented following models
  Norgett-Robinson-Torrens (NRT) model
  Athermal recombination corrected (arc) model (Nordlund model)
    Nature comm. 9, 1084, 2018
NRT (Cu Ed 33 eV):
Nordlund (Cu Ed 33 eV):
ー NRT
ー Nordlund
Nd different for Td>83 eV
Nd: Number of displacement
Td: Displ. energy

## Slide 25: Comparison with models calculation
NRT model
overestimates ~ x3
Nordlund model
good agreement
NRT/Nordlund
Present data imply that the DPA should be calculated with Nordlund model.
Ratio of NRT/Nord is constant above ~200 MeV.
If the displacement cross section sustains to NRT for Ep< 10 MeV, the cross section for Ep>100 MeV is ~2 times.

## Slide 26: Comparison with MARS

## Slide 27: Al and W results
As Mokhov suggestion, should be improved

## Slide 28: Analysis of contribution for DPA
Fission and spallation fragment dominating

## Slide 29: Plan at MR for 3〜30 GeV
MR abort dump
  PAC will approve soon
  Next year will be performed.
990 mm
616 mm

## Slide 30: Possibility at FNAL and HPTW
Relatively easy experiment
Equipment
  GM cooler
  Vacuum chamber
  Instruments to observe sample resistance
Instruments should be placed at near the sample with low radiation
Requirement of experiment
  Beam monitor and properties
    not only for beam position but also width and Twiss parameter
  Beam scan procedure
  If beam loss allowed, thick sample holder should be applied to cool the sample

## Slide 31: Impact on material property analysis
5
6
7
8
Gas production is good index to determine the lifetime

## Slide 32: Summary
Displacement cross section, measurement for 0.4〜30 GeV protons has conducted in J-PARC.
  Experiment performed for Al, Fe, Cu and W with 0.8, 1.2, 2.2 and 3 GeV protons.
  Calculation compared with the present data.
    NRT: ~3 times overestimation
    Arc-dpa (Nordlund) : pretty good agreement
NRT cross section will be discussed in IAEA.
In future, similar experiment will be performed at FNAL and HiRatMat.