## Slide 1: Progress of X-band High-Gradient Choke-mode Accelerating Structures
Xiaowei Wu
on behalf of the Tsinghua X-band team and collaboration
2019/3/13

## Slide 2: Outline
Introduction
Design and fabrication of Choke-mode structures
Breakdown phenomenon study of Choke-mode structures
High-gradient performance of Choke-mode structures
Summary

## Slide 3: Outline
Introduction
Design and fabrication of Choke-mode structures
Breakdown phenomenon study of Choke-mode structures
High-gradient performance of Choke-mode structures
Summary

## Slide 4: Choke-mode structure
Proposed by T. Shintake in 1992
  HOM absorbed by the absorption materials in the end of the radial line
  λ/4 choke reflects the fundamental mode
Applied in Spring-8 and SACLA XFEL
  working at C-band (5.712 GHz)
  damp the HOM via the radial line
  gradient around 35-40 MV/m
Alternative choice for CLIC main linac
T. Shintake, Japanese J.Appl.Phys.31:L1567-L1570 (1992)
R. M. Jones, Phys. Rev. ST Accel. Beams 12, 104801, 2009.
http://www.spring8.or.jp
Notes: The choke reflects the accelerating mode, but unwanted HOMs can pass the choketobeabsorbedintheload

## Slide 5: Why Choke-mode structure?
Beam line
Possible welding joint
Cylinder structure
Choke-mode
Circular symmetric, easy fabrication
Low surface magnetic field, low pulse heating, low breakdown rate
Low magnetic field at the welding joint
High-gradient performance of X-band choke is still unknown
Hao.Zha, ph.D thesis
Cylinder structure vs Choke-mode structure
Magnetic field of Choke-mode structure

## Slide 6: Players
Tsinghua University
  Xiaowei Wu, Jiaru Shi, Hao Zha, Huaibi Chen, et al.
KEK
  Linac shift leaders and Mitsubishi operators
  Karube, Kawabata, Asai from CarrierCom
  Matsui, et al from PlusWork
  Tetsuo Abe, Toshiyasu Higo, Shuji Matsumoto, Toshikazu Takatomi, Yoshio Arakida,
CERN
  Walter Wuensch, et al.

## Slide 7: Recent publication

## Slide 8: Outline
Introduction
Design and fabrication of Choke-mode structures
Breakdown phenomenon study of Choke-mode structures
High-gradient performance of Choke-mode structures
Summary

## Slide 9: Single-cell standing-wave structure study
  Single-cell structure
  Z-axis E field
To study the X-band choke high-gradient performance
Single-cell structure consists of three cells
  Firstly conducted in SLAC
  Easy fabrication, short testing time
  Field in middle cell (test cell) is two times of that in other cells

## Slide 10: Design of Choke-mode cavities
Choke-mode cavity
Reference cavity
Compare the effect of different choke dimensions to high-gradient performance
Design six single-cell standing-wave (SW) structures, working at 11.424 GHz
  THU-CHK-#1~ THU-CHK-#5 (different choke dimensions)
  THU-REF (single-cell structure without choke)
Notes:   (1C-SW-A3.75-T2.6-CHOKE2.1)

## Slide 11: Middle cell design
  Model
  Model
Create single cell model for choke designing
represents the leakage of the accelerating mode to the radial line
  Optimize the choke dimension to keep at 11.424 GHz
is the power absorbed by the radial line
is the power loss of the main cavity
Notes: The choke reflects the accelerating mode, but unwanted HOMs can pass the choketobeabsorbedintheload

## Slide 12: Choke absorption curve
Absorption Curve
Coaxial-radial line with choke model
  Determine the absorption of higher-order-modes (HOMs) by the choke
Some dipole modes have high kick factor between 15 GHz and 40 GHz from the wakefield impedance spectrum
  The fully reflected frequencies were kept out of this region
Wake spectrum
Dangerous region!
Notes: zero absorption points in the curve indicate that modes at these frequencies are fully reflected by the choke, which are so called parasitic modes. Some dipole modes have high kick factor between 15 GHz and 40 GHz from the wakefield impedance spectrum of choke-mode accelerating structure

## Slide 13: Cavity tuning
THU- |  |  |  |  |  | 
REF | 2.05 | 130 | 0.212 | 9010 | … | 143
CHK-#1 | 2.10 | 109 | 0.182 | 7519 | 0.76 | 92.3
CHK-#2 | 2.05 | 104 | 0.172 | 7247 | 0.92 | 82.8
CHK-#3 | 2.04 | 110 | 0.185 | 8006 | 0.73 | 98.4
CHK-#4 | 2.06 | 112 | 0.187 | 8210 | 0.69 | 102
CHK-#5 | 2.05 | 103 | 0.180 | 7864 | 0.84 | 91.1
THU- |  |  |  |  |  | 
REF | 2.05 | 130 | 0.212 | 9010 | … | 143
CHK-#1 | 2.10 | 109 | 0.182 | 7519 | 0.76 | 92.3
CHK-#2 | 2.05 | 104 | 0.172 | 7247 | 0.92 | 82.8
CHK-#3 | 2.04 | 110 | 0.185 | 8006 | 0.73 | 98.4
CHK-#4 | 2.06 | 112 | 0.187 | 8210 | 0.69 | 102
CHK-#5 | 2.05 | 103 | 0.180 | 7864 | 0.84 | 91.1
RF parameters
Choke-mode structure E field
*Normalized to
Tune the full structure
  Work at π-mode, 11.424 GHz
  Critical coupling
Modify choke dimension to change the choke field
  THU-CHK-#1~ THU-CHK-#5
Structure tuning

## Slide 14: Choke field distributions
The loss power of the whole structure is normalized to 1 MW
E field
H field

## Slide 15: Fabrication
Cell manufacture and diffusion bonding at Tsinghua University
A diffusion bonding test of choke-mode cavity was done to check the quality as contact areas of each choke-mode structure disks are not consistent vertically
Good results were seen after cutting the test structure
Choke-mode cavity cell
Diffusion bonding test

## Slide 16: Low-power RF measurements
Bench test, tuning, and baking were done in Tsinghua
Structures shipped to KEK after being closed by vacuum valves to keep vacuum environment
Frequency check at KEK kept consistent with the test results in Tsinghua University
Notes: THU-CHK-#3

## Slide 17: Outline
Introduction
Design and fabrication of Choke-mode structures
Breakdown phenomenon study of Choke-mode structures
High-gradient performance of Choke-mode structures
Summary

## Slide 18: High-gradient test stand
High-gradient test was conducted in Nextef at KEK (New X-band Test Facility)
Frequency: 11.424 GHz
Repetition rate: 50 Hz
Shield-A, traveling-wave structure test stand, max power of 100 MW
Shield-B, standing-wave structure test stand, max power of 33 MW

## Slide 19: Shield-B setup
High-gradient test carried out in Shield-B of Nextef
Shield-B test stand
  Incident and reflection waves collected by Directional Couplers
  Dark current captured by Faraday Cups
  Other detection equipment
T. Abe et al., Proceedings of PASJ2016

## Slide 20: Shield-B setup
Faraday Cups
Test Cavity
WR90 Waveguide
Power Flow
TM01 Mode Launcher

## Slide 21: RF pulse shaping
Use double step input waveform
Filling time around 100ns
Keep the ratio of the two steps constant to make flat E field inside cavity
Increase the width of the second step
Increase the width of the second step

## Slide 22: Typical breakdowns w or w/o current flash
Two types of breakdown events were observed
  Breakdown with current flash (CF-BD) speculated to be occur in the cylinder cavity
  Breakdown without current flash speculated to be occur in choke
98.6% breakdown events were accompanied with current flash in THU-REF
  Faraday Cup has good capture rate for the dark current
Normal event
Breakdown event
without current flash
Breakdown event with current flash：CF-BD
FC Current
FC Current
FC Current
Incident
Reflect
Incident
Reflect
Incident
Reflect

## Slide 23: Two types of breakdowns
Breakdowns were accompanied by the current flash into the Faraday cup during the initial ramping stage of THU-CHK-#1
After initial ramping, few current flash breakdowns were observed in the detected events
Same phenomenon was seen in THU-CHK-#1 and THU-CHK-#2
Zoom of the beginning
Notes: tendency

## Slide 24: Postmortem of choke-mode structure
B1
B2
The red lines are bonding joints
We kept the bonding joint to check whether there are any flaw during the diffusion bonding in the second cutting
Cut THU-CHK-#1 twice (B1 and B2)

## Slide 25: After the cutting
The surfaces of the irises and cavity are very clean.
KEYENCE VE-8800 was used to do the further inspections
This surface is also clean.
The surface of this choke groove seems to be very bad.
On this surface, the surface roughness is the worse than the choke groove in the left photo.
Modified from Abe’s presentation

## Slide 26: Inner surface observation results
D
B
H
G
E
A
H
B
D
F
G
C
A
E
C
100 μm
100 μm
100 μm
100 μm
100 μm
F
100 μm
100 μm
100 μm
Choke E field
Conclusion：
Many breakdown spots at B、C
Copper sputtering at E、F、G
Choke was damaged
Iris area was clean

## Slide 27: Inner surface observation results
D
B
H
G
E
A
H
B
D
F
G
C
A
E
100 μm
100 μm
100 μm
100 μm
F
100 μm
100 μm
100 μm
Choke E field
Conclusion：
Many breakdown spots at B、C
Copper sputtering at E、F、G
Choke was damaged
Iris area was clean
High-gradient performance limited by the breakdown events at choke area!
C
100 μm

## Slide 28: THU-CHK-#3 breakdown signals
Breakdown events accompanied with current flash observed during the whole test
Both of the two types occurred when gradient got saturated
Same phenomenon was seen in THU-CHK-#4 and THU-CHK-#5

## Slide 29
  THU-CHK-#3 observation results
Choke E field

## Slide 30
  THU-CHK-#3 observation results
Conclusion：
Many breakdown spots at B、C、E、H、J
Both choke and iris areas were damaged
High-gradient performance limited by the breakdown events at choke and iris areas!
Choke E field

## Slide 31: Outline
Introduction
Design and fabrication of Choke-mode structures
Breakdown phenomenon study of Choke-mode structures
High-gradient performance of Choke-mode structures
Summary

## Slide 32: High-gradient history of Choke-mode structures
THU-CHK-#1
  Cannot ramp input power after RF pulses, same as THU-CHK-#2
  Max gradient reached 83.9 MV/m at longer pulse operation
THU-CHK-#4
  Fast ramping speed, same as THU-CHK-#3
  Max gradient reached 123 MV/m at longer pulse operation
THU-CHK-#1
THU-CHK-#4

## Slide 33: High-gradient history of THU-REF
Max gradient reached 145 MV/m
Validate Tsinghua X-band single-cell fabrication technology
98.6% breakdown events were accompanied with current flash

## Slide 34: Comparison of single-cell structures
THU-CHK- |  |  | 
#1 | 80.1 | 128 | 0.76
#2 | 68.3 | 129 | 0.92
#3 | 110 | 163 | 0.73
#4 | 125 | 177 | 0.69
#5 | 100 | 172 | 0.84
THU-CHK- |  |  | 
#1 | 80.1 | 128 | 0.76
#2 | 68.3 | 129 | 0.92
#3 | 110 | 163 | 0.73
#4 | 125 | 177 | 0.69
#5 | 100 | 172 | 0.84
Same max value of in THU-CHK-#1 and THU-CHK-#2
  Breakdown in choke limits high-gradient performance
Fast ramping speed in THU-CHK-#4
  Increase choke dimension can increase the and high-gradient performance
is normalized to a flat top width of 250 ns and a bpp of
A. Degiovanni, et al. PRAB 19, 032001, 2016

## Slide 35: High-gradient performance evaluation of chokes
Study the relationship between max normalized gradient G, and dimension [mm] by applying the high-gradient test data of choke-mode structures
THU-CHK- | / |  | 
#1 | 0.76 | 1.26 | 250
#2 | 0.92 | 1.26 | 213
#3 | 0.73 | 1.89 | 343
#4 | 0.69 | 2.21 | 391
#5 | 0.84 | 1.88 | 312
THU-CHK- |  |  | 
#1 | 0.76 | 1.26 | 250
#2 | 0.92 | 1.26 | 213
#3 | 0.73 | 1.89 | 343
#4 | 0.69 | 2.21 | 391
#5 | 0.84 | 1.88 | 312
CHK can be used to guide choke design, evaluate high-gradient performance
Only determined by the geometry
*The data above is based on the BDR measurements results

## Slide 36: Summary
Several single-cell SW structures were designed, fabricated, and tuned at Tsinghua University
High-gradient test was conducted in Nextef at KEK
  THU-CHK-#4 reached 123 MV/m at a flat top width of 100 ns
Choke-mode structure breakdown phenomenon was studied
  Two types of breakdown events were seen
  Current signal can be used to classify the breakdown type
A new quantity was proposed to guide the design of high-gradient choke-mode structures
  Obtained from the summary of the high-gradient experiments

## Slide 37: Next step…
Wakefield calculation and optimization of the travelling-wave choke-mode structure (TD26-CDS-E) based on latest choke dimension
High-gradient test of TD26-CDS-E

## Slide 38: Related paper
More details can be found via the link:
https://journals.aps.org/prab/abstract/10.1103/PhysRevAccelBeams.22.031001#
Thank you!

## Slide 39: Backup

## Slide 40: High-gradient history of THU-CHK-#2

## Slide 41: High-gradient history of THU-CHK-#3

## Slide 42: High-gradient history of THU-CHK-#5