## Slide 1
ILGAD TCAD Simulations: first approximations
F.R. Palomo1, S.Hidalgo2, I.Vila3
fpalomo@us.es
1Dept. Ingeniería Electrónica, Escuela Superior de Ingenieros
Universidad de Sevilla, Spain
2CNM-IMB Barcelona, Spain
3IFCA Santander, Spain

## Slide 2
Introduction
Development of several ILGAD models to test gain variation with bias and n+/pwell doping
Improvement in the ILGAD models compared with experimental data
Analisis of radiation effects in ILGAD
  300um New Perugia Trap + Kramberger Acceptor removal models
  50um New Perugia Trap + Kramberger Acceptor removal models

## Slide 3
Doping profiles under confidenciality rules
Simulation Setup:
Red Pulsed Laser: 670 nm, 10 mm spot, 50W/cm2, 200 ps,
BackIllumination at P1 Right
FrontIllumination aligned with P1 Right
IR Pulsed Laser: 1064nm, 30W/cm2,10 mm spot, 30W/cm2, 200 ps at P1 Right
2D detector model: 1 mm in Z direction, 5 mm in X direction,
300/50 mm in Y direction)
Inverse Low Gain Avalanche Detector
(ILGAD) cross-section
y
x
z
30 mm
50 mm
P1Right
P1Left
Sentaurus TCAD Simulation SetUp

## Slide 4
ILGAD IV Experimental
I.Vila, Update on the ILGAD characterization, RD50 Nov 22th 2016
Experimentally we see a full
depletion at the n++-p junction
(multiplication layer) around
30V and a soft behaviour in the
IV plot up to ~400 V

## Slide 5
ILGAD IV Simulation
Both ILGAD models (300 mm, 50 mm thickness) show full depletion at n++-p (multiplication layer) around 30 V, as expected.
For the 300 mm we choose 150V, 300V, 450V as bias voltage, for the 50 mm we choose 50V, 100V, 150V as bias voltage
300mm ILGAD
50mm ILGAD

## Slide 6
ILGAD 300 mm Red Laser Back Transient: Simulation shows gain (~4)
Laser 670nm (red), illuminating on P1 right strip (just in the middle), signal observed in the N electrode (cathode). Comparing ILGAD and its associated PIN (PINILGAD) the plot
shows a gain factor around 4 (model verification).

## Slide 7
ILGAD Red Laser Back Transient Experimental 300K
Experimental data illuminating the anode (back side), with a red laser (670nm) in the P1 Right strip
I.Vila, Update on the ILGAD characterization, RD50 Nov 22th 2016

## Slide 8
ILGAD 300 um Red Laser (670nm) Back Transient P1Right
Primary Electrons
Secondary
Holes
Multiplication Onset
Q PINILGAD~2,9e-16C
Q 150V 7e-16C
Q 300V 8,24e-16C
Q 450V 9,22e-16C

## Slide 9
ILGAD Red Laser Front Transient Experimental 300K
I.Vila, Update on the ILGAD characterization, RD50 Nov 22th 2016
Experimental data illuminating the cathode (front side), with a red laser (670nm) alligned with P1 Right strip

## Slide 10
ILGAD 300mm Red Laser (670nm) Front
Multiplication Onset
Primary and Secondary hole current
Q PINILGAD~2,6e-16C
Q 150V 7e-16C
Q 300V 8,34e-16C
Q 450V 9,41e-16C

## Slide 11
LGAD IR Laser Experimental Results
I.Vila, Update on the ILGAD characterization, RD50 Nov 22th 2016
Experimental data TCT laser (IR, 1064nm) alligned with P1 Right strip

## Slide 12
ILGAD 300um IR (1064nm) Laser
Q PINILGAD~6,98e-17C
Q 150V 2,1e-16C
Q 300V 2,30e-16C
Q 450V 2,55e-16C

## Slide 13
ILGAD 50 um Red Laser (670nm) Back Transient P1Right
Q PINILGAD~2,9e-16C
Q 50V 9,21e-16C
Q 100V 1,19e-15C
Q 450V 9,21e-15C

## Slide 14
ILGAD 50 um IR (1064nm) Laser Transient P1Right
Q PINILGAD~2,47e-17C
Q 50V 2,47e-17C
Q 100V 1,02e-16C
Q 150V 1,24e-16C

## Slide 15
Radiation Damage Models
One damage model, Traps+Acceptor Removal
New Perugia Model f =1e15 up to 7,5e15 neq/cm2
Acceptor Removal
New Perugia
Modeling of radiation damage effects in silicon detectors at high fluences
HL-LHC with Sentaurus TCAD, D.Passeri et al, NIMA 824 (2016), 443-445
c=10e-16 cm-2
Radiation effects in Low Gain Avalanche Detectors after hadron irradiations, G.Kramberger et al., JINST 2015 10 P07006

## Slide 16
LGAD 300 um RedLaserBack 300K Irradiation P1 Right
Fluence n/cm2 | Charge P1 Right ILGAD (fC) | % of reduction
NoIrrad | 8,24e-1 | -
1e14 | 5,26e-1 | 63,8%
1e15 | 2,79e-1 | 33,8%
7,5e15 | 6,69e-2 | 8,1%

## Slide 17
LGAD 300 um IR Laser 300K Irradiation P1 Right
Fluence n/cm2 | Charge P1 Right ILGAD (fC) | % of reduction
NoIrrad | 2,29e-1 | -
1e14 | 1,37e-1 | 59,8%
1e15 | 6,03e-2 | 26,3%
7,5e15 | 3,22e-3 | 1,4%

## Slide 18
LGAD 50 um RedLaserBack 300K Irradiation P1 Right
Fluence n/cm2 | Charge P1 Right ILGAD (fC) | % of reduction
NoIrrad | 1,45 | -
1e14 | 7,52e-1 | 51,8%
1e15 | 2,91e-2 | 20,1%
7,5e15 | 2,4e-1 | 16,5%

## Slide 19
LGAD 50 um IR Laser 300K Irradiation P1 Right
Fluence n/cm2 | Charge P1 Right ILGAD (fC) | % of reduction
NoIrrad | 1,23e-1 | -
1e14 | 5,38e-2 | 43,7%
1e15 | 2,48e-2 | 20,1%
7,5e15 | 1,45e-3 | 1,1%

## Slide 20
Conclusions
The ILGAD model shows reasonable agreement with experiments (experimental results available are for a similar model, no exactly the same).
The timing behavior (rising edge) at the central right anode strip shows no dependence with radiation
The gain and signal general behaviour under irradiation is similar to the LGAD as expected
As expected, the 50 mm device shows better behaviour under radiation

## Slide 21
Thanks for your attention
fpalomo@us.es