## Slide 1
F2D2:
the CEA Dipole Model
for the FCC
CEA: E. Rochepault, V. Calvelli, M. Durante, H. Felice, P. Mallon, P. Manil, J.F. Millot, G. Minier, J.M. Rifflet, L. Ramos-Vieira
CERN: S. Izquierdo Bermudez, D. Tommasini, J. Fleiter
27/06/2019
F2D2 =
FCC Flared-ends Dipole Demonstrator
TM & © Lucasfilm Ltd.
All Rights Reserved

## Slide 2: Strong Interaction with Magnet Programs
[1] M. Segreti et al., “2D and 3D Design of the Block-coil Dipole Option for the Future Circular Collider”, IEEE TAS, 2019
[2] See “Evolution of the block-coils design”, this conference
ECC block-coil design [1-2]
16T Conceptual design
Double aperture
CEA-CERN Program
CERN Programs
F2D2 short model [3]
Design/fabrication at CEA
Test at CERN
Single aperture
Same coil design as ECC
[3] H. Felice et al. “F2D2: a Block-coil Short Model Dipole Toward FCC”, IEEE TAS, 2019
SMC models
Technology development
Conductor qualification
ERMC/RMM models [4,5]
  16T magnet R&D
[4] S. Izquierdo et al., “Design of ERMC and RMM, the Base of the Nb3Sn 16 T Magnet Development at CERN”, IEEE TAS, 2017
[5] See “Mechanical validation of the support structure of the eRMC and RMM, the 16-T R&D magnets for the FCC”, this conference
EPFL-CERN Program
R&D on jonction technology [6-7]
[6] M. Kumar et al. “Preliminary Tests of Soldered and Diffusion-Bonded Splices Between Nb3Sn Rutherford Cables for Graded High-Field Accelerator Magnets”, IEEE TAS, 2019
[7] See “Soldered and diffusion-bonded splices between Nb3Sn Rutherford cables for graded high-field accelerator magnets “”, this conference

## Slide 3: 2D Magnetic Design - Finalized
Maximize central field with margins:
Harmonics representative of an accelerator magnet:
Nominal Current Inom | 10378 A
Short sample current Iss | 12118 A
Bore field By0 at Inom (Iss) | 15.54 (17.81) T
Peak Field at Inom (HF/LF) | 16.20 / 11.85 T
Peak Field at Iss (HF/LF) | 18.58 / 13.62 T
Loadline Margin at Inom (HF/LF) | 14.0 / 15.4 %
Stored Energy Inom | 1.4 MJ/m
+/- 3 units
15 units
Today:
1200 A/mm2
Tomorrow:
1500 A/mm2

## Slide 4: 2d Mechanical Design - Finalized
89 MPa
<150 MPa
0.6 mm interference
Post-Coil
Contact pressure
σ Von Mises
Provide coil-pole contact during nominal operation
Keep peak stress below (reversible) degradation limits
V4.8.14a
10.3 kA, 15.5 T
197 MPa
<200 MPa
144 MPa
<150 MPa
6 MPa
1.9 K

## Slide 5: 2d Magneto-Mechanical Design - Finalized
Field map B(x,y)
Stress map
S(x,y)
ISS limit
= Ic(Bmax)
Slimit
= 150 MPa
Traditional approach

## Slide 6: 2d Magneto-Mechanical Design - Finalized
Chart: Interference [mm]
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1 | 1.2 | 1.6
Current limit | 95.8333 | 100 | 100 | 99.1667 | 98.3333 | 97.5 | 94.1667 | 85.8333
Nominal current | 86
Coil in contact | 8 | 11 | 23 | 44 | 73 | 98 | 100 | 100
Coil in contact at Nominal | 100
Field map B(x,y)
Stress map
S(x,y)
Ic(B,S) for a cable [8]
Map of Ic reduction Ic(x,y)
Stress induced current limit of the magnet [9]
short sample
Trade-off on the pre-stress (interference):
Minimize Ic reduction
Provide sufficient pre-stress
At nominal current :
Negligible Ic reduction  Ilimit = 99% Iss
100 % coil in contact with the post
[8] See “Electro-mechanical properties of Nb3Sn conductors for application to high-field magnets”, this conference
[9] E. Rochepault et al., “Current Limits in Nb3Sn Superconducting Magnets Considering Magnetic Field and Stress”, submitted to IEEE TAS
ISS limit
= Ic(Bmax)
Slimit
= 150 MPa

## Slide 7: 2D Quench Protection - Ongoing
Quench Study using Comsol
Protection Criteria (same as ECC):
Every coil has a quench heater
Detection delay = 20 ms
Detection voltage = 5 mV
Heater activation delay = 20 ms
Max hot spot temperature = 350 K
Max to ground = 1200 V
Model Hypotheses:
Adiabatic Regime
Cryocomp material database
Magnetoresistivity included
Transverse+longitudinal propagations considered
Case study : QH HF1+HF3 off
 Magnetic, electrical, thermal models validated

## Slide 8: Preliminary CAD Design - Ongoing
Turn-by-turn coil model
 Define paths for the leads
3. Coil fabrication tooling
 Winding + reaction + splicing + impregnation
 Study compatibility with the fabrication process
2. Coil components
 Study concepts for external joints
Winding
Splicing
(external)
Turn-by-turn coil model
 External joints option
 Define path for cable exits

## Slide 9: Winding Mockups - Finalized
Winding trials with SMC-11T cable:
A:  Hard-way only
 1 layer jump shim
B:  Easy-way + Hard-way
 2 layer jump shims
2 options for cable exits:

## Slide 10: 3D Magnetic design - Finalized
3D simplified Opera FEM:
  Central field:
    Magnetic Length = 1042 mm
    Uniform field region (±1%) = 249 mm
  Field in critical areas:
    Peak field in straight section
    Field in the layer jumps < 14 T
Preliminary CAD model of the coils
V4.8.14

## Slide 11: 3D Mechanical Design - Ongoing
V4.8.15
Preliminary CAD model of the structure
3D simplified Ansys FEM:
  Optimize the transverse preload
  Stay below the stress limits:
    Coil
    Components

## Slide 12: 3d Mechanical Design - Ongoing
68 MPa
0.6 mm interference
Post-Coil
Contact pressure
σ Von Mises
Verified consistency with 2D model at z=0
Coil peak stress within targets at z=0
V4.8.15e
10.3 kA, 15.5 T
200 MPa
140 MPa
0 MPa
1.9 K

## Slide 13: 3D Mechanical Design - Ongoing
68 MPa
<150 MPa
200 MPa
~200 MPa
147 MPa
<150 MPa
σ Von Mises
Coil
233 MPa
~230 MPa
163 MPa
<200 MPa
σ Von Mises
Peak stress in coil and critical components within targets
Next step: optimize longitudinal pre-load
112 MPa
<480 MPa
Yoke
X-Pad
Shell

## Slide 14: Conclusion 1/2
Goal: Demonstrate some key concepts for FCC block-coil dipoles:
     Grading between blocks
     Joint technology
How?
   Relying on proven technology:
    Block-coil
    Bladders and keys structure
  Using state of the art conductors
   Developing engineering solutions for joints
    2 proposed solutions: internal and external
    External joints selected to reduce the risks
    Room to implement internal joints
With today’s state of the art conductors:
    15.5 T achievable at 14 % margin
    ~18 T at short sample

## Slide 15: Conclusion 2/2
Status:
   Integrated magnetic and mechanical design:
    2D magnetic + 2D mechanical completed
    Protection ongoing
    3D magnetic completed, 3D mechanical ongoing
   Engineering design:
    Conceptual design of the coil ends and structure finalized
    Technical solution validated with mock-ups
   Challenging magnet!
Future plans: preserve complexity and mitigate risks
  1st stage: Proof-of-concept graded racetrack coils
       Assembly and test in the F2D2 structure
  2nd stage: F2D2 graded flared-end coils
         Assembly and test of the final F2D2 magnet

## Slide 16
Backup Slides

## Slide 17: Grading concept in Block-coils
2D: “grading” needed for FCC [3]
2 cable sizes, same current
Optimizing the current density
Compact coils = less conductor
High Field “HF” blocks, low current density
Low Field “LF” blocks, high current density
3D: need “joints” between the cable grades
Internal joints explored within EPFL-CERN Program
External joints explored at CEA
3D integrated design
CAD
Magnetic
Mechanical
HF
LF

## Slide 18: V1.1.1: from double to single aperture
ECC double aperture
Translation in a single aperture
97 mm
interbeam
100 mm
Ø576 mm
Ø770 mm
 15,8 T @ 86 %
Peak stress: 186 MPa
Min contact : -3 MPa
Peak stress: 193 MPa
Min contact : 36 MPa
 16,1 T @ 86 %
0 mm
interbeam

## Slide 19: Main Design Features
Rectangular Block-coils
Shell-based structure with Bladders&Keys
Conductor with present performances
Nominal Current Inom | 10378 | A
Short sample current Iss | 12118 | A
Bore field at Inom (Iss) | 15.54 (17.81 ) | T
Peak Field at Inom (HF/LF) | 16.20 / 11.85 | T
Peak Field at Iss (HF/LF) | 18.58 / 13.62 | T
Loadline Margin at Inom (HF/LF) | 14.0 / 15.4 | %
Stored Energy Inom | 1.4 | MJ/m

## Slide 20: Parameter table
Parameter | Initial (Clément) V1 |  | Updated (Jerôme) |  | Proposed v4 |  | Unit
 | HF | LF | HF | LF | HF | LF | 
Strand diameter | 1.1 | 0.7 | 1.1 | 0.7 | 1.1 | 0.7 | mm
Number of strands | 21 | 34 | 21 | 34 | 21 | 34 | -
Unreacted width | 12.47 | 12.47 | 12.310 | 12.579 | 12.579 | 12.579 | mm
Unreacted thickness | 1.94 | 1.23 | 1.969 | 1.253 | 1.969 | 1.253 | mm
Reacted width | 12.6 | 12.6 | 12.433 | 12.705 | 12.74 | 12.74 | mm
Reacted thickness | 2.00 | 1.27 | 2.028 | 1.291 | 2.06 | 1.31 | mm
Copper/non-Copper ratio | 0.8 | 2.0 | 0.8 | 2.0 | 0.8 | 2.0 | -
Insulation thickness | 0.15 | 0.15 | 0.15 | 0.15 | 0.15 | 0.15 | mm
Bare cable compaction | 11.8 | 12.0 | 10.5 | 10.5 | 10.5 | 10.5 | %
Packing factor | 85.4 | 88.2 | 85.9 | 86.6 | 84.9 | 87.5 | %
Pitch angle | 15 | 15 | 16.5 | 16.5 | 16.5 | 16.5 | °
Transposition pitch | 93 | 93 | 83.1 | 84.9 | 84.0 | 84.0 | mm

## Slide 21: Cable Dimensions V4
 |  | HF: 1.1mmx21 strands |  | LF: 0.7mmx34 strands |  | 
Parameter | Unit | Thick. | Width | Thick. | Width | Source
Bare Virgin | μm | 1969 | 12579 | 1253 | 12579 | Cabling formulas
Insulation thick. | μm | 150 | 150 | 150 | 150 | ECC spec
Room for expansion during reaction | % | 4.6 | 1.3 | 4.5 | 1.3 | Bare reacted/ virgin
Insulated Reacted | mm | 2.36 | 13.04 | 1.61 | 13.04 | Rounded values
Cable does not exist, baseline defined as:
  Thickness compaction after cabling: 9 to 12 %  baseline 10.5 %
  Expansion during reaction  ECC baseline: +3 % thickness / +1 % width
  Insulation  ECC baseline: 150 µm
Strategy: fixed insulated reacted cable dimensions for the CAD design
  Baseline cable with increased room for expansion
   compensation of thicker cables
  Insulation used to compensate thinner cables

## Slide 22: Integrated 2D Magnetic and Mechanical Optimization
Magnetic
Mechanical
V4.1.1
+ F2D2 Cable V4
V1.1.1
ECC 2017 design single aperture
V4.4.1
+ Coil position from ECC 2018
V4.4.3
Mechanical optimization
V4.4.n
Magnetic optimization
Geometry transfer
V4.4.2
Structure optimized for harmonics
Non ferromagnetic pad
Ferromagnetic filler

## Slide 23: Insulated Reacted Cable for the CAD
Uncertainty due to cabling R&D
1st margin to compensate the bare cable
Bare Virgin Cable
Nominal 150 μm,
2nd possible margin
______________________
Fixed Ins. React. Th. for the CAD design
Insulation
Bare Reacted Cable
POLE
RAIL
SHIM
3rd margin: variable shims (insulated fiberglass)
Fixed value in the nominal drawings
Free value in the as-built drawings

## Slide 24: Internal Vs External
 | Internal joints | External joints
Potential show-stoppers | margin at high field room for operations (placing parts, splicing) | room for support room for operations (placing parts, splicing)
Clues that it can work | Low joint resistances in FRESCA samples and for EPFL joints | Concept similar to FRESCA2 endshoes
End harmonics | Compact ends possible | Ends longer « naturally » more homogeneous
Axial loads | Behavior under Lorentz forces ? (detachment, motions…) | Impact of pre-load ? (sharp wedges, relative motion…)
Layer jumps | No LF layer jump | Need additional room for LF layer jump

## Slide 25: 1st Solution for F2D2: Internal Joints
Ideal solution for FCC
Concepts:
  Nb3Sn-HF to Nb3Sn-LF joint
  Performed in an end-spacer
Winding layout:
  HF Double-layer pancakes + layer jump
  LF single layer pancakes
Courtesy C. Lorin
HF block
LF block
Joints
High technical risk for F2D2
High risk for the schedule
Status:
  Joints under development by EPFL-SPC (See presentation “R&D on Nb3Sn cable splices”, P. Bruzzone and Poster “Preliminary investigations of Rutherford cable splicing techniques for high field accelerator magnets”, M. Kumar)
    Several explored technical solutions
    Test on joints in Sultan
Engineering implementation in coils remains an open question

## Slide 26: Alternative solution for F2D2: External Joints
Decoupling grading and joints for the demonstrator
Goal:
  Minimize risks in coil fabrication
  Each coil heat-treated and impregnated individually
  Use a known joint technique outside of the coil
CAD Geometric investigation ongoing:
  Large footprint outside of the coil
  Routing and supporting the cable
5
5
21
21
10
10
22
22
1 coil = 1 HF double pancake
+ 1 LF double pancake
HF
blocks
______________________
1 pole = 2 coils
LF blocks

## Slide 27: Alternative solution for F2D2: External Joints
HF double-layer pancake with layer jump in the pole

## Slide 28: Alternative solution for F2D2: External Joints
2. Routing of the HF leads in an “inter-coil wedge”  take advantage of flared ends

## Slide 29: Alternative solution for F2D2: External Joints
3. LF double-layer pancake with layer jump in the end-spacer
4. LF leads in the end-shoe
5. Heat treatment and impregnation of the coil
6. Joints Nb3Sn-NbTi outside the coil in the inter-coil wedges
External
joints
1 coil

## Slide 30: Alternative solution for F2D2: External Joints
7. Same concept for the other coils
1 pole

## Slide 31: Alternative solution for F2D2: External Joints
8. Assembly of the coils
9. NbTi-NbTi joints to connect LF and HF leads
1 Dipole