## Slide 1
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
Task4.6: Measurements on cryogenic
beam vacuum system prototype
1
2
3
4
5
L.A. Gonzalez,1, 2 M. Gil Costa,3, 2 P. Chiggiato,2 V. Baglin,2 C. Garion,2 R.Kersevan,2 S. Casalbuoni,4 E. Huttel,4 I. Bellafont2,5 and F. Perez5

## Slide 2: FCC-hh Beam Screen
 | FCC-hh | LHC
Energy collision [TeV] | 100 | 14
Perimeter [km] | 100 | 28
Dipole field [T] | 16 | 8.3
Arc SR Photon Flux (E above 4 eV)* [ph/s/m] | 1.48x1017 | 4.8x1016
Arc SR Photon Flux [ph/s/m] | 1.7x1017 | 1.0x1017
SR Heat load [W/m] | 35.4 | 0.22
SR Critical Energy [eV] | 4269 | 44
FCC-hh BS has been redisigned in order to fulfill:
-Higher cooling capacity
-Higher pumping speed
also
-Due to the high SR power power deposited on it, the working temperature needs to be rised in the range 20-40K (FCC-hh arcs) vs 4-20K (LHC arcs)
Synchrotron radiation (SR) parameters at FCC-hh bending magnets
 | FCC-hh | LHC
BS Working temperature[TeV] | 20-40 | 4-20
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
1
*FCC Conceptual Design Report. Volume 3: The Hadron Collider

## Slide 3: FCC-hh Beam Screen
S. Steel
Side View
Front View
Side View
Front View
Cu
SR
Coolant
Coolant
Cu
Cu
SR
Coolant
Coolant
Tip
Reflection
Sawtooth
Absorption
Pumping
holes
Pumping
holes
First Design
Baseline Design
FCC-hh Beam Screen
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
2
For full description of BS evolution and functionality please review:
Francis Perez - 24 jun. 2019 11:30
Ignasi Bellafont - 26 jun. 2019 8:30

## Slide 4: FCC-hh Beam Screen
S. Steel
Side View
Front View
Side View
Front View
Cu
SR
Coolant
Coolant
Cu
Cu
SR
Coolant
Coolant
Tip
Reflection
Sawtooth
Absorption
Pumping
holes
Pumping
holes
First Design
Baseline Design
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
2
2 m long FCC-hh BS prototypes have been manufactured in faithful compliance with such designs.
The samples where irradiated to validate their performance under significant levels of SR flux and power and benchmark simulations techniques.
As a first step of the experimental campaign, the experiments were performed at RT on baked samples.
Experimental Samples

## Slide 5: Samples: FCC-hh Beam Screen Prototypes
Prototype #1 July- Oct ‘17
Prototype #2 Jan- May ‘18
Prototype #3 June-Aug‘18
Experimental Samples
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
4
#1: Validation of temperature profile and validity of photon reflector.
#2: #1 + Cold sprayed electrode for photoelectron current measurements*. Isolation to sample performed by ceramic layer.
#3: Surface treatments as for baseline. Updated internal screen and pumping slots. Sawtooth profile substituted reflector. LASE surface at top and bottom.
*Luis Gonzalez- 10 April. 2018

## Slide 6: Samples: FCC-hh Beam Screen Prototypes
Prototype #1 July- Oct ‘17
Prototype #2 Jan- May ‘18
Prototype #3 June-Aug‘18
#1: Validation of temperature profile and validity of photon reflector.
#2: #1 + Cold sprayed electrode for photoelectron current measurements*. Isolation to sample performed by ceramic layer.
#3: Surface treatments as for baseline. Updated internal screen and pumping slots. Substitution Reflector for Sawtooth. LASE surface at top and bottom.
Experimental Samples
- Irradiation on Tip
- Irradiation on Tip
-Irradiation on Sawtooth
-Irradiation on LASE
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
5
*Luis Gonzalez- 10 April. 2018

## Slide 7
KARA
(KArlsruhe Research Accelerator)
The FCC-hh’s photon spectrum and linear power are reasonambly reproduced in KARA, even at nominal beam energy
FCC-hh Beam Screen -> Samples
Experiment at KARA
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
6

## Slide 8: The Setup: BESTEX
BESTEX (Beam Screen Testbench Experiment) is an experimental instrument designed to study SR related effects on non-leak tight samples under UHV.
The SR photon beam originated at KARA’s bending magnet is collimated so as to irradiate the samples on the selected region.
Experiment at KARA-BESTEX
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
7

## Slide 9: The Setup: BESTEX
After collimation :
83% of Photon Flux Cropped
69% of Photon Power Cropped
 | KARA | FCC-hh
SR Flux | 8.7E+16ph/s | 1.7E+17 ph/s
SR Power | 32W/m | 35.4 W/m
Angle | 18mrad | <2 mrad
Ec | 6.2KeV | 4.2KeV
BESTEX (Beam Screen Testbench Experiment) is an experimental instrument designed to study SR related effects on non-leak tight samples under UHV
The SR photon beam originated at KARA’s bending magnet is collimated so as to irradiate the samples on the selected region.
Experiment at KARA-BESTEX
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
8

## Slide 10: The Setup: BESTEX
Reflected photons
towards photon cup
Several gauges allow to obtain relevant data on PSD, reflectivity, heat loads and photoelectron generation.
A photon cup equipped with a biased electrode and placed downstream the photon direction allows to perform reflectivity studies.
Experiment at KARA-BESTEX
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
9

## Slide 11
The Setup: BESTEX
Several gauges allow to obtain relevant data on PSD, reflectivity, heat loads and photoelectron generation.
A photon cup equipped with a biased electrode and placed downstream the photon direction allows to perform reflectivity studies.
A chimney connection allows to explore the molecular desorption yields from the inner walls of the samples as they are irradiated (PSD studies).
Experiment at KARA-BESTEX
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
10

## Slide 12
PSD results
-At low doses, the molecular yield of Prototype #2 is one order of magnitude higher than for Prototype #1.
-At higher doses the values for prototype #2 remain always higher than for prototype #1 (x3 at 2E22 ph/m).
-Such effect is ascribed to the high PSD yields of cold sprayed Cu and ceramics in Prototype #2.
-A large amount of photons are reflected towards the inner chamber of the BS. For prototype #2, those reflected photons play an extremely relevant role. This effect was previously foreseen by simulations.*
-The large photon reflectivity towards the inner chamber is due to
the limitations to manufacture a perfectly shrap tip.
- Large photon reflectivity enhances electron cloud developement.
PSD Results
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
11
  Prototype #1
  Prototype #2
  Prototype #3
*FCC Week’19. I. Bellafont et al

## Slide 13
PSD results
*FCC Week’19. I. Bellafont et al
PSD Results
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
12
-At low doses, the molecular yield of Prototype #2 is one order of magnitude higher than for Prototype #1.
-At higher doses the values for prototype #2 remain always higher than for prototype #1 (x3 at 2E22 ph/m).
-Such effect is ascribed to the high PSD yields of cold sprayed Cu and ceramics in Prototype #2.
-A large amount of photons are reflected towards the inner chamber of the BS. For prototype #2, those reflected photons play an extremely relevant role. This effect was previously foreseen by simulations.*
-The large photon reflectivity towards the inner chamber is due to
the limitations to manufacture a perfectly shrap tip.
- Large photon reflectivity enhances electron cloud developement.
  Prototype #1
  Prototype #2
  Prototype #3

## Slide 14
PSD results
-At low doses, the molecular desorption yields of Prototype #3, when irradiating the sawtooth profile, is one order of magnitude lower than for prototype #1.
-Such effect is ascribed to the high photon absorption capacity of the sawtooth profile.
-At doses higher than E20 ph/m the molecular desorption yield of prototype #1 and prototype #3 are similar.
-Such result has an important effect on the reduction of the conditioning time.
PSD Results
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
13
  Prototype #1
  Prototype #2
  Prototype #3

## Slide 15
PSD results
-The molecular desorption yield of Prototype #3, when irradiating the LASE surface, is considerably lower than for the rest of the irradiated surfaces
-Such effect is in good agreement with the low reflectivity and low photoelectron yields associate to the very rough LASE surfaces*
- Due to the low reflectivity associated to the previously irradiated sawtooth structure, preconditioning of the LASE surface has been assumed to b negligible.
-Such assumption is confirmed by the flat part of the curve at low doses, typical of newly irradiated surfaces.
-LASE treatment provides both low PSD yields and low SEY, with respect to standard Cu surfaces
*PRST- Photo Reﬂectivity and Photoelectron Yield from Copper Technical Surfaces. E. La Francesca et al - Submitted
PSD Results
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
14
  Prototype #1
  Prototype #2
  Prototype #3

## Slide 16
PSD results
PSD Results
7
[1] Yusuke Suetsugu et al; Test Fabrication of a Copper Beam Duct for KEK B-Factory
[2] D. Brandt et al; CAS CERN Accelerator School
[3] R. Calder et al; Synchrotron Radiation induced gas desorption from a prototype of the
LHC beam screen prototype at cryogenic temperatures
[4] Herbeaux et al; Photon stimulated desorption of an unbaked stainless steel chamber by 3.75 KeV critical energy photons
[5] M. Ady; PhD Thesis
[6] O. Grobner et al; Gas desorption form an OFHC copper Vacuum chamber by synchrotron radiation photons
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
15
SS |  |  | Cu |  | 
 | Surface | [ref] |  | Surface | [ref]
0.99 | Unbaked/RT Ec=3.75 KeV | [4] | 0.88 | Baked/RT Ec=26.3 KeV | [1]
0.54 | Baked/RT Ec=4 KeV | [5] | 0.61 | Unbaked/RT Ec=486 eV | [2]
 |  |  | 0.32 | Unbaked/77K Ec=50 eV | [3]
 |  |  | 0.88 | Baked/RT Ec=3.75 KeV | [6]
SS |  |  | Cu |  | 
 | Surface | [ref] |  | Surface | [ref]
0.99 | Unbaked/RT Ec=3.75 KeV | [4] | 0.88 | Baked/RT Ec=26.3 KeV | [1]
0.54 | Baked/RT Ec=4 KeV | [5] | 0.61 | Unbaked/RT Ec=486 eV | [2]
 |  |  | 0.32 | Unbaked/77K Ec=50 eV | [3]
 |  |  | 0.88 | Baked/RT Ec=3.75 KeV | [6]
  Prototype #1
  Prototype #2
  Prototype #3
SS
Cu

## Slide 17
SS |  |  | Cu |  | 
 | Surface | [ref] |  | Surface | [ref]
0.99 | Unbaked/RT Ec=3.75 KeV | [4] | 0.88 | Baked/RT Ec=26.3 KeV | [1]
0.54 | Baked/RT Ec=4 KeV | [5] | 0.61 | Unbaked/RT Ec=486 eV | [2]
 |  |  | 0.32 | Unbaked/77K Ec=50 eV | [3]
 |  |  | 0.88 | Baked/RT Ec=3.75 KeV | [6]
SS |  |  | Cu |  | 
 | Surface | [ref] |  | Surface | [ref]
0.99 | Unbaked/RT Ec=3.75 KeV | [4] | 0.88 | Baked/RT Ec=26.3 KeV | [1]
0.54 | Baked/RT Ec=4 KeV | [5] | 0.61 | Unbaked/RT Ec=486 eV | [2]
 |  |  | 0.32 | Unbaked/77K Ec=50 eV | [3]
 |  |  | 0.88 | Baked/RT Ec=3.75 KeV | [6]
PSD Results
of Prototype #1 decreases with the same rate as SS at similar Ec under the same surface conditions
of Prototype #3 (sawtooth) decreases with a rate much lower than for Cu at the same surface conditions and similar Ec. Closer to Cu at 77K and Ec = 50eV
of Prototype #3 (LASE) decreases with an extremely low rate.
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
16
7
  Prototype #1
  Prototype #2
  Prototype #3

## Slide 18
Beam
Reflectivity Studies
Experimental Equipment
RI=
Reflectivity Results
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
17

## Slide 19: Experiment at KARA
Reflectivity Studies
Experimental Equipment
1
1
2
2
Base Line
First
Prototype
Reflectivity Studies
Experimental Equipment
Reflectivity Results
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
Reflectivity measurements show a reduction of photons reflected downstream the sample in good agreement
with a reduction of PSD yield due to photon absorption
18
RI=

## Slide 20: Summary and Conclusions
Molecular desorption yields have been measured for:
  Stainless steel reflector tip on prototype #1
  Stainless steel reflector tip on prototype #2
  Cu Sawtooth profile on prototype #3
  Cu LASE Surface on prototype #3
The decreasing rate of molecular desorption yield with the dose accumulated on protoype #1 is similar to that previously measured at similar Ec on leak tight vacuum chambers
Molecular yields on prototype #2 (cold sprayed electrode and ceramics). have been found to be considerably higher than for Prototype #. 1This suggests that a large amount of photons are reflected towards the inner chamber of the BS when irradiating the tip. Such experimental results are in good agreement with previous simulation results.
Sample #3 shows a satisfactory behavior under SR in terms of vacuum when irradiating the sawtooth profile and confirms the strategy of changing from reflection to absorption of photons.
Photon cup measurements showed a lower reflectivity for the sawtooth profile than for the reflector tip. Such a result is in good agreement with the reduction of the molecular desorption yield due to an increase of photon absorption by the sawtooth profile.
The molecular desorption yield of LASE, in the geometry of prototype #3, shows a drastic reduction with respect to the sawtooth profile.
Measurements on samples at LN2 temperature are to be performed in the near future.
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA
19
  Prototype #1
  Prototype #2
  Prototype #3

## Slide 21
Thank You
Luis Gonzalez
CERN TE-VSC
FCC Week 2019 June 26th
Photodesorption studies on FCC-hh Beam Screen Prototypes at KARA