## Slide 1: Falcon Dipole The INFN dipole model for the FCC
R. U. Valente
G. Bellomo, A. Bersani, P. Fabbricatore, S. Farinon, S. Mariotto, A. Pampaloni, M. Sorbi, M. Statera

## Slide 2: Outline
Introduction
Electromagnetic design
Quench protection
Mechanical design
Conclusions

## Slide 3: Introduction
Who?
  Agreement between CERN and INFN
What?
  Construction of a demonstrator/model cos-theta dipole able to reach 14 T
When?
  Next 5 years
Where?
  INFN-LASA & INFN Genova (Italy)
Why?
  Milestone technology for the FCC main dipole

## Slide 4: Electromagnetic design - requirements
General magnet characteristics:
  Cos-theta dipole, 1.5 m long
  One aperture of Ø 50 mm
  Winding type: 1 double pancake
Rutherford cable:
  Nb3Sn, JC (@ 4.2K, 16T) = 1500 A/mm2
  Minimum bending radius 10 mm
Magnet performance:
  14 T bore field, with a margin ≥ 14%
  All high order harmonics < 40 units

## Slide 5: Electromagnetic design - cable
Rutherford Cable Parameters | 
Superconducting material | Nb3Sn
Jc @4.2K,16T (A/mm2) | 1500
Filament diameter (μm) | 20
Cu/non-Cu | 1
Strand number | 34 (2x17)
Strand diameter (mm) | 1.1
Height (mm) | 19.8
Inner width (mm) | 1.892
Outer width (mm) | 2.065
Keystone angle | 0.5°
Twist pitch (mm) | 100
Insulation thickness (mm) | 0.15
19.8 mm
2.065 mm
1.892 mm
34 strands
Ø 1.1 mm

## Slide 6: Electromagnetic design - coils
Minimum bending
radius
9.7 mm
Input Magnet Parameter | 
Aperture number | 1
Aperture radius (mm) | 25
Current (A) | 25000
Operation temperature (K) | 1.9
Blocks | Min. wedge thickness (mm)
1-2 | 1.08
2-3 | 1.35
4-5 | 1.77
FEM analysis results (ROXIE 10.2) | 
Bore field (T) | 14
Minimum margin | 14% (block 3)
Jcu (A/mm2) | 1547
Stored energy (MJ/m) | 0.68

## Slide 7: Electromagnetic design – iron yoke
Square window (180 mm x 180 mm) is needed to use bladder & keys technology
Holes (Ø 70 mm, Ø 20 mm) for the coolant system have no effect on the field quality
180 mm
180 mm
Ø 70 mm
260 mm
Ø 20 mm

## Slide 8: Electromagnetic design – field quality
Chart: Current (A)
| 1250 | 2041.7 | 2833.3 | 3625 | 4416.7 | 5208.3 | 6000 | 6791.7 | 7583.3 | 8375 | 9166.7000000000007 | 9958.2999999999993 | 10750 | 11542 | 12333 | 13125 | 13917 | 14708 | 15500 | 16292 | 17083 | 17875 | 18667 | 19458 | 20250 | 21042 | 21833 | 22625 | 23417 | 24208 | 25000
B3 | -17.798 | -17.798 | -17.798 | -17.798 | -17.797 | -17.791 | -17.752 | -17.634 | -17.305 | -16.501 | -15.339 | -14.008 | -12.621 | -11.233 | -9.888 | -8.6029 | -7.3853 | -6.2362 | -5.1554 | -4.1432 | -3.202 | -2.346 | -1.5913 | -0.93982 | -0.39002 | 0.056166 | 0.43797 | 0.74588 | 0.98616 | 1.1632 | 1.2764
B5 | -5.5527 | -5.5527 | -5.5527 | -5.5527 | -5.5527 | -5.553 | -5.5549 | -5.5602 | -5.5752 | -5.6111 | -5.6577 | -5.7058 | -5.7513 | -5.7931 | -5.8309 | -5.8647 | -5.8952 | -5.9229 | -5.9483 | -5.9718 | -5.994 | -6.0158 | -6.0379 | -6.0606 | -6.0844 | -6.1094 | -6.1345 | -6.1601 | -6.1863 | -6.213 | -6.2403
B7 | 17.15 | 17.15 | 17.15 | 17.15 | 17.15 | 17.15 | 17.151 | 17.154 | 17.163 | 17.184 | 17.217 | 17.256 | 17.3 | 17.347 | 17.395 | 17.442 | 17.489 | 17.534 | 17.579 | 17.621 | 17.663 | 17.704 | 17.743 | 17.783 | 17.822 | 17.862 | 17.901 | 17.941 | 17.98 | 18.02 | 18.06
Chart: Current (A)
| 1250 | 2041.7 | 2833.3 | 3625 | 4416.7 | 5208.3 | 6000 | 6791.7 | 7583.3 | 8375 | 9166.7000000000007 | 9958.2999999999993 | 10750 | 11542 | 12333 | 13125 | 13917 | 14708 | 15500 | 16292 | 17083 | 17875 | 18667 | 19458 | 20250 | 21042 | 21833 | 22625 | 23417 | 24208 | 25000
B9 | 1.9539 | 1.9539 | 1.9539 | 1.9539 | 1.9539 | 1.9539 | 1.954 | 1.9544 | 1.9553 | 1.9576 | 1.9612 | 1.9657 | 1.9706 | 1.9759 | 1.9813 | 1.9867 | 1.992 | 1.9972 | 2.0022 | 2.0071 | 2.0119 | 2.0165 | 2.021 | 2.0255 | 2.03 | 2.0346 | 2.039 | 2.0435 | 2.048 | 2.0526 | 2.0572
B11 | 0.92336 | 0.92336 | 0.92336 | 0.92336 | 0.92336 | 0.92337 | 0.92342 | 0.92358 | 0.92403 | 0.92513 | 0.92684 | 0.92894 | 0.93128 | 0.93378 | 0.93632 | 0.93886 | 0.94137 | 0.94382 | 0.94621 | 0.94852 | 0.95076 | 0.95294 | 0.95509 | 0.95721 | 0.95934 | 0.96149 | 0.9636 | 0.96572 | 0.96784 | 0.96999 | 0.97218
B13 | -0.68685 | -0.68685 | -0.68685 | -0.68685 | -0.68685 | -0.68686 | -0.6869 | -0.68701 | -0.68735 | -0.68816 | -0.68943 | -0.691 | -0.69274 | -0.6946 | -0.69649 | -0.69838 | -0.70025 | -0.70207 | -0.70384 | -0.70556 | -0.70723 | -0.70885 | -0.71045 | -0.71203 | -0.71361 | -0.71521 | -0.71678 | -0.71835 | -0.71993 | -0.72153 | -0.72316
Harmonics @ 25 kA | units
b3 | 1.3
b5 | -6.2
b5 | 18
b9 | 2
The field quality has been optimized keeping constructive parameters within safe limits:
Minimum wedge thickness > 1 mm
Minimum bending radius around 10 mm
Minimum steel pad thickness around 20 mm
(superconductor magnetization not considered)

## Slide 9: Electromagnetic design – different conductor performances
EuroCirCol target cable
(actually reached only in short units)
Conductor in procurement
(value requested in specs)
JC (@ 4.2K, 16T) = 1200 A/mm2 |  | 
B0 | margin | Current (kA)
13.3 T | 14% | 23.7
14 T | 9.5% | 25.0
15.4 T | 0% | 27.8
JC (@ 4.2K, 16T) = 1500 A/mm2 |  | 
B0 | margin | Current (kA)
14 T | 14% | 25.0
16 T | 1.3% | 28.9
16.2 T | 0% | 29.3
Conductor used to design Falcon Dipole short model
Conductor now available

## Slide 10: Quench analysis – short model protection
QUENCH
Quench heaters
(outer radius only)
Quench analysis performed with QLASA
Parameter | Value
Magnet length | 1.5 m
Dump resistor | 35 mΩ
Max ground voltage | 400 V
Heater delay | 40 ms
Voltage threshold | 100 mV
Parameter | Value
Magnet length | 1.5 m
Dump resistor | 35 mΩ
Max ground voltage | 
Heater delay | 40 ms
Voltage threshold | 100 mV
Hot-spot temperature
175 K

## Slide 11: Quench analysis – long magnet protection
QUENCH
Quench heaters
Parameter | Value
Magnet length | 15 m
Dump resistor | 0 mΩ
Heater delay | 40 ms
Voltage threshold | 100 mV
Hot-spot temperature
322 K
Quench analysis performed with QLASA

## Slide 12: Mechanical design – requirements
Coil in compression up to nominal field
Stress in the conductor
  Room temperature, < 150 MPa
  Cryo temperature (1.9 K), < 200 MPa
Stress on mechanical structure < yield strength (see Table below)
Material | Stress limit (MPa) |  | E (GPa) |  | ν | α (mm/m)
 | RT | 1.9 K | RT | 1.9 K |  | RT → 1.9 K
Austenitic steel (316LN) | 350 | 1050 | 193 | 210 | 0.28 | 2.8
Al7075 | 480 | 690 | 70 | 79 | 0.3 | 4.2
Coil Radial dir. Azimuthal dir. | 150 | 200 | 30 25 | 33 27.5 | 0.3 | 3.1 3.4
Ferromagnetic iron | 230 | 720 | 213 | 224 | 0.28 | 2.0
Ti6Al4V | 800 | 1650 | 115 | 126 | 0.3 | 1.7

## Slide 13: Mechanical design - ANSYS model
AL alloy shell (50 mm thick)
Iron yoke (Ø 700 mm)
Cold mass: Ø 800 mm
Steel pads: 180 mm x 180 mm
Ø 70 mm
Ø 20 mm
Stainless steel pad
Titanium pole
Copper wedge
Conductor
Horizontal key (interference: 0.1 mm)
Vertical key (interference)

## Slide 14: Mechanical design - ANSYS model
Simulation steps
Assembly  keys insertion
Cool down  thermal contractions
Energization  Lorentz forces in the conductor element
Load cases | Bore field | Margin | Required vertical key interference
Nominal field | 14 T | 14% | 0.5 mm
Cable in procurement short sample | 15.5 T | 0% | 0.6 mm
EuroCirCol cable short sample | 16 T | 0% | 0.7 mm

## Slide 15: Mechanical design – contact pressure
ASSEMBLY
COOL DOWN
ENERGIZATION
Contact pressure [MPa]
Gap (where contact pressure = 0 MPa) < 3.2 μm
14 T
Key interference 0.5 mm
Contact pressure [MPa]
15.5 T
Key interference 0.6 mm
Gap (where contact pressure = 0 MPa) < 11.3 μm
Contact pressure [MPa]
16 T
Key interference 0.7 mm
Gap (where contact pressure = 0 MPa) < 10.6 μm

## Slide 16: Mechanical design – Von Mises stress in conductors
ASSEMBLY
COOL DOWN
ENERGIZATION
VM stress [MPa]
σVM,max = 72.4 MPa
σVM,max = 172 MPa
σVM,max = 177 MPa
VM stress [MPa]
σVM,max = 86 MPa
σVM,max = 192 MPa
σVM,max = 201 MPa
VM stress [MPa]
σVM,max = 99.5 MPa
σVM,max = 210 MPa
σVM,max = 209 MPa
14 T
Key interference 0.5 mm
15.5 T
Key interference 0.6 mm
16 T
Key interference 0.7 mm

## Slide 17: Conclusions
We designed a model dipole for FCC (named Falcon Dipole) with the goal of making the winding and assembly procedure as feasible as possible.
The results of our analysis satisfy the requirements:
The magnet is able to reach 14 T in the bore within the margin of 14%, using the conductor with EuroCirCol specs
In principle the same target of 14 T may be reached using the specs of the conductor under procurement, but with a reduced margin of 9.5%
All the stress in the magnet are always below the limits, in particular in the coil the maximum stress is 177 MPa at energization
Notice that:
A bore field of 16 T theoretically may be reached with the current at the ‘short sample limit’ (EuroCirCol target cable)

## Slide 18
Thank you
for
your attention

## Slide 19: Mechanical analysis – gap at pole
ASSEMBLY
COOL DOWN
ENERGIZATION
Gap [μm]
Gap [μm]
Gap [μm]
14 T
interference 0.5 mm
15.5 T
interference 0.6 mm
16 T
interference 0.7 mm