## Slide 1
A.Romanov1, J. Gutierrez1 , P.Krkotic2, J. O’Callaghan3, F. Perez2, M. Pont2, X. Granados1 , S. Calatroni4, M. Taborelli4 and T. Puig1
1 Institut de Ciència de Materials de Barcelona, CSIC, Bellaterra (Spain)
2 ALBA Synchrotron Light source, Cerdanyola del Vallés (Spain)
3 Universitat Politècnica de Catalunya, Barcelona (Spain) 4 CERN - The European Organization for Nuclear Research, Geneva (Switzerland)
-talk
REBa2Cu3O7 coated conductors as a beam screen coating:
Linking surface resistance to microstructure
BRUSSELS, BELGIUM
24 – 28 June 2019
Crowne Plaza Brussels
Le Palace
FCC
WEEK
2019

## Slide 2
Outline
REBCO CCs for beam screen coating
Linking CC´s surface resistance to microstructure
Evaluation of secondary electron yield

## Slide 3
Synchrotron radiation in FCC much higher:
100MW
Superconductors belong to only material class where
Limit the cryogenic load to 100 MW
Cu may not provide low enough surface impedance at 40-60K
Cryogenic load
Impacts
Motivation: REBCO CCs for beam screen coating

## Slide 4
REBCO coated conductors are layered structures consisting of:
Multifunctional oxides
  HTS REBa2Cu3O7-x
  Buffers that allow epitaxial growth
Flexible, metallic substrate
REBCO (1 – 3)
Buffers (0.2 – 1 )
Metallic substrate (30 - 100 )
Protective layer (Ag+Cu)
Superconductive at FCC conditions:
High customization through microstructure tailoring :
Motivation: REBCO CCs for beam screen coating
Commercially available in km length (5000 km/a).
Participating manufacturers in FCC study
Rare earth | Intrinsic PC | Artificial PC
Y | Grain boundaries | BaZrO3
Gd | Secondary phases | BaHaO3
Eu | Stacking faults | …
Dy | Point defects | 
… | … | 

## Slide 5
Outline
REBCO CCs for beam screen coating
Linking CC´s surface resistance to microstructure
Evaluation of secondary electron yield

## Slide 6
2. Linking to microstructure
FCC Cu (300 on st.st.)
Within the consortium, ALBA and UPC developed 8 GHz cavity dielectric resonator
compatible with 25mm bore 9 T magnet at ICMAB
State of the art REBCO CCs outperform Cu at 50K, 8 GHz and up to 9T
SuperOx
Bruker
Fujikura
Theva
SuperPower
Fujikura NP
SuNAM
T. Puig et al. (SUST accepted)

## Slide 7
FCC Cu (300 on st.st.)
State of the art REBCO CCs outperform Cu at 50K, 8 GHz and up to 9T
REBCO nano engineered region
REBCO pristine region
RS is microstructure dependent
2. Linking to microstructure
S. Kang, Science 311 (2006)
Microstructure of YBCO with BZO nanorods
T. Puig et al. (SUST accepted)

## Slide 8
Flux tube lattice
Equation of motion for fluxons:
Surface resistance:
S. Calatroni and R. Vaglio, IEEE Transactions on Applied Superconductivity 27, 2017
Assumptions:
Fluxon shape cannot be deformed
Rigid flux tube lattice
Depinning frequency:
2. Linking to microstructure
Classical rigid-fluxon model

## Slide 9
Overestimation of with rigid-fluxon model:
Calculated from transport values
Measured with resonator
Introducion of correction factor :
2. Linking to microstructure

## Slide 10
Correction factor depends on the microstructure of CC
2. Linking to microstructure

## Slide 11
Tsuchiya, Yoshishige, et al. "Electronic state of vortices in YBa2CuO7-x investigated by complex surface impedance measurements." Physical Review B 63.18 (2001): 184517.
Underestimation of compared to literature
2. Linking to microstructure

## Slide 12
2. Linking to microstructure
Ignore the depinning frequency derived from rigid-fluxon model:
Use as fitting parameter.
Fitted value
No correction factor needed
Matches better with literature

## Slide 13
Provider | (9T) in GHz | in GHz | in GHz
Bruker | 3.0 | 29.3 | 30.0
SuNAM | 0.9 | 19.6 | 19.0
SuperOx | 0.8 | 25.1 | 24.5
SuperPower | 1.2 | 35.4 | 35.2
Theva | 3.1 | 60.4 | 57.0
Fujikura | 3.3 | 33.9 | 34.2
Fujikura NP | 1.3 | 67.8 | 71.0
Provider |  |  | 
Bruker | 3.0 | 29.3 | 30.0
SuNAM | 0.9 | 19.6 | 19.0
SuperOx | 0.8 | 25.1 | 24.5
SuperPower | 1.2 | 35.4 | 35.2
Theva | 3.1 | 60.4 | 57.0
Fujikura | 3.3 | 33.9 | 34.2
Fujikura NP | 1.3 | 67.8 | 71.0
identified as weakness of model Gives potential to adjust model.
2. Linking to microstructure

## Slide 14
Predicted by rigid-fluxon model: Out performance of Cu by HTS CC at FCC conditions even more pronounced!
FCC Cu (300 on st.st.)
x175
Extrapolation of using rigid-fluxon model with to 1GHz and 16T:
2. Linking to microstructure

## Slide 15
Outline
REBCO CCs for beam screen coating
Linking CC´s surface resistance to microstructure
Evaluation of secondary electron yield

## Slide 16
3. Beam instability: Secondary electron yield
In untreated form not suitable for use in particle accelerators
Conditioning treatment not sufficient
Roughness of a-C decreases SEY under desired limit
Ti as adhesion and protection layer
50 nm a-C
100 nm Ti + 50 nm a-C
untreated
3.8e-3 C/mm2
150 nm Ti + 100 nm a-C
SuperPower
Thin layers of a-C and Ti decrease the SEY below threshold value 1.3.

## Slide 17
3. Beam instability: Secondary electron yield
Increase of for 150 nm Ti + 100 nm a-C not detrimental.
vs. @ 50K
FCC Cu
Uncoated
50 nm a-C
100 nm Ti + 50 nm a-C
150 nm Ti + 100 nm a-C
SuperPower

## Slide 18
Conclusions
State of the art REBCO CCs outperform Cu at 50K, 8 GHz and up to 9T
a-C (50-100 nm) and Ti (100-150 nm) capping to reduce the secondary electron yield below required limit
Increase in due to capping is not significant at 50K, 8GHz, up to 9T
Extraction of as for all CCs by means of ridig-fluxon model
Extrapolation of surface resistance to FCC conditions 1 GHz, 16 T, 50K  outperformance of Cu by CCs by two order of magnitude expected at FCC conditions

## Slide 19
Outlook: REBa2Cu3O7 coated conductors for beam screen coating
1. Characterization of CCs up to 16T:
Cylindrical dielectric resonator
Resonator configuration with (currently in development at UPC/ALBA)
Experimental system to assess 2D /3D stress maps based in optical image correlation with in situ monitoring the Ic has been finished and will be taken into operation in Q3/Q4 2019
Full evaluation of stresses accociated to new welding solution targeted
4. Mechanical tests of aC/REBCO/Steel stacks
3. Welding solutions of aC/REBCO/Steel stacks
Soldering of REBCO CCs to st. st. with delamination of superconducting layer possible in large scales
Delaminated bottom layer shows no degradation in performance
Poster 448. Coating the FCC-hh beam screen chamber with REBa2Cu3O7-x coated conductors at FCC week 2019
Compatible with
Surface impedance measurable at FCC conditions.
Wide Temp. range
Up to 16 T
 Understanding the influence of magnetic field on vortex dynamics up to 16T.
2. Evaluation of persistent currents
New cryostat with 16 T SC magnet to be installed in Q1 2020 at ICMAB.
Hall mapping measurement of CC done at ICMAB
Analyzing persistent currents will define the required aspect ratio of Cu and REBCO CC in beam screen
Construction of proof-of-concept device based on generated knowledge
Superconducting perfomance of delaminated layers still to be investigated

## Slide 20
Acknowledgement
The authors acknowledge the support and samples provided by Bruker, Fujikura, Sunam, SuperOx, SuperPower and Theva. Authors acknowledge CERN funding FCC-GOV-CC0073/1724666/KE3359, MAT2014-51778-C2 COACHSUPENERGY, 2017-SGR 1519 from Generalitat de Catalunya and COST Action NANOCOHYBRI (CA16218). ICMAB authors acknowledge the Center of Excellence award Severo Ochoa SEV2015-0496 and its Future Interdisciplinary Projects action.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 754397”. Financial support from the Spanish Ministry of Science, Innovation and Universities, through the “Severo Ochoa” Programme for Centres of Excellence in R&D (SEV-2015-0496)

## Slide 21
Thank you for your attention!