## Slide 1: Development of Nb3Sn in Japan
T. Ogitsu, T. Nakamoto, M. Sugano, K. Suzuki; KEK,
S. Awaji; Tohoku Univ., H. Oguro; Tokai Univ.,
A. Ballarino, S. Hopkins; CERN,
D. Larbalestier; NHMFL
S. Kawashima, T. Kawarada, Y. Murakami, K. Saito; Kobe Steel and JASTEC
D. Asami, H. Ii, H. Sakamoto, T. Kato; Furukawa Electric

## Slide 2: R&D Plan
CERN, KEK and Tohoku & Tokai university have jointly launched a R&D program
The scope of the program is to develop, produce in representative lengths and characterize Nb3Sn wire with enhanced characteristics.
The final goal is to achieve in representative unit lengths of material the development targets defined, on the basis of magnets performance, for the FCC Nb3Sn conductor: 1500A/mm2 @ 16T
Contract with 2 Japanese companies: Task 3; 4 R&D contracts each
  JASTEC/Kobelco: Distributed Tin (DT) Method
  Furukawa Electric: Nb Tube Method
Task1
Review past technologies and select.
First review meeting in Feb. 2016
Task2
Design wire layout and composition
Procure material (possible trial billets)
Task3
Production of R&D billets
L>3km * N>3
Task4
Select candidate
Produce 5km wire
Heat treatment study
Task5
Production of 20km wire
with unit length > 100m
4 Years Plan

## Slide 3
Development of DT Nb3Sn wire
for FCC in KSL/JASTEC
Notes: Future

## Slide 4
Improvement of Sn diffusion ： Reduction of Sn diffusion distance
(2) Increase of Nb volume fraction： Reduction of useless volume
(3) Ternary additive elements ： Amount and method
(4) Optimization of heat treatment ：Stoichiometry, Refinement
Confidential
KSL/JASTEC are developing the DT wire for FCC.
Key factors for higher JC Nb3Sn
Nb
Nb
Sn
Sn
Cross-section of DT wire (before Heat treatment)
For higher Jc…
• Multi Nb module (pure Nb)
• Mono Sn module (Sn-Ti alloy)
• Nb common barrier
• Stabilized Cu outside barrier

## Slide 5
Non Cu JC v.s. B
 | T1-A | T1-B | T1-C | T3-A | T3-B
Wire diameter (mm) | 0.80 | 0.74 | 0.64 | 0.80 | 0.80
Sn diffusion distance (µm) | 60 | 58 | 48 | 32 | 32
Ti ratio (wt%) | 0.55 | 0.55 | 0.55 | 0.48 | 0.35
non Cu JC ( A/mm2 )@16T | 800 | 930 | 1025 | 1137 | 1032
Non Cu Jc of 1,100 A/mm2 at 16 T, 4.2 K has been achieved
by improving Sn diffusion and optimizing Ti content.

## Slide 6
Magnetization characteristics
・The magnetization were measured at 4.2 K at CERN and Tohoku University, separately.
・For high Jc wire (T3-A,B), KSL/JASTEC evaluated magnetization characteristics and changes of Jc and RRR after rolling.
【Magnetizations of T3-A 】
at Tohoku University.
@ CERN
@ Tohoku Uni.
Sample name | T3-A | T3-B
deff by CERN (µm) | 54.5 | 55.0
deff by Tohoku Uni. (µm) | 35.1 | 30.6
【Calculated deff 】
※Nominal Nb module dia.: 32µm
・ There is no large flux jump.
・ The calculated deff (effective filament diameter) were 30 to 60 μm, which was for one or two modules. It is possible to achieve a value close to the current target ( ≤ 60 μm).

## Slide 7
Rolling test (JC, RRR)
←Spec.
【 Normalized non Cu Jc 】
【RRR】
T3-A
T3-B
T3-A
T3-B
Rolling reduction
Required specifications for FCC wire (16 T dipole mag.)
After 10 % rolling : 1) IC (JC) > 95 % for round wires, and 2) RRR > 100.
・Both JC and RRR after rolling meet the specifications.
・From the SEM images of cross section, at any rolling reduction level, the deformation of Nb/Sn modules were only partial.
Also at 10% reduction, there was no Nb barrier break.

## Slide 8
Cross section of T3-A after rolling (after heat treatment)
10％ (0.72mmt) | 15％ (0.68mmt) | 20％ (0.64mmt)
 | － | 
・At any rolling reduction, the deformation of the Nb / Sn modules were only partial.
・At 15 and 20% of rolling reduction, there were Nb barrier breaks,
but at 10% reduction, there was no Nb barrier break.

## Slide 9
Current Results and Next steps
KSL/JASTEC have achieved non Cu Jc @16T 1,100 A/mm2,
by improving Sn diffusion and optimize Ti content.
These wires also showed reasonable results in deff and rolling test.
We will investigate the followings to overcome the provisional
Jc target of 1,200A/mm2:
Increase of Nb area ratio
Control of ternary additive element
Further refinement of Nb3Sn grain by controlling
heat-treatment condition
(4) Artificial Pinning Center (APC)

## Slide 10: Materials for the FCC Week 2019

## Slide 11: Wire Design of Nb tube type Nb3Sn wire
Items | Wire A | Wire B | Wire C | Wire D
No. of Filament | 85 | 132 |  | 
Filament Material | Nb |  |  | Nb-7.5wt%Ta
Nb/Sn ratio | ~2.1 |  | ~3.3 | 
Filament Dia. (at φ0.83) | 64 mm | 45 mm |  | 
Cu/non-Cu ratio | ~1 | ~1.6 |  | 
Nb pretreatment(℃) | 1,150 |  | 850 | 
Wire A
Wire B~D

## Slide 12: Drastic improvement of wire workability
Wire A , φ4.8 mm
Wire B , φ0.83 mm
Improvement
of production
process
Wire A , φ0.83 mm
✓Some improvements were conducted for
wire workability.
・material pretreatment
・Cleaning method of strands
・drawing parameter
✓Wire drawing is succeeded to φ0.83 mm.
✓The filament diameter is reduced to 45 μm.
Wire C , φ0.83 mm
Wire D , φ0.83 mm

## Slide 13: Improvement of filament shape
Wire | Nb tube grain (before drawing) | Filament shape (Cross section)
A |  | 
C |  | 
✓Nb tube grain size greatly affects filament shape.
✓Filament shape is improved by optimization of Nb tube pretreatment.

## Slide 14: Non-Cu Jc
✓Non-Cu Jc of 580 A/mm2 @16 T was obtained in Wire D.
✓Some improvements have been conducted for higher non-Cu Jc.
・Optimization of heat-treatment condition
・Nb/Sn ratio in filaments
・Grain size reduction of Nb3Sn (including APC technique)
Wire | A | B | C | D
No. of Filament | 85 | 132 |  | 
Filament Material | Nb |  |  | Nb-7.5wt%Ta
Nb/Sn ratio | ~2.1 |  | ~3.3 | 
Filament Dia. (at φ0.83) | 64 mm | 45 mm |  | 
Cu/non-Cu ratio | ~1 | ~1.6 |  | 
Nb pretreatment(℃) | 1,150 |  | 850 | 

## Slide 15: Summary
✓Nb3Sn wire with 85 or 132 Nb-tube filaments was tried.
✓Multiple wire was drawn to 0.83 mm by improvements for wire workability.
✓Nb pre-treatment optimization give a good influence on the
filament shape.
✓Non-Cu Jc of 580 A/mm2 @16 T was obtained in Wire D.

## Slide 16: Summary
Task 3 almost completed
Review
  May 17-24: D. Larbalestier, S. Hopkins, T. Ogitsu
  Visit JASTEC, Furukawa, and Tohoku Univ.
  Review R&D plan and discuss new plan
The R&D work so far
  8 R&D contracts: DT reach 1100 A/mm2, Nb Tube workability improved
Propose to modify Task 4 and Task 5
  Task 4: R&D contracts 4 more each for JASTEC and Furukawa
    With advanced technologies to aim for 1500 A/mm2
  Task 5: Produce 5 km x 2 with best conductors
Task1
Review past technologies and select.
First review meeting in Feb. 2016
Task2
Design wire layout and composition
Procure material (possible trial billets)
Task3
Production of R&D billets
1 ~ 5kg * N=8
Task 5
Select candidate
Produce 2*5km wire
Heat treatment study
Task 4
Production of R&D billets with Advanced Technologies
1 ~ 5kg * N=8