## Slide 1: Mid-Term Review 10 December 2018, Brussels
Mattia, DONATO
ESR7, WP3
donato.mattia@as-g.it

## Slide 2: ESR7, WP3 - Background
Background:
  2006 – 2010: Bachelor in Physics (Laurea Triennale) at University of Genova (Italy)
  2010 – 2013: Master in Physics (Laurea Magistrale) at University of Genova (Italy)
    10 months: ERASMUS Student Mobility for Study at Uppsala University (Sweden)
    8 months: ERASMUS Student Mobility for Placement at Applied Nuclear Division of Department of Physics and Astronomy - Uppsala University (Sweden) – Master Thesis
  19.08.2013 – 18.08.2017: European XFEL GmbH (Detector Group), Hamburg as Doctoral Candidate
  Enrolled at University of Hamburg
  11.12.2018 (Tomorrow afternoon 2pm in Hamburg): Oral Doctoral Defence - “Commissioning and Characterization of the first DSSC Ladder X-ray Camera Prototype for the European XFEL”
    PhD University: Universität Hamburg
    PhD Supervisor: prof. Erika Garutti

## Slide 3: ESR7, WP3 - Background
Contract start date: 1st June 2018
EASITrain Supervisor(s): Dr. Matteo Tropeano
Company: Columbus Superconductors SRL
(Small enterprise, about 25 employee)
(Industry, about 150 employee)
The 1st November 2018 the three companies merged into ASG Superconductors SpA

## Slide 4: Columbus Superconductors
The actual plant is fully operational for
MgB2 wire production
MgB2 chemical synthesis
Wire unit length today up to 2- 4 Km in a single-piece length
GENOVA
LA SPEZIA
LIGURIA
ITALY
ASG Columbus MgB2 Unit
SAN DESIDERIO, GENOVA

## Slide 5: Production
s
+
B
Mg
MgB2
billet
~ 1 meter
I phase
II phase
Single-core
Multi-core assembling
Rolling
Multi-core Drawing
Sheath
Assembled wire
~ 2-4 km
III phase
Spool
Thermal Treatment
(Mechanical feature)
Quality Assurance
Cryogenic
Temperature
Magnetic Field
SC Wire
Critical Current
Measurement
Current
~ 100 m
800 - 900 °C
300 – 500 °C
Final Thermal Treatment
(Sintering)
MgB2
Residual-resistance ratio
Sample

## Slide 6: Role in the Project & Objectives
CERN
BRUKER
CNR
HZB
TUW
COLUMBUS
USIEGEN
I-CUBE
INFN
WP3
Main Objective: Development of MgB2 wire for high-field magnet application.
WP3 (Manufacturing workpackage),
The goal is oriented to the optimization of the superconductors production processes.
Develop and define procedures to control and improve the manufacturing process of MgB2 wires, in particular of the wires suitable for use in high field magnets.
Improve the critical current testing capabilities of the production plant improving cooling efficiency and introducing automatic measurements.
Enhance automatization and control of the manufacturing process parameter
MgB2 tape 3.6mm x 0.6mm
MgB2 round wire diameter 1mm

## Slide 7: Research, Methodology, Results & Next Steps
  1. TUW (ATI), Vienna:
    Evaluation of superconducting properties of MgB2
    wires to understand mechanism and enhance in-field performance
  2. TUW (USTEM), Vienna:
  Microscopy on MgB2 powder and wire for characterization and
    study of the impact of the wire design and the production process on its performance
  Planned secondments:
    TUW, ATI 04.03.2019 – 17.03.2019
    TUW, USTEM 14.10.2019 – 27.10.2019:
TUW, both ATI and USTEM, are key collaboration partner
MgB2 tape 3.6mm x 0.6mm
MgB2 round wire diameter 1mm

## Slide 8: Research, Methodology, Results & Next Steps
Activities and training topics: | 1 – 6 | 6 – 12 | 12 – 18 | 18 – 24 | 24 – 30 | 30 – 36
Superconductivity and application (introduction) |  |  |  |  |  | 
Materials characterization (powder, X-ray diffraction, XRF, Granulometry, Micro-Hardness, Stress-strain) |  |  |  |  |  | 
Critical Current tests – Cryogen coolant free (Cryogenics system, principle of measurement techniques, LabView ACQ system, improvement test, post-processsing data analysis) |  |  |  |  |  | 
Manufacturing process – phase I (introduction to PIT technique and related critical issues) |  |  |  |  |  | 
Critical Current tests – Liq. Helium (defining the technical specification of a new test facility; commissioning and test) |  |  |  |  |  | 
Manufacturing process – phase II (Relationship between PIT aspect and Jc enhancement; process control; wires parameters control; automatization; in-line quality assurance) |  |  |  |  |  | 
EASI Schools |  |  |  |  |  | 
Secondments at TUW ATI and TUW USTEM |  |  |  |  |  | 
Project Management |  |  |  |  |  | 
1st June 2018

## Slide 9: Research, Methodology, Results & Next Steps
Critical Current Test Facility:
  Improvements Control Software
    Introducing facility diagnostic measurments
    (current leads, voltage meas)
  Improvements Data Analysis Scripts/Macros
Cryogenic
Temperature
Magnetic Field
SC Wire
Current
Current
Generator
Nano-Voltmeter
Temperature
Control (PID)
Up to 1000A
Magnetic Probe
Facility Diagnostic

## Slide 10: Research, Methodology, Results & Next Steps
Control of process:
  Heat Treatments, Temperature Real-time Monitoring
Raspberry PI
Picotech TC08
●A ●4 ●3
●8 ●5 ●2
●7 ●6 ●1
SPOOL

## Slide 11: Research, Methodology, Results & Next Steps
Tensile testing machine
EXTENSOMETER
Force
PC
DAQ

## Slide 12: Training, Conferences & Workshops
Attended EASITrain events:
  EASISCHOOL 1 Vienna 2018 :
    EASITRAIN/ESAS SUMMER SCHOOL on Applied Superconductivity (2 ECTS)
    EASITRAIN Training Course on Project Management (2 ECTS)
    Terra Mater EASITRAIN Media Training
Training
  Safety Training: general risks and specific high risks (16h)
  Privacy and Security Awareness
  Tensile testing machine Training
Conferences & Workshops
  For the first year the participation to conferences or workshop is not expected.
  Planned conference:
    EUCAS 2019 and ICEC-ICMC International Cryogenics Engineering Conference)

## Slide 13: Outreach, Dissemination & Networking
Outreach activities
  The work in EASITrain will be described through the ASG Superconductors official page on several social media
  Every year in Genova there is Festival of Science, an event which involves whole town and scholar, students and adults come to visit the scientific expositions, the lectures or public debate. I would like to organize one event or stand.
Dissemination activities
  For the next year the participation to the EUCAS 2019 is planned
Networking activities:
  EASISchool week
  Seminar “Thermomagnetic Mechanism for Self-Cooling Cables” meeting scientists and visiting to CNR-SPIN laboratory 20.11.2018
  Meetings with providers of cryogenic systems and electronic equipments for building new test facility

## Slide 14: Impact
The improvement of MgB2 superconducting wire performance and quality will extend the market possibilities
The core business of the MgB2 wire is now related to cable for electricity transport (superconducting link project at CERN-HVDC line)
and for low field MRI magnet (Paramed MRI magnets).
This is really a big opportunity for me, it’s giving me the possibility to:
Work in high-technology field industry
Have a training and learning
Local and International networking
Open new possibilities for future employement (companies or reasearch institutes)
Wires with improved characteristic will extend the market to medium-high field MRI and to magnets for scientific experiment (FCC).

## Slide 15: Thank you for your attention!