## Slide 1: Mid-Term Review 10 December 2018, Brussels
1
Advanced surface coating techniques for superconducting radiofrequency cavities
Vanessa Andreina, GARCIA DIAZ
ESR 10, WP 3 (Manufacturing)

## Slide 2: ESR 10, WP 3 - Background
Background: Master in Physics, Caracas-Venezuela. Master in surface treatments for industrial applications, Padova-Italy
Host Institution: INFN – LNL
Contract start date : 01/02/2018
Supervisor: Dr. Cristian Pira
PhD University: Ferrara University
Planned secondments:
  1. I-Cube, Electro-hydro forming technique for seamless cavities, early 2019 for 2 weeks.
  2. CERN, RF characterization, end of 2019 for 2 weeks.
  3. RI, Coated cavities production and efficiency, early 2020 for 2 weeks.
2

## Slide 3: Research, Methodology, Results & Next Steps
Superconducting Radio Frequency Cavities
Nb bulk 6 GHz Cavity
Nb/Cu 6 GHz Cavity

## Slide 4: Research, Methodology, Results & Next Steps
Mechanical Finishing
PVD process
Chemical Polishing
RF Characterization
Cavity Fabrication
Collaboration with I-Cube (ESR-09)
Improve spinning process
Insert 6 GHz tumbling
Collaboration with CERN (ESR-01) and HZB (ESR-08)
Study effects of different sputtering parameters
Insert Active magnetic shielding

## Slide 5: Research, Methodology, Results & Next Steps
In order to overcome the Q slope on the Nb/Cu cavities, in this research is used a thick film approach in a multilayer deposition mode
4
Total Thickness (on the cell) = 70 µm
Copper
Niobium
Niobium
Multilayer

## Slide 6: Research, Methodology, Results & Next Steps
4
IR Lamp
Cavity
Target
Thermocouple

## Slide 7: Research, Methodology, Results & Next Steps
Deposition parameters and system
Baking = 600°C for 48 hours
Temperature = 550 °C
Base pressure < 2 x 10-9 mbar
Magnetic Field = 830 Gauss
Current = 1 A
6GHz Nb/Cu Cavity

## Slide 8: Research, Methodology, Results & Next Steps
5
RF characterization
At 4,2K and 1,8K

## Slide 9: Research, Methodology, Results & Next Steps
5
RF characterization
At 4,2K and 1,8K

## Slide 10: Research, Methodology, Results & Next Steps
5
Chart: Eacc (MV/m)
Cav 21 500nm +5um | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Cav 24 4.2K | 21700000 | 21800000 | 21900000 | 22000000 | 22000000 | 21800000 | 21000000 | 20800000 | 19700000 | 19400000 | 19400000 | 19300000 | 19300000 | 19200000 | 18900000 | 18800000 | 18000000 | 17800000 | 17600000 | 17300000 | 16800000 | 16000000 | 14900000 | 14600000 | 13800000 | 13600000 | 13100000 | 12600000 | 12400000
Cav 23 4.2K | 23310000000 | 23500000 | 23500000 | 23600000 | 23100000 | 24200000 | 23000000 | 22900000 | 22400000 | 22300000 | 21700000 | 21400000 | 21400000 | 20300000 | 20200000 | 20000000 | 19700000 | 19400000 | 19000000 | 18600000 | 18500000 | 17800000 | 17600000 | 17400000 | 17100000 | 16900000 | 16800000 | 16900000 | 16600000 | 16800000 | 16600000 | 16600000 | 16400000 | 16400000 | 16100000 | 16100000
Cav 21 4.2K | 24200000 | 24200000 | 24800000 | 24500000 | 24800000 | 25000000 | 24700000 | 25700000 | 28000000 | 28500000 | 24700000 | 24100000 | 24000000 | 23900000 | 23700000 | 23700000 | 23800000 | 23500000 | 23400000 | 23400000 | 23400000 | 23600000 | 23500000 | 22300000 | 23200000 | 23400000 | 23400000 | 23300000 | 23200000 | 23200000 | 23200000 | 23200000 | 23100000 | 23000000 | 23000000 | 22900000 | 22800000 | 22700000 | 22600000 | 20800000 | 20600000 | 20400000 | 21200000 | 20300000 | 20000000 | 19800000 | 19700000 | 19300000 | 19200000 | 19000000
Nb Bulk 4.2K | 20745196 | 20272608 | 20117484 | 19659196 | 19508764 | 19359484 | 19211348 | 19064344 | 18918464 | 18630046 | 18487490 | 18487490 | 18066334 | 17928092 | 17790906 | 17519678 | 17385618 | 17385618
6GHz

## Slide 11: Research, Methodology, Results & Next Steps
5
Chart: Eacc (MV/m)
Cav 21 500nm +5um | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Cav 24 200nm+5um | 21700000 | 21800000 | 21900000 | 22000000 | 22000000 | 21800000 | 21000000 | 20800000 | 19700000 | 19400000 | 19400000 | 19300000 | 19300000 | 19200000 | 18900000 | 18800000 | 18000000 | 17800000 | 17600000 | 17300000 | 16800000 | 16000000 | 14900000 | 14600000 | 13800000 | 13600000 | 13100000 | 12600000 | 12400000
Cav 23 300nm+5um | 23310000000 | 23500000 | 23500000 | 23600000 | 23100000 | 24200000 | 23000000 | 22900000 | 22400000 | 22300000 | 21700000 | 21400000 | 21400000 | 20300000 | 20200000 | 20000000 | 19700000 | 19400000 | 19000000 | 18600000 | 18500000 | 17800000 | 17600000 | 17400000 | 17100000 | 16900000 | 16800000 | 16900000 | 16600000 | 16800000 | 16600000 | 16600000 | 16400000 | 16400000 | 16100000 | 16100000
Cav 21 500nm+5um | 24200000 | 24200000 | 24800000 | 24500000 | 24800000 | 25000000 | 24700000 | 25700000 | 28000000 | 28500000 | 24700000 | 24100000 | 24000000 | 23900000 | 23700000 | 23700000 | 23800000 | 23500000 | 23400000 | 23400000 | 23400000 | 23600000 | 23500000 | 22300000 | 23200000 | 23400000 | 23400000 | 23300000 | 23200000 | 23200000 | 23200000 | 23200000 | 23100000 | 23000000 | 23000000 | 22900000 | 22800000 | 22700000 | 22600000 | 20800000 | 20600000 | 20400000 | 21200000 | 20300000 | 20000000 | 19800000 | 19700000 | 19300000 | 19200000 | 19000000
Nb Bulk | 20745196 | 20272608 | 20117484 | 19659196 | 19508764 | 19359484 | 19211348 | 19064344 | 18918464 | 18630046 | 18487490 | 18487490 | 18066334 | 17928092 | 17790906 | 17519678 | 17385618 | 17385618
4,2K

## Slide 12: Research, Methodology, Results & Next Steps
5
Chart: Eacc (MV/m)
Cav 21 500nm +5um | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Cav 24 4.2K | 21700000 | 21800000 | 21900000 | 22000000 | 22000000 | 21800000 | 21000000 | 20800000 | 19700000 | 19400000 | 19400000 | 19300000 | 19300000 | 19200000 | 18900000 | 18800000 | 18000000 | 17800000 | 17600000 | 17300000 | 16800000 | 16000000 | 14900000 | 14600000 | 13800000 | 13600000 | 13100000 | 12600000 | 12400000
Cav 23 4.2K | 23310000000 | 23500000 | 23500000 | 23600000 | 23100000 | 24200000 | 23000000 | 22900000 | 22400000 | 22300000 | 21700000 | 21400000 | 21400000 | 20300000 | 20200000 | 20000000 | 19700000 | 19400000 | 19000000 | 18600000 | 18500000 | 17800000 | 17600000 | 17400000 | 17100000 | 16900000 | 16800000 | 16900000 | 16600000 | 16800000 | 16600000 | 16600000 | 16400000 | 16400000 | 16100000 | 16100000
Cav 21 4.2K | 24200000 | 24200000 | 24800000 | 24500000 | 24800000 | 25000000 | 24700000 | 25700000 | 28000000 | 28500000 | 24700000 | 24100000 | 24000000 | 23900000 | 23700000 | 23700000 | 23800000 | 23500000 | 23400000 | 23400000 | 23400000 | 23600000 | 23500000 | 22300000 | 23200000 | 23400000 | 23400000 | 23300000 | 23200000 | 23200000 | 23200000 | 23200000 | 23100000 | 23000000 | 23000000 | 22900000 | 22800000 | 22700000 | 22600000 | 20800000 | 20600000 | 20400000 | 21200000 | 20300000 | 20000000 | 19800000 | 19700000 | 19300000 | 19200000 | 19000000
Nb Bulk 4.2K | 20745196 | 20272608 | 20117484 | 19659196 | 19508764 | 19359484 | 19211348 | 19064344 | 18918464 | 18630046 | 18487490 | 18487490 | 18066334 | 17928092 | 17790906 | 17519678 | 17385618 | 17385618
1,8K

## Slide 13: Research, Methodology, Results & Next Steps
5
Chart: Eacc (MV/m)
Cav 21 500nm +5um | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Cav 24 4.2K | 21700000 | 21800000 | 21900000 | 22000000 | 22000000 | 21800000 | 21000000 | 20800000 | 19700000 | 19400000 | 19400000 | 19300000 | 19300000 | 19200000 | 18900000 | 18800000 | 18000000 | 17800000 | 17600000 | 17300000 | 16800000 | 16000000 | 14900000 | 14600000 | 13800000 | 13600000 | 13100000 | 12600000 | 12400000
Cav 23 4.2K | 23310000000 | 23500000 | 23500000 | 23600000 | 23100000 | 24200000 | 23000000 | 22900000 | 22400000 | 22300000 | 21700000 | 21400000 | 21400000 | 20300000 | 20200000 | 20000000 | 19700000 | 19400000 | 19000000 | 18600000 | 18500000 | 17800000 | 17600000 | 17400000 | 17100000 | 16900000 | 16800000 | 16900000 | 16600000 | 16800000 | 16600000 | 16600000 | 16400000 | 16400000 | 16100000 | 16100000
Cav 21 4.2K | 24200000 | 24200000 | 24800000 | 24500000 | 24800000 | 25000000 | 24700000 | 25700000 | 28000000 | 28500000 | 24700000 | 24100000 | 24000000 | 23900000 | 23700000 | 23700000 | 23800000 | 23500000 | 23400000 | 23400000 | 23400000 | 23600000 | 23500000 | 22300000 | 23200000 | 23400000 | 23400000 | 23300000 | 23200000 | 23200000 | 23200000 | 23200000 | 23100000 | 23000000 | 23000000 | 22900000 | 22800000 | 22700000 | 22600000 | 20800000 | 20600000 | 20400000 | 21200000 | 20300000 | 20000000 | 19800000 | 19700000 | 19300000 | 19200000 | 19000000
Nb Bulk 4.2K | 20745196 | 20272608 | 20117484 | 19659196 | 19508764 | 19359484 | 19211348 | 19064344 | 18918464 | 18630046 | 18487490 | 18487490 | 18066334 | 17928092 | 17790906 | 17519678 | 17385618 | 17385618
1,8K
Higher Q0 for 500nm thickness single layer Cav 21

## Slide 14: Research, Methodology, Results & Next Steps
Chart: Eacc (MV/m)
Cav 21 500nm +5um | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Cav 24 4.2K | 21700000 | 21800000 | 21900000 | 22000000 | 22000000 | 21800000 | 21000000 | 20800000 | 19700000 | 19400000 | 19400000 | 19300000 | 19300000 | 19200000 | 18900000 | 18800000 | 18000000 | 17800000 | 17600000 | 17300000 | 16800000 | 16000000 | 14900000 | 14600000 | 13800000 | 13600000 | 13100000 | 12600000 | 12400000
Cav 23 4.2K | 23310000000 | 23500000 | 23500000 | 23600000 | 23100000 | 24200000 | 23000000 | 22900000 | 22400000 | 22300000 | 21700000 | 21400000 | 21400000 | 20300000 | 20200000 | 20000000 | 19700000 | 19400000 | 19000000 | 18600000 | 18500000 | 17800000 | 17600000 | 17400000 | 17100000 | 16900000 | 16800000 | 16900000 | 16600000 | 16800000 | 16600000 | 16600000 | 16400000 | 16400000 | 16100000 | 16100000
Cav 21 4.2K | 24200000 | 24200000 | 24800000 | 24500000 | 24800000 | 25000000 | 24700000 | 25700000 | 28000000 | 28500000 | 24700000 | 24100000 | 24000000 | 23900000 | 23700000 | 23700000 | 23800000 | 23500000 | 23400000 | 23400000 | 23400000 | 23600000 | 23500000 | 22300000 | 23200000 | 23400000 | 23400000 | 23300000 | 23200000 | 23200000 | 23200000 | 23200000 | 23100000 | 23000000 | 23000000 | 22900000 | 22800000 | 22700000 | 22600000 | 20800000 | 20600000 | 20400000 | 21200000 | 20300000 | 20000000 | 19800000 | 19700000 | 19300000 | 19200000 | 19000000
Nb Bulk 4.2K | 20745196 | 20272608 | 20117484 | 19659196 | 19508764 | 19359484 | 19211348 | 19064344 | 18918464 | 18630046 | 18487490 | 18487490 | 18066334 | 17928092 | 17790906 | 17519678 | 17385618 | 17385618
1,8K
Higher Eacc for 400nm thickness single layer Cav 18

## Slide 15: Research, Methodology, Results & Next Steps
Refurbishing of deposition system
Vacuum chamber
Vacuum chamber

## Slide 16: Research, Methodology, Results & Next Steps
6
Vibro-tumbling and active shielding techniques are being studied and will be installed as a part of our protocol

## Slide 17: Research, Methodology, Results & Next Steps
6
Vibration
Rotation
Active magnetic shielding
Vibro-tumbling
Reproducibility issue
Understand trapped magnetic flux

## Slide 18: Research, Methodology, Results & Next Steps
6
Vibro-tumbling and active shielding techniques are being studied and will be installed as a part of our protocol
Deposition of different thickness in multilayer mode and N – doping
Implementation of post sputtering treatments such as baking before RF characterization

## Slide 19: Training, conferences and Workshops
Tesla meeting (Milano, February)
FCC week (Amsterdam, April)
EASITrain Lectures Spring (CERN, March)
EASISchool (Wien, September)
8th International Workshop on Thin Films and new ideas for pushing the limits of RF superconductivity (Legnaro, October). Member of the organizing committee.
TTC/ARIES topical workshop on flux trapping and magnetic shielding (CERN, November)
Safety courses. English and Italian Course

## Slide 20: Outreach, Dissemination & Networking
Presentation in conferences:
  FCC week
  8th International Workshop on Thin Films and new ideas for pushing the limits of RF Superconductivity
6

## Slide 21: Outreach, Dissemination & Networking
Presentation in conferences:
  FCC week
  8th International Workshop on Thin Films and new ideas for pushing the limits of RF Superconductivity
Dissemination to high school students as part of their stages at LNL-INFN
Guidance to cryogenic laboratory during Thin Film Workshop at LNL-INFN
6

## Slide 22: Outreach, Dissemination & Networking
Presentation in conferences:
  FCC week
  8th International Workshop on Thin Films and new ideas for pushing the limits of RF Superconductivity
Dissemination to high school students as part as their stages at LNL-INFN
Guidance to cryogenic laboratory during Thin Film Workshop at LNL-INFN
Guidance to ESR 01, 08, 09, 14 in the Material Science and Technologies for Nuclear Physics Service at LNL-INFN.
6
ESR09
ESR14
ESR12
ESR08
ESR01
ESR09
ESR14
ESR12
ESR10
ESR01
ESR08

## Slide 23: Outreach, Dissemination & Networking
Presentation in conferences:
  FCC week
  8th International Workshop on Thin Films and new ideas for pushing the limits of RF Superconductivity
Dissemination to high school students as part as their stages at LNL-INFN
Guidance to cryogenic laboratory during Thin Film Workshop at LNL-INFN
Guidance to ESR 01, 08, 09, 14 in the Material Science and Technologies for Nuclear Physics Service at LNL-INFN.
Guidance during ESR01 secondment at LNL-INFN
6
ESR 01
Dorothea Fonnesu

## Slide 24: Outreach, Dissemination & Networking
6
Constant dissemination in social media: Twitter

## Slide 25: Outreach, Dissemination & Networking
6
Constant networking due to constant collaborations between lab and industry or others research groups.
Wide networking during workshops and conferences.
8th International Workshop on Thin Films and new ideas for pushing the limits of RF Superconductivity

## Slide 26: Impact
7
Research
Medical physics
Industrial applications
Material identification
Cancer treatments and imaging
Change mechanical properties of materials
Fundamental physics research
Non destructives methods

## Slide 27: Impact
Learned:
How to push myself out of the comfort zone
Different languages
How to work in a international and collaborative environment
Different cultures
Give presentations
… and still learning
Being where I want to be in the scientific field
Traveling and getting to know a lot of people
7

## Slide 28: Conclusions
The project at INFN-LNL has started successfully.
The PhD has started at Ferrara University.
The project has been an opportunity to be part of a scientific community.
Conferences and workshop are fundamental for the networking.
Dissemination is a fundamental part of being a scientist.
Being a Marie Curie Fellow in EASITrain has been an
incredible experience!

## Slide 29: Thank you!