## Slide 1
Organic semiconductor radiation detectors for alpha and neutron detection
Aled Matthew Horner
09/10/23
a.m.horner@qmul.ac.uk
Supervisors: Prof. A Bevan, Dr. T Kreouzis
Copyright 2023 UK Ministry of Defence © Crown Owned Copyright 2023/AWE

## Slide 2
Overview
Introduction
Alpha detection by organic semiconductor devices
Neutron detection by organic semiconductor devices
Organic material: Carborane-NDI
Detector array
Conclusions and future trajectory

## Slide 3
Introduction
Stockpiled and production rates of He-3 used historically in neutron detectors is not enough to meet demand for global security coverage[1]
Neutron detector usages:
  Security (detecting fissile materials shielded from gamma radiation)
  Scientific research (dark matter, radiation monitoring)
Organic materials:
  Tunable, scalable, low-cost, sensitisable
  Can be used for detecting alpha, beta, gamma and x-ray radiation
  Alpha detection possible, can adjust to neutrons
[1] RT Kouzes, The 3He Supply Problem, US Department of Energy, PNNL-18388 (2009), https://doi.org/10.2172/956899.

## Slide 4
Organic semiconductor detectors: Alpha particles
Use organic polymers to detect alpha particles
Many different polymers and polymer blends used successfully internally (P3HT, P3HT:PC60BM, PNDI(2HD)2T, etc.)
Alpha particles come in, electron-hole pairs form (depending on HOMO/LUMO levels, medium’s thickness), make a current when under a voltage bias
Tested by opening and closing a shutter: significant increase in current when shutter is opened → radiation is being detected
Figure 1: Left: Composition of a simple "diode-style" device.
Above: Formation of electron-hole pairs in organic medium
of devices irradiated by alpha radiation.

## Slide 5
Organic semiconductor devices: How to build
Photolithography: Pattern ITO on glass substrate into desired “fingers” shape
Drop-casting: Using a pipette, drop polymer/solvent mixture onto substrate (left to set)
Evaporation: Evaporate aluminium top contact through shadow mask
Uncovering: Dissolve/scrape away polymer to give access to ITO contacts
Device: each area of overlapping top/bottom contacts (typically 4 mm2)
Figure 2: Step-by-step animation of device fabrication.

## Slide 6
Organic semiconductor detectors: Neutrons
Neutrons do interact with matter, but require different ways to detect
Thermal neutrons have a high cross section with 10B, making detectable alpha particles (and lithium)
One solution: stir in some boron nanoparticles, i.e., boron carbide, boron nitride, elemental boron, etc.
Issue: big problem with clumping and causing conductive paths between electrodes
Solution in [2] to add a surfactant to prevent agglomeration + ultrasonic dispersion
Currently only alpha sources easily accessible without travelling to external neutron source (NPL, ISIS, AWE) until upcoming source arrival
[2] Chatzispyroglou, P.; Keddie, J. L.; Sellin, P. J., Boron-Loaded Polymeric Sensor for the Direct Detection of Thermal Neutrons. ACS Appl. Mater. Interfaces 2020, 12 (29), 33050-33057.
[3] J. Borowiec et al, Scalable Organic Semiconductor Neutron Detectors, arXiv:2212.08438.
[4] IAEA, Modern Neutron Detection: Proceedings of a Technical Meeting, IAEA-TECDOC-1935.
6%
94%
Figure 3: Three schematic neutron interactions are indicated. Left: Thermal neutron 10B capture at a B4C microparticle, Middle: Elastic neutron-proton scattering at a PNDI H site. Right: Inelastic 12C decay into 3 α particles at a PNDI C site. Fig from [3].

## Slide 7
Organic material: Carborane-NDI
Carborane: a polyhedral cluster of carbon, boron and hydrogen [3]
Carborane derivatives highly relevant for medical applications, particularly for potential cancer treatments via boron neutron capture therapy
Carborane-NDI: a variant of PNDI(2OD)2T with carborane directly incorporated in the molecular backbone
If carborane-NDI can detect alpha particles, boron inside should allow it to detect neutrons like the nanoparticles
Given a small supply of meta-, ortho-, and para-carborane-NDI by authors of [5]
Figure 4: Top: Chemical structure of the oCbT2-NDI form of carborane-NDI. Bottom: Picture of two carborane-NDI films before top contacts were added via evaporation. Left: oCbT2-NDI. Right: pCbT2-NDI. A noticeable difference in colour may be seen in this picture between the two isomer forms.
[5] Aniés, F. et al, N-type polymer semiconductors incorporating para, meta, and ortho-carborane in the conjugated backbone, Polymer 2022 240 124481.

## Slide 8
oCbT2-NDI: Alpha detection
Figure 5: Left: Raw current response data of oCbT2-NDI device under 10V bias being exposed to 370 kBq Americium-241 alpha source showing distinct periods of a shutter being closed and opened (data from day 59 of air exposure). Right: Plot showing variation of current enhancement (ΔI) and leakage current (IL) in the same device under the same conditions over the course of 517 days.
10 V bias
= Current enhancement = Leakage (dark) current

## Slide 9
oCbT2-NDI: Alpha detection
Leakage current and current enhancement both increased with voltage bias
Enhancement appears to saturate whilst leakage continues to rise
Figure 6: Left: Plot showing current enhancement (“signal”) of oCbT2-NDI device under different (positive) voltage biases being exposed to alpha source after 40 days' exposure to air with leakage current (“dark current”) subtracted away. Right: Variation of current enhancement (ΔI) and leakage current (IL) with voltage bias. Both plots show same device as each other but differ from previous slide.

## Slide 10
oCbT2-NDI: Neutron detection
Figure 7: Left: Variation of current enhancement (ΔI) due to exposure to various neutron beam fluxes under 10V bias for a 4mm2 and a 36mm2 oCbT2-NDI device. Right: Absolute values of current enhancement versus voltage bias of one 4mm2 device and one 36mm2 device exposed to neutrons at NPL. Dashed lines made by fitting to equation above. Under negative voltage biases these enhancements are negative.
NPL site visit (using thermal pile)
a = Saturation current
b = 1/Characteristic V0
Neutron tests: ~4 times signal with 9x scale. Alpha tests: ~5 times.

## Slide 11
Organic material: PNDI(2OD)2T
The material on which oCbT2-NDI is based (carborane in between the thiophenes)
Also taken to NPL for neutron testing: with and without enriched B4C nanoparticles included for thermal neutron sensitization
Amount of B4C chosen specifically to match 10B content of oCbT2-NDI for direct sensitizing comparison
Much lower concentration compared to previous trip: didn’t clump as much
Figure 8: Top: Chemical structure of PNDI(2OD)2T. Arrow shows where, in oCbT2-NDI, carborane is included. Bottom: Reflected microscope image of PNDI(2OD)2T with dispersed B4C microparticles.
50µm

## Slide 12
NDI Polymers: Radiation detection
Figure 9: Left: Plot showing current enhancement of three 4mm2 devices under 10V bias exposed to 370 kBq Americium-241 alpha source with leakage current (“dark current”) subtracted away. Right: Plot showing current enhancement of the same three devices under 10V bias exposed to neutrons at the NPL thermal pile. Legend in this plot corresponds to both graphs. Time exposed to air significantly above 10 day settling period.
Alpha tests NPL site visit (using thermal pile)
10 V bias

## Slide 13
NDI Polymers: Neutron detection
Figure 10: Left: Plot showing current enhancement of three 4mm2 devices under 10V bias exposed to 370 kBq Americium-241 alpha source with leakage current (“dark current”) subtracted away. Right: Plot showing current enhancement of the same three devices under 10V bias exposed to neutrons at the NPL thermal pile. Legend in this plot corresponds to both graphs. Time exposed to air significantly above 10 day settling period.
NPL site visit (using thermal pile)

## Slide 14
Large-area OSC detector
Scaled up detector
  Simply take current method, make it larger
  Less resolution
  Two sizes done with 3 PNDI variants
Array of detectors
  Increase effective area
  Triangulate location of source
  Use a data acquisition device with multiple channels to simultaneously get results such as DAQ6510 with 7700 multiplexer
  Working on a single channel before scaling up once the setup is working
Figure 11: Keithley DAQ6510 with 7700 multiplexer containing 20 channels.

## Slide 15
Large-area OSC detector
Scaled up detector
  Simply take current method, make it larger
  Less resolution
  Two sizes done with 3 PNDI variants
Array of detectors
  Increase effective area
  Triangulate location of source
  Use a data acquisition device with multiple channels to simultaneously get results such as DAQ6510 with 7700 multiplexer
  Working on a single channel before scaling up once the setup is working
Figure 11: Keithley DAQ6510 with 7700 multiplexer containing 20 channels.

## Slide 16
Detector array
Capacitor bank to integrate charge over time, increase signal-to-noise ratio, higher standoff distance:
includes four unknowns to be appropriately obtained. Experimentation results in I ∼ 10 pA under a voltage bias V0 = 10V and time to walk past a device Δt ∼1s lead to choosing a C = 1 pF capacitor.
B
C
V0
A
Figure 12: Circuit diagram of single detector-capacitor unit. Switches and voltage readout done by multiple channels of a multiplexer. This diagram may be scaled to include multiple capacitors, detectors, and readouts, all working together.
Battery charges capacitor up to V0, which discharges through diode, resulting in lower voltage across capacitor when read out after 1s
A closed → A opened, B closed → B opened, C closed → repeat
Multiple “units” of Fig. 12 configuration can be made using more multiplexer channels to expand (1 unit = 4 channels out of 20)

## Slide 17
Detector array: Current circuit design
Multiplexer switches not high enough isolation resistance
Replaced with high isolation resistance optocoupled transistors working as switches
Multiplexer switches still used to control LEDs in optocoupled switches (red switches)
Effectively the same working principle as previous setup
Figure 13: Left: A phototransistor optically coupled to a gallium arsenide infrared-emitting diode. Above: Circuit diagram of single detector-capacitor system incorporating the optocoupled system shown on the left.
=
V
1V
V0
A
B
C
1pF

## Slide 18
Conclusions/Future trajectory
Organic materials can be used as alpha and neutron radiation detectors
Increasing the area of detectors increases the detection capability, but there is not enough data to draw any conclusions on a relationship. More sizes are incoming…
Incorporating boron-containing carborane into the backbone of PNDI(2OD)2T sensitises it to thermal neutrons
Papers: In process of writing neutron detection paper based on NPL results, followed by an alpha detection paper
Detector array: switches without leaking for single unit, followed by scaling up to multiple detectors
Simulation: investigating detection capabilities with respect to Soviet era cruise missile [6], IAEA historically reported illicitly trafficked materials [7]
[6] Fetter et al., Gamma-Ray Measurements of a Soviet Cruise-Missile Warhead, https://doi.org/10.1126/science.248.4957.828.
[7] IAEA, Combating Illicit Trafficking in Nuclear and other Radioactive Material, https://www-pub.iaea.org/MTCD/Publications/PDF/pub1309_web.pdf.

## Slide 20
Appendix: Fitting Parameters
Linear fit parameters for ΔI vs flux graphs:
Exponential fit parameters for ΔI vs V graphs:
a = Saturation current
b = 1/Characteristic V0

## Slide 21
Appendix: DAQ
0.03s
Each reading takes minimum ∼ 0.025s
∼V0 *
0.03s?
Above: Capacitor discharge graph. Right: Readings taken as quickly as possible with DAQ start around ⅓V0

## Slide 22
Appendix: Large vs Small PNDI(2OD)2T
AH020: 4mm2 sample taken to NPL
AH024: 36mm2 larger area sample

## Slide 23
Appendix: Results Plotter
Massive amount of data to sift through, made easier with automatic plotting GUI