## Slide 2: 3rd ALICE & VSC LS2 preparation meeting Update on production and preparation works
Josef Sestak, Giuseppe Bregliozzi, Chiara di Paolo, Jerome Gilles Chaure
on behalf of TE – VSC – BVO

## Slide 3: Update on production of VC2C
Qualification phase ongoing
Coating qualification samples
  Vacuum acceptance – Completed
  NEG coating – Completed
  NEG activation – Ongoing
We hope to give approval on final production by today or beginning of the next week.

## Slide 4: Update on production of VC2C
NEG coating process

## Slide 5: Update on production of VC2C
Activation for 24 hours at 200 °C
Cool-down by Friday 1st of June
Vacuum acceptance and NEG activation

## Slide 6: X-ray photoelectron spectroscopy (XPS) on the NEG coated samples
EDMS 1978615 v.1 by Holger NEUPERT
According to EDMS 630214 (standard control procedure for the assessment of the quality of TiZrV NEG coatings by XPS) the ALICE NEG coated samples are activated correctly.

## Slide 7: Peel-off tests on the minimized flanges
CLEANING:
Degreasing with NGL17/40 (US 5’+5’) during 1h of the two flanges.
Etching with a mix of phosphoric acid and nitric acid during 15min of one flange plus the welding.
ACTIVATION:
10 thermal cycles in vacuum performed (to simulate the life cycle of the chamber)
No visual sign of peel-off has been detected on the cone treated by etching
A very small mark detected on the end of the degreased cone, checked with SEM
Validation of the NEG coating of the test minimized aluminium flanges (EN AW-2219).

## Slide 8: SEM & EDS inspections
Etched cone
Spectrum 32
SECONDARY ELECTRON (MORPHOLOGY)
BACKSCATTERED ELECTRONS (COMPOSITION qualitative)
ENERGY-DISPERSIVE X-RAY SPECTROSCOPY (COMPOSITION quantitative)

## Slide 9: SEM & EDS inspections
Degreased cone
Spectrum 12

## Slide 10: ALICE chambers from Materion
About 10m of EN AW-2219 aluminium tubes and two bimetallic CF100 flanges (316L to EN AW-5083) are being shipped to CERN for production of ALICE LS2 central chambers.
The material will be cleaned and etched with the procedures for experimental chambers (EDMS 1674505) by beginning of the next week.
Presence of witness samples for XPS analysis during the treatments.

## Slide 11: Spare double bellows assembly
Bellows forming process
Production of bellows – completed
Welding – completed
Leak detection – completed
Final machining – next week
2 conform spare assemblies
Available quantity for production at Materion
3 + 2