## Slide 1
Testing of composite materials samples and structures
Corrado Gargiulo
14 October 2018

## Slide 2
Tests done to determine intrinsic Composite material properties such as modulus and strength for use in design and analysis
Tests done to determine quality or acceptability of specific Composite components after manufacturing

## Slide 3
FIBRE & RESIN
Micromechanical behaviour of a lamina
;
Estimation by the rule of mixtures
;
;
While these micromechanics equations are useful for a first estimation of lamina properties when no data are available, they generally do not yield sufficiently accurate values for design purposes. For design purposes, basic lamina and laminate properties should be determined using actual mechanical property testing.
fibres
resin
Human hair
1
2
lamina
+
=
You can check Vf experimentally if you know the fiber areal weight (FAW) and measure the cured-ply thickness (CPT)
How calculate and ?
;
we need ...
or
Removal of resin matrix from composite sample by either chemical digestion with acids or other chemicals (carbon fiber composites), or resin burn-off in a furnace (glass fiber composites) according to ASTM Standard D3171-09
How to measure and ?

## Slide 4
UNIAXIAL LOAD TESTS
on
composite laminate samples

## Slide 5
Constitutive equations for an ortotropic lamina, plane stress
LAMINA
1
2
2
1
X
Y
=
=
=
1
2
can be shown to be where the superscript T denotes the matrix transpose.
x
y
==
The relation between stress and strain is expressed in a coordinate system aligned to the fibres, through a certain number of elastic parameters
The lamina is used in a laminate with a certain angle, the elastic relation can then be rotated to be expressed respect to a common reference system
Ѳ
Determined elastic properties enter in the constitutive relation (follow the red)

## Slide 6
ASTM D3039/D3039M, EN 2561, EN 2597
±45◦C -axis
90◦C -axis
0◦C -axis
E1 , , XT
x
y
TEST
E2 , , YT
G12 , S
P
P
XC, YC
Lamina mechanical properties experimental determination
Compressive test
Shear test (alternative to ±45◦C -axis tensile test)
G12 , S
ASTM D5379
Thin pipe
Tensile tests
Iosipescu Shear Test
ASTM D3410
Celanese

## Slide 7
ASTM D3410
CELANESE
ASTM D3039/D3039M, EN 2561, EN 2597
ASTM D3518
TEST
Test specimens
Standard Test Method for In-Plane Shear Response of Polymer Matrix Composite Materials by Tensile Test of a ±45° Laminate
Standard Test Method for Tensile Properties of Polymer Matrix Composite Materials
Standard Test Method for Compressive Properties of Polymer Matrix Composite Materials with Unsupported Gage Section by Shear Loading
The most nearly ideal test from a theoretical standpoint involves torsion of thin walled filament wound tubes
MIL-HDBK-17

## Slide 8
TEST
=+
Han Tsai
Lamina mechanical properties experimental determination
E1
E2
G12
Most of laminated composites used in modern structures exhibit nonlinearity even under elastic conditions. Probably, the most evident case that reveals this effect is the plane shear test, where the stress strain diagram is apparently nonlinear directly from low values of load.
This test demonstrates the decrease in shear modulus during increase of shear stress and strain.

## Slide 9
2
1
X
Y
Nx
Ny
Nxy
Nyx
My
Mx
Myx
Mxy
X
Y
From lamina to LAMINATE
Cinematic equations
Constitutive equations
Equilibrium Equations
P
[B]=0 Decoupling between in-plane and out-of plane action *
A16=A26= 0 Decoupling between traction/compression and shear actions**
D16= D26= 0 Decoupling between flexural and torsional actions***
* at each lamina + Ѳ at +z correspond a lamina of the some thickness + Ѳ at – z Ex. [-45/+35/0/0/+35/-45]= [-45/+35/0]s
** at each lamina +Ѳ corresponds a lamina of the some thickness – Ѳ Ex. [+45/-45/0/0/+35/-35]
*** at each lamina +Ѳ corresponds a lamina of the some thickness – Ѳ at – z Ex. [+45/-35/0/0/+35/-45]
Lamina k

## Slide 10
Usually, the mechanical loads N and M , are known, so that the strains and curvatures can be obtained by multiplying these loads by the inverse of the compliance matrix. The strains and curvatures so obtained can be used to find the stresses in each lamina through the laminate stress-strain equations.
2
1
X
Y
Nx
Ny
Nxy
Nyx
My
Mx
Myx
Mxy
X
Y
From applied load on the laminate to lamina stress
Equilibrium Equations
P
Lamina k

## Slide 11
are experimentally determined material strength parameters
Failure criteria are quadratic empirical formulation
Tsai Hill, Hoffman, Tsai Wu, ...
Various failure criteria have been proposed to enable the onset of failure to be estimated
2
1
X
Y
Form lamina stress to lamina failure
Each stress component is tested against an allowable stress which is based on measured properties from unidirectional specimens. If the stress distribution in any layer exceed the Failure criteria, the layer is deemed to have suffered “First Ply Failure” .
The matrix stiffness values for that layer are then suppressed and the load which caused the failures is re-applied. If no further layer failures occur at this load. the loading procedure continues until more layer failures are detected, up to the failure of the last ply, “Last Ply Failure”.
1

## Slide 12
MULTI AXIAL LOAD TESTS
on
Composite laminate samples

## Slide 13
Multiaxial load: pressure, axial load, torsion
Biaxial load
a
a
h
h
a




a




h
h
a
a




a
h
h
Failure envelope surface
Hoop stress (MPa)
Axial stress (MPa)
Axial stress (MPa)
Shear stress (MPa)
Hoop stress (MPa)
Shear stress (MPa)
ref
Failure envelope curve
Pressure, axial load
Torsion, axial load
Torsion, pressure
Macro mechanics based failure theories applied to composite laminates under static loading conditions shows that there is a need to validate failure models for composite laminates under multiaxial loading conditions.
1

## Slide 14
6,11
6,11
42
300
54,22
45
40
130
45
40
0,86
t
a
[±]
[+35/-35/+35/-35]
[+55/-55/+55/-55]
[+75/-75/+75/-75]
Specimens production by filamnet winding
Conical reinforce to avoid stress concentration at the clamping area
Without conical reinforcement
l =130mm
r =42mm
t = 0.86mm
Without conical reinforcement
TEST
Test specimens

## Slide 15
Hoop stress
Axial stress
Shear stress
X
R=cost
failure
P/F= cost
TENSION
COMPRESSION
Specimen
PRESS est
Pressure internal/est & axial load
PRESS int
F
oil
olio
TENSION
COMPRESSION
Mt
Press int
Mt/F= cost
Mt/P= cost
specimen
oil
Pressure internal & axial load & torsion
F
Experimental set-up and procedure
TEST

## Slide 16
Failure prediction; Failure envelope numerical
Failure criteria influence
Winding angle effect
Non linear shear stress strain influence
a
Axial stress
Axial stress
Hoop stress.
Hoop stress.
Procedure implemented in Finite Element Code
Hoop stress (Mpa)
Axial stress (Mpa)
Hoop stress (Mpa)
Axial stress (Mpa)

## Slide 17
Experimental test: failure
55° axial compression
35° axial compress
75° axial compression
55° axial traction 7800 N
55° internal press 260 bar
55° ext press 25 bar
75° ext pressure
55°
Test results
Hoop stress
Axial stress
1
Composite structural behavior prediction: failure
Net Theory
Reference

## Slide 18
TESTS
on
HEP composite structures

## Slide 19
Human hair
~5µm mech
~ 10 µm therm
Carbon
filament
Use of Composite material in HEP mainly address requirements on
… stiffness…
… thermal management
Thermal Pyrolytic Graphite: Thermal management material with very high thermal conductivity and flexibility
E [GPa] | Xt [GPa] | HT fiber
240 | 4,4 | 
Carbon Fleece: continuous-strand mat finished with a chemical binder to hold fibers in place. Filament diameter= 5µm, th=20 µm, 8g/m2.
20 µm
 | Filaments [K=1000] | E1 [GPa] | Xt /Xc [MPa] | E2 [GPa] | Yt [MPa] | K [W/mK] | CTE [10-6K-1]
K13D2U [0] fibre | 2K | 935 | 3688 |  |  | 800 | -1,1
K13D2U [0] prepreg | 2K | 563 | 1800/340 | 6 | 25 | ~450 | -1,2 / 61
Carbon Unidirectional Prepreg: Ready to mold or cure material in sheet form which contains fiber all aligned in one direction. Filament diameter=11 µm
 | Filaments [K=1000] | Tex [g/km] | E [GPa] | Xt [GPa] | K [W/mK] | CTE [K-1]
M60j | 3K | 103 | 588 | 3,92 | 151 | -1,1x 10-6
M55j | 6K | 218 | 540 | 4,02 | 155 | -1,1x 10-6
Carbon Roving: Bunches of filament parallel to each other. Filament diameter=5 µm
45 (g/m2) FAW
 | Thick. [µm] | Density [g/cm3] | K pl [W/mK] | K th [W/mK]
Amec FGS_003 | 30 | 1.6 | 1500 | 15
Typical Carbon Composite material used in HEP
K thousand
of filament in a fibre tow
M60J
K13D2U
Mech
fibre
Therm
fibre
Carbon «thermal fibres» are thicker and stiffer, they break if bent to minimum radius

## Slide 20
290 mm , 1.7 gram
ALICE ITS Inner Barrel
ITS Inner Barrel
3 layers
Array of MAPS chip
FPC
Manual lay-up on mould 1: Cfleece/K13D2U 90°/Cfleece
Manual lay-up on mould 2: Pipes/Cpaper/Cfleece
Mould 1 and 2 closure
Curing at 24°C for 24h
Post Curing at 125°C for 3h
Remove pipes mandrels @ 80°C
Cold Plate Finishing
Locate the Cold Plate in the winding moulds
Place the three vertex M55J longitudinal threads
Wind with M60J
Cure at 24°C for 24h
Remove inside mandrel
Cut wound thread at moulds interfaces
Space Frame Finishing
Connectors gluing
Hydraulic Fitting gluing
Typical Carbon Composite structure used in HEP
Receipt
Non standard use of composite material tailored to fulfil requirements of minimum material, high stiffness and high thermal conductivity

## Slide 21
1.5 m, 35 gram
1.5 kg
1.5mm
Bending test
Sine sweep test & Random vibration
Beam with Concentrated Mass:
Mile’s equation SDOF, Constant PSD input (P value),
damping ratio
Bending test results
Characterization test of HEP composite structure
Type of fixation |  | a
Both ends free | concentrated load | a=48
Both ends fixed | concentrated load | a=192
ASTM RUM40%
…to validate stiffness
3D Scanning Vibrometry System
Touchless (fibre bragg grating, laser scan ) deformation measurement
dynamic
static

## Slide 22
Inlet
Outlet
Tin=18.25 °C
Thermal Test: operative mode, start-up, alternatives modes
Inlet
Outlet
Δl resolution: 0.125 nm / 1.25 nm
Composite Thermal Expansion
Characterization test of HEP composite structure
operative condition
during start up
Tin=18.25 °C
Composite Thermal Management
measured by LVDT
MME
x2 speed
24.1 0C
18.2 0C
23 0C
18 0C

## Slide 23
Experimental determination of Carbon Composite material properties is key for a correct prediction of the structure behavior, as well the understanding of their use in the calculation
For Composite, as the “material” is produced at the same time of the “final product”, it is often necessary that the manufacturer characterizes it own material
Characterization and Qualification of the final product, in particular for ultra light weight structure, often requires specific test procedures and equipment to avoid that the measure is affected by the test itself
CONCLUSION

## Slide 24
Back up

## Slide 25
Subscript | Meaning
1, 2, 3 | ply directions
x, y, z | laminate directions
f | fiber property
m | matrix property
v | void
c | compression
t | tension
Property | Meaning
E | tensile modulus
G | shear modulus
ν | Poisson ratio
X | tensile strength fibre direction
Y | tensile strength ⊥ fibre direction
S | shear strength
ρ | volume fraction
α | coefficient of thermal expansion
β | coefficient of moisture expansion
V | volume fraction
M | mass fraction
FAW | fiber areal weight
PAW | prepreg areal weight
CPT | cured ply thickness