## Slide 1
Sam Posen, Fermilab SRF Team
TTC Topical Workshop on Flux
9 November 2018
CERN
Experimental Study of Flux Expulsion and Cold Work

## Slide 2: Heavy deformation degrades expulsion behavior
Heavy tuning
Influence of stress/dislocations?
Tantalizing hint that cold work plays a major role in flux expulsion
This presentation presents new results from an experiment to follow up on influence of cold work
From SRF 2017

## Slide 3: Large Grain Experiment
Large Grain Ingot
Cut 2 slices, 3 mm thick
1-cell 1.3 GHz cavity fabrication (now)
Cut 2 slices, 5 mm thick
Roll to 3 mm thickness
Cut down to disc size
1-cell 1.3 GHz cavity fabrication (now)
Large grains, low dislocation content
Large grains, high dislocation content
Experiment designed to distinguish effects of dislocations independent of grain size: does LG material inherently expel strongly?

## Slide 4: Wire EDM from Ingot
2 sheets 3 mm thick -> BCP + send direct to cavity vendor
2 sheets 5 mm thick -> BCP + send for rolling

## Slide 5: Sheets Rolled by ATI
Thickness reduction from 5 mm to 3 mm (area increase)
Cold worked so that no longer flat even after roller levelling
Material sent to cavity vendor
Photo courtesy ATI

## Slide 6: Half Cell Forming
RI received the sheet material and began deep drawing
The non-rolled material formed half cells well
The rolled material tore during the forming process
This is not entirely unexpected as the material was not annealed at any point during the manufacturing process
Photos courtesy RI

## Slide 7: Repair Developed by RI
RI used the extra rolled material to plug the holes in the half cells
Some extra beam welds, but should still be representative!
ATI
Photos courtesy RI
Extra material

## Slide 8: Completed Cavities
Photos courtesy RI

## Slide 9: Expulsion Measurement
Assembled as-received cavities with only vacuum connections (no RF)
Cavities cooled quickly through range 150-100 K to avoid formation of hydrides
Thermal cycles to measure expulsion

## Slide 10: Material
Cavities are made:
  From the same ingot
  By the same vendor
  And both have large grains
Key difference:
  Cold work
Non-rolled
Rolled
Orientation Map
Local Misorientation Angle
Cold work shows in both maps

## Slide 11: Expulsion Measurement
Non-rolled
Rolled sheets

## Slide 12: Expulsion Measurement
Non-rolled
Rolled sheets
Cold worked material very strong trapping
Incomplete expulsion for both LG cavities

## Slide 13: Q vs E Curves after Bulk EP + 600 C 3 hr + Light EP
TE1RILG001
(non rolled)
TE1RILG002
(rolled)
Note: processing quenches at 2 K led to some Q0 degradation

## Slide 14: Expulsion Measurement
Non-rolled
Rolled sheets
Low expulsion even after 800 C 3 hour heat treatment

## Slide 15: Conclusions
Strong trapping behavior is possible with large grain material even after 800 C 3 hour heat treatment, especially for rolled material
These results contribute to a body of evidence that cold work in SRF-grade niobium is crucially important to determining the flux trapping behavior
Implicates rolling steps in producing material that requires very high temperature heat treatment to have acceptable flux expulsion
Further motivate studies of dislocations in strongly trapping material
See also P. Dhakal (JLab), TTC Topical 2017