## Slide 1: EuroCirCol Cosθ 16 T dipole
BARBARA CAIFFI
G. Bellomo, P. Fabbricatore, S. Farinon, s. MARIOTTO, A.Pampaloni A. M. RICCI, M. Sorbi, M. STatera
Presented @ FCC week
9-13 April 2018
Amsterdam

## Slide 2: Outlook
Magnetic design
  2D and 3D magnetic model
  Field qualty & peak field
Mechanical design
  VM stress
  Contact pressure to the pole
  Preliminary 3D mechanical design
Conclusions and Future Work

## Slide 3: Design parameters

## Slide 4: Magnetic model
Bpeak (HF cable)= 16.44 T
Wedge = 0.86 mm
 | HF Cable (inner) | LF Cable (outer)
Strand number | 22 | 38
Strand diameter | 1.1 mm | 0.7 mm
Bare width | 13.2 mm | 14 mm
Bare inner thickness | 1.892 mm | 1.204 mm
Bare outer thickness | 2.007 mm | 1.3261 mm
Insulation | 0.15 mm | 0.15 mm
Keystone angle | 0.5° | 0.5°
Cu/Ncu | 0.82 | 2.1
Operating current | 11390 A | 11390 A
Operating point on LL (1.9 K) | 86 % | 86 %
Bpeak (LF cable) = 12.8 T
Number of turns:
Layer 1: 13
Layer 2: 19
Layer 3: 29
Layer 4: 39
Tot: 200/ap.
B[T]
Jc[A/mm2]
LF cable
HF cable
Load Line
1.9 K

## Slide 5: Magnetic model
Fringe field
Fringe field along r
Distance from yoke [mm]
B[T]
Outer yoke radius: 300 mm
B=0.1 T @ 245 mm from the yoke
(545 mm from the center)

## Slide 6: Field Quality (geometrical + iron saturation)
Chart: B[T]
| 0.85569300000000004 | 1.3976280000000001 | 1.9395309999999999 | 2.4808050000000001 | 3.0212859999999999 | 3.561356 | 4.1007819999999997 | 4.6366759999999996 | 5.1657390000000003 | 5.6851989999999999 | 6.1959910000000002 | 6.7016799999999996 | 7.2037680000000002 | 7.7030450000000004 | 8.1999549999999992 | 8.6949609999999993 | 9.1882929999999998 | 9.6800949999999997 | 10.170500000000001 | 10.659452 | 11.147188999999999 | 11.634017999999999 | 12.120164000000001 | 12.60568 | 13.090630000000001 | 13.575092 | 14.059108999999999 | 14.542721999999999 | 15.025963000000001 | 15.508823 | 15.991307000000001
b2 | -2.2004 | -2.2001 | -2.2006 | -2.2122 | -2.2375 | -2.2699 | -2.3581 | -3.1553 | -4.9044 | -7.6185 | -10.966 | -14.23 | -17.271 | -20.136 | -22.848 | -25.447 | -27.963 | -30.424 | -32.84 | -35.245 | -37.618 | -39.912 | -42.105 | -44.198 | -46.201 | -48.114 | -49.947 | -51.703 | -53.392 | -55.023 | -56.604
b3 | -7.2056 | -7.205 | -7.2003 | -7.1346 | -7.0267 | -6.9234 | -6.813 | -6.7107 | -6.5282 | -6.1656 | -5.7047 | -5.1615 | -4.5791 | -3.9957 | -3.4282 | -2.8944 | -2.4011 | -1.949 | -1.5359 | -1.1594 | -0.81633 | -0.49981 | -0.20695 | 0.065638 | 0.31942 | 0.55574 | 0.77603 | 0.98134 | 1.1725 | 1.3506 | 1.5163
Chart: B[T]
| 0.85569300000000004 | 1.3976280000000001 | 1.9395309999999999 | 2.4808050000000001 | 3.0212859999999999 | 3.561356 | 4.1007819999999997 | 4.6366759999999996 | 5.1657390000000003 | 5.6851989999999999 | 6.1959910000000002 | 6.7016799999999996 | 7.2037680000000002 | 7.7030450000000004 | 8.1999549999999992 | 8.6949609999999993 | 9.1882929999999998 | 9.6800949999999997 | 10.170500000000001 | 10.659452 | 11.147188999999999 | 11.634017999999999 | 12.120164000000001 | 12.60568 | 13.090630000000001 | 13.575092 | 14.059108999999999 | 14.542721999999999 | 15.025963000000001 | 15.508823 | 15.991307000000001
b4 | -0.080525 | -0.080545 | -0.080586 | -0.08081 | -0.081129 | -0.08168 | -0.084127 | -0.11024 | -0.16543 | -0.25077 | -0.35417 | -0.4482 | -0.52958 | -0.59981 | -0.66113 | -0.71548 | -0.7648 | -0.81008 | -0.85191 | -0.89097 | -0.92738 | -0.96091 | -0.99191 | -1.0206 | -1.0473 | -1.0722 | -1.0954 | -1.1171 | -1.1375 | -1.1566 | -1.1746
b5 | -0.70626 | -0.70626 | -0.70626 | -0.70609 | -0.70586 | -0.70576 | -0.70648 | -0.71086 | -0.72118 | -0.7405 | -0.76392 | -0.78599 | -0.80563 | -0.82308 | -0.83865 | -0.8526 | -0.86525 | -0.87684 | -0.88755 | -0.89756 | -0.9069 | -0.91557 | -0.92361 | -0.93108 | -0.93805 | -0.94455 | -0.95063 | -0.95632 | -0.96165 | -0.96666 | -0.97137
b6 | -0.0011577 | -0.0011574 | -0.0011557 | -0.0011466 | -0.0011311 | -0.0011202 | -0.0011392 | -0.0014574 | -0.0020571 | -0.0031288 | -0.0045001 | -0.0056599 | -0.0065902 | -0.0073614 | -0.0080172 | -0.0085805 | -0.0090668 | -0.0094955 | -0.0098782 | -0.010222 | -0.010533 | -0.010812 | -0.011068 | -0.011301 | -0.011517 | -0.011718 | -0.011906 | -0.012081 | -0.012246 | -0.012398 | -0.012539
b7 | 1.6673 | 1.6673 | 1.6674 | 1.6678 | 1.6685 | 1.6692 | 1.6699 | 1.6718 | 1.6754 | 1.6812 | 1.6884 | 1.6957 | 1.7029 | 1.7097 | 1.7162 | 1.7224 | 1.7282 | 1.7337 | 1.7388 | 1.7438 | 1.7485 | 1.753 | 1.7572 | 1.7611 | 1.7649 | 1.7684 | 1.7718 | 1.775 | 1.778 | 1.7809 | 1.7836
b8 | -1.2471e-05 | -1.2466e-05 | -1.2483e-05 | -1.2568e-05 | -1.2753e-05 | -1.2982e-05 | -1.3618e-05 | -1.9639e-05 | -2.8863e-05 | -4.8328e-05 | -7.3406e-05 | -9.1497e-05 | -0.00010402 | -0.00011327 | -0.00012057 | -0.00012601 | -0.00012967 | -0.00013221 | -0.00013403 | -0.00013541 | -0.00013641 | -0.00013717 | -0.0001378 | -0.00013832 | -0.00013883 | -0.00013935 | -0.00013989 | -0.00014039 | -0.00014093 | -0.00014145 | -0.00014196
b9 | 1.3522 | 1.3522 | 1.3522 | 1.3526 | 1.3532 | 1.3538 | 1.3544 | 1.3559 | 1.3589 | 1.3636 | 1.3695 | 1.3755 | 1.3813 | 1.3869 | 1.3923 | 1.3973 | 1.402 | 1.4065 | 1.4107 | 1.4148 | 1.4186 | 1.4222 | 1.4256 | 1.4289 | 1.4319 | 1.4348 | 1.4375 | 1.4401 | 1.4426 | 1.4449 | 1.4471
B | b2 | b3 | b4 | b5 | b6 | b7 | b8 | b9
16T | -56.6 | 1.5 | 1.2 | -1.0 | -0.01 | 1.8 | -0.001 | 1.4

## Slide 7: 3D magnetic end design
Roxie
Opera
Connection side
Side opposite to connection

## Slide 8: 3D magnetic end design
Bpeak = 16.39 T (Opera)
16.44 T (Roxie 3D)
16.44 T (Roxie 2D)
Good agreements between
2D and 3D models
Peak field in straight section

## Slide 9: 3D magnetic end design
NORMAL 3D INTEGRAL RELATIVE MULTIPOLES
End of yoke
B | b2 | b3 | b4 | b5 | b6 | b7 | b8 | B9
16T | -65.3 | 2.1 | -1.2 | -0.6 | -0.01 | 1.7 | -0.0002 | 1.4
Iron Length: 890 mm
Magnetic length:1032 mm
Physical length: 1100 mm

## Slide 10: Mechanical constrains
Stress in the conductor < 150 MPa @ RT, < 200 MPa @ 1.9 K
Stress on mechanical structure < yield strength
No detachment between coil and pole

## Slide 11: Lorentz Forces
RH | FX sum (MN) | FY sum (MN) | Fq sum (MN) | sq sum (MPa)
1 | 2,1 | -0,1 | -1,2 | -90,5
2 | 2,3 | -0,5 | -1,6 | -120,4
3 | 2,0 | -1,1 | -1,8 | -125,9
4 | 0,3 | -2,0 | -2,1 | -145,8
Total RH | 6,8 | -3,7 | -6,7 | -118,0
LH | FX sum (MN) | FY sum (MN) | Fq sum (MN) | sq sum (MPa)
1 | -2,1 | -0,2 | 1,3 | -92,9
2 | -2,4 | -0,6 | 1,7 | -125,9
3 | -2,2 | -1,2 | 2,0 | -136,9
4 | -0,7 | -2,3 | 2,4 | -166,9
Total LH | -7,4 | -4,2 | 7,3 | -127,9
total winding | -0,6 | -7,9 | 0,6 | /
In cosq configuration, Lorentz forces push the coil:
Outward in the radial direction
Toward the midplane in the azimuthal direction

## Slide 12: Cosq mechanical layout
Riron = 300 mm
50 mm
20 mm
Inter-beam = 204 mm
40 mm
110 mm
Yoke outer diameter: 600 mm
Al alloy shell thickness: 50 mm
SS shell thickness: 20 mm
Outer magnet diameter: 740 mm
Inter-beam distance: 204 mm

## Slide 13: ANSYS mechanical models
Conductor
Copper wedges
Steel pad
Titanium pole
Iron yoke
Aluminum shell
Outer steel shell

## Slide 14: Mechanical analysis
Conductor
Copper wedges
Steel pad
Titanium pole
Iron yoke
Aluminum shell
Outer steel shell
Glued contact elements

## Slide 15: Mechanical analysis
Conductor
Copper wedges
Steel pad
Titanium pole
Iron yoke
Aluminum shell
Outer steel shell
Sliding permitted contact elements

## Slide 16: Mechanical analysis
Conductor
Copper wedges
Steel pad
Titanium pole
Iron yoke
Aluminum shell
Outer steel shell
Sliding and detachment permitted contact elements

## Slide 17: Mechanical analysis
Step 1: assembly (key insertion)
Step 2: assembly under compression of SS shell 0.2 mm per side cut on midplane
Step 3: cooling down
Step 4: energization to 16 T (application of Lorentz forces to the conductor elements)
Conductor
Copper wedges
Steel pad
Titanium pole
Iron yoke
Aluminum shell
Outer steel shell

## Slide 18: Contact Pressure at Pole
Contact pressure [Pa]
Contact pressure increases after cool down (Al + SS shell shrinking)
Pcont,med > 0 for 1° layer after energization at 16T
ASSEMBLY
COOL DOWN
16 T
LEFT
RIGHT
<Pcont,1°layer (16 T)> = 2 MPa
Pcont,1°layer (16 T)|mid-point = 1 MPa
<Pcont,1°layer (16 T)> = 2 MPa
Pcont,1°layer (16 T)|mid-point < 1 MPa

## Slide 19: VM stress in the conductors
VM stress [Pa]
ASSEMBLY
COOL DOWN
16 T
sVM,max = 145 MPa
sVM,max = 192 MPa
sVM,max = 199 MPa
VM stress far below current degradation limit (150 MPa @ RT -200 MPa @ 1.9K)
Localized hot spot due to wedge edges after cooling down
After energization, the high stress region is located in the fourth layer (low field region), VM(peak field region)< 50 MPa
LEFT
RIGHT

## Slide 20: VM stress in the mechanical structures
ASSEMBLY
MATERIAL | Stress limit [MPa]
 | RT
Austenitic steel (316LN) | 350
Al7075 | 480
Ferromagnetic iron | 230
Ti6Al4V | 800
sVM,max = 749 MPa

## Slide 21: VM stress in the mechanical structures
COOL DOWN
MATERIAL | Stress limit [MPa]
 | 1.9 K
Austenitic steel (316LN) | 1050
Al7075 | 690
Ferromagnetic iron | 720
Ti6Al4V | 1650

## Slide 22: VM stress in the mechanical structures
ENERGIZATION
MATERIAL | Stress limit [MPa]
 | 1.9 K
Austenitic steel (316LN) | 1050
Al7075 | 690
Ferromagnetic iron | 720
Ti6Al4V | 1650

## Slide 23: 3D mechanical design
3D mechanical ANSYS model, very preliminary

## Slide 24: 3D mechanical design
3D mechanical ANSYS model, very preliminary
End spacers ( from Roxie)
Straight section
Conductor ends
Wedges
Conductors

## Slide 25
3D mechanical design
06/07/18
FCC Week 2018 Costheta 16T dipole
25
3D mechanical ANSYS model, very preliminary
VM stress after cool down
Average VM stress in reasonable agreement with 2D results
Work still on going
Still open issues ( e.g. how to treat proprieties of conductor ends? Isotopically?)

## Slide 26
3D mechanical design
06/07/18
FCC Week 2018 Costheta 16T dipole
26
After assembly and cool down...
VM stress in straight section of conductor in agreement with 2D
End design still not optimized from mechanical point of view

## Slide 27: Conclusions
We have designed a 4 layer cosine-theta bending dipole for the FCC, according to the EuroCirCol constraints:
  Able to produce 16 T bore field
  Operation point on the load-line is 86% at 1.9 K
  Good field quality (2D and 3D)
  B&K mechanical structure able to keep azimuthal pre-stress, within stress limits
The magnet is mature enough to go in a more advanced design phase:
  3D mechanical analysis for longitudinal pre-stress
  Finalization of the harmonic optimization (b2 and iron saturation)
  Starting the development of a prototype

## Slide 28: Thank you

## Slide 30: Displacements Undeformed - Assembly
X displacement [m]
MAX X DISP: 392 mm
Full pole
Notch in the pole
MIN X DISP: -167 mm
MAX X DISP: 389 mm
MIN X DISP: -10 mm

## Slide 31: Displacements Assembly - Cool Down
MAX X DISP: 61 mm
Full pole
Notch in the pole
MIN X DISP: -635 mm
MAX X DISP: 61 mm
MIN X DISP: -640 mm
X displacement [m]

## Slide 32: Displacements Cool Down- Energization 16T
MIN X DISP: -134 mm
Full pole
Notch in the pole
MAX X DISP: 401mm
MIN X DISP: - 85 mm
MAX X DISP: 249 mm
Displacement [m]

## Slide 33: Cosq mechanical layout
Yoke outer diameter: 600 mm
Al alloy ring thickness: 75 mm and 50 mm
SS shell thickness: 20 mm
Outer magnet diameter: 750 mm and 740 mm
New pole design
Inter-beam distance: 204 mm
Alluminum shell
Alluminum + SS shell

## Slide 34: Persistent Currents
50 µm filament diameter
-50 units on b3 at injection
+8 units on b5 at injection
No effect on b2
Negligible effect at operation current

## Slide 35: Persistent Currents
Possible solution: iron on the beam pipe?
Field quality to be optimized