## Slide 1
US Magnet Development Program
Lawrence Berkeley National Laboratory
CCT5 Impregnation Process
10/08/2018

## Slide 2: Epoxy Impregnation of Individual CCT Layers has been Implemented for CCT5
CCT4 magnet reached 86% of short sample critical current but required significant training
Changes to CCT5 are focused on reducing training due to epoxy failure at the layer-to-layer interfaces
  Tougher epoxy has been introduced (FSU mix-61 instead of CTD-101K)
  New method for pre-loading and mechanically coupling the layers (bend-and-shim)
Epoxy impregnation of individual layers has several advantages
  Individual layer impregnation enables bend-and-shim assembly method
  Methods for individual layer impregnation are scalable to long lengths and require minimal tooling
  Most materials required for impregnation are inexpensive consumables
  May be possible to disassemble magnet after test and replace layers for accelerated R&D

## Slide 3: CCT3/CCT4 Assembly and Impregnation Process
Layer 2
Layer 1
G10 slip plane
Linear driver
Step 1. Assemble Layers
3
Step 2. Layers 1+2 into shell
Step 3. all impregnated together
with the shell used as tooling
Reacted coils are assembled together with G10 shim between layers
Coils are inserted into the Aluminum shell and the entire assembly is vacuum impregnated with epoxy
Areas of unfilled epoxy remain between the layers
  G10 shim has to be substantially thinner than gap between layers due to distortion of the mandrels during heat treatment

## Slide 4: CCT5 Assembly Process
Layer 1 / 2 Assembly
  Layer 1 is inserted into layer 2 and centered with end shims
  Shims and glass filled Kapton bags are inserted on both sides of the midplane
  Kapton bags are filled with epoxy
Coils / Shell Assembly
  Coil / Shell assembly is inserted in press
  Shell is deformed vertically (horizontal gap opens by 0.1 mm)
  Shims and glass filled bags are inserted on the midplane
  Kapton bags are filled with epoxy and allowed to cure
  Force is released from the press
layer 1
layer 2
shell
epoxy filled Kapton bag
Force Release After Cure
Applied Force
Directional
Pre-Load on Coils
Notes: Angular coverage of Kapton bag is chosen so that all areas with outward radial Lorentz force are covered

## Slide 5: New Method for Coupling of Individually Potted Layers (Bend-and-Shim)
Contact location between layers is controlled by using shims and Kapton bags that are filled with glass and epoxy
  Allows for control of contact location
  Fracture in interface epoxy can not propagate to the coil
  Improved cooling at the pole regions from direct contact with LHe
Directional preload to reduce energized stress can be applied by bending layers or shell, filling and curing epoxy in bent state, releasing bending pressure
Kapton Bag and Shims
Shims and Bag Inserted Between Layers
Kapton Bag Filled with Cured Epoxy was Extracted

## Slide 6: CCT5 Is Impregnated With FSU Mix-61 Due to its Higher Toughness
Mix 61 has excellent performance in thermal shock tests when compared to CTD-101K
Stress-Strain curve of Mix-61 has been measured at room temperature
CTD-101K after one thermal cycle to 77 K
Mix-61 epoxy after one thermal cycle to 77 K
Extensive cracks
No crack
Room Temperature, test standard - ASTM-D638
NHMFL
61 mix
F
F
Courtesy of T. Shen and S. Yin
Notes: Mix 61 is cured at 100 degrees C for 24 hours

## Slide 7: Further Studies And Development of High Performance Epoxies Are Ongoing at LBNL
Mechanical testing at 77K
Viscosity test
High specific heat epoxies by adding fillers

## Slide 8: Impregnation Process for CCT5
Coils are impregnated with mix 61 epoxy
Did not deviate too far from usual LBNL potting procedures to avoid delaying CCT5 test
  Use vacuum vessel for impregnation
  Seal coil ends with Aluminum end plugs as with CCT3/4
  Sealing of external coil surface is done with inexpensive consumable materials
Use common techniques and materials from vacuum bag process
  Peel ply to minimize epoxy on surface of mandrel
  Flow media for epoxy flow
  Use Nylon vacuum bag
  Use shrink tape to compress the compress the bag and flow media layer tightly onto the mandrel

## Slide 9: Potting Tooling and Release Film
Holes for heaters
O-ring Seals
Holes for Leads
Peel-Ply
(Teflon Coated Fiberglass)
Heater Slug is inside of coil bore

## Slide 10: Flow Media and Vacuum Bag
Teflon strip to separate seam after potting
Vacuum Bag
(Seam Sealed with Tape)
Flow Media
Sealing tape for seal to end plug

## Slide 11: Shrink Tape Applies Pressure
Coil is wrapped with shrink tape and heated in oven
Coil after removing from oven

## Slide 12: Coil Impregnation in Vacuum Vessel
Coil Inside of Vacuum Vessel
Coil after removing flow media and Peel Ply
Epoxy Inlet

## Slide 13: Impregnation of CCT5 1 Meter Long Coils
CCT5 coils were successfully impregnated with new process
Instrumentation traces were included in the impregnation
Instrumentation Trace After Potting
V taps
Heater
Thermometer
Wrapped Coil After Impregnation

## Slide 14: Bend and Shim Assembly Process
Bend and shim assembly process was performed after coil impregnation
CTD 528 epoxy was used due to cryogenic toughness, sufficiently long working life, and near room temperature cure
CCT Layers after Filling and Curing of Epoxy Filled Kapton Bag
Shell and Coils in Press After Epoxy Cure
Notes: CTD 528 was cured at 45 degrees C for 24 hours

## Slide 15: Conclusions
New assembly process for CCT magnets has been developed with goal to reduce training due to layer-to-layer interfaces
Method for epoxy impregnation of individual CCT layers has been developed
  Minimal tooling
  Scalable to longer lengths
Methods have been applied for CCT5, the next magnet in CCT 2-layer series at LBNL