## Slide 1: Effect of transverse stress applied during reaction heat treatment on the stiffness of Nb3Sn Rutherford cable stacks Felix Wolf1,2, Friedrich Lackner1, Christian Scheuerlein1, Daniel Schoerling1, Davide Tommasini1 1 European Organization for Nuclear Research (CERN), CH 1211 Geneva 23, Switzerland 2 TU Bergakademie Freiberg, D 09599 Freiberg, Germany
Second workshop “Nb3Sn Rutherford cable characterization for accelerator magnets”
11th October 2018, CEA, Paris, France

## Slide 2: Content
The samples
Stress-strain measurements in tension and in compression
Determination of elastic modulus from stress-strain curves
Setups used for stress-strain measurements in compression and validation tests
Axial tensile stress-strain measurements of Nb3Sn wires
Estimation of axial ten stack stiffness by the rule of mixtures
Effect of epoxy volume fraction on axial ten-stack stiffness
Effect of unloading stress on ten-stack stiffness
Effect of epoxy volume fraction on transverse ten-stack stiffness
Load direction dependency of the ten-stack stiffness
Comparison of ten-stack and 11 T coil segment stiffness

## Slide 3: The samples
All samples are made of Nb3Sn 11 T dipole Rutherford cable.
Cube samples with approximate edge lengths of 15 mm and with parallel surfaces enable compression tests in axial, transverse and radial directions.
Ten-stack samples reacted in a dedicated mould with three different levels of compaction, due to a clearance variation.
11 T dipole coil block machined out of the coil after magnet cold test, containing adjacent coil wedges to compensate the keystone angle.
The samples are impregnated with an epoxy resin system, so-called CTD-101K from Composite Technology Development, Inc.
All samples have a Mica and S2 glass insulation.
Transverse
Axial
Radial
Nb3Sn Rutherford cable sample types: (a) ten-stack, (b) 11 T dipole coil segment and
(c) non impregnated ten-stack (d) Sample orientations.
a)
b)
c)
d)

## Slide 4
(a) Metallographic cross section of 11 T dipole coil CR107 with six conductor blocks. Courtesy M. Meyer, CERN. (b) Extracted conductor block sample used for compression tests. Courtesy CERN central workshop team.
11 T dipole conductor block segment

## Slide 5: Stress-strain measurements in tension and in compression
Comparison of tensile and compressive stress-strain curves of Ti-6Al-4V and DISCUP up to 0.5 % strain [1].
Tensile tests:
Flat tensile test samples DIN 50125-E 3mm × 8mm × 30mm
Clip on extensometer with 25 mm gauge length
Compression tests
Cylinder sample  10 mm, height 15 mm (small ratio height to diameter in order to sample buckling)
  Use lubricant between contact surfaces to limit friction artefacts
Clip on extensometer with 8 mm gauge length
  The direct strain measurement using extensometers is crucial in order to avoid an influence of the load frame compliance.
  For metals differences between tensile and compression stress-strain curves are usually small.
[1] IEEE Trans. Appl. Supercond., 27(4), (2017), 4003007
Notes: Mechanical Properties of the HL-LHC 11 T Nb3Sn Magnet Constituent Materials
Christian Scheuerlein; Friedrich Lackner; Frederic Savary; Birgit Rehmer; Monika Finn; Patrick Uhlemann
IEEE Transactions on Applied Superconductivity Year: 2017, Volume: 27, Issue: 4
Article Sequence Number: 4003007
Referenced in:
IEEE Journals & Magazines

## Slide 6: Determination of elastic moduli from stress-strain curves
Comparison of stainless-steel 316LN and Ti-6Al-4V stress-strain curves. For 316LN a precise measurement of elastic modulus from the initial loading curve is not possible [1].
Comparison of hard-drawn and annealed Cu wire stress-strain curves with unloading slopes for determination of the elastic modulus [1].
In favourable cases the elastic modulus can be determined from the initial linear slope of the stress-strain curve (e.g. for Ti-6Al-4V).
Many metals like Cu or stainless don’t exhibit linear elastic behaviour. For these metals the elastic modulus can be estimated from unloading stress-strain curves.
[1] IEEE Trans. Appl. Supercond., 27(4), (2017), 4003007
Notes: Mechanical Properties of the HL-LHC 11 T Nb3Sn Magnet Constituent Materials
Christian Scheuerlein; Friedrich Lackner; Frederic Savary; Birgit Rehmer; Monika Finn; Patrick Uhlemann
IEEE Transactions on Applied Superconductivity Year: 2017, Volume: 27, Issue: 4
Article Sequence Number: 4003007
Referenced in:
IEEE Journals & Magazines

## Slide 7: Test parameters for ten-stack sample compression tests
Two different setups have been used for compressive stress-strain measurements.
The sample strain in load direction was directly measured with calibrated clip-on extensometers.
Load plateaus were kept constant for one hour/
Load rate between plateaus was 50 N/s.
Stiffness is defined as the initial linear slope of the unloading engineering stress-strain curves.
Validation tests were performed with known materials (Ti-6Al-4V and Al 7075).
Good agreement of stress-strain results achieved with both compressive stress-strain measurement set-ups.
Notes: Why compressive test?
  Tensile test data are valid until the uniform expansion limit (necking) occurs
  Due to the complex material structure it is useful, to apply the load in procedure similar to the application
  Error range for small loads can be caused due to imperfection in the tool-Surface parallelism
  Compressive test does not indicate a characteristic yield strength
  Friction between tooling and sample surface can cause a barrelling of the sample

## Slide 8: Two setups used for stress-strain measurements in compression
Sample holder
Sample
Extensometer
Ten-stack sample with clip-on extensometer with 6 mm gauge length.
Reference measurement Ti-6Al-4V
Set-up at CERN
  Load measured with calibrated load cells (Burster type 8526)
  Strain measured with clip on extensometer (Epsilon 3442-006M-010-LT Class B-1 6mm gauge length)
Validation measurement:
  Cubic Ti-6Al-4V sample
  Determined E modulus: 117.4 GPa
  Literature E modulus: 115 GPa [1]
[1] IEEE Trans. Appl. Supercond., 27(4), (2017), 4003007

## Slide 9: Two setups used for stress-strain measurements in compression
Sample with clip-on extensometer with 12 mm gauge length installed in the load frame at StressSpec.
Extensometer
Sample
Sample holder
Reference measurement Al7075
Setup at MLZ StressSpec beam line
Load measured with calibrated load cells (HBM Typ 03, 50 kN)
Strain measured with clip on extensometer (Instron 2620-602 12 mm gauge length)
Validation measurement:
  Cubic Al7075 sample
  Determined E modulus: 72.7 GPa
  Lit: 71.7 GPa [2]
[2] Metals Handbook, Vol.2 ASM International 10th Ed. 1990.
Notes: Metals Handbook, Vol.2 - Properties and Selection: Nonferrous Alloys and Special-Purpose Materials, ASM International 10th Ed. 1990.

## Slide 10: Elastic modulus of RRP type Nb3Sn wire
Test performed with a tensile test machine “Inspekt table BLUE 05” from Hegwald & Peschke
Load measured with AST KPA-S load cell with a maximum load of 1 kN
Strain measured with a MTS clip-on extensometer 632.27F-21 with 25 mm gauge length
E is defined as the initial linear slope of the unloading curve.
Determined elastic modulus of the reacted RRP wire: 126 GPa
Reversible elastic strain
Irreversible plastic strain
Stress-strain curves measured at room temperature on a reacted RRP wire and its extracted filaments. [3]
[3] IEEE Trans. Appl. Supercond., 25(6), (2015), 8400605
Notes: Elastic Anisotropy in Multifilament hboxNb 3 hboxSn Superconducting Wires
C. Scheuerlein; B. Fedelich; P. Alknes; G. Arnau; R. Bjoerstad; B. Bordini
IEEE Transactions on Applied Superconductivity Year: 2015, Volume: 25, Issue: 3
Article Sequence Number: 8400605
Referenced in:
Cited by: Papers (3)
IEEE Journals & Magazines

## Slide 11: Estimation of the ten stack stiffness in axial direction from the wire and epoxy properties according to the Rule of Mixtures (ROM)
[4]
… Young’s modulus fibre (strand)
… Volume fraction fibre
… Young’s modulus matrix (epoxy impregnation)
… Volume fraction matrix
[3]
Sample | * (mm2) | ** (mm2) | (%) | (GPa)
1 | 175.7 | 236.6±0.33 | 74.3 | 94.6
2 | 175.7 | 241.3±0.24 | 72.8 | 92.8
3 | 175.7 | 252.4±0.18 | 69.6 | 88.9
* Determined with image analysis with a Zeiss Axio Imager optical microscope. Courtesy M. Crouvizier, EN-MME ** Determined with contact measurement |  |  |  | 
Sample |  |  |  | 
1 | 175.7 | 236.6±0.33 | 74.3 | 94.6
2 | 175.7 | 241.3±0.24 | 72.8 | 92.8
3 | 175.7 | 252.4±0.18 | 69.6 | 88.9
* Determined with image analysis with a Zeiss Axio Imager optical microscope. Courtesy M. Crouvizier, EN-MME ** Determined with contact measurement |  |  |  | 
Metallographic cross section of ten stack samples for the determination of the epoxy volume fraction by digital image analysis. Courtesy M. Crouvizier, EN-MME
Axial
Definition of axial sample orientation
[3] IEEE Trans. Appl. Supercond., 25(6), (2015), 8400605
[4] Mechanics of composite materials, Taylor and Francis, 1999
Notes: Mechanics of composite materials
Second edition
Robert M. Jones
Taylor and Francis, Inc. London 1999
Elastic Anisotropy in Multifilament hboxNb 3 hboxSn Superconducting Wires
C. Scheuerlein; B. Fedelich; P. Alknes; G. Arnau; R. Bjoerstad; B. Bordini
IEEE Transactions on Applied Superconductivity Year: 2015, Volume: 25, Issue: 3
Article Sequence Number: 8400605
Referenced in:
Cited by: Papers (3)
IEEE Journals & Magazines

## Slide 12: Comparison between stiffness in axial direction in tension (wire, Vstrand=100%) and compression (ten-stack)
Comparison of stress-strain curves of Nb3Sn wire (axial tension) and ten-stack samples (axial compression).
Wire (Vstrand=100%), E=126 GPa
Ten-stack Vstrand=69.6%, E= 94.1 GPa
(ROM estimate EComposite = 88.9 GPa)
Ten-stack Vstrand=74.3%, E= 99.5 GPa
(ROM estimate EComposite = 94.6 GPa)

## Slide 13: Stiffness comparison between experiment and rule of mixture estimation
Stiffness estimation of the axial and transverse compression with
stiffness dependence on Vwire and comparison with experiment.
[4]
[4]
Iso-strain condition
Iso-stress condition

## Slide 14: Effect of unloading stress on ten-stack stiffness in transverse direction– first loading
The ten-stack stiffness increases with increasing unloading stress.
A creep behaviour is observed when the transversal load exceeds about 125 MPa.
Transverse compressive stress-strain curve of the ten-stack sample (Vstrand=69.6%).
Transverse compressive stiffness at different unloading stress levels of a ten stack.

## Slide 15: Indications for creep behaviour of a free standing ten-stack
Curve changes in unloading - loading transition after 135 MPa applied load
Increased displacement at constant load
Small displacement at constant load
Transverse compressive stress-strain curve of the ten-stack sample (Vstrand=69.6%).

## Slide 16: Effect of epoxy volume fraction on transverse ten-stack stiffness (first loading cycle)
Compaction level | HT clearance (mm) | (%)
High | 14.6 | 74.3
Medium | 14.8 | 72.8
Low | 15.0 | 69.6
Compaction level | HT clearance (mm) | 
High | 14.6 | 74.3
Medium | 14.8 | 72.8
Low | 15.0 | 69.6
Samples with three different compaction levels during RHT have been investigated.
The stiffness increases with increasing unloading stress.
The stiffness in transverse direction increases with increasing compaction level during RHT and varies between 40 - 60 GPa
Transverse stiffness of ten-stack samples with different epoxy volume fraction at different unloading levels

## Slide 17: Effect of load direction on the ten-stack stiffness (first loading cycle)
Transverse
Axial
Radial
Stiffness in different load directions of a ten stack (Vstrand=72.8%)
Stiffness is strongly dependent to the load direction
Axial stiffness is 2 × transverse stiffness
Radial stiffness is 1.3 × transverse stiffness
Sample orientation

## Slide 18: Comparison of a first loaded and a reloaded ten-stack sample
Transverse compressive stress-strain curve of the ten-stack sample (Vstrand=69.6%) (first loaded).
Transverse compressive stress-strain curve of the ten-stack sample (Vstrand=69.6%) (reloaded).

## Slide 19: Comparison of ten-stack and 11 T coil segment stiffness
Stiffness is dependent from the loading level
Strong creep behaviour starting at 125 MPa
Transverse compressive stress strain measurement of 11 T dipole coil segment
Transverse compressive stiffness comparison of ten-stacks with different wire volume fraction and 11T coil segemt.
Stiffness is depended to the unloading stress

## Slide 20: Conclusion I
Good agreement of the stiffness results for identical Nb3Sn Rutherford cable ten-stack samples measured with two independent test set-ups.
In axial load direction the ten-stack stiffness can be predicted by the rule of mixtures assuming iso-strain conditions.
In the 11 T coil block and in the ten-stack samples made of the same conductor and with similar epoxy volume fraction, the macroscopic stiffness and creep behaviour under compressive loading are similar, suggesting that the ten-stack samples can represent well the 11 T dipole conductor block.
It remains to be studied if the test configuration of free-standing samples can represent the conductor loading in a magnet coil, where the conductor is constrained in axial and radial directions.

## Slide 21: Conclusion II
The ten stack stiffness depends on:
    Epoxy volume fraction (depending on the sample compression during the RHT)
    The unloading stress level
    The load history
    The load direction (axial stiffness is 2 × transverse stiffness, radial stiffness is 1.3 × transverse stiffness).
    The transverse stiffness of 11 T dipole coil block corresponds with that of the ten stack samples with similar epoxy volume fraction.
    A strong creep behaviour is observed when the transversal load exceeds about 125 MPa.

## Slide 22: Some open questions and outlook
How is the load case of free standing ten-stack samples related to the loading of constraint coils in a magnet?
What is the conductor block stiffness at 4.2 K?
What is the effect of the load rate?
What is the effect of creep?

## Slide 23: References
[1] C. Scheuerlein, F. Lackner, F. Savary, B. Rehmer, M. Finn, and P. Uhlemann, “Mechanical properties of the HL-LHC 11 Tesla Nb3Sn magnet constituent materials”, IEEE Trans. Appl. Supercond., vol. 27, no. 4, Jun. 2017, Art. no. 4003007.
[2] Metals Handbook, Vol.2 - Properties and Selection: Nonferrous Alloys and Special-Purpose Materials, ASM International 10th Ed. 1990.
[3] C. Scheuerlein, B. Fedelich, P. Alknes, G. Arnau, R. Bjoerstad, and B. Bordini, “Elastic anisotropy in multifilament Nb3Sn superconducting wires”, IEEE Trans. Appl. Supercond., vol. 25, no. 3, Jun. 2015, Art. no. 8400605.
[4] Robert M. Jones, “Mechanics of composite materials”, Second edition, Taylor and Francis, Inc. London 1999