## Slide 1: The History of Transverse Pressure Tests of Nb3Sn Rutherford Cables
Workshop on Nb3Sn Technology for Accelerator Magnets Paris, October 12, 2018
Arno Godeke Varian Medical Systems Particle Therapy GmbH

## Slide 2: Agenda
A learning curve for “low Jc“ conductors
Converging to stable results
A learning curve for “high Jc” conductors
Keeping up with magnet performance…
In reflection

## Slide 3: Many Transverse Pressure Experiments on Wires
Relatively simple, but not representative for cables in magnets
Lines: Elastic deformed cylinder (analytical)
Points: Wire with plastically deformed matrix

## Slide 4: An Early (first?) Nb3Sn Rutherford “Cable” Experiment
“Three-stage flat” cable for SULTAN: Measurement on one sub-cable
Pressure adjusted at
room temperature

## Slide 5: First (?) Measurements on Full-Size Rutherford Cables
192 filament PIT wire in ECN LHC-B and ECN-SULTAN cables
Stycast filled
Not filled
Voltage taps per
strand and globally
Trans. Magn. V27 n2 1991
Field and current within 1%
Pressure within 2%
Voltage within 50 nV

## Slide 6: Better Statistics and Experience (& smaller filaments), Better Results
Twente 11 T MSUT & LBNL 13 T D20
  Basic studies on 2D samples and wires
  Full size cable measurements
About 15 cables measured in Twente in the early 1990’s
“Filament”
count
192
50,000
6
36
Pressure

## Slide 7: Stable Cable Characterizations
MJR with 120 or 378 sub-elements (…):
D20 will work!
1
0.95
0
200 MPa
0%
-7%
0
200 MPa
Total
Irreversible

## Slide 8: Independent Confirmation by LBNL
Long straight cable sections with 122 mm pressure in NHMFL 12 T split pair
IGC 19 sub-elem.
- 40% at 200 MPa
MJR 122 sub-elem.
- 11% at 200 MPa
Magnet
Bore
Cables
Helium bellows for pressure

## Slide 9: Lessons learned
Impregnate cable
G10 above and below (UT)
  Or dummy cables (LBNL)
Solid side support
No correlation to V-tap location
  Current distribution not known
  Global is not equipotential
U(I) is not proportional to In
Small filaments survive > 150 MPa
  If the experiment is done properly
(And a couple of anecdotes…)
Global
Straight
Kink
Kink thin edge
Global = about average
n = 40
n = 4

## Slide 10: High Jc Strands in Copper Dummy Cables
Impregnated ✅
Dummy cable below ✅
G10 side plates ?
SC strand in Cu cable ?
Kink under pressure block with “soft” surroundings ?
A possible cheap and fast way to characterize “cables”?
Reaction holder
Copper cable
Copper cable with
“kink” SC strand

## Slide 11: High Jc Strands in Copper Dummy Cables
Some selected results
Are high Jc cables more sensitive to transverse pressure?

## Slide 12: Transverse Pressure on High Jc Wires
Bronze
RRP
Initially on bare wires
Later on impregnated wires
Seeber, et al. 2007:
Barzi, et al. 2008:
…so, is there, or is there not, a problem with the stress sensitivity of high Jc cables?
(LBNL attempted to test high Jc cables at the NHMFL but the experiment failed)

## Slide 13: What do Magnets Tell Us?
US LARP Technology Quadrupole TQS03 tested at CERN under high stress

## Slide 14: TQS03 Performance Under Intentionally High Stress
Unloading during magnet excitation and corresponding training
Insufficient pre-load and training
but closest to short sample
Higher pre-load
has reduced Ic
Higher pre-load
has again
reduced Ic
All reductions seem
irreversible since
the limit is measured
at minimal load!
Discussion points:
We observe that above 180 MPa permanent damage does occur (?)
We still not seem to know if reaching 93% of short sample is caused by damage at 180 MPa (?)

## Slide 15: Summary
A learning curve for “low Jc“ conductors
Converging to stable results
A learning curve for “high Jc” conductors
Keeping up with magnet performance
In reflection…some provocative thoughts!
Data showing less stress sensitivity is the better measurement…
(…similar to a critical current measurement where the highest value is correct!)
Discussion:
Are cable measurements indeed necessary as long as filaments are small?
Was the TQS03 test indeed undecisive, even for 180 MPa?
Proper cable
measurements
are tough!

## Slide 16
Less than 3% of cancer patients that would benefit from proton therapy has access
Thank You
EVERY DAY COUNTS!
Notes: Demand is high and growing
But currently, only 1% of cancer patients receive proton therapy
(when 20% of them would benefit)
In fact, a patient in this city would have to travel XX miles for proton therapy