## Slide 1: An Introduction to Axial Strain Characterization of Nb3Sn Wires
Workshop on Nb3Sn Technology for Accelerator Magnets Paris, October 12, 2018
Arno Godeke Varian Medical Systems Particle Therapy GmbH

## Slide 2: Agenda
High strain sensitivity of Nb3Sn explained
Evolution of axial strain experiments

## Slide 3: Nb3Sn: Limits on T, H, and J
Maximum J
  Critical current density Jc
Maximum H
  Critical magnetic field Hc2
Maximum T
  Critical temperature Tc
Critical surface
  Jc  Jc(H,T,e)
  Determines performance envelope for applications
Limits on T and H are affected by strain, leading to a change in the maximum J

## Slide 4: Probing Hc2(e) or Ic(e)
Nb3Sn has due to sub-lattice instability a relatively high sensitivity to strain
Compared to other LTS
Compared to HTS
Godeke, Hellman, ten Kate, Mentink
Supercond. Sci. Techn. 31 105011 (2018)
Bottura, Godeke
Rev. Acc. Sci. Techn. 5 25 (2012)

## Slide 5: Fundamental origin of high strain sensitivity of Nb3Sn
Ab-initio calculations + GLAG microscopic theory + experiments (Mentink PhD)
Godeke, Hellman, ten Kate, Mentink
Supercond. Sci. Techn. 31 105011 (2018)
Electron DOS collapses
causing reduced SC properties
Strain sensitivity is for 80%
caused by electronic properties
20% is cause by phonons
Electron DOS as proxy for sensitivity:
Sub-lattice distortion causes
large strain sensitivity

## Slide 6: Early Ic(e) results
Tensile tests on short wire sections
Ekin
Cryogenics 20 611 (1980)
OK for fine-filament
bronze, but modern
high-Jc wires break
in this region

## Slide 7: University of Twente, early 1990’s
MSUT: An 11 T Nb3Sn dipole magnet
Supporting R&D: Ic(strain, stress)
  Nb3Sn cables under load: Ic(H,F⊥)
Dietderich and Godeke, Cryogenics 48 331 (2008)
den Ouden, et al.,
IEEE Trans. Appl. Supercond. 7 733 (1997)
ten Haken, Godeke, ten Kate,
IEEE Trans Appl. Supercond. 3 1273 (1993)
Boschman, et al.
IEEE Trans. Magn. 27 1829 (1991)
  Nb3Sn tapes under load: Ic(H,F⊥,eaxial)

## Slide 8: 1992: U-shaped bending springs
CTE Nb3Sn is low: Wires in compression
  Look at compressive axial strain
Novel variable temperature
  Flow cryostats have large time constants
  Helium gas bubble under Kapton cup
ten Haken, Godeke, ten Kate,
IEEE Trans Appl. Supercond. 3 1273 (1993)
Walters, Davidson, Tuck,
Cryogenics 26 406 (1986)
Godeke, Graduation Report (1992)
ten Haken, Godeke, ten Kate, IEEE Trans Appl. Supercond. 5 1909 (1995)
First Ic(H,e)
with variable T !
Soldering a sample
on a substrate enables
compression and
homogenizes strain

## Slide 9: 1996: Does the lattice strain follow externally applied strain?
Is solder strong enough to transfer close to 1% longitudinal strain?
  Low temperature X-ray diffraction experiment on tape with exposed Nb3Sn
Measured with strain gauge
Lattice strain follows externally applied strain
ten Haken, Godeke, ten Kate,
Adv. Cryo. Eng. 42B 1463 (1997)
Measured with x-rays

## Slide 10: 1997: Variable temperature, Ti-6Al-4V U-spring for wires
  Ti-6Al-4V elastic limit is 1.3% (Brass = 0.3%, Cu2w.%Be = 1%)
  Ti-6Al-4V CTE matches barrels
  Brazed Cu buffer layer to enable “regular” soldering
  Highest current in non-strained regions
Godeke, et al., EFDA Report (1998)
Godeke, ten Haken, ten Kate, IEEE Trans. Appl. Supercond. 9 161 (1999)
ten Haken, Godeke, ten Kate, J. Appl. Phys. 85 3247 (1999)

## Slide 11: 2002: Longer length strain experiments: “Pacman”
From U-spring to Pacman
  10 x sample length (> 50 mm vs. < 5 mm)
  10 x voltage resolution (0.1 mV/cm vs. 1 mV/cm)
  Thermodynamically optimized
Godeke, et al., Rev. Sci. Instr. 75 5112 (2004)

## Slide 12: 2011: 0.1 mV/cm resolution possible on U-shaped springs
Going from I // B to I ⊥ B causes current redistributions that can be done earlier
Godeke, et al.,
Adv. Cryo. Eng. 58 209 (2012)
Entrance voltages
Redistribution voltages

## Slide 13: Selected Axial Strain Devices
Twente setups already mostly shown
Cheggour, Hampshire
Rev. Sci. Instr. 71 4521 (200)
Durham Walters spring
Reproduced at NIST,
now at NHMFL
Seeber, et al.
Rev. Sci. Instr. 76 093901 (2005)
Geneva Walters spring
Extended to transverse pressure
“Bending” springs at:
NIMS Tsukuba, Kyoto Univ., …