## Slide 1: ERMC, RMM and Study Towards a CERN-DEMO for a 16 T FCC Dipole
12/07/2018
Susana Izquierdo Bermudez, Davide Tomasini,

## Slide 2: Outline
The CERN roadmap towards a 16 T FCC dipole
  ERMC&RMM Non Graded
  ERMC&RMM Graded
  DEMO
  SMC – Parallel program to develop key technologies in smaller coils
DEMO design

## Slide 3: Outline
The CERN roadmap towards a 16 T FCC dipole
  ERMC&RMM Non Graded
  ERMC&RMM Graded
  DEMO
  SMC – Parallel program to develop key technologies in smaller coils
DEMO design

## Slide 4: Design strategy – ERMC/RMM Non Graded
Demonstrate the field
      Design based on the “available” critical current density (~20% lower than FCC target at 18 T, 4.2 K).
      As field quality is not an objective, profit from the use of an iron pole to decrease the ratio between the field in the aperture and in the coil to ~ 1.
      18 % margin on the load line.
Study the mechanics
Produce the magnet in the shortest possible delay.
  Use FRESCA2 cable (biggest available cable)
Plan: 1 eRMC magnet and 1 RMM magnet (RMM contains eRMC coils)
1 eRMC & 1 RMM spare coils planned

## Slide 5: Features & Outcome
Mica in-between the pole turn and the pole to avoid bonding  Faster training?
  Required the development of new concepts for coil handling.
Enhanced mica insulation (larger mica coverage to avoid stress concentration on the cable edges)  Issue of impregnation?
  Required several iterations of insulation tests
  Outcome:
    Summer 2018 (coil visual inspection)
    End 2018 (first fold powering test results)
    End 2019 (destructive inspection)
Study of assembly parameters. Understand what are the limits in terms of stress/Jc degradation in the 16-18 T range.
  Plans for eRMC (Test: end 2018 – mid 2019):
    Assembly 1: Azimuthal load to 16 T, axial load to be defined
    Assembly 2: Azimuthal load to 18 T, axial load to be defined
  And then, in RMM configuration (Test: mid 2019 – end 2019):
    Assembly 3: Azimuthal load to 16 T, axial load to be defined
    Assembly 3: Azimuthal load to 18 T, axial load to be defined
    Assembly 4: Azimuthal load to 18 T, axial load to be defined
  Risk: we have only one magnet of each type, so the statistics will be very low.

## Slide 6: Design strategy – ERMC/RMM Graded
Coil size  Grading
  High Field Nb3Sn splice development needed
Field quality (bn<10 units, including iron saturation)
Other definitions/requirements:
  Design based on the “available” critical current density Tc0 = 16 K, Bc20 =28.8T, α = 0.96, C0 = 255230 A/mm2T. Cable degradation = 5%.
  Stay within “CERN-knowledge-boundaries” in terms of cable geometry (<40 strands,<1 mm, cu/sc>=1)
  Needs to be accommodated within the same structure, changing only the coil pack assembly
  Baseline design in terms of LF margin and inner support structure more conservative than EuroCirCol.
  https://indico.cern.ch/event/464602/contributions/1139555/attachments/1205091/1755702/151212_Grading.pdf
Plan: 5 eRMC magnets and 3 RMM magnet (RMM contains eRMC coils)
3 eRMC & 2 RMM spare coils planned

## Slide 7: Features
If successful in the non-graded, we will keep:
  Un-bonded pole turn to pole
  Mica insulation
Internal splice in higher field than SMC
  First test beginning of 2020
Internal support requirements
  First magnet has 4 mm inner support, 2 mm can be explored. Feedback end of 2021.
Study of assembly parameters
New resins qualification, after pre-qualification in SMC

## Slide 8: Design strategy – Demonstrator
Could we accommodate in RMM structure a magnet with flared ends?
For the demonstrator, I would step towards EuroCirCol criteria for designing the magnet:
  FCC Jc: Tc0 = 16 K, Bc20 =29.38 T, α = 0.96, C0 = 1.03*267845 A/mm2 T. Cable degradation = 3%.
    14 % margin on the LF (and HF)
  Inner support = 2 mm (maybe a bit more)
  Explore cable options outside “CERN-knowledge-boundaries” in terms of cable geometry (<60 strands,<1.1 mm, cu/sc>=0.8)

## Slide 9: Features
If successful in the non-graded & graded programs, we will keep:
  Un-bonded pole turn to pole
  Mica insulation
  2 mm inner support
  Internal splice
  New resin
  Well defined loading strategy

## Slide 10: SMC
Internal splice
New resins & insulation systems qualification
Conductor qualification

## Slide 11: Overview on magnet parameters
RMM non graded
RMM graded
DEMO
 |  | RMM non graded | RMM |  | DEMO | 
 |  |  | graded |  |  | 
 |  |  | HF | LF | HF | LF
strand diameter | mm | 1 | 1 | 0.7 | 1.1 | 0.85
Cu/SC | -- | 1 | 1 | 1.2 | 0.8 | 1.2
# of strands/cable | -- | 40 | 28 | 40 | 44 | 56
# turns/quadrant | -- | 132 | 30 | 132 | 13 | 42
coil width | mm | 86 | 69 |  | 53 | 
Inom | A | 8850 | 8625 |  | 21000 | 
Joverall | A/mm2 | 248 | 259 | 350 | 339 | 422
Jcu | A/mm2 | 735 | 805 | 1236 | 904 | 1454
Jsc | A/mm2 | 735 | 805 | 1075 | 1130 | 1212
Ratio LF/JF | -- | n.a. | 1.35 |  | 1.25 | 
B0 at Inom | T | 16 | 16 |  | 15.43 | 
Bp at Inom | T | 16 | 16.6 | 13.67 | 16.08 | 13.22
1-Bp(Inom)/Bss(1.9 K)1 | % | 17 | 14 | 20 | 14 | 18
1-Inom/Iss1 | % | 19 | 16 | 23 | 15 | 21
Fx/h at Inom | MPa | 122 | 145 |  | 141 | 
Fy/w at Inom | MPa | -46 | -65 |  | -72 | 

## Slide 12: Outline
The CERN roadmap towards a 16 T FCC dipole
  ERMC&RMM Non Graded
  ERMC&RMM Graded
  DEMO
  SMC – Parallel program to develop key technologies in smaller coils
DEMO design

## Slide 13: Cable Parameters
 |  | Strands | Dstrand | CU/SC | Width | Thickness | Keystone angle
 |  | (-) | (mm) | - | (mm) | (mm) | (degrees)
Option 1: Same width LF and HF | DEMO HF | 44 | 1.10 | 0.8 | 25.700 | 2.002 | 0.00
 | DEMO LF | 56 | 0.85 | 1.2 | 25.700 | 1.547 | 0.00
Option 2: Best width LF and HF | DEMO HF | 44 | 1.10 | 0.8 | 25.958 | 2.002 | 0.00
 | DEMOLF | 56 | 0.85 | 1.2 | 25.475 | 1.547 | 0.00
In the design we assume:
  3 % thickness expansion during HT
  1 % with expansion during HT
The baseline for FCC is to use cored cables
Assumed degradation during cabling: 3 %

## Slide 14: Critical Current Density
 | Hi-Lumi | FCC models | FCC target
Tc0 (K) | 16 | 16 | 16
Bc20 (T) | 29.38 | 28.8 | 29.38
α | 0.96 | 0.96 | 0.96
C0(A/mm2T) | 188870 | 255230 | 275880
Jc at 4.2 K | Hi-Lumi | FCC models | FCC target
12 T | 3200 | 3850 | 4700
16 T | 1580 | 1900 | 1960
18 T | 1040 | 1250 | 1520

## Slide 15: Magnetic design
Inom = 21 kA
RMM yoke
Pads under
optimization
R= 13.5 mm
R= 34 mm

## Slide 16: Grading, several ideas…
Internal splice in the coil ends, “transparent” for the 2D cross section.
External splices, with wedge in the straight section to have space for the layer jump (only 2 leads).
External splices, “transparent” for the 2D cross section but with 4 leads to extract (difficult find the space).
External splices, with layer jump in the coil ends (only 2 leads, CEA approach).
Courtesy CEA

## Slide 17: Mechanical design
First 2D analysis fulfills EuroCircolCriteria
Key aspects under study
  Impact of the vertical force of the magnetic pad on the coil stress
  Pads/pushers geometries and contact surfaces