## Slide 1: Breakdown classification & new results with He implanted copper electrodes
anton.saressalo@helsinki.fi
Mini MeVArc 2018, November 13th
A. Saressalo, A. Kyritsakis, V. Jansson, M. Veske, E. Baibuz, J. Lahtinen, F. Djurabekova
Helsinki Institute of Physics
I. Profatilova, W. Wuensch
CERN

## Slide 2: Outline
Reminder: Pulsed DC setup Breakdown statistics Pulses between breakdowns - primary & secondary events? BD series after primaries He implanted Cu electrodes Effect of the implantation Possible explanations
What is next?

## Slide 3: Experimental setup: DC Spark System & Marx Generator
Cu electrodes
  62 mm diameter
  60 µm gap
Short DC pulses
  Electric fields even > 100 MV/m
  Pulse length ~ 1 µs
  Frequency up to 6 kHz
  High Vacuum (~ 10-8 mbar)

## Slide 4: Large Electrode System

## Slide 5: Flat mode & ramping
Flat mode = Constant target voltage regardless of breakdowns
Steady pulsing at 1-2 kHz, small pauses every 100 000 pulses
  Change of “period”
Pulsing stops at BD, after which the voltage is asymptotically ramped back to target from 1/5th
  “Exponential ramping”, 20 steps of 100 pulses on each

## Slide 6: Breakdown statistics

## Slide 7: BD classification based on double Poissonian?
1
1 Wuensch, W., Degiovanni, A., Calatroni, S., Korsbäck, A., Djurabekova, F., Rajamäki, R., & Giner-Navarro, J. (2017).

## Slide 8: BD classification based on double Poissonian?

## Slide 9: BD classification based on location?
Distance (mm)
0 5 10 15 20 25 30 35
Distance between consecutive BDs
Separated by number of pulses in between
Data: Iaroslava Hard Cu 007
Peak disappears at ~5000 pulses!

## Slide 10: BD classification based on location?
Distance (µm)
0 100 200 300
Distance between consecutive BDs
Distance between consecutive BDs
Separated by number of pulses in between
Data: Iaroslava Hard Cu 007
Zoomed to closest 300 µm
Peak disappears at ~3000 pulses!

## Slide 11: BD classification based on BD currents?

## Slide 12: Currents after a big BD

## Slide 13: Mean of all the followup-currrents

## Slide 14: He implanted Cu electrodes

## Slide 15: He implantation
Irradiation in 2015
  He+ with 30 keV
  Fluence 6.7 x 1016 He/cm2 (around 5 at.%) 🠞 vacancy clusters up to 300 nm from the surface

## Slide 16: First results in June Cathode Anode He He noHe noHe

## Slide 17: Twisting the electrodes Cathode Anode He He noHe noHe

## Slide 18: Twisting the electrodes makes a difference Cathode Anode He-He He-He He He He-noHe He-noHe noHe noHe He He noHe noHe noHe-noHe noHe-He noHe-He noHe-noHe

## Slide 19: Surface composition
Both halves investigated using ERDA
Helium still detectable: 3 x 1016 He/cm2 detected
  Surface now distorted due to BDs, so far exact
Also hydrogen, carbon and oxygen visible
  Carbon appears to be slightly deeper on He side

## Slide 20: Next: Further investigation with He implantation
Pristine Hard Cu pair has just been implanted
  Same energy & fluence as previously
  Elemental composition & surface smoothness analysis before breakdowns
Differences between implanted Hard and Soft Cu?

## Slide 21: Next challenges Right now Longer term plans
Surface chemistry
BD experiments with smaller electrodes
Field Emission measurements
Wrapping up the statistics as a publication
Smaller Cu samples with different hardness levels
  Annealing & polishing
  Measuring with ultrasound & XRD
Quantifying the effect of ramping

## Slide 22: Conclusions
Anton Saressalo
anton.saressalo@helsinki.fi
BD classification possible, but more proof needed
He irradiation seems to introduce BDs
Tradeoff between fundamental physics & applications
Mini MeVArc 2018, November 13th