## Slide 1: Why do we need coated collimators?
S. Antipov, D. Amorim, N. Biancacci, X. Buffat, E. Carideo, J. Guardia, E. Metral, N. Mounet, B. Salvant
HL-LHC WP2 Meeting, 28.08.18

## Slide 2: What is the motivation for collimator impedance reduction?

## Slide 3: Impedance of LHC collimators has to be reduced for the Hi-Lumi upgrade
Octupole current close to threshold
x2 margin
Linear coupling
Magnet imperfections
Feedback noise
Optics errors
Uncertainty of beam distribution
Present operational experience:
Need a factor 2 margin at least
Compared to pure impedance
Current study:
Ultimate OP scenario
Right before collision
No beam-beam
No help from ATS

## Slide 4: Impedance of LHC collimators has to be reduced for the Hi-Lumi upgrade
Octupole current close to threshold
To be upgraded
4 to be replaced during LS 2
To be upgraded*
2 to be replaced during LS 2
* 2 approved at the moment
Everything else - < 10 A
All other collimators - 70 A
4 primaries - 100 A
11 secondaries in IR-7 - 200 A
Dominant component is the
collimator impedance
x2 margin

## Slide 5: Study of the low impedance collimator in LHC
Primary collimators:
  MoGr to replace CFC
Secondary collimators:
  MoGr jaw
  Low-resistivity coating
N. Biancacci
MoGr
Currently, both primary and secondary collimators have CFC jaws (ρc = 5 μΩm)
Notes: The TCSPM is unusual from the jaw point of view: prototype built to benchmark the HL-LHC impedance reduction achieved with conductive coatings.
Three stripes of different material (MoGr bulk and TiN - Mo coatings on MoGr).

## Slide 6: The largest reduction of the resistive wall tune shift measured for Mo coating
CFC
TiN
MoC
Mo
model
exp.
S. Antipov, et al., IPAC’18
Good
Better
Best

## Slide 7: IR-7 Secondary collimators are the right target for impedance reduction
Collimator Tune shift goes down
Significant reduction in impedance was measured in the TMCI MD
Measured tune shift of 1 collimator: TCSG.D4, TCSPM
That’s a huge tune shift!
1.8x1011 p

## Slide 8: Low impedance collimators

## Slide 9: How does the gain scale with coating resistivity?

## Slide 10: One collimator, closer to the beam: Coating is very efficient
Damper suppresses coupled-bunch motion
Vertical collimator, Halfgap: 1.4 mm

## Slide 11: One collimator, closer to the beam: Coating is very efficient
Damper suppresses coupled-bunch motion
Vertical collimator, Halfgap: 1.4 mm

## Slide 12: Coating is less efficient when other sources of impedance take part
Damper suppresses coupled-bunch motion
Horizontal collimator, Halfgap: 3.1 mm

## Slide 13: Coating is less efficient when other sources of impedance take part
Damper suppresses coupled-bunch motion
Horizontal collimator, Halfgap: 3.1 mm

## Slide 14: Broadband components of impedance limit how much the total can be reduced
Being refined by E. Carideo
Being checked by T. Dascalu

## Slide 15: Stability diagram: Full machine
Coating IR7
TCSGs
Other sources

## Slide 16: Further reducing the resistivity gets less effective as one goes to better conductors
Cu
Mo
MoGr
CFC
Mo (TCSPM)
Cu (TDIS)
Resistivity (nW-m)

## Slide 17: What could be different (go wrong)?
Need tighter collimator settings for machine protection
Mo coating does not perform as expected
Have to settle for uncoated secondary collimators
Something left unaccounted for in the model
  Refining the model of geometric impedance
  Noise leading to instabilities with large latency times
  Beam-beam interaction reducing the Stability Diagram

## Slide 18: LHC keeps tightening the collimator gaps during its operation
Originally, there were three collimator scenarios for HL-LHC:
  1.0 s: TCP – 6, TCS – 7 (for 3.5 mm ref. emittance, “Nominal” design report)
  1.5 s: TCP – 5, TCS – 6.5
  2.0 s: TCP – 5.7, TCS – 7.7
Ultimately became the baseline
Chart: Year
| 2016 | 2017 | 2017.33 | 2017.67 | 2018
Primary | 5.5 | 5.5 | 5 | 5 | 5
Secondary | 7.5 | 7 | 6.5 | 6 | 6
Are we sure the settings are not going to change in the future?

## Slide 19: Little or no safety margin for tighter settings if the full impedance reduction is not done
Nominal settings
Tight (non-baseline) settings

## Slide 20: Not coating the secondary collimators: Octupole current threshold – similar to post-LS2

## Slide 21: The actual resistivity of Mo coating might be higher than the model value
Material | Model | Beam | Lab: DC | Lab: RF
CFC | 5000 | 4030 ± 380 | 5000 – 6000 | -
MoGr | 1000 | 760 ± 60 | 900 ± 100 | -
TiN | 400 | 340 ± 40 | - | ~400
Mo | 53.5 | 250 ± 50 | 100 – 300 | ~300
S. Antipov, et al., IPAC’18

## Slide 22: Surface studies
Higher Mo resistivity could be related to:
  Coating grain size and number of boundaries – affect the resistivity
  Coating surface roughness – affect the imaginary impedance
  Presence of large (m ) bumps on the surface – affect the imaginary impedance
Surface impurities could also increase effective resistivity
1
2
3
N. Biancacci, et al., IPAC’18

## Slide 23: Bench RF measurements suggest the importance of the microstructure
Change in Q-factor → Real part of longitudinal impedance
Agreement within error bars on TiN stripe
Lower impedance reduction measured on Mo stripe 300 Mo resistivity (expected 53)
DUT
Resonant wire measurement setup
N. Biancacci, et al., IPAC’18

## Slide 24: Impact of higher than expected Mo resistivity
Assuming measured Mo resistivity (250 vs 54 n-m): 25 (20) A reduction in margin for BCMS (Standard) beam

## Slide 25: Latest Mo-coated samples show good electrical conductivity
Eddy current measurement is required to qualify the coating
  DC not enough – not ‘beam’ frequency, does not account for surface roughness
Newer coatings show 60-70 nW-m
Some (older ones) feature up to 300 nW-m
N. Biancacci, Update on Mo coating resistivity, 18.05.18

## Slide 26: The increase in Mo resistivity is likely to be governed by its microstructure
J. Guardia, Impedance Meeting, 24.08.18

## Slide 27: The increase in Mo resistivity is likely to be governed by its microstructure
J. Guardia, Impedance Meeting, 24.08.18
The larger the better
The less the better

## Slide 28: Propose to set the limit for production such that a degradation of the octupole current is < 10%
Cu
Mo
MoGr
CFC
Mo (TCSPM)
Cu (TDIS)
Resistivity (nW-m)
Limit for production

## Slide 29: Changes in geometric impedance: New taper geometries
This is the only geometry in the model at the moment
Simulated as a broadband flat taper impedance
E. Carideo
TCS | TCSP | TCSPM
11,6° | 16°, 16,5° | 16,5°, 5°
97 mm | 37 mm, 27 mm | 36 mm, 80 mm
Optimized for Imp.

## Slide 30: Noise triggers an instability with high latency time at Flat-Top
Increasing noise amplitude

## Slide 31: Stability diagram collapses as the beams are brought into collision
Minimum at a certain beam separation
Predicted theoretically and observed in a dedicated MD
X. Buffat et al., CERN-ACC-NOTE-2018-0036, 2018
Octupole
Beam-beam

## Slide 32: Conclusions
IR-7 primary and secondary collimators are the right target for impedance reduction
  From the past operational experience, a x2 margin in octupole threshold is required
  Mo coating on MoGr offers the largest reduction of impedance and octupole current in HL-LHC
  For the ultimate scenario one gains up to 150 A (BCMS beam) by coating all the secondaries in IR-7
  Additional 30 A (BCMS) can be gained by replacing the 2 primary collimators with MoGr
  1/2 the gain with LS2 upgrade (2 primary + 4 secondary) or with uncoated MoGr secondaries
A collimator resistive wall component of the octupole threshold scales as r-1/2
  Coating provides a large gain
  Only for the collimators that are close to the beam; further away – the taper geometry plays a role
In a realistic accelerator the scaling is worse than r-1/2
  Other sources of impedance: beam screen, tapers, etc. Act on 50% of effective beam impedance
  At small resistivities, a further reduction is less effective
  Can set a limit of 100 nW-m for the production Mo coatings

## Slide 33: Back-up

## Slide 34: Stability diagram: 1 Collimator
RW
Geom

## Slide 35: Geometric component of collimator tapers is comparable to resistive wall after the upgrade

## Slide 36: Staged installation of low impedance collimators in LS2: Maximizing reduction in the most critical, horizontal plane
  Impedance reduction
  Injection/extraction failure events or asynchronous dumps
  Steady exposure to beam losses

## Slide 37: Fitting the taper impedance:
Name | A | α
TCS | 2,07*10-3 | 1.9
TCSP | 2,57*10-3 | 2.0
TCSPM | 1,02*10-3 | 2.0
E. Carideo
The model can be used to refine the prediction for HL-LHC
Work ongoing

## Slide 38: TMCI Threshold for different coating scenarios
Simulated Measured
Simulated
D. Amorim
Looser settings

## Slide 39
J. Guardia