## Slide 1: ATS-KT Innovation Day
Lucia Lain Amador
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland
Development of copper electroformed NEG coated vacuum chambers

## Slide 2: Outline
Motivation
Idea
Prototypes
Next steps
Applications

## Slide 3: Why?
Next generation synchrotron light sources and CLIC (beam focussing) demand the use of small-aperture beam pipes: magnetic poles closer to the beam.
Big impact on the vacuum system: low conductance vacuum chambers.
Distributed pumping , as getter coating, is needed to keep gas density low.
H. D. Nuhn et al., Presentation at FLS (2012),
Delta undulator, SLAC
Vacuum chamber ID 5mm
M. Modena et al. (2014)
CLIC MB quadrupole [1]
Vacuum chamber ID ~8 mm
[1] http://clic-study.web.cern.ch
New generation light source accelerators and CLIC

## Slide 4
NEG thin film coating, developed at CERN, is usually performed by DC magnetron sputtering from a twisted Ti, Zr, V wire cathode that is positioned in the vacuum chamber centre.
Before coating
After coating
TiZrV cathode
Physical vapor deposition techniques are difficult to apply to few-mm diameter pipes that are several meter long.
Vacuum chamber
Vacuum chamber
?
Why?
NEG thin film coating

## Slide 5: Production/coating technique based on mandrel technology
The vacuum chamber is produced by copper electroforming around a sacrificial aluminium mandrel which is pre-coated with a NEG thin film.

## Slide 6
During the electroforming, the stainless steel flanges are assembled to the chamber without any welding/brazing.
Production/coating technique based on mandrel technology

## Slide 7
Production/coating technique based on mandrel technology
Advantages of this technique:
Stainless steel joining is produced without EB welding or brazing step.
Uniform coating (composition + thickness) is obtained along the length of the chamber.
Coating reproduces the mandrel topography: If mandrel is polished, coating is very smooth.
Very complex shapes can be coated if a mandrel can be machined.

## Slide 8
Prototypes
8
Chamber 16 mm diameter
Chamber 5 mm diameter
0.3 m
0.4 m
Chamber 3 mm diameter
Chamber 4 mm diameter
0.1 m
0.15 m
Chamber 6 mm diameter
0.15 m
Chamber 12 mm diameter
0.3 m
TiZrV coated chamber
Lowest diameter ever NEG coated tube
Diameter constraint?

## Slide 9
Length [mm]
4mm internal diameter, 2 m length TiZrV coated chamber
Ø4mm
2 m
Thickness (μm)
M (%)
Prototypes
Length constraint?
TiZrV coated chamber
Limited only by the depth of the plating bath.

## Slide 10
Prototypes
10
TiZrV coated chamber
Pumping performance
H2 sticking probability (  pumping performance)
H2 sticking factor reaches reference values (standard coating method), but there is a delay in activation temperature.
NEG reference
Prototypes

## Slide 11
Transfer of the technology to non circular and/or complex geometries.
Joining stiffeners and/or cooling lines by the electroforming process.
Optimization of plating procedures at CERN. Reverse pulse plating to optimize thickness distribution.
Decrease the in-situ activation temperature of the coating.
Further steps
11
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland

## Slide 12
Vacuum in the beampipes of CLIC quadrupoles
The idea has been pursued as a PhD work at CERN, in collaboration with the Université de Franche Comté.
High interest is shown from Berkeley Lab (US) and PSI (Zurich) for vacuum chambers of wigglers.
Industrial companies that manufacture vacuum chambers for HEP have also shown interest
Origin of the idea
12
Interest in HEP community

## Slide 13
Other applications outside CERN and HEP
13
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland
Advanced onco-therapy beam-pipes // accelerator for medical research
Free Electron Lasers
TiZrV coated beampipes
A. Degiovanni et al. Proceedings of NAPAC2016, Chicago, IL, USA
LIGHT (LINAC for Image Guided Hadron Therapy)
General idea: thin-film coated copper electroformed assembly
Applications can be expanded to other thin film coatings in complex and/or small geometries.

## Slide 14
Other applications
14
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland
Aluminium mandrel polished
No EB welding in the process
High RRR for electroformed copper
Cu cavities made with Cu PVD layer
Nb/Cu cavities made by deposition of Nb and Cu PVD layers on the mandrel
RF cavities (to be tested)
1.3 GHz cavity
LHC cavity

## Slide 15
Thank you very much for the attention!
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland
https://home.cern/about/updates/2018/05/honey-i-shrunk-vacuum-chambers
More info:
L. Lain Amador, P. Chiggiato, L. M.A Ferreira, V. Nistor, A. T. Perez Fontenla, M. Taborelli, W. Vollenberg, M-L Doche, J-Y Hihn,J. Vac. Sci. Technol. A, 36, 021601 (2018)

## Slide 16
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland
Non evaporable getter (NEG)
Non Evaporable Getter are materials than can pump residual gaseous molecules after thermal activation in vacuum.
During the activation, the surface oxygen diffuses inside the bulk.
T = RT
T = Tactivation
T = RT
Metal oxide
15

## Slide 17
ATS-KT Innovation day
26th October 2018, Geneva, Switzerland
17
Mechanical performance
350-400 MPa
180-220 MPa
Chambers before and after bake-out exhibit a tensile strength comparable to Cu OFE
(280°C)
Cu OFE cold-worked
Cu OFE annealed