## Slide 1
M.C. Jiménez-Ramos1*, J. García López 1, 2, M. Rodriguez 1, A. Villalpando 1, I. Vila2, S. Hidalgo3, G. Pellegrini3, A. Doblas3, E. Currás2, R. Jaramillo2, J. Gómez Camacho1,2
1 Centro Nacional de Aceleradores (CNA)
2 Departamento de Física Atómica, Molecular y Nuclear. Universidad de Sevilla
3Instituto de Física de Cantabria (IFCA-UC-CSIC).
4Instituto de Microelectrónica de Barcelona (IMB-CNM, CSIC)
(*) mcyjr@us.es
Thin LGADs characterization using Ion Beam Induced Charge (IBIC) and Time-resolved IBIC at the Centro Nacional de Aceleradores.

## Slide 2
33th RD50 Workshop
What is Ion Beam Induced Charge?
MeV
ion beam
V0
Electrodes
Charge sensitive
preamplifier
Vout
Amplifier
ADC
+
MCA
Same electronic chain as used in nuclear spectroscopy
Einitial
h
e-
1- Deposited Energy
2- Carriers generation
3- Transport
4- Output signal
Vout=f (E deposited
&
free carrier transport)

## Slide 3
Nuclear microprobe
~ 2 mm spot
sample
B
E
A
M
X, Y scanning system
Magnetic Q-poles
Ion beam current: nA to few pps (micrometric slits)
Scanning system: few mm2
Synchronous signal acquisition system with scanning: mappings
What is Ion Beam Induced Charge?
33th RD50 Workshop

## Slide 4
What is Ion Beam Induced Charge?
Sum spectrum from the whole scan
Channel ~ Q generated ~ E measured
33th RD50 Workshop

## Slide 5
What is Ion Beam Induced Charge?
0
1
2
3
4
5
6
7
8
9
10
11
33th RD50 Workshop
Scan area
A
B
C
D
E
A
B
C
D
E
Irradiated zone
Pristine zone

## Slide 6
RD50 Proposal
33th RD50 Workshop

## Slide 7
Four sectors 50 µm LGAD fabricated by IMB-CNM
33th RD50 Workshop
Lateral charge collection homogeneity
Peripheral Structures
Gain curve
TRIBIC

## Slide 8
Four sectors 50 µm LGAD assembly by IFCA
33th RD50 Workshop
- Bonding and electrical characterization by IFCA/CERN
- Dedicated PCB for laser and IBIC measuremts

## Slide 9
Charge generated across the detector
33th RD50 Workshop
Total charge in 50 µm:
3 MeV protons → 50fC
MIP → 0,6 fC

## Slide 10
Charge Collection homogeneity
LGAD W4-B231 #3: 3 MeV protons & +90V; 2.5*2.5 mm2
Lateral charge collection is not homogeneous (<10%)
Peripheral Structures are observed
A defect is seen (red circle)
The wire bonding is well resolved
E
F
G
H
I
The color intensity is related to the number of counts in each position and the maps are related to the different energy windows

## Slide 11
Peripheral Structures
Channel 1
Channel 2
 1960 µm
Signals from channel 1 & 2
 80 µm
V1= V2 = +90V
 20 µm
 20 µm
33th RD50 Workshop

## Slide 12
Peripheral Structures: LGAD vs PIN
33th RD50 Workshop
End of multiplication layer of each sector
P-stop common for the two sectors
PIN
Single structure with  1/2 CCE shared by the two sectors
LGAD
One structure for each sector with a CCE value lower than 50%.
Analysis along the vertical direction
90 µm

## Slide 13
30th RD50 Workshop 5-7 June 2017 Kraków
LGAD W4-B231 #3 vs W4-B232P #3

## Slide 14
Gain Curve
Gain vs Voltage for different positions within the sensor
3 MeV protons
33th RD50 Workshop
G(40V) > G(45V) > G(50V)!!!

## Slide 15
LGAD W4-B231: Gain calculations
Multiplication Factor
a
b
Ionization coefficients
electrons
holes
80 V
40 V
Gain (80V)/ Gain (40 V)=
Calculation: 1.09
IBIC: 1.07
Absolute Gain (@40V)=
Calculation: 4.4
IBIC: 5.7
Y. Musienko et al., NIMA, 2000.

## Slide 16
TRIBIC (preliminary measurements)
MeV
ion beam
Electrodes
Generation of e-h pairs
Ionization profile dE/dx (SRIM)
Einitial
h
e-
Fast oscilloscope
Transient signal
(TRIBIC)
Without amplification stage between detector and scope
Self-trigger: working in DAQ improvements
External trigger system ongoing
33th RD50 Workshop

## Slide 17
New sample holder for IBIC at -20ºC

## Slide 18
Thank you for your attention

## Slide 19
LGAD W4-B231: Gain Curve
G (LGAD)/G (PIN) = 5.8 for 3 MeV protons (@40V)
G (LGAD)/G (PIN)= 3.2 for 5.5 MeV protons (@40V)

## Slide 20
Generated charge profile
33th RD50 Workshop