## Slide 1
Defect investigations in 1 MeV neutron irradiated PiN pads and LGADs
Cristina Besleaga Stan, Roxana Radu, Raluca Negrea and Ioana Pintilie
National Institute of Materials Physics, Bucharest-Magurele, Romania

## Slide 2
Motivation: new structures based on p-type silicon

## Slide 3
The general objective is to improve the radiation hardness of different types of silicon sensors (single pads, pixel and strips, LGAD and HVCMOS) built on
p-type standard float zone (different Boron content)
And
defect engineered material:
Carbon enrichment of Boron doped silicon
Gallium doped silicon, Carbon enrichment
– point defects
V+O→VO
V2
I+Cs→Ci
Ci+Cs→CiCs
Ci+Oi→CiOi
I+Bs→Bi
Bi+Oi→BiOi
……?……..
Competing reactions involving Boron, Carbon, Sii and Oi
Samples:standard B doped and/or C co-doped , Ga doped
p-type pad silicon
LGAD and HVCMOS
Irradiations with:
1 MeV neutrons (Ljubliana)
23 GeV protons (CERN)

## Slide 4
2 p-type bulk Boron doped STFZ diodes from
National Center for Micro-electronics (CNM)–irradiated with 1MeV neutrons, fluences of 1x1014 and 1x1015 cm-2
PiN pads
LGADs
4 LGAD structures produced on STFZ silicon from
-National Center for Micro-electronics (CNM) with Boron implanted gain layer– irradiated with 1MeV neutrons, fluences of 1x1014 and 1x1015 cm-2
Investigated p-type Samples irradiated with 1 MeV neutrons
- Preliminary results

## Slide 5
Investigated p-type Samples
RUN 9088 neutron irradiated-for TSC measurements |  |  |  |  |  |  | 
NR. | Name | Fluence n/cm2 | Type | Thickness | Full depletion voltage (V) | Depletion voltage of the gain layer (V) | Leakage current at Vdep(20 C) (A)
1 | W5-LGB-82P | 1x1015 | PIN- no gain layer | 50 µm | 16.8 |  | 1.64x10-5
2 | W5-LGB-72P | 1x1014 | PIN- no gain layer | 50 µm | 5.6 |  | 1.73x10-6
3 | W3-LGB71, dose 1.8E13 | 1x1014 | LGAD | 49 µm bulk, 1 µm B implanted layer | 28.95 | 26.1 | 3.78x10-6
4 | W11-LGB74, dose 2.0E13 | 1x1015 | LGAD | 49 µm bulk, 1 µm B implanted layer | 28.5 | 15.9 | 2x10-5
5 | W3-LGB74, dose 1.8E13 | 1x1015 | LGAD | 49 µm bulk, 1 µm B implanted layer | 30.4 | 11.6 | 1.89x10-5
6 | W11-LGB52, dose 2.0E13 | 1x1014 | LGAD | 49 µm bulk, 1 µm B implanted layer | 33.79 | 31.04 | 1.03x10-5
[B]gain layer ~ 4x1016 cm-3
[B]bulk = 2-5x1012 cm-3

## Slide 6
Electrical characteristics
- Bulk LC LGADs > bulk PiN
[B]gain layer ~ 4x1016 cm-3
[B]bulk = 2-5x1012 cm-3

## Slide 7
TSC investigations
As irradiated
=1014 cm-2
- In PiN diodes all defects increase in concentration with fluence (including BiOi)
=1015 cm-2

## Slide 8
TSC investigations
=1014 cm-2
UR = 50V
In LGAD diodes most of the defects increase in concentration with fluence but the BiOi
 A saturation of BiOi possible caused by the limited amount of Oi

## Slide 9
TSC investigations
=1014 cm-2 , 30min@80C
point defects and clusters are detected in both PiN and LGAD diodes.
The generation rates are different in the gain layer compared with the bulk (measured on PiN pad diodes) –e.g. more BiOi in LGAD
All these defects and their impact on the electrical performances of the PIN and LGAD diodes are now under evaluation.
Comparison between LGAD and PiN

## Slide 10
Impact on Neff
=1014 cm-2
=1015 cm-2
- Neff evaluated with defect concentrations determined from TSC > Neff evaluated from CV
- The missing acceptors concentration from TSC increase with the fluence
 possible cause - the existence of Bi – not electrically active (cannot be determined by TSC and deactivates the B dopant)

## Slide 11
Impact on Neff
Defect concentrations – comparison between gain layer and bulk
For the gain layer even large differences between Neff from TSC and that from CV
– suggesting the same cause, the generation of Bi (not electrically active), in larger amount in the implanted layer than in the bulk
[B] = 4.8x1012 cm-3
=1014 cm-2
[B] = 4x1016 cm-3

## Slide 12
Conclusions and further work
A saturation of BiOi defect in the gain layer is observed starting with a fluence of 1014 cm-2
The TSC evaluation underestimate the acceptor removal process (cannot determine also the Bi defect) and underestimation increases with the amount of B dopant
Annealing studies on 1 MeV CNM samples to be continued up to 10.000 min@800 C
TSC investigations after 1MeV neutrons irradiation, fluences of 1015 cm-2 are reliable – one can try to go for higher fluences.
Start the investigations on irradiated defect engineered FBK samples
Start investigation on irradiated EPI PiN pad samples (STFZ has large amount of processing induced defects)

## Slide 13
Thank you for your attention !