## Slide 1: Niobium welding tests at CERN
Thomas Demazière
04-09-2018

## Slide 2: Weldabilty of Nb
Niobium welded at CERN :
RRR300 (99%)
RRR40 for RFD welding tests to come
3D printed Niobium (1 test only)
Niobium welding processes :
EBW
Manual TIG in glove box (sputtering cathodes,…)

## Slide 3
Properties | Niobium | Nb45Ti55 | Copper
Thermal conductivity (W.m-1.K-1) | 54 | 10 | 400
Melting temperature (°C) | 2500 | 1900 | 1080
Density (g.cm-3) | 8.57 | 5.7 | 8.96
Linear energy to weld 3 mm (J/mm) | 225 |  | 300
plasma color during welding | bright white (RRR300) bright red (500 ppm) |  | green
Copper
Beam power : 10 kW
Niobium
Beam power : 5 kW

## Slide 4: Weldabilty of Nb RRR300
Typical joint preparation :
Machined welded interface
Butt weld (square edges, with or without backing)
BCP 5-25 µm less than 8hrs before welding
Assembly of the parts under laminar flow
Vacuum below 5.10-5

## Slide 5
Weldability of Nb RRR300
3 main types of parameters :
Full penetration weld with focused beam
  Lowest distortion
  Root concavity  smoothing mandatory
Smoothing pass
  Necessary for proper surface finish
  Adds shrinkage
Full penetration weld with under focused beam
  Largest distortion
  Parameters challenging to control (risk of lack of fusion or burn through is significant)
  Smooth surface finish, no spatter

## Slide 6
Weldability of Nb RRR300
X-ray results :

## Slide 7
Weldability of Nb RRR300
4 mm / 2 passes
  Energy : 315-350 J/mm per pass
  Rp0.2 : 71 Mpa
  Rm : 170 Mpa
  A% : 36%
3 mm / 1 pass (with backing)
  Energy : 340 J/mm
  Rp0.2 : 57 Mpa
  Rm : 180 Mpa
  A% : 61%
3 mm / 1 pass
  Energy : 605 J/mm
  Rp0.2 : 70 Mpa
  Rm : 144 Mpa
  A% : 23%

## Slide 8
Welded only in dissimilar joints (for Crab Cavities project)
Nb to NbTi (EBW)
Weldability of Nb45Ti55
The beam is focused on the Nb to compensate for the lower energy required to melt NbTi

## Slide 9
Welded only in dissimilar joints (for Crab Cavities project)
Ti Gr.2 to NbTi (manual TIG)
More challenging to accomodate the difference in melting point
Requirements less stringent than for EBW (partial penetration joints, only leak tightness is required)
Weldability of Nb45Ti55

## Slide 10: Conclusion
Niobium and NbTi welded at CERN :
No particular defects observed
Easier parameter setting than with copper
Difficulties come mostly with the high quality requirement and complicated design and tooling assemblies

## Slide 11: Thank you for your attention